CTAB-assisted AgBr -bismuth oxybromide based novel SERS substrate for label-free, non-invasivequantitative detection of detrimental synthetic food colorants

Arti Saroj1, Venkatnarayan Ramanathan1*

1 Department of Chemistry, Indian Institute of Technology (BHU) Varanasi 221005, Uttar Pradesh, India

*author to whom correspondence must be addressed at vraman.chy@iitbhu.ac.in

Supporting Information

Figure S1. BT-SEM image of (a) BOB (b) Ag0.09BOB (c) Ag0.15BOB

Figure S2 XPS spectrum of Ag0.15BOB(CTAB- AgBr- Bi3O4Br/BiOBr) (A) survey spectrum and high resolution spectrum for (B) Bi 4f, (C) O 1s, (D) Br 3d, (E) Ag 3d.

Figure S3 SERS spectra of 100 µM ethanolic solution of R6G on BOB and Ag0.09BOB.

Table ST1. Tentative assignment for the vibrational Raman modes of Rhodamin 6G, Allura red, Amaranth, Tartrazine and Sunset yellow.

| Analytes | Raman Peak ( cm-1) | Tentative Assignment |
| --- | --- | --- |
| Rhodamin 6G | 607 768 1117/1179 1302 1360/1504/1593/1644 | ipδ(C-C-C) ring op δ(C-H) ip δ(C-H) ipδ(N-H) ν (C-C) (36, 37) |
| Allura red | 751 974 1129/1578 1188 1223 1266 1383/1496 1407 1604 | ω(R1) ω(C-H)R2 νas(R1) νas(SO2) ρ (C-H- R1) ν(O-C- R1) ω(C-H) ρ (C-H) νas( R2)(15) |
| Amaranth | 738 1052 1138/1175 1231 1363 1405/1434 1478 1572 | ρ(C-H) νas (SO2) ω(C-H) ω(O-S) ν(C-C) ω(C-H) ν (N-N) νas (ring)(38-39) |
| Tartrazine | 623 802 1044 1132 1177 1217 1361 1414 1499 1597 | def(R1) ν(C-O) op (C – H); def. (R2) op def(C-H-R1); δ(R1) τ(R1) ν(R1) ν(C-N=N-C); νs(COO);wagg(R1) ν(R1) δ(R1); δ(C=C) δ(R1);ipdef(C-H-R1); δ(O-H); νs(COO) (40) |
| Sunset yellow | 986 1123 1178 1231 1336 1384 1496 1545 1594 | ω(C-H-R2) ν (N=N); ω(C-H- R1) ν (N=N); ρ(C-H-R1); ρ(R1) δ(C-C-R1); ν (C-N); ν (C-C- R2); ν (C-N); νas(H-C-C-H-R1); ρ(R1) νs(C-C-R2);ip δ(R1,R2) ν (C-N); ν (C-O); ρ(N-H) δ(C-C-R2); ρ(N-H); ρ(C-H) νs(C-C-R1); ω(C-H-R1) (16) |

ν=stretching; δ=bending; ρ=rocking; τ=twisting; ω=wagging; s=symmetric; as=asymmetric; def=deformation;ip=in-plane; op=out-plane; R1=benzene ring;R2 =naphthalene ring

Table ST2: Comparison of the detection limits foranalytes with the previous report on different SERS substrates

| Substrate | Analytes | LOD (M) | Ref |
| --- | --- | --- | --- |
| Bi thin films Au−BiOI Ag/BR/Ag NPs Gold nanodumbells Ag0.15 BOB | R6G R6G TR SY R6G TR SY | 1× 10−2M 0.5 × 10−5M 2.1 × 10−5 M 1.1 × 10−5 M 1.0 × 10−5M 4.0 × 10−5M 4.0 × 10−5M | (21) (26) (*) (**) This work |

References

* Liu, H. et al. based sandwich type SERS sensor based on silver nanoparticles and biomimetic recognizer. Sensors Actuators B Chem.2020, 313, 127989.

** Meng, J.; Qin, S.; Zhang, L.; Yang, L. Designing of a novel gold nanodumbbells SERS substrate for detection of prohibited colorants in drinks. Appl. Surf. Sci. 2016, 366, 181–186.