## Slide 1
No | General name | Scientific name | Vessel arrange | Bulk density (g/cm3) | MC (%) | N
1 | Red toon | Toona sinensis. | Rp | 0.575 | 7.91 | 15
 |  |  |  | (SD: 0.023) |  | 
2 | Korean castanea | Castanea crenata Sievold & Zucc. | Rp | 0.546 | 7.59 | 15
 |  |  |  | (0.023) |  | 
3 | East Asian hackverry | Celtis sinensis Pers. | Rp | 0.731 | 6.50 | 15
 |  |  |  | (0.015) |  | 
4 | Korean aspen | Populus davidiana Dode. | Dp | 0.396 | 7.59 | 15
 |  |  |  | (0.017) |  | 
5 | Oriental plane tree | Platanus orientalis L. | Dp | 0.576 | 7.24 | 15
 |  |  |  | (0.025) |  | 
6 | East Asian alder | Alnus japonica (Thunb.) Steud. | Dp | 0.477 | 7.93 | 10
 |  |  |  | (0.030) |  | 
Table. 1 Information of six species of hardwoods (n=85)
Note: Rp is ring-porous wood, Dp is diffuse-porous wood, MC is moisture content, and SD is standard deviation.

## Slide 2
No | General name | Gas permeability (Darcy) | Maximum pore size (μm) | Mean pore size (μm) | Through pore porosity (%) | Blind pore porosity (%) | Closed pore porosity (%)
1 | Red toon | 5.750 | 148.201 | 70.251 | 12.721 | 13.542 | 35.385
 |  | (SD: 1.499) | (44.342) | (25.730) | (4.455) | (5.744) | (9.746)
2 | Korean castanea | 0.420 | 97.011 | 35.404 | 14.620 | 29.253 | 19.696
 |  | (0.322) | (60.517) | (30.460) | (3.541) | (2.797) | (2.585)
3 | East Asian hackverry | 10.787 | 102.138 | 29.237 | 17.936 | 11.038 | 22.290
 |  | (1.036) | (9.983) | (4.074) | (1.965) | (1.158) | (2.094)
4 | Korean aspen | 36.002 | 47.852 | 22.027 | 41.090 | 26.582 | 5.908
 |  | (3.409) | (2.364) | (1.094) | (7.363) | (7.321) | (2.450)
5 | Oriental plane tree | 9.923 | 27.500 | 4.477 | 29.561 | 24.080 | 7.943
 |  | (3.224) | (4.823) | (1.350) | (2.403) | (2.492) | (2.043)
6 | East Asian alder | 5.528 | 7.523 | 1.990 | 25.511 | 37.203 | 5.473
 |  | (1.105) | (0.376) | (0.206) | (1.708) | (1.858) | (1.050)
Table. 2 Results of gas permeability, pore size, and porosity analysis of six species of hardwoods (n=85)

## Slide 3
 | SAC @ 250-500 Hz | SAC @ 500-1000 Hz | SAC @ 1,000-2,000 Hz | SAC @ 2,000-6,400 Hz
Max pore size (m) | -.764** | -.505** | -.237* | -.118
mean pore size (m) | -.657** | -.387** | -.147 | -.110
Through pore Porosity (%) | .698** | .872** | .774** | .728**
Blind pore porosity (%) | .618** | .251* | .011 | -.148
Closed pore porosity (%) | -.802** | -.647** | -.427** | -.348**
Table. 3 Results of Pearson‘s correlation analysis (n=85)
Note: ** 1% significance level and * 5% significance level.