





[bookmark: _Hlk159480971]Supplementary Figure 1. Visible plastic pollution

























[bookmark: _Hlk159481377]Supplementary Figure 2. Microplastics isolated from some sediment samples
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Suplementary Table 1. Presence and similarity rates of LDPE because of FTIR analysis of sediment samples
	LDPE
	Van1
	Van2
	Van3
	Tatvan1
	Tatvan2
	Tatvan3
	Gevaş1
	Gevaş2
	Gevaş3
	Erciş1
	Erciş2
	Erciş3 

	2917
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+
	-

	2852
	+
	+
	+
	+
	+
	+
	-
	-
	-
	+
	+
	+

	1377
	+
	-
	+
	-
	+
	+
	+
	+
	+
	+
	+
	+

	718
	+
	+
	+
	+
	+
	+
	+
	+
	+
	-
	+
	+

	Benzerlik
	100%
	75%
	100%
	75%
	100%
	100%
	75%
	75%
	75%
	75%
	100%
	75%
























Suplementary Table 2. Presence and similarity rates of PP because of FTIR analysis of sediment samples
	PP
	Van1
	Van2
	Van3
	Tatvan1
	Tatvan2
	Tatvan3
	Gevaş1
	Gevaş2
	Gevaş3
	Erciş1
	Erciş2
	Erciş3 

	2956, 2875
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+
	-

	2921, 2840
	+
	+
	+
	+
	+
	+
	-
	+
	-
	+
	+
	-

	1377
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+

	Benzerlik
	100%
	100%
	100%
	100%
	100%
	100%
	67%
	100%
	67%
	100%
	100%
	34%
























Suplementary Table 3. Presence and similarity rates of PET because of FTIR analysis of sediment samples
	PET
	Van1
	Van2
	Van3
	Tatvan1
	Tatvan2
	Tatvan3
	Gevaş1
	Gevaş2
	Gevaş3
	Erciş1
	Erciş2
	Erciş3 

	1721
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+

	1245
	+
	+
	+
	+
	+
	+
	-
	-
	+
	+
	-
	+

	1100
	-
	+
	+
	-
	-
	-
	+
	+
	+
	-
	-
	-

	Benzerlik
	67%
	100%
	100%
	67%
	67%
	67%
	67%
	67%
	100%
	67%
	34%
	67%

























Suplementary Table 4. Presence and similarity rates of PS because of FTIR analysis of sediment samples
	PS
	Van1
	Van2
	Van3
	Tatvan1
	Tatvan2
	Tatvan3
	Gevaş1
	Gevaş2
	Gevaş3
	Erciş1
	Erciş2
	Erciş3 

	3081, 3059,3025
	+
	+
	+
	+
	+
	-
	+
	+
	+
	+
	+
	-

	2923, 2850
	+
	-
	+
	+
	+
	+
	-
	+
	+
	+
	+
	-

	1600, 1492
	+
	+
	-
	+
	+
	+
	+
	+
	+
	+
	+
	+

	756
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+
	+

	698
	+
	+
	+
	+
	+
	+
	-
	+
	+
	-
	+
	+

	Benzerlik
	%100
	%80
	%80
	%100
	%100
	%80
	%60
	%100
	%100
	%80
	%100
	%60














Van

Fiber 	Van 1	Van 2	Van 3	Foam	Van 1	Van 2	Van 3	1	1	Film	Van 1	Van 2	Van 3	2	5	4	Fragment	Van 1	Van 2	Van 3	3	8	3	Microbead	Van 1	Van 2	Van 3	



Tatvan

Fiber 	Tatvan 1	Tatvan 2	Tatvan 3	2	5	Foam	Tatvan 1	Tatvan 2	Tatvan 3	1	Film	Tatvan 1	Tatvan 2	Tatvan 3	2	2	3	Fragment	Tatvan 1	Tatvan 2	Tatvan 3	6	3	6	Microbead	Tatvan 1	Tatvan 2	Tatvan 3	1	1	



Gevaş

Fiber 	Gevaş 1	Gevaş 2 	Gevaş 3	2	1	Foam	Gevaş 1	Gevaş 2 	Gevaş 3	1	Film	Gevaş 1	Gevaş 2 	Gevaş 3	3	3	3	Fragment	Gevaş 1	Gevaş 2 	Gevaş 3	2	3	5	Microbead	Gevaş 1	Gevaş 2 	Gevaş 3	



Erciş

Fiber 	Erciş 1	Erciş 2 	Erciş 3	2	1	Foam	Erciş 1	Erciş 2 	Erciş 3	Film	Erciş 1	Erciş 2 	Erciş 3	1	1	3	Fragment	Erciş 1	Erciş 2 	Erciş 3	1	1	1	Microbead	Erciş 1	Erciş 2 	Erciş 3	



Van

White/Transparent	Van 1	Van 2	Van 3 	2	7	5	Blue	Van 1	Van 2	Van 3 	2	3	2	Yellow	Van 1	Van 2	Van 3 	1	Red	Van 1	Van 2	Van 3 	1	Green	Van 1	Van 2	Van 3 	1	Black	Van 1	Van 2	Van 3 	1	2	



Tatvan

White/Transparent	Tatvan 1	Tatvan 2	Tatvan 3	4	3	10	Blue	Tatvan 1	Tatvan 2	Tatvan 3	3	1	Yellow	Tatvan 1	Tatvan 2	Tatvan 3	1	1	Red	Tatvan 1	Tatvan 2	Tatvan 3	1	1	2	Green	Tatvan 1	Tatvan 2	Tatvan 3	1	Black	Tatvan 1	Tatvan 2	Tatvan 3	1	1	2	



Gevaş

White/Transparent	Gevaş 1	Gevaş 2 	Gevaş 3	2	4	4	Blue	Gevaş 1	Gevaş 2 	Gevaş 3	1	2	3	Yellow	Gevaş 1	Gevaş 2 	Gevaş 3	1	Red	Gevaş 1	Gevaş 2 	Gevaş 3	1	1	Green	Gevaş 1	Gevaş 2 	Gevaş 3	2	Black	Gevaş 1	Gevaş 2 	Gevaş 3	1	1	



Erciş

White/Transparent	Erciş 1	Erciş 2	Erciş 3 	1	2	3	Blue	Erciş 1	Erciş 2	Erciş 3 	1	1	2	Yellow	Erciş 1	Erciş 2	Erciş 3 	1	Red	Erciş 1	Erciş 2	Erciş 3 	Green	Erciş 1	Erciş 2	Erciş 3 	Black	Erciş 1	Erciş 2	Erciş 3 	
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