Supporting Information

Ligand induced chirality in NEA2BiBr5 lead-free perovskite

- Materials: (R)-(+)-α-Methyl-1-naphthalenemethylamine(99%) and (S)-(-)-1-(1-Naphthyl)ethylamine(99%) were purchased from macklin. Hydrobromic acid（48wt%）were purchased from macklin. Bismuth oxide（99%）were purchased from macklin.

- Experimental Section

Synthesis of R/SNEA2BiBr5: Single crystals of RNEA2BiBr5, SNEA2BiBr5 were grown by dissolving a proper amount of Bi2O3 in a large excess of 48% wt% aqueous HBr, heating the mixture to 90°C. After the solid dissolution, the stoichiometric amount of the liquid amine R-/S-NEA was added. The crystals formation was obtained by a slow cooling down to room temperature at 5°C h-1.

Morphology and Structural Characterizations: Single crystal X-ray diffraction (SCXRD) data were collected on a Agilent supernova diffractometer with Mo Kα radiation (λ = 0.71073 Å ) at 150 and 197 K. Using Olex2, the structure was solved with the XS structure solution program using Direct Methods and refined with the XL refinement package using Least Squares minimisation. Powder X-ray diffraction (PXRD) patterns were collected by a D/Max2500PC. UV-vis absorbance spectra were registered with a UV-vis spectrophotometer (UV 2600).FTIR spectra were registered with a Nicolet iS10. The linear circular dichroism (CD) spectra were collected using a JASCO J-1500 CD spectrometer in a transmission geometry,and the ratio of sample to KCl is 1:100.TG spectra were registered with a HITACHI STA200.

FigureS1.The photos of RNEA2BiBr5 andSNEA2BiBr5(from top to bottom).

\

FigureS2.The distorted [BiBr6]3- octahedron unit of RNEA2BiBr5.(left) and SNEA2BiBr5 (right).

RNEA2BiBr5              SNEA2BiBr5

Figure S3. Two crystal structures of R/SNEA2BiBr5 observed from the three axes of abc.

| Table 1 Crystal data and structure refinement for RNEA2BiBr5. |  |
| --- | --- |
| Identification code | RNEA2BiBr5 |
| Empirical formula | C24H28N2BiBr5 |
| Formula weight | 953.01 |
| Temperature/K | 150.00(10) |
| Crystal system | monoclinic |
| Space group | P21 |
| a/Å | 11.8438(5) |
| b/Å | 7.9001(4) |
| c/Å | 15.8023(7) |
| α/° | 90.00 |
| β/° | 104.373(5) |
| γ/° | 90.00 |
| Volume/Å3 | 1432.30(11) |
| Z | 2 |
| ρcalcg/cm3 | 2.210 |
| μ/mm-1 | 13.144 |
| F(000) | 888.0 |
| Crystal size/mm3 | 0.37 × 0.1 × 0.08 |
| Radiation | Mo Kα (λ = 0.71073) |
| 2Θ range for data collection/° | 7.1 to 51.34 |
| Index ranges | -14 ≤ h ≤ 14, -9 ≤ k ≤ 9, -19 ≤ l ≤ 19 |
| Reflections collected | 10434 |
| Independent reflections | 5214 [Rint = 0.0393, Rsigma = 0.0608] |
| Data/restraints/parameters | 5214/1/293 |
| Goodness-of-fit on F2 | 1.014 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0346, wR2 = 0.0684 |
| Final R indexes [all data] | R1 = 0.0404, wR2 = 0.0714 |
| Largest diff. peak/hole / e Å-3 | 1.68/-1.38 |
| Flack parameter | -0.040(8) |

| Table 2 Fractional Atomic Coordinates (×104) and Equivalent Isotropic Displacement Parameters (Å2×103) for RNEA2BiBr5. Ueq is defined as 1/3 of the trace of the orthogonalised UIJ tensor. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Atom | x | y | z | U(eq) |
| Bi1 | 3891.2(3) | 1942.6(5) | 931.6(2) | 19.95(8) |
| Br1 | 3027.7(9) | -166.9(11) | 1940.8(7) | 32.1(2) |
| Br2 | 5051.2(8) | -1075.1(12) | 380.7(6) | 31.6(2) |
| Br3 | 6121.8(8) | 2657.9(11) | 2214.8(6) | 27.2(2) |
| Br4 | 2847.1(8) | 4802.1(11) | 1374.6(6) | 28.9(2) |
| Br5 | 2101.2(8) | 1494.9(12) | -530.7(7) | 35.6(3) |
| C1 | 6586(8) | 8546(11) | 4599(6) | 28(2) |
| C2 | 6925(8) | 10203(12) | 4460(6) | 32(2) |
| C3 | 7279(9) | 11291(13) | 5166(8) | 46(3) |
| C4 | 7343(10) | 10764(16) | 6018(8) | 54(3) |
| C5 | 7008(10) | 9143(15) | 6160(7) | 50(3) |
| C6 | 6644(8) | 7986(13) | 5463(6) | 32(2) |
| C7 | 6298(8) | 6336(13) | 5610(7) | 39(3) |
| C8 | 5927(8) | 5253(13) | 4924(7) | 36(2) |
| C9 | 5867(8) | 5782(12) | 4067(7) | 31(2) |
| C10 | 6205(7) | 7355(10) | 3886(6) | 22(2) |
| C11 | 6181(8) | 7942(12) | 2975(6) | 28(2) |
| C12 | 7401(8) | 7852(13) | 2783(7) | 38(2) |
| C13 | 9700(6) | 2010(14) | 2720(5) | 25.3(18) |
| C14 | 9435(8) | 3674(12) | 2892(6) | 31(2) |
| C15 | 9733(9) | 4314(14) | 3723(7) | 41(3) |
| C16 | 10318(9) | 3308(13) | 4431(7) | 40(3) |
| C17 | 10592(8) | 1671(14) | 4293(6) | 35(2) |
| C18 | 10287(8) | 976(12) | 3448(6) | 30(2) |
| C19 | 10576(8) | -709(12) | 3292(7) | 35(2) |
| C20 | 10311(8) | -1393(12) | 2477(8) | 43(3) |
| C21 | 9749(9) | -377(12) | 1770(7) | 37(2) |
| C22 | 9447(7) | 1241(11) | 1874(6) | 28(2) |
| C23 | 8853(7) | 2262(15) | 1080(6) | 35(3) |
| C24 | 9457(8) | 2269(15) | 343(7) | 45(3) |
| N1 | 7632(6) | 1642(16) | 725(5) | 58(3) |
| N2 | 5389(6) | 6856(12) | 2305(5) | 33.4(17) |

| Table 3 Anisotropic Displacement Parameters (Å2×103) for RNEA2BiBr5. The Anisotropic displacement factor exponent takes the form: -2π2[h2a*2U11+2hka*b*U12+…]. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Atom | U11 | U22 | U33 | U23 | U13 | U12 |
| Bi1 | 19.66(15) | 24.80(16) | 16.12(16) | 0.68(16) | 5.80(11) | 0.46(16) |
| Br1 | 38.0(6) | 33.2(5) | 30.1(6) | 2.7(4) | 17.8(5) | -4.8(4) |
| Br2 | 36.3(6) | 37.4(6) | 21.4(5) | -2.5(4) | 8.0(4) | 12.6(5) |
| Br3 | 25.9(5) | 33.5(5) | 19.6(5) | -0.4(4) | 0.6(4) | -0.4(4) |
| Br4 | 31.2(5) | 29.5(5) | 26.5(6) | -1.4(4) | 8.3(4) | 6.2(4) |
| Br5 | 25.8(5) | 51.2(7) | 25.1(6) | -1.5(4) | -2.6(4) | -1.6(4) |
| C1 | 22(5) | 34(6) | 27(6) | -4(4) | 5(4) | 4(4) |
| C2 | 28(5) | 38(6) | 24(6) | -3(4) | -3(4) | 0(4) |
| C3 | 49(7) | 42(6) | 42(8) | -10(5) | 2(6) | -1(5) |
| C4 | 42(7) | 77(9) | 38(8) | -30(7) | 0(6) | -5(6) |
| C5 | 48(7) | 77(9) | 23(6) | -12(6) | 9(5) | -5(6) |
| C6 | 26(5) | 48(7) | 21(6) | -1(5) | 3(4) | 3(5) |
| C7 | 29(6) | 67(8) | 24(6) | 19(5) | 12(5) | 3(5) |
| C8 | 30(6) | 40(6) | 40(7) | 14(5) | 13(5) | -2(5) |
| C9 | 34(6) | 26(6) | 34(6) | -4(4) | 9(5) | -7(4) |
| C10 | 16(4) | 24(6) | 23(5) | -1(4) | 2(4) | 5(4) |
| C11 | 35(5) | 29(5) | 16(5) | -5(4) | -4(4) | -5(4) |
| C12 | 27(5) | 57(6) | 31(6) | 8(5) | 11(5) | -4(5) |
| C13 | 11(4) | 40(5) | 24(5) | 1(5) | 3(3) | -7(5) |
| C14 | 35(6) | 38(6) | 20(6) | 3(4) | 5(4) | 4(5) |
| C15 | 39(6) | 54(7) | 27(6) | -4(5) | 1(5) | 5(5) |
| C16 | 33(6) | 64(8) | 18(6) | -4(5) | -1(4) | -5(5) |
| C17 | 26(5) | 52(7) | 27(6) | 9(5) | 5(4) | 5(5) |
| C18 | 19(5) | 42(6) | 26(6) | 14(5) | 2(4) | -6(4) |
| C19 | 25(5) | 35(6) | 48(7) | 14(5) | 12(5) | 3(4) |
| C20 | 32(6) | 25(5) | 73(9) | 5(6) | 14(6) | 6(5) |
| C21 | 36(6) | 40(6) | 36(7) | -9(5) | 9(5) | -3(5) |
| C22 | 16(4) | 38(6) | 30(6) | 0(4) | 3(4) | -6(4) |
| C23 | 27(5) | 52(8) | 21(5) | 0(4) | -4(4) | 6(5) |
| C24 | 40(6) | 64(8) | 31(6) | 3(5) | 11(5) | 2(6) |
| N1 | 25(4) | 122(10) | 26(5) | -6(6) | 5(4) | 12(6) |
| N2 | 39(4) | 30(4) | 26(4) | 7(4) | -2(3) | 0(5) |

| Table 4 Bond Lengths for RNEA2BiBr5. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| Bi1 | Br1 | 2.6788(9) |  | C10 | C11 | 1.507(12) |
| Bi1 | Br21 | 3.1002(9) |  | C11 | C12 | 1.550(12) |
| Bi1 | Br2 | 2.9871(9) |  | C11 | N2 | 1.497(11) |
| Bi1 | Br3 | 2.9582(10) |  | C13 | C14 | 1.394(14) |
| Bi1 | Br4 | 2.7481(9) |  | C13 | C18 | 1.441(12) |
| Bi1 | Br5 | 2.7435(10) |  | C13 | C22 | 1.431(12) |
| Br2 | Bi12 | 3.1002(9) |  | C14 | C15 | 1.368(13) |
| C1 | C2 | 1.403(13) |  | C15 | C16 | 1.406(13) |
| C1 | C6 | 1.421(13) |  | C16 | C17 | 1.364(14) |
| C1 | C10 | 1.451(12) |  | C17 | C18 | 1.407(13) |
| C2 | C3 | 1.388(13) |  | C18 | C19 | 1.411(13) |
| C3 | C4 | 1.394(16) |  | C19 | C20 | 1.360(14) |
| C4 | C5 | 1.375(16) |  | C20 | C21 | 1.402(14) |
| C5 | C6 | 1.413(14) |  | C21 | C22 | 1.349(12) |
| C6 | C7 | 1.403(13) |  | C22 | C23 | 1.510(13) |
| C7 | C8 | 1.365(14) |  | C23 | C24 | 1.510(12) |
| C8 | C9 | 1.403(13) |  | C23 | N1 | 1.498(11) |
| C9 | C10 | 1.357(13) |  |  |  |  |

11-X,1/2+Y,-Z; 21-X,-1/2+Y,-Z

| Table 5 Bond Angles for RNEA2BiBr5. |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| Br1 | Bi1 | Br21 | 171.81(3) |  | C7 | C8 | C9 | 120.6(9) |
| Br1 | Bi1 | Br2 | 87.03(3) |  | C10 | C9 | C8 | 121.9(10) |
| Br1 | Bi1 | Br3 | 96.82(3) |  | C1 | C10 | C11 | 118.1(8) |
| Br1 | Bi1 | Br4 | 95.59(3) |  | C9 | C10 | C1 | 118.8(8) |
| Br1 | Bi1 | Br5 | 95.27(3) |  | C9 | C10 | C11 | 123.1(8) |
| Br2 | Bi1 | Br21 | 85.225(11) |  | C10 | C11 | C12 | 112.0(7) |
| Br3 | Bi1 | Br21 | 85.50(3) |  | N2 | C11 | C10 | 111.1(7) |
| Br3 | Bi1 | Br2 | 87.43(3) |  | N2 | C11 | C12 | 106.7(8) |
| Br4 | Bi1 | Br21 | 92.13(3) |  | C14 | C13 | C18 | 117.8(8) |
| Br4 | Bi1 | Br2 | 177.31(3) |  | C14 | C13 | C22 | 125.3(9) |
| Br4 | Bi1 | Br3 | 92.87(3) |  | C22 | C13 | C18 | 116.9(10) |
| Br5 | Bi1 | Br21 | 81.82(3) |  | C15 | C14 | C13 | 121.3(9) |
| Br5 | Bi1 | Br2 | 88.10(3) |  | C14 | C15 | C16 | 120.9(10) |
| Br5 | Bi1 | Br3 | 166.87(3) |  | C17 | C16 | C15 | 119.9(10) |
| Br5 | Bi1 | Br4 | 91.03(3) |  | C16 | C17 | C18 | 120.4(9) |
| Bi1 | Br2 | Bi12 | 152.82(4) |  | C17 | C18 | C13 | 119.7(9) |
| C2 | C1 | C6 | 119.6(9) |  | C17 | C18 | C19 | 121.2(9) |
| C2 | C1 | C10 | 122.0(9) |  | C19 | C18 | C13 | 119.1(10) |
| C6 | C1 | C10 | 118.4(9) |  | C20 | C19 | C18 | 122.1(10) |
| C3 | C2 | C1 | 119.5(10) |  | C19 | C20 | C21 | 118.7(9) |
| C2 | C3 | C4 | 121.6(10) |  | C22 | C21 | C20 | 122.2(10) |
| C5 | C4 | C3 | 119.1(10) |  | C13 | C22 | C23 | 119.7(9) |
| C4 | C5 | C6 | 121.3(11) |  | C21 | C22 | C13 | 121.1(9) |
| C5 | C6 | C1 | 118.7(10) |  | C21 | C22 | C23 | 119.2(9) |
| C7 | C6 | C1 | 120.2(10) |  | C24 | C23 | C22 | 115.5(8) |
| C7 | C6 | C5 | 121.1(10) |  | N1 | C23 | C22 | 110.1(8) |
| C8 | C7 | C6 | 120.0(9) |  | N1 | C23 | C24 | 108.1(8) |

11-X,1/2+Y,-Z; 21-X,-1/2+Y,-Z

| Table 6 Hydrogen Bonds for RNEA2BiBr5. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| D | H | A | d(D-H)/Å | d(H-A)/Å | d(D-A)/Å | D-H-A/° |
| N1 | H1B | Br3 | 0.91 | 2.50 | 3.387(8) | 166.6 |
| N2 | H2A | Br3 | 0.91 | 2.54 | 3.440(9) | 169.1 |

| Table 7 Torsion Angles for RNEA2BiBr5. |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A | B | C | D | Angle/˚ |  | A | B | C | D | Angle/˚ |
| Br1 | Bi1 | Br2 | Bi11 | 153.24(9) |  | C10 | C1 | C6 | C5 | -179.7(8) |
| Br22 | Bi1 | Br2 | Bi11 | -24.09(7) |  | C10 | C1 | C6 | C7 | -2.3(14) |
| Br3 | Bi1 | Br2 | Bi11 | -109.79(8) |  | C13 | C14 | C15 | C16 | 0.0(15) |
| Br4 | Bi1 | Br2 | Bi11 | -13.3(7) |  | C13 | C18 | C19 | C20 | -0.4(13) |
| Br5 | Bi1 | Br2 | Bi11 | 57.86(8) |  | C13 | C22 | C23 | C24 | 127.4(9) |
| C1 | C2 | C3 | C4 | 2.1(16) |  | C13 | C22 | C23 | N1 | -109.8(9) |
| C1 | C6 | C7 | C8 | 1.4(14) |  | C14 | C13 | C18 | C17 | -1.2(12) |
| C1 | C10 | C11 | C12 | 81.5(10) |  | C14 | C13 | C18 | C19 | -179.4(8) |
| C1 | C10 | C11 | N2 | -159.3(7) |  | C14 | C13 | C22 | C21 | 179.3(9) |
| C2 | C1 | C6 | C5 | 2.1(14) |  | C14 | C13 | C22 | C23 | 0.4(12) |
| C2 | C1 | C6 | C7 | 179.5(9) |  | C14 | C15 | C16 | C17 | -0.2(16) |
| C2 | C1 | C10 | C9 | -178.7(8) |  | C15 | C16 | C17 | C18 | -0.4(15) |
| C2 | C1 | C10 | C11 | 0.0(13) |  | C16 | C17 | C18 | C13 | 1.1(13) |
| C2 | C3 | C4 | C5 | -2.3(17) |  | C16 | C17 | C18 | C19 | 179.2(9) |
| C3 | C4 | C5 | C6 | 2.5(17) |  | C17 | C18 | C19 | C20 | -178.6(9) |
| C4 | C5 | C6 | C1 | -2.4(16) |  | C18 | C13 | C14 | C15 | 0.7(13) |
| C4 | C5 | C6 | C7 | -179.7(10) |  | C18 | C13 | C22 | C21 | 0.0(12) |
| C5 | C6 | C7 | C8 | 178.7(10) |  | C18 | C13 | C22 | C23 | -178.8(7) |
| C6 | C1 | C2 | C3 | -2.0(14) |  | C18 | C19 | C20 | C21 | 1.0(14) |
| C6 | C1 | C10 | C9 | 3.2(13) |  | C19 | C20 | C21 | C22 | -1.1(15) |
| C6 | C1 | C10 | C11 | -178.2(8) |  | C20 | C21 | C22 | C13 | 0.6(14) |
| C6 | C7 | C8 | C9 | -1.2(15) |  | C20 | C21 | C22 | C23 | 179.4(8) |
| C7 | C8 | C9 | C10 | 2.2(15) |  | C21 | C22 | C23 | C24 | -51.4(12) |
| C8 | C9 | C10 | C1 | -3.1(13) |  | C21 | C22 | C23 | N1 | 71.3(11) |
| C8 | C9 | C10 | C11 | 178.3(9) |  | C22 | C13 | C14 | C15 | -178.5(9) |
| C9 | C10 | C11 | C12 | -99.9(10) |  | C22 | C13 | C18 | C17 | 178.1(8) |
| C9 | C10 | C11 | N2 | 19.3(12) |  | C22 | C13 | C18 | C19 | -0.1(11) |
| C10 | C1 | C2 | C3 | 179.9(8) |  |  |  |  |  |  |

11-X,-1/2+Y,-Z; 21-X,1/2+Y,-Z

| Table 8 Hydrogen Atom Coordinates (Å×104) and Isotropic Displacement Parameters (Å2×103) for RNEA2BiBr5. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Atom | x | y | z | U(eq) |
| H2 | 6912 | 10578 | 3886 | 38 |
| H3 | 7484 | 12423 | 5065 | 55 |
| H4 | 7615 | 11514 | 6495 | 65 |
| H5 | 7021 | 8794 | 6737 | 59 |
| H7 | 6322 | 5972 | 6188 | 47 |
| H8 | 5708 | 4130 | 5029 | 43 |
| H9 | 5580 | 5017 | 3599 | 37 |
| H11 | 5895 | 9137 | 2902 | 34 |
| H12A | 7684 | 6683 | 2850 | 57 |
| H12B | 7943 | 8583 | 3194 | 57 |
| H12C | 7346 | 8235 | 2185 | 57 |
| H14 | 9040 | 4377 | 2424 | 38 |
| H15 | 9543 | 5452 | 3822 | 50 |
| H16 | 10522 | 3769 | 5004 | 48 |
| H17 | 10991 | 996 | 4772 | 42 |
| H19 | 10968 | -1386 | 3772 | 43 |
| H20 | 10502 | -2536 | 2389 | 52 |
| H21 | 9574 | -846 | 1198 | 45 |
| H23 | 8807 | 3461 | 1272 | 42 |
| H24A | 9454 | 1121 | 107 | 67 |
| H24B | 10262 | 2655 | 563 | 67 |
| H24C | 9044 | 3034 | -119 | 67 |
| H1A | 7274 | 2284 | 258 | 87 |
| H1B | 7232 | 1722 | 1147 | 87 |
| H1C | 7648 | 543 | 556 | 87 |
| H2A | 5676 | 5783 | 2339 | 50 |
| H2B | 5344 | 7283 | 1763 | 50 |
| H2C | 4666 | 6843 | 2408 | 50 |

| Table S9 Crystal data and structure refinement for SNEA2BiBr5 |  |
| --- | --- |
| Identification code | SNEA2BiBr5 |
| Empirical formula | C24H28N2BiBr5 |
| Formula weight | 953.01 |
| Temperature/K | 197(30) |
| Crystal system | monoclinic |
| Space group | P21 |
| a/Å | 11.8780(4) |
| b/Å | 7.9257(2) |
| c/Å | 15.8128(5) |
| α/° | 90.00 |
| β/° | 104.541(3) |
| γ/° | 90.00 |
| Volume/Å3 | 1440.96(8) |
| Z | 2 |
| ρcalcmg/mm3 | 2.196 |
| m/mm-1 | 13.065 |
| F(000) | 888.0 |
| Crystal size/mm3 | 0.41 × 0.1 × 0.08 |
| 2Θ range for data collection | 6.92 to 51.36° |
| Index ranges | -14 ≤ h ≤ 14, -9 ≤ k ≤ 9, -19 ≤ l ≤ 18 |
| Reflections collected | 9561 |
| Independent reflections | 4897[R(int) = 0.0460] |
| Data/restraints/parameters | 4897/1/293 |
| Goodness-of-fit on F2 | 1.027 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0585, wR2 = 0.1417 |
| Final R indexes [all data] | R1 = 0.0637, wR2 = 0.1482 |
| Largest diff. peak/hole / e Å-3 | 2.30/-2.66 |
| Flack parameter | -0.067(13) |

| Table S10 Fractional Atomic Coordinates (×104) and Equivalent Isotropic Displacement Parameters (Å2×103) for SNEA2BiBr5. Ueq is defined as 1/3 of of the trace of the orthogonalised UIJ tensor. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Atom | x | y | z | U(eq) |
| Bi1 | 3896.8(2) | 2383.6(4) | 930.46(15) | 19.19(6) |
| Br2 | 2853.3(8) | -466.4(10) | 1373.4(5) | 29.8(2) |
| Br5 | 6129.4(7) | 1667.4(11) | 2215.3(5) | 27.7(2) |
| Br1 | 3040.5(8) | 4496.5(11) | 1938.6(6) | 33.6(2) |
| Br4 | 4938.2(8) | 385.4(11) | -378.5(5) | 32.5(2) |
| Br3 | 2104.9(7) | 2842.4(12) | -536.2(6) | 37.3(3) |
| C19 | -577(7) | 10046(12) | 6709(6) | 36(2) |
| C17 | -590(7) | 7649(13) | 5710(6) | 39(3) |
| C6 | 6197(6) | 6960(10) | 3883(5) | 22(2) |
| C16 | -326(9) | 6059(13) | 5566(5) | 41(3) |
| C9 | 6928(8) | 4108(12) | 4473(5) | 35(3) |
| C23 | 1128(6) | 7034(11) | 8926(5) | 31(3) |
| C24 | 527(8) | 7069(17) | 9658(6) | 56(3) |
| C12 | 7012(8) | 5219(14) | 6174(6) | 43(3) |
| C22 | 551(7) | 8095(11) | 8143(6) | 28(2) |
| C18 | -282(7) | 8384(11) | 6563(6) | 30(2) |
| C14 | 579(8) | 5675(12) | 7112(6) | 36(2) |
| C10 | 7295(9) | 3040(13) | 5179(7) | 47(3) |
| C4 | 6644(8) | 6364(13) | 5474(6) | 37(3) |
| C20 | -314(8) | 10746(13) | 7510(7) | 46(3) |
| C5 | 6571(7) | 5795(12) | 4589(5) | 28(2) |
| N1 | 2361(6) | 7639(16) | 9256(5) | 63(3) |
| C8 | 7412(7) | 6452(13) | 2800(5) | 35(2) |
| C21 | 230(7) | 9730(12) | 8249(6) | 36(2) |
| C15 | 262(9) | 5045(15) | 6250(6) | 45(3) |
| C11 | 7332(9) | 3619(16) | 6034(7) | 59(3) |
| C1 | 5865(8) | 8530(12) | 4071(5) | 32(2) |
| N2 | 5399(6) | 7484(11) | 2294(4) | 38(2) |
| C13 | 283(6) | 7353(13) | 7274(5) | 24.8(18) |
| C7 | 6193(7) | 6398(10) | 2970(5) | 25(2) |
| C2 | 5921(9) | 9088(14) | 4920(6) | 44(3) |
| C3 | 6278(8) | 7995(14) | 5594(6) | 47(3) |

| Table S11 Anisotropic Displacement Parameters (Å2×103) for SNEA2BiBr5. The Anisotropic displacement factor exponent takes the form: -2π2[h2a*2U11+...+2hka×b×U12] |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Atom | U11 | U22 | U33 | U23 | U13 | U12 |
| Bi1 | 20.81(11) | 22.09(12) | 16.32(11) | -0.77(11) | 7.76(9) | -0.60(12) |
| Br2 | 35.7(4) | 26.6(4) | 28.9(4) | 1.8(3) | 11.3(3) | -8.7(3) |
| Br5 | 28.0(4) | 33.2(4) | 19.9(3) | 0.4(3) | 2.4(3) | -0.3(3) |
| Br1 | 42.6(4) | 32.0(4) | 32.4(4) | -4.6(3) | 20.8(3) | 6.2(4) |
| Br4 | 40.3(4) | 36.1(5) | 22.5(4) | -4.3(3) | 10.6(3) | 13.3(4) |
| Br3 | 27.4(4) | 52.1(6) | 28.1(4) | 1.2(4) | -0.9(3) | 2.3(4) |
| C19 | 30(4) | 31(5) | 52(5) | 23(4) | 19(4) | 11(4) |
| C17 | 36(4) | 50(6) | 32(4) | 19(4) | 11(3) | 5(4) |
| C6 | 14(3) | 26(5) | 25(3) | 2(3) | 2(3) | 9(3) |
| C16 | 47(5) | 62(6) | 12(4) | -9(4) | 4(4) | -6(5) |
| C9 | 38(5) | 46(5) | 18(4) | 3(4) | -1(4) | -10(4) |
| C23 | 22(4) | 31(6) | 35(4) | -5(3) | -1(3) | 8(3) |
| C24 | 45(5) | 94(9) | 33(4) | 4(6) | 14(4) | -17(6) |
| C12 | 41(5) | 64(7) | 26(4) | 10(4) | 12(4) | 11(5) |
| C22 | 18(3) | 34(4) | 34(4) | -8(4) | 6(3) | -5(3) |
| C18 | 17(3) | 41(5) | 35(4) | 19(4) | 11(3) | -3(4) |
| C14 | 32(4) | 35(5) | 38(5) | -10(4) | 5(4) | 5(4) |
| C10 | 50(6) | 29(5) | 57(6) | 11(4) | 5(5) | 7(4) |
| C4 | 34(4) | 48(6) | 31(4) | 4(4) | 11(4) | 1(4) |
| C20 | 35(5) | 28(5) | 73(7) | 6(5) | 9(5) | 9(4) |
| C5 | 20(4) | 36(5) | 28(4) | 2(4) | 5(3) | -10(3) |
| N1 | 20(3) | 141(9) | 26(4) | -27(5) | 4(3) | -8(5) |
| C8 | 36(4) | 50(6) | 24(4) | 3(4) | 16(3) | 5(4) |
| C21 | 24(4) | 40(5) | 48(5) | -19(4) | 16(4) | -9(4) |
| C15 | 48(6) | 53(6) | 31(5) | -8(4) | 3(4) | 1(5) |
| C11 | 45(6) | 90(8) | 39(5) | 38(5) | 7(5) | 13(6) |
| C1 | 30(4) | 43(5) | 19(4) | 2(3) | 2(3) | 9(4) |
| N2 | 49(4) | 34(4) | 30(3) | -3(4) | 5(3) | 5(4) |
| C13 | 15(3) | 32(4) | 28(3) | 0(4) | 5(3) | -4(4) |
| C7 | 31(4) | 17(4) | 26(4) | 6(3) | 5(3) | 1(3) |
| C2 | 60(6) | 45(5) | 32(4) | -7(4) | 21(4) | 9(5) |
| C3 | 40(5) | 79(8) | 27(4) | -15(4) | 18(4) | 11(5) |

| Table S12 Bond Lengths for SNEA2BiBr5. |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Atom | Atom | Length/Å |  | Atom | Atom | Length/Å |
| Bi1 | Br2 | 2.7505(9) |  | C23 | C22 | 1.512(12) |
| Bi1 | Br5 | 2.9626(8) |  | C23 | N1 | 1.504(10) |
| Bi1 | Br1 | 2.6823(10) |  | C12 | C4 | 1.413(13) |
| Bi1 | Br41 | 2.9906(9) |  | C12 | C11 | 1.357(17) |
| Bi1 | Br4 | 3.0996(9) |  | C22 | C21 | 1.373(12) |
| Bi1 | Br3 | 2.7500(8) |  | C22 | C13 | 1.454(11) |
| Br4 | Bi12 | 2.9906(9) |  | C18 | C13 | 1.415(11) |
| C19 | C18 | 1.397(13) |  | C14 | C15 | 1.411(13) |
| C19 | C20 | 1.346(14) |  | C14 | C13 | 1.416(14) |
| C17 | C16 | 1.332(14) |  | C10 | C11 | 1.418(16) |
| C17 | C18 | 1.430(12) |  | C4 | C5 | 1.452(13) |
| C6 | C5 | 1.431(11) |  | C4 | C3 | 1.392(15) |
| C6 | C1 | 1.361(12) |  | C20 | C21 | 1.433(14) |
| C6 | C7 | 1.509(12) |  | C8 | C7 | 1.538(13) |
| C16 | C15 | 1.387(13) |  | C1 | C2 | 1.399(13) |
| C9 | C10 | 1.381(14) |  | N2 | C7 | 1.506(10) |
| C9 | C5 | 1.429(14) |  | C2 | C3 | 1.356(14) |
| C23 | C24 | 1.505(13) |  |  |  |  |

11-X,1/2+Y,-Z; 21-X,-1/2+Y,-Z

Table S13 Bond Angles for SNEA2BiBr5.

| Atom | Atom | Atom | Angle/˚ |  | Atom | Atom | Atom | Angle/˚ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Br2 | Bi1 | Br5 | 92.92(2) |  | C21 | C22 | C23 | 120.5(8) |
| Br2 | Bi1 | Br4 | 91.80(3) |  | C21 | C22 | C13 | 119.7(8) |
| Br2 | Bi1 | Br41 | 177.18(3) |  | C13 | C22 | C23 | 119.8(8) |
| Br5 | Bi1 | Br4 | 85.50(2) |  | C19 | C18 | C17 | 121.6(8) |
| Br5 | Bi1 | Br41 | 87.28(2) |  | C19 | C18 | C13 | 120.1(8) |
| Br1 | Bi1 | Br2 | 95.68(3) |  | C13 | C18 | C17 | 118.2(8) |
| Br1 | Bi1 | Br5 | 96.88(3) |  | C15 | C14 | C13 | 119.3(8) |
| Br1 | Bi1 | Br4 | 172.02(3) |  | C9 | C10 | C11 | 120.0(10) |
| Br1 | Bi1 | Br41 | 87.08(3) |  | C12 | C4 | C5 | 119.2(9) |
| Br1 | Bi1 | Br3 | 95.16(3) |  | C3 | C4 | C12 | 122.3(9) |
| Br41 | Bi1 | Br4 | 85.418(10) |  | C3 | C4 | C5 | 118.4(8) |
| Br3 | Bi1 | Br2 | 91.18(3) |  | C19 | C20 | C21 | 119.1(9) |
| Br3 | Bi1 | Br5 | 166.83(3) |  | C6 | C5 | C4 | 118.9(8) |
| Br3 | Bi1 | Br4 | 81.87(3) |  | C9 | C5 | C6 | 123.3(8) |
| Br3 | Bi1 | Br41 | 88.03(3) |  | C9 | C5 | C4 | 117.8(8) |
| Bi12 | Br4 | Bi1 | 153.23(3) |  | C22 | C21 | C20 | 120.9(9) |
| C20 | C19 | C18 | 122.4(8) |  | C16 | C15 | C14 | 120.5(10) |
| C16 | C17 | C18 | 122.1(8) |  | C12 | C11 | C10 | 121.0(10) |
| C5 | C6 | C7 | 118.8(7) |  | C6 | C1 | C2 | 123.6(8) |
| C1 | C6 | C5 | 118.0(8) |  | C18 | C13 | C22 | 117.7(9) |
| C1 | C6 | C7 | 123.2(7) |  | C18 | C13 | C14 | 119.2(8) |
| C17 | C16 | C15 | 120.6(8) |  | C14 | C13 | C22 | 123.1(7) |
| C10 | C9 | C5 | 120.9(9) |  | C6 | C7 | C8 | 112.5(6) |
| C24 | C23 | C22 | 114.5(7) |  | N2 | C7 | C6 | 111.2(7) |
| N1 | C23 | C24 | 109.7(7) |  | N2 | C7 | C8 | 108.0(7) |
| N1 | C23 | C22 | 108.0(8) |  | C3 | C2 | C1 | 118.8(10) |
| C11 | C12 | C4 | 121.1(9) |  | C2 | C3 | C4 | 122.2(9) |

11-X,1/2+Y,-Z; 21-X,-1/2+Y,-Z

| Table S14 Torsion Angles for SNEA2BiBr5. |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| A | B | C | D | Angle/˚ |  | A | B | C | D | Angle/˚ |
| Br2 | Bi1 | Br4 | Bi11 | -41.75(7) |  | C20 | C19 | C18 | C17 | 178.6(9) |
| Br5 | Bi1 | Br4 | Bi11 | 51.05(7) |  | C20 | C19 | C18 | C13 | 1.9(14) |
| Br1 | Bi1 | Br4 | Bi11 | 158.70(15) |  | C5 | C6 | C1 | C2 | 3.1(13) |
| Br42 | Bi1 | Br4 | Bi11 | 138.67(8) |  | C5 | C6 | C7 | C8 | -79.3(9) |
| Br3 | Bi1 | Br4 | Bi11 | -132.68(7) |  | C5 | C6 | C7 | N2 | 159.5(7) |
| C19 | C18 | C13 | C22 | -0.8(12) |  | C5 | C9 | C10 | C11 | -0.6(15) |
| C19 | C18 | C13 | C14 | -179.7(8) |  | C5 | C4 | C3 | C2 | -3.8(15) |
| C19 | C20 | C21 | C22 | 4.1(15) |  | N1 | C23 | C22 | C21 | -74.1(10) |
| C17 | C16 | C15 | C14 | 0.7(16) |  | N1 | C23 | C22 | C13 | 108.8(9) |
| C17 | C18 | C13 | C22 | -177.7(8) |  | C21 | C22 | C13 | C18 | 1.5(12) |
| C17 | C18 | C13 | C14 | 3.5(12) |  | C21 | C22 | C13 | C14 | -179.7(8) |
| C6 | C1 | C2 | C3 | -2.9(16) |  | C15 | C14 | C13 | C22 | 178.6(9) |
| C16 | C17 | C18 | C19 | -179.2(9) |  | C15 | C14 | C13 | C18 | -2.6(13) |
| C16 | C17 | C18 | C13 | -2.4(13) |  | C11 | C12 | C4 | C5 | 2.0(15) |
| C9 | C10 | C11 | C12 | -0.1(17) |  | C11 | C12 | C4 | C3 | 178.0(10) |
| C23 | C22 | C21 | C20 | 179.8(8) |  | C1 | C6 | C5 | C9 | 179.3(8) |
| C23 | C22 | C13 | C18 | 178.6(7) |  | C1 | C6 | C5 | C4 | -3.5(12) |
| C23 | C22 | C13 | C14 | -2.6(12) |  | C1 | C6 | C7 | C8 | 100.5(9) |
| C24 | C23 | C22 | C21 | 48.3(11) |  | C1 | C6 | C7 | N2 | -20.8(11) |
| C24 | C23 | C22 | C13 | -128.7(9) |  | C1 | C2 | C3 | C4 | 3.2(16) |
| C12 | C4 | C5 | C6 | 180.0(8) |  | C13 | C22 | C21 | C20 | -3.1(13) |
| C12 | C4 | C5 | C9 | -2.7(13) |  | C13 | C14 | C15 | C16 | 0.5(15) |
| C12 | C4 | C3 | C2 | -179.8(10) |  | C7 | C6 | C5 | C9 | -0.9(12) |
| C18 | C19 | C20 | C21 | -3.5(15) |  | C7 | C6 | C5 | C4 | 176.3(7) |
| C18 | C17 | C16 | C15 | 0.3(15) |  | C7 | C6 | C1 | C2 | -176.7(9) |
| C10 | C9 | C5 | C6 | 179.2(9) |  | C3 | C4 | C5 | C6 | 3.9(13) |
| C10 | C9 | C5 | C4 | 2.0(13) |  | C3 | C4 | C5 | C9 | -178.8(9) |
| C4 | C12 | C11 | C10 | -0.6(16) |  |  |  |  |  |  |

11-X,-1/2+Y,-Z; 21-X,1/2+Y,-Z

| Table S15 Hydrogen Atom Coordinates (Å×104) and Isotropic Displacement Parameters (Å2×103) for SNEA2BiBr5. |  |  |  |  |
| --- | --- | --- | --- | --- |
| Atom | x | y | z | U(eq) |
| H19 | -977 | 10706 | 6225 | 44 |
| H17 | -996 | 8316 | 5231 | 47 |
| H16 | -542 | 5615 | 4989 | 50 |
| H9 | 6914 | 3714 | 3903 | 42 |
| H23 | 1149 | 5839 | 8728 | 37 |
| H24A | 931 | 6313 | 10126 | 85 |
| H24B | -280 | 6697 | 9438 | 85 |
| H24C | 540 | 8221 | 9885 | 85 |
| H12 | 7037 | 5576 | 6752 | 52 |
| H14 | 988 | 4980 | 7578 | 43 |
| H10 | 7523 | 1918 | 5092 | 56 |
| H20 | -488 | 11899 | 7584 | 55 |
| H1A | 2363 | 8772 | 9349 | 94 |
| H1B | 2766 | 7408 | 8852 | 94 |
| H1C | 2699 | 7104 | 9765 | 94 |
| H8A | 7364 | 6084 | 2200 | 53 |
| H8B | 7933 | 5698 | 3211 | 53 |
| H8C | 7714 | 7607 | 2880 | 53 |
| H21 | 372 | 10194 | 8820 | 43 |
| H15 | 453 | 3917 | 6137 | 54 |
| H11 | 7583 | 2877 | 6517 | 70 |
| H1 | 5580 | 9288 | 3601 | 38 |
| H2A | 4654 | 7365 | 2339 | 57 |
| H2B | 5445 | 7161 | 1752 | 57 |
| H2C | 5618 | 8583 | 2383 | 57 |
| H7 | 5902 | 5210 | 2892 | 30 |
| H2 | 5713 | 10213 | 5023 | 53 |
| H3 | 6278 | 8354 | 6168 | 56 |