Supporting Information

Oil well produced water pollutants photodegradation using an innovative double Z-scheme ternary heterostructure of MIL-101(Cr)/Fe3O4-SiO2/nanorod-graphitic carbon nitride

Parisa Azmoon1, Mehrdad Farhadian 1*, Alireza Pendashteh2,3, Shahram Tangestaninejad4

1 Department of Chemical Engineering, Faculty of Engineering, University of Isfahan, Isfahan, Iran

2 Department of Chemical Engineering, Faculty of Engineering, University of Guilan, Rasht, Iran

3 Department of Water and Environmental Engineering, Caspian Sea Basin Research Center, University of Guilan, Rasht, Iran

4 Department of Chemistry, Catalysis Division, University of Isfahan, Iran

* Corresponding authors:

Tel.: +98 313 793 7032; E-mail address: m.farhadian@eng.ui.ac.ir (Mehrdad Farhadian).

(a)

153.9 °

151.7 °

150.4 °

(b)

(c) 5.7

Fig. S1 a wettability of the ternary composite nanoparticles, b magnetic saturation values, and c point of zero charges (pHpzc) of synthesized nanoparticles.

| (b) | (a) |
| --- | --- |

Fig. S2 Plots of a normal probability vs. residuals, and b predicted vs. actual values.

(d)

(c)

(a)

(b)

Fig. S3 2D plots of the effect of a pH, b illumination time, c catalyst dosage, and d pollutant initial concentration on the S-OPW removal efficiency.

(a)

Fig. S4 Real oilfield-produced water treatment by synthesized nanoparticles.

| (b) |  |
| --- | --- |
| (c) |  |

(b)

(a)

Fig. S5 a Pseudo-first-order, b pseudo-second-order, and c intraparticle diffusion kinetic models plots for S-OPW adsorption onto as-prepared nanoparticles.

| (b) | (a) |
| --- | --- |

Fig. S6 a Langmuir and b Freundlich isotherm plots for S-OPW adsorption onto as-prepared nanoparticles.

Fig. S7 Photocatalytic degradation kinetic of S-OPW by as-prepared nanoparticles.

|  | S-OPW (Binak, Bushehr, Iran) (weight percentage) | R-OPW (Sarvak Azar Oilfield, Ilam, Iran) (weight percentage) |
| --- | --- | --- |
| Saturated | 49.1 | 43.1 |
| Aromatic | 32.3 | 33.8 |
| Resin | 12.2 | 11.3 |
| Asphaltene | 6.4 | 11.8 |

Table S1 Characterization of the crude oil in the real and synthetic produce water.

| Source | Sum of Squares | df | Mean Square | F-value | p-value |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 14310.84 | 14 | 1022.2 | 2489.8 | < 0.0001 | significant |
| A-pH | 10292.04 | 1 | 10292.04 | 25068.57 | < 0.0001 | significant |
| B-Time | 590.04 | 1 | 590.04 | 1437.18 | < 0.0001 | significant |
| C-g | 100.04 | 1 | 100.04 | 243.67 | < 0.0001 | significant |
| D-C0 | 1683.38 | 1 | 1683.38 | 4100.24 | < 0.0001 | significant |
| AB | 22.56 | 1 | 22.56 | 54.96 | < 0.0001 | significant |
| AC | 22.56 | 1 | 22.56 | 54.96 | < 0.0001 | significant |
| AD | 5.06 | 1 | 5.06 | 12.33 | 0.0031 | significant |
| BC | 1.56 | 1 | 1.56 | 3.81 | 0.07 | not significant |
| BD | 0.0625 | 1 | 0.0625 | 0.1522 | 0.7019 | not significant |
| CD | 14.06 | 1 | 14.06 | 34.25 | < 0.0001 | significant |
| A² | 658 | 1 | 658 | 1602.71 | < 0.0001 | significant |
| B² | 836.64 | 1 | 836.64 | 2037.83 | < 0.0001 | significant |
| C² | 41.3 | 1 | 41.3 | 100.6 | < 0.0001 | significant |
| D² | 14.5 | 1 | 14.5 | 35.32 | < 0.0001 | significant |
| Residual | 6.16 | 15 | 0.4106 |  |  |  |
| Lack of Fit | 5.08 | 10 | 0.5083 | 2.36 | 0.1773 | not significant |
| Pure Error | 1.07 | 5 | 0.215 |  |  |  |

Table S2 ANOVA for Quadratic Model response for S-OPW using MIL-Cr/F@S/nr-GCN (20 wt%) ternary heterostructure.

| Adsorbent | qe,exp (mg/g) | Pseudo-first-order |  |  | Pseudo-second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | qe | k1 | R2 | qe | k2 | R2 |
| nr-GCN | 904 | 281 | 0.0248 | 0.851 | 909 | 0.0004 | 0.9996 |
| MIL-Cr/F@S-OA (35 wt%) | 1044 | 296 | 0.023 | 0.793 | 1250 | 0.0004 | 0.9998 |
| MIL-Cr/F@S/nr-GCN-OA (20 wt%) | 1388 | 169 | 0.0191 | 0.644 | 1250 | 0.0007 | 0.9998 |

Table S3 Pseudo-first-order and Pseudo-second-order kinetic model constants for S-OPW adsorption onto as-prepared nanoparticles.

| Adsorbent | Intraparticle-diffusion (part-1) |  |  | Intraparticle-diffusion (part-2) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | kp | C | R2 | kp | C | R2 |
| nr-GCN | 148.4 | 113.2 | 0.9127 | 7.5 | 803.3 | 0.997 |
| MIL-Cr/F@S-OA (35 wt%) | 202.3 | 225.9 | 0.8313 | 8.61 | 1138.9 | 0.9899 |
| MIL-Cr/F@S/nr-GCN-OA (20 wt%) | 200.4 | 324.2 | 0.7031 | 8.17 | 1161.2 | 0.9911 |

Table S4 Intraparticle-diffusion kinetic model constants for S-OPW adsorption onto as-prepared nanoparticles.

| Adsorbent | qe,exp | Langmuir |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | qmax | k1 | R2 | 1/n | kf | R2 |
| nr-GCN | 2070 | 2500 | 0.004 | 0.953 | 0.46 | 86.7 | 0.996 |
| MIL-Cr/F@S-OA (35 wt%) | 2634 | 2500 | 0.0127 | 0.992 | 0.304 | 317.9 | 0.997 |
| MIL-Cr/F@S/nr-GCN-OA (20 wt%) | 4220 | 5000 | 0.0116 | 0.931 | 0.407 | 328.9 | 0.979 |

Table S5 Isotherm study of S-OPW adsorption onto as-prepared nanoparticles.