Supplementary Information

Steering diffusion selectivity of chemical isomers within aligned nanochannels of metal-organic framework thin film

Tanmoy Maity, Susmita Sarkar, Susmita Kundu, Suvendu Panda, Arighna Sarkar, Kalyaneswar Mandal, Soumya Ghosh,* Jagannath Mondal* and Ritesh Haldar*

Tata Institute of Fundamental Research Hyderabad, Gopanpally, Hyderabad 500046, Telangana, India

Figure S1: 1BP (red) and 2BP (green) vapour uptake profiles at 298 K for Cu(bdc)(azbpy) thin film; black line is the exponential fit.

Figure S2: Mean square displacement (MSD) plots of 1BP and 2BP molecules along the [001] direction of rigid (a-b) and flexible (c-d) Cu(bdc)(azbpy) MOF at (a and c) high concentration gradient and (b and d) low concentration gradient.

Table S1: Diffusivity values of Cu(bdc)(Azbpy) and Cu(Br2-bdc)(Azbpy) MOFs from MSD calculations.

| Guest loading % | Guest molecules | Rigid Cu(bdc)(Azbpy) MOF |  |
| --- | --- | --- | --- |
|  |  | Diffusivity (x 10-9 m2/s) | Error value (x 10-9 m2/s) |
| 0 | 1BP | 0.0004 | ±0.0001 |
|  | 2BP | 0.0003 | ±0.0001 |
| 20 | 1BP | 0.1005 | ±0.0290 |
|  | 2BP | 0.0121 | ±0.0024 |
|  |  | Flexible Cu(bdc)(Azbpy) MOF |  |
| 0 | 1BP | 0.0015 | ±0.0023 |
|  | 2BP | 0.0049 | ±0.0019 |
| 20 | 1BP | 1.2921 | ±0.0398 |
|  | 2BP | 2.1047 | ±0.0595 |
|  |  | Flexible Cu(Br2-bdc)(Azbpy) MOF |  |
| 0 | 1BP | 0.0047 | ±0.0017 |
|  | 2BP | 0.0036 | ±0.0024 |

Figure S3: Pair correlation function of 1BP and 2BP with respect to three different parts of the Cu(bdc)(azbpy) MOF (flexible) structure [azo (-N=N-), bipyridyl group (bpy) and benzene-1,4-carboxylic acid (bdc)].

Figure S4: Pair correlation function of Br and Cα (of Br) of 1BP and 2BP with respect to three different parts of the Cu(bdc)(azbpy) MOF (flexible) are represented; a) and d) for azo (-N=N-), b) and e) for bpy, c) and f) for bdc.

Figure S5: a) MSD vs time plots for the 2 substrates obtained from AIMD simulations of 1 molecule in a periodic unit cell. The regions of the plots considered for the calculation of the diffusion constants, 5.37x10-5 and 5.97x10-5 cm2/s for 1BP and 2BP, respectively, are shown with fitted black lines; b-c) AIMD optimized (most probable) structure comparison Cu(bdc)(azbpy) (blue) and Cu(Br2-bdc)(azbpy) (red) MOF at 300 K; c shows the 2D square grid view along [001] direction.

Figure S6: MSD plot of 1BP and 2BP molecules along the [001] direction of flexible Cu(Br2-bdc)(azbpy) MOF at a) high and b) low concentration gradient.

Figure S7: Pair correlation function of 1BP and 2BP with respect to three different parts of the Cu(Br2-bdc)(azbpy) MOF (flexible) structure, [azo (-N=N-), bipyridyl group (bpy) and benzene-1,4-carboxylic acid (bdc)].

Figure S8: Pair correlation function of Br and Cα of 1BP and 2BP with respect to three different parts of the Cu(Br2bdc)(azbpy) MOF (flexible) are represented; a) and d) for azo (-N=N-), b) and e) for bpy, c) and f) for bdc.

Figure S9: Out-of-plane PXRD pattern of Cu+(Br2bdc)+(azbpy) thin film (red) in comparison with Cu(Br2-bdc)(azbpy) simulated pattern (black)

Figure S10: (RP) HPLC data of Br2bdc linker in solution after thin film digestion (black) and in calibration solutions (red)

Figure S11: SEM images of Cu(Br2-bdc)x(bdc)1-x(azbpy) a) x = 0.012 and b) x = 0.026 thin films.

Figure S12: EDS elemental mapping (Cu and Br) for Cu(Br2-bdc)x(bdc)1-x(azbpy) (a) x = 0.012 and (b) x = 0.026 thin films.

Figure S13: XPS spectra of Cu(Br2-bdc)x(bdc)1-x(azbpy) (x = 0, 0.012, 0.026, 0.058 and 0.169) thin films.

Figure S14: XPS spectra of Br 3d for Cu(Br2-bdc)x(bdc)1-x(azbpy) (x = 0, 0.012, 0.026, 0.058 and 0.169) thin films.

Figure S15: 1BP (red) and 2BP (green) vapour uptake profiles at 298 K for Cu(Br2-bdc)x(bdc)1-x(azbpy) a) x = 0.012, b) x = 0.026 and c) x = 0.058 thin films, black line is the exponential fit.

Figure S16: Out-of-plane XRD patterns of Cu(Br2-bdc)x(bdc)1-x(azbpy) (x = 0.169) thin film (green) in comparison with Cu(bdc)(azbpy) (black) and Cu(Br2-bdc)(azbpy) (red) simulated patterns.

Figure S17: IRRA spectra of Cu(Br2-bdc)x(bdc)1-x(azbpy) (x = 0, 0.012, 0.026, 0.058, and 0.169) and Cu+(Br2-bdc)+(azbpy) thin films.

Figure S18: a) Normalized [002] peak in out-of-plane XRD patterns of Cu(Br2bdc)x(bdc)1-x(azbpy) (x = 0, 0.012, 0.026, 0.058 and 0.169) thin films; Gaussian fitting plots for Cu(Br2bdc)x(bdc)1-x(azbpy) thin films b) x = 0, c) x = 0.012, d) x = 0.026, e) x = 0.058 and f) x = 0.169 (black line is the fitting).

Optimized structure of Cu(bdc)(azbpy) MOF at 0K

data_CIF\file\optimized\azo

_audit_creation_date              2022-06-10

_audit_creation_method            'Materials Studio'

_symmetry_space_group_name_H-M    'P1'

_symmetry_Int_Tables_number       1

_symmetry_cell_setting            triclinic

loop_

_symmetry_equiv_pos_as_xyz

x,y,z

_cell_length_a                    10.8920

_cell_length_b                    10.8920

_cell_length_c                    15.9140

_cell_angle_alpha                 90.0000

_cell_angle_beta                  90.0000

_cell_angle_gamma                 90.0000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

O1     O     0.38139   0.82233   0.10038   0.00000  Uiso   1.00

O2     O     0.38128   0.76457  -0.03806   0.00000  Uiso   1.00

O3     O     1.01980   0.82127  -0.03798   0.00000  Uiso   1.00

O4     O     1.02038   0.76374   0.10055   0.00000  Uiso   1.00

Cu5    Cu    0.20089   0.79378   0.11421   0.00000  Uiso   1.00

Cu6    Cu    0.20043   0.79265   0.94862   0.00000  Uiso   1.00

C7     C     0.96795   0.79210   0.03135   0.00000  Uiso   1.00

C8     C     0.82966   0.79139   0.03145   0.00000  Uiso   1.00

C9     C     0.43355   0.79296   0.03127   0.00000  Uiso   1.00

C10    C     0.57179   0.79187   0.03141   0.00000  Uiso   1.00

C11    C     0.76528   0.79005  -0.04569   0.00000  Uiso   1.00

C12    C     0.63620   0.78871  -0.04569   0.00000  Uiso   1.00

C13    C     0.63615   0.79443   0.10856   0.00000  Uiso   1.00

C14    C     0.76527   0.79254   0.10861   0.00000  Uiso   1.00

N15    N     0.19856   0.80562   0.24617   0.00000  Uiso   1.00

C16    C     0.22158   0.70510   0.29418   0.00000  Uiso   1.00

C17    C     0.22420   0.70901   0.38222   0.00000  Uiso   1.00

C18    C     0.20147   0.82344   0.42201   0.00000  Uiso   1.00

C19    C     0.17826   0.92822   0.37199   0.00000  Uiso   1.00

C20    C     0.17801   0.91489   0.28410   0.00000  Uiso   1.00

N21    N     0.19753   0.84245   0.51036   0.00000  Uiso   1.00

N22    N     0.22481   0.74689   0.55303   0.00000  Uiso   1.00

C23    C     0.21607   0.76511   0.64133   0.00000  Uiso   1.00

C24    C     0.16880   0.87247   0.68025   0.00000  Uiso   1.00

C25    C     0.16430   0.87549   0.76825   0.00000  Uiso   1.00

N26    N     0.20212   0.78039   0.81692   0.00000  Uiso   1.00

C27    C     0.24710   0.67814   0.77983   0.00000  Uiso   1.00

C28    C     0.25589   0.66615   0.69203   0.00000  Uiso   1.00

H29    H     0.23740   0.61976   0.25840   0.00000  Uiso   1.00

H30    H     0.24233   0.62665   0.42014   0.00000  Uiso   1.00

H31    H     0.16053   1.01735   0.40217   0.00000  Uiso   1.00

H32    H     0.16069   0.99227   0.24099   0.00000  Uiso   1.00

H33    H     0.13657   0.94974   0.64167   0.00000  Uiso   1.00

H34    H     0.12975   0.95579   0.80325   0.00000  Uiso   1.00

H35    H     0.27488   0.60453   0.82344   0.00000  Uiso   1.00

H36    H     0.29208   0.58233   0.66243   0.00000  Uiso   1.00

H37    H     0.58342   0.79739   0.16745   0.00000  Uiso   1.00

H38    H     0.58358   0.78619  -0.10464   0.00000  Uiso   1.00

H39    H     0.81799   0.78933  -0.10463   0.00000  Uiso   1.00

H40    H     0.81782   0.79249   0.16762   0.00000  Uiso   1.00

O41    O     0.17296   0.61122   0.96594   0.00000  Uiso   1.00

O42    O     0.23354   0.61180   1.10408   0.00000  Uiso   1.00

O43    O     0.16947  -0.02522   1.09669   0.00000  Uiso   1.00

O44    O     0.22810  -0.02520   0.95827   0.00000  Uiso   1.00

C45    C     0.19926   0.02619   1.02753   0.00000  Uiso   1.00

C46    C     0.20311   0.42189   1.03416   0.00000  Uiso   1.00

C47    C     0.08995   0.35900   1.03006   0.00000  Uiso   1.00

C48    C     0.08859   0.22971   1.02889   0.00000  Uiso   1.00

C49    C     0.20054   0.16449   1.02892   0.00000  Uiso   1.00

C50    C     0.31375   0.22735   1.03169   0.00000  Uiso   1.00

C51    C     0.31503   0.35663   1.03568   0.00000  Uiso   1.00

H52    H     0.00353   0.41131   1.02831   0.00000  Uiso   1.00

H53    H     0.00095   0.17945   1.02727   0.00000  Uiso   1.00

H54    H     0.40026   0.17509   1.03139   0.00000  Uiso   1.00

H55    H     0.40272   0.40664   1.03912   0.00000  Uiso   1.00

C56    C     0.20347   0.56017   1.03508   0.00000  Uiso   1.00

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_ccdc_geom_bond_type

O1     Cu5     2.003   .     S

O1     C9      1.279   .     S

O2     C9      1.280   .     D

O2     Cu6     2.005   1_554 S

O3     C7      1.280   .     S

O3     Cu6     2.003   1_654 S

O4     C7      1.278   .     D

O4     Cu5     2.005   1_655 S

Cu5    N15     2.104   .     S

Cu5    O4      2.005   1_455 S

Cu5    Cu6     2.635   1_554 S

Cu5    O42     2.020   1_554 S

Cu5    O43     2.020   1_564 S

Cu6    N26     2.100   .     S

Cu6    O41     2.018   .     S

Cu6    O3      2.003   1_456 S

Cu6    O2      2.005   1_556 S

Cu6    Cu5     2.635   1_556 S

Cu6    O44     2.013   1_565 S

C7     C8      1.506   .     S

C8     C11     1.414   .     S

C8     C14     1.414   .     D

C9     C10     1.506   .     S

C10    C12     1.414   .     S

C10    C13     1.414   .     D

C11    C12     1.406   .     D

C11    H39     1.100   .     S

C12    H38     1.100   .     S

C13    C14     1.406   .     S

C13    H37     1.100   .     S

C14    H40     1.100   .     S

N15    C16     1.358   .     D

N15    C20     1.353   .     S

C16    C17     1.402   .     S

C16    H29     1.104   .     S

C17    C18     1.420   .     D

C17    H30     1.099   .     S

C18    C19     1.414   .     S

C18    N21     1.422   .     S

C19    C20     1.406   .     D

C19    H31     1.100   .     S

C20    H32     1.103   .     S

N21    N22     1.278   .     D

N22    C23     1.422   .     S

C23    C24     1.420   .     S

C23    C28     1.415   .     D

C24    C25     1.402   .     D

C24    H33     1.099   .     S

C25    N26     1.357   .     S

C25    H34     1.103   .     S

N26    C27     1.352   .     D

C27    C28     1.407   .     S

C27    H35     1.103   .     S

C28    H36     1.100   .     S

O41    C56     1.277   .     S

O42    C56     1.276   .     D

O42    Cu5     2.020   1_556 S

O43    C45     1.277   .     S

O43    Cu5     2.020   1_546 S

O44    C45     1.275   .     D

O44    Cu6     2.013   1_545 S

C45    C49     1.507   .     S

C46    C47     1.412   .     D

C46    C51     1.411   .     S

C46    C56     1.506   .     S

C47    C48     1.408   .     S

C47    H52     1.101   .     S

C48    C49     1.411   .     D

C48    H53     1.101   .     S

C49    C50     1.411   .     S

C50    C51     1.410   .     D

C50    H54     1.101   .     S

C51    H55     1.101   .     S

Most probable AIMD structure of Cu(bdc)(azbpy) MOF at 300K

data_i11570_CuAMOF

_audit_creation_date              2023-12-14

_audit_creation_method            'Materials Studio'

_symmetry_space_group_name_H-M    'P1'

_symmetry_Int_Tables_number       1

_symmetry_cell_setting            triclinic

loop_

_symmetry_equiv_pos_as_xyz

x,y,z

_cell_length_a                    10.8920

_cell_length_b                    10.8920

_cell_length_c                    15.9140

_cell_angle_alpha                 90.0000

_cell_angle_beta                  90.0000

_cell_angle_gamma                 90.0000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

O1     O     0.42675   0.74685   0.24513   0.00000  Uiso   1.00

O2     O     0.42238   0.79192   0.10208   0.00000  Uiso   1.00

O3     O     1.05269   0.77409   0.08955   0.00000  Uiso   1.00

O4     O     1.05421   0.80288   0.23173   0.00000  Uiso   1.00

Cu5    Cu    0.25050   0.77455   0.24388   0.00000  Uiso   1.00

Cu6    Cu    0.23114   0.78338   1.07591   0.00000  Uiso   1.00

C7     C     1.00525   0.79187   0.16069   0.00000  Uiso   1.00

C8     C     0.86625   0.77216   0.16603   0.00000  Uiso   1.00

C9     C     0.47309   0.77157   0.17317   0.00000  Uiso   1.00

C10    C     0.61252   0.76355   0.17363   0.00000  Uiso   1.00

C11    C     0.80111   0.72213   0.09781   0.00000  Uiso   1.00

C12    C     0.67054   0.71658   0.10218   0.00000  Uiso   1.00

C13    C     0.67966   0.79690   0.24392   0.00000  Uiso   1.00

C14    C     0.80823   0.80624   0.24258   0.00000  Uiso   1.00

N15    N     0.23442   0.79660   0.37302   0.00000  Uiso   1.00

C16    C     0.32192   0.74716   0.42258   0.00000  Uiso   1.00

C17    C     0.32544   0.76824   0.50841   0.00000  Uiso   1.00

C18    C     0.24127   0.84550   0.54483   0.00000  Uiso   1.00

C19    C     0.15178   0.90700   0.49308   0.00000  Uiso   1.00

C20    C     0.15645   0.87973   0.40680   0.00000  Uiso   1.00

N21    N     0.24239   0.87291   0.63361   0.00000  Uiso   1.00

N22    N     0.30852   0.80298   0.67840   0.00000  Uiso   1.00

C23    C     0.28510   0.81007   0.76641   0.00000  Uiso   1.00

C24    C     0.22455   0.90731   0.81120   0.00000  Uiso   1.00

C25    C     0.20426   0.88561   0.89549   0.00000  Uiso   1.00

N26    N     0.24630   0.78603   0.94107   0.00000  Uiso   1.00

C27    C     0.30867   0.69958   0.89915   0.00000  Uiso   1.00

C28    C     0.33104   0.71150   0.81044   0.00000  Uiso   1.00

H29    H     0.38466   0.69039   0.38568   0.00000  Uiso   1.00

H30    H     0.40457   0.73165   0.54980   0.00000  Uiso   1.00

H31    H     0.08123   0.96708   0.52176   0.00000  Uiso   1.00

H32    H     0.08569   0.91411   0.35920   0.00000  Uiso   1.00

H33    H     0.20741   0.99195   0.77399   0.00000  Uiso   1.00

H34    H     0.16349   0.95696   0.93802   0.00000  Uiso   1.00

H35    H     0.33592   0.62171   0.93555   0.00000  Uiso   1.00

H36    H     0.39096   0.64689   0.77773   0.00000  Uiso   1.00

H37    H     0.62991   0.82881   0.29895   0.00000  Uiso   1.00

H38    H     0.61938   0.68521   0.04476   0.00000  Uiso   1.00

H39    H     0.85210   0.67761   0.04449   0.00000  Uiso   1.00

H40    H     0.86201   0.83535   0.30093   0.00000  Uiso   1.00

O41    O     0.22938   0.59890   1.09483   0.00000  Uiso   1.00

O42    O     0.22893   0.60163   1.24101   0.00000  Uiso   1.00

O43    O     0.26715  -0.04733   1.23414   0.00000  Uiso   1.00

O44    O     0.21829  -0.03669   1.09185   0.00000  Uiso   1.00

C45    C     0.24648   0.00778   1.16552   0.00000  Uiso   1.00

C46    C     0.24268   0.40838   1.17401   0.00000  Uiso   1.00

C47    C     0.27791   0.34867   1.10200   0.00000  Uiso   1.00

C48    C     0.28373   0.21835   1.09563   0.00000  Uiso   1.00

C49    C     0.24677   0.14417   1.16552   0.00000  Uiso   1.00

C50    C     0.20807   0.20766   1.24054   0.00000  Uiso   1.00

C51    C     0.20575   0.33847   1.24553   0.00000  Uiso   1.00

H52    H     0.29755   0.40700   1.04722   0.00000  Uiso   1.00

H53    H     0.31206   0.17986   1.03118   0.00000  Uiso   1.00

H54    H     0.19530   0.15894   1.29863   0.00000  Uiso   1.00

H55    H     0.16654   0.38249   1.30497   0.00000  Uiso   1.00

C56    C     0.23189   0.55185   1.16897   0.00000  Uiso   1.00

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_ccdc_geom_bond_type

O1     Cu5     1.943   .     S

O1     C9      1.280   .     S

O2     Cu6     2.126   1_554 S

O2     C9      1.278   .     S

O3     Cu6     1.958   1_654 S

O3     C7      1.259   .     S

O4     Cu5     2.169   1_655 S

O4     C7      1.256   .     S

Cu5    O4      2.169   1_455 S

Cu5    Cu6     2.683   1_554 S

Cu5    N15     2.077   .     S

Cu5    O42     1.899   1_554 S

Cu5    O43     1.955   1_564 S

Cu6    O3      1.958   1_456 S

Cu6    O2      2.126   1_556 S

Cu6    Cu5     2.683   1_556 S

Cu6    N26     2.152   .     S

Cu6    O41     2.032   .     S

Cu6    O44     1.981   1_565 S

C7     C8      1.531   .     S

C8     C11     1.407   .     S

C8     C14     1.422   .     S

C9     C10     1.521   .     S

C10    C12     1.398   .     S

C10    C13     1.385   .     S

C11    C12     1.425   .     S

C11    H39     1.124   .     S

C12    H38     1.124   .     S

C13    C14     1.404   .     S

C13    H37     1.087   .     S

C14    H40     1.143   .     S

N15    C16     1.349   .     S

N15    C20     1.353   .     S

C16    C17     1.386   .     S

C16    H29     1.093   .     S

C17    C18     1.373   .     S

C17    H30     1.156   .     S

C18    C19     1.441   .     S

C18    N21     1.444   .     S

C19    C20     1.406   .     S

C19    H31     1.108   .     S

C20    H32     1.144   .     S

N21    N22     1.268   .     S

N22    C23     1.426   .     S

C23    C24     1.437   .     S

C23    C28     1.376   .     S

C24    C25     1.380   .     S

C24    H33     1.111   .     S

C25    N26     1.383   .     S

C25    H34     1.122   .     S

N26    C27     1.339   .     S

C27    C28     1.439   .     S

C27    H35     1.069   .     S

C28    H36     1.092   .     S

O41    C56     1.287   .     S

O42    Cu5     1.899   1_556 S

O42    C56     1.269   .     S

O43    Cu5     1.955   1_546 S

O43    C45     1.266   .     S

O44    Cu6     1.981   1_545 S

O44    C45     1.305   .     S

C45    C49     1.486   .     S

C46    C47     1.372   .     S

C46    C51     1.427   .     S

C46    C56     1.569   .     S

C47    C48     1.424   .     S

C47    H52     1.100   .     S

C48    C49     1.433   .     S

C48    H53     1.150   .     S

C49    C50     1.443   .     S

C50    C51     1.427   .     S

C50    H54     1.075   .     S

C51    H55     1.143   .     S

Optimized structure of Cu(Br2bdc)(azbpy) MOF at 0K

data_CIF\file\optimized\Cu-bdc-azo\(2)

_audit_creation_date              2023-05-08

_audit_creation_method            'Materials Studio'

_symmetry_space_group_name_H-M    'P1'

_symmetry_Int_Tables_number       1

_symmetry_cell_setting            triclinic

loop_

_symmetry_equiv_pos_as_xyz

x,y,z

_cell_length_a                    10.8920

_cell_length_b                    10.8920

_cell_length_c                    15.9140

_cell_angle_alpha                 90.0000

_cell_angle_beta                  90.0000

_cell_angle_gamma                 90.0000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

O1     O     0.38139   0.82233   0.10038   0.00000  Uiso   1.00

O2     O     0.38128   0.76457  -0.03806   0.00000  Uiso   1.00

O3     O     1.01980   0.82127  -0.03798   0.00000  Uiso   1.00

O4     O     1.02038   0.76374   0.10055   0.00000  Uiso   1.00

Cu5    Cu    0.20089   0.79378   0.11421   0.00000  Uiso   1.00

Cu6    Cu    0.20043   0.79265   0.94862   0.00000  Uiso   1.00

C7     C     0.96795   0.79210   0.03135   0.00000  Uiso   1.00

C8     C     0.82966   0.79139   0.03145   0.00000  Uiso   1.00

C9     C     0.43355   0.79296   0.03127   0.00000  Uiso   1.00

C10    C     0.57179   0.79187   0.03141   0.00000  Uiso   1.00

C11    C     0.76528   0.79005  -0.04569   0.00000  Uiso   1.00

C12    C     0.63620   0.78871  -0.04569   0.00000  Uiso   1.00

C13    C     0.63615   0.79443   0.10856   0.00000  Uiso   1.00

C14    C     0.76527   0.79254   0.10861   0.00000  Uiso   1.00

N15    N     0.19856   0.80562   0.24617   0.00000  Uiso   1.00

C16    C     0.22158   0.70510   0.29418   0.00000  Uiso   1.00

C17    C     0.22420   0.70901   0.38222   0.00000  Uiso   1.00

C18    C     0.20147   0.82344   0.42201   0.00000  Uiso   1.00

C19    C     0.17826   0.92822   0.37199   0.00000  Uiso   1.00

C20    C     0.17801   0.91489   0.28410   0.00000  Uiso   1.00

N21    N     0.19753   0.84245   0.51036   0.00000  Uiso   1.00

N22    N     0.22481   0.74689   0.55303   0.00000  Uiso   1.00

C23    C     0.21607   0.76511   0.64133   0.00000  Uiso   1.00

C24    C     0.16880   0.87247   0.68025   0.00000  Uiso   1.00

C25    C     0.16430   0.87549   0.76825   0.00000  Uiso   1.00

N26    N     0.20212   0.78039   0.81692   0.00000  Uiso   1.00

C27    C     0.24710   0.67814   0.77983   0.00000  Uiso   1.00

C28    C     0.25589   0.66615   0.69203   0.00000  Uiso   1.00

H29    H     0.23740   0.61976   0.25840   0.00000  Uiso   1.00

H30    H     0.24233   0.62665   0.42014   0.00000  Uiso   1.00

H31    H     0.16053   1.01735   0.40217   0.00000  Uiso   1.00

H32    H     0.16069   0.99227   0.24099   0.00000  Uiso   1.00

H33    H     0.13657   0.94974   0.64167   0.00000  Uiso   1.00

H34    H     0.12975   0.95579   0.80325   0.00000  Uiso   1.00

H35    H     0.27488   0.60453   0.82344   0.00000  Uiso   1.00

H36    H     0.29208   0.58233   0.66243   0.00000  Uiso   1.00

H37    Br    0.58342   0.79739   0.16745   0.00000  Uiso   1.00

H38    H     0.58358   0.78619  -0.10464   0.00000  Uiso   1.00

H39    Br    0.81799   0.78933  -0.10463   0.00000  Uiso   1.00

H40    H     0.81782   0.79249   0.16762   0.00000  Uiso   1.00

O41    O     0.17296   0.61122   0.96594   0.00000  Uiso   1.00

O42    O     0.23354   0.61180   1.10408   0.00000  Uiso   1.00

O43    O     0.16947  -0.02522   1.09669   0.00000  Uiso   1.00

O44    O     0.22810  -0.02520   0.95827   0.00000  Uiso   1.00

C45    C     0.19926   0.02619   1.02753   0.00000  Uiso   1.00

C46    C     0.20311   0.42189   1.03416   0.00000  Uiso   1.00

C47    C     0.08995   0.35900   1.03006   0.00000  Uiso   1.00

C48    C     0.08859   0.22971   1.02889   0.00000  Uiso   1.00

C49    C     0.20054   0.16449   1.02892   0.00000  Uiso   1.00

C50    C     0.31375   0.22735   1.03169   0.00000  Uiso   1.00

C51    C     0.31503   0.35663   1.03568   0.00000  Uiso   1.00

H52    H     0.00353   0.41131   1.02831   0.00000  Uiso   1.00

H53    Br    0.00095   0.17945   1.02727   0.00000  Uiso   1.00

H54    H     0.40026   0.17509   1.03139   0.00000  Uiso   1.00

H55    Br    0.40272   0.40664   1.03912   0.00000  Uiso   1.00

C56    C     0.20347   0.56017   1.03508   0.00000  Uiso   1.00

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_ccdc_geom_bond_type

O1     Cu5     2.003   .     S

O1     C9      1.279   .     S

O2     C9      1.279   .     D

O2     Cu6     2.005   1_554 S

O3     C7      1.280   .     S

O3     Cu6     2.003   1_654 S

O4     C7      1.278   .     D

O4     Cu5     2.005   1_655 D

Cu5    N15     2.104   .     S

Cu5    O4      2.005   1_455 D

Cu5    Cu6     2.635   1_554 D

Cu5    O42     2.020   1_554 S

Cu5    O43     2.020   1_564 S

Cu6    N26     2.100   .     S

Cu6    O41     2.018   .     S

Cu6    O2      2.005   1_556 S

Cu6    O3      2.003   1_456 S

Cu6    Cu5     2.635   1_556 D

Cu6    O44     2.013   1_565 D

C7     C8      1.506   .     S

C8     C11     1.414   .     S

C8     C14     1.414   .     D

C9     C10     1.506   .     S

C10    C12     1.414   .     S

C10    C13     1.414   .     D

C11    C12     1.406   .     D

C11    H39     1.100   .     S

C12    H38     1.100   .     S

C13    C14     1.407   .     S

C13    H37     1.100   .     S

C14    H40     1.100   .     S

N15    C16     1.358   .     D

N15    C20     1.353   .     S

C16    C17     1.402   .     S

C16    H29     1.104   .     S

C17    C18     1.420   .     D

C17    H30     1.099   .     S

C18    C19     1.414   .     S

C18    N21     1.422   .     S

C19    C20     1.406   .     D

C19    H31     1.100   .     S

C20    H32     1.103   .     S

N21    N22     1.278   .     D

N22    C23     1.422   .     S

C23    C24     1.420   .     S

C23    C28     1.415   .     D

C24    C25     1.402   .     D

C24    H33     1.099   .     S

C25    N26     1.357   .     S

C25    H34     1.103   .     S

N26    C27     1.352   .     D

C27    C28     1.407   .     S

C27    H35     1.103   .     S

C28    H36     1.100   .     S

O41    C56     1.277   .     S

O42    C56     1.276   .     D

O42    Cu5     2.020   1_556 S

O43    C45     1.277   .     S

O43    Cu5     2.020   1_546 S

O44    C45     1.275   .     D

O44    Cu6     2.013   1_545 D

C45    C49     1.507   .     S

C46    C47     1.412   .     D

C46    C51     1.411   .     S

C46    C56     1.506   .     S

C47    C48     1.408   .     S

C47    H52     1.101   .     S

C48    C49     1.411   .     D

C48    H53     1.101   .     S

C49    C50     1.411   .     S

C50    C51     1.410   .     D

C50    H54     1.101   .     S

C51    H55     1.101   .     S

Most probable AIMD structure of Cu(Br2bdc)(azbpy) MOF at 300K

data_i18380_CuBrAMOF

_audit_creation_date              2023-12-14

_audit_creation_method            'Materials Studio'

_symmetry_space_group_name_H-M    'P1'

_symmetry_Int_Tables_number       1

_symmetry_cell_setting            triclinic

loop_

_symmetry_equiv_pos_as_xyz

x,y,z

_cell_length_a                    10.8920

_cell_length_b                    10.8920

_cell_length_c                    15.9140

_cell_angle_alpha                 90.0000

_cell_angle_beta                  90.0000

_cell_angle_gamma                 90.0000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

O1     O     0.36207   0.76606   0.19648   0.00000  Uiso   1.00

O2     O     0.35860   0.70045   0.06045   0.00000  Uiso   1.00

O3     O     0.99024   0.77866   0.05664   0.00000  Uiso   1.00

O4     O     1.00216   0.71394   0.19262   0.00000  Uiso   1.00

Cu5    Cu    0.18738   0.73467   0.20328   0.00000  Uiso   1.00

Cu6    Cu    0.16813   0.73109   1.03782   0.00000  Uiso   1.00

C7     C     0.94440   0.73437   0.12198   0.00000  Uiso   1.00

C8     C     0.80803   0.72625   0.12639   0.00000  Uiso   1.00

C9     C     0.41130   0.74134   0.12671   0.00000  Uiso   1.00

C10    C     0.54686   0.74119   0.12697   0.00000  Uiso   1.00

C11    C     0.73189   0.64160   0.17135   0.00000  Uiso   1.00

C12    C     0.59907   0.64377   0.17349   0.00000  Uiso   1.00

C13    C     0.61661   0.82987   0.08647   0.00000  Uiso   1.00

C14    C     0.74347   0.82779   0.08872   0.00000  Uiso   1.00

N15    N     0.15567   0.74732   0.34018   0.00000  Uiso   1.00

C16    C     0.25178   0.74486   0.39566   0.00000  Uiso   1.00

C17    C     0.23725   0.75109   0.48427   0.00000  Uiso   1.00

C18    C     0.11571   0.75704   0.51298   0.00000  Uiso   1.00

C19    C     0.01793   0.74811   0.45688   0.00000  Uiso   1.00

C20    C     0.03984   0.74345   0.37077   0.00000  Uiso   1.00

N21    N     0.08726   0.76783   0.60111   0.00000  Uiso   1.00

N22    N     0.15030   0.69983   0.64693   0.00000  Uiso   1.00

C23    C     0.12556   0.71114   0.73440   0.00000  Uiso   1.00

C24    C     0.08878   0.81868   0.77295   0.00000  Uiso   1.00

C25    C     0.10702   0.81549   0.86054   0.00000  Uiso   1.00

N26    N     0.16200   0.72166   0.90226   0.00000  Uiso   1.00

C27    C     0.18420   0.61063   0.86394   0.00000  Uiso   1.00

C28    C     0.17621   0.60594   0.77667   0.00000  Uiso   1.00

H29    H     0.34353   0.74140   0.36488   0.00000  Uiso   1.00

H30    H     0.31181   0.74574   0.53133   0.00000  Uiso   1.00

H31    H    -0.07402   0.74262   0.48391   0.00000  Uiso   1.00

H32    H    -0.02722   0.73033   0.31919   0.00000  Uiso   1.00

H33    H     0.06307   0.90478   0.74321   0.00000  Uiso   1.00

H34    H     0.09552   0.90077   0.90018   0.00000  Uiso   1.00

H35    H     0.23242   0.54307   0.90104   0.00000  Uiso   1.00

H36    H     0.21094   0.52252   0.74621   0.00000  Uiso   1.00

Br37   Br    0.53061   0.96762   0.03081   0.00000  Uiso   1.00

H38    H     0.54074   0.58041   0.20941   0.00000  Uiso   1.00

Br39   Br    0.81173   0.50091   0.22527   0.00000  Uiso   1.00

H40    H     0.78987   0.89651   0.04754   0.00000  Uiso   1.00

O41    O     0.13732   0.54956   1.04115   0.00000  Uiso   1.00

O42    O     0.23337   0.54724   1.17001   0.00000  Uiso   1.00

O43    O     0.15061  -0.07932   1.17766   0.00000  Uiso   1.00

O44    O     0.20257  -0.08727   1.03902   0.00000  Uiso   1.00

C45    C     0.17047  -0.03199   1.10511   0.00000  Uiso   1.00

C46    C     0.18913   0.36268   1.10898   0.00000  Uiso   1.00

C47    C     0.07575   0.30089   1.13168   0.00000  Uiso   1.00

C48    C     0.06810   0.17284   1.13036   0.00000  Uiso   1.00

C49    C     0.17201   0.10600   1.10105   0.00000  Uiso   1.00

C50    C     0.27119   0.16213   1.06501   0.00000  Uiso   1.00

C51    C     0.28097   0.29285   1.06872   0.00000  Uiso   1.00

H52    H    -0.00485   0.35904   1.14298   0.00000  Uiso   1.00

Br53   Br   -0.08599   0.09309   1.13471   0.00000  Uiso   1.00

H54    H     0.34584   0.11102   1.03462   0.00000  Uiso   1.00

Br55   Br    0.42502   0.37158   1.02006   0.00000  Uiso   1.00

C56    C     0.18329   0.49806   1.10808   0.00000  Uiso   1.00

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_ccdc_geom_bond_type

O1     Cu5     1.936   .     S

O1     C9      1.262   .     S

O2     Cu6     2.132   1_554 S

O2     C9      1.280   .     S

O3     Cu6     2.028   1_654 S

O3     C7      1.250   .     S

O4     Cu5     2.037   1_655 S

O4     C7      1.307   .     S

Cu5    O4      2.037   1_455 S

Cu5    Cu6     2.642   1_554 S

Cu5    N15     2.210   .     S

Cu5    O42     2.168   1_554 S

Cu5    O43     2.105   1_564 S

Cu6    O2      2.132   1_556 S

Cu6    O3      2.028   1_456 S

Cu6    Cu5     2.642   1_556 S

Cu6    N26     2.161   .     S

Cu6    O41     2.006   .     S

Cu6    O44     2.014   1_565 S

C7     C8      1.490   .     S

C8     C11     1.432   .     S

C8     C14     1.441   .     S

C9     C10     1.477   .     S

C10    C12     1.413   .     S

C10    C13     1.388   .     S

C11    C12     1.447   .     S

C11    Br39    1.960   .     S

C12    H38     1.099   .     S

C13    C14     1.382   .     S

C13    Br37    1.978   .     S

C14    H40     1.116   .     S

N15    C16     1.370   .     S

N15    C20     1.353   .     S

C16    C17     1.421   .     S

C16    H29     1.114   .     S

C17    C18     1.402   .     S

C17    H30     1.106   .     S

C18    C19     1.393   .     S

C18    N21     1.441   .     S

C19    C20     1.392   .     S

C19    H31     1.092   .     S

C20    H32     1.108   .     S

N21    N22     1.246   .     S

N22    C23     1.423   .     S

C23    C24     1.382   .     S

C23    C28     1.439   .     S

C24    C25     1.408   .     S

C24    H33     1.087   .     S

C25    N26     1.358   .     S

C25    H34     1.130   .     S

N26    C27     1.376   .     S

C27    C28     1.392   .     S

C27    H35     1.080   .     S

C28    H36     1.097   .     S

O41    C56     1.304   .     S

O42    Cu5     2.168   1_556 S

O42    C56     1.247   .     S

O43    Cu5     2.105   1_546 S

O43    C45     1.283   .     S

O44    Cu6     2.014   1_545 S

O44    C45     1.261   .     S

C45    C49     1.504   .     S

C46    C47     1.452   .     S

C46    C51     1.411   .     S

C46    C56     1.476   .     S

C47    C48     1.397   .     S

C47    H52     1.097   .     S

C48    C49     1.424   .     S

C48    Br53    1.891   .     S

C49    C50     1.367   .     S

C50    C51     1.429   .     S

C50    H54     1.098   .     S

C51    Br55    1.949   .     S