Fixed-bed column dynamics of ultrasound and Na-functionalized diatomite to remove phosphate from water

Junxiu Ye, Min Yang, Xuemei Ding, Wei Tan, Guizhen Li , Shuju Fang, Hongbin Wang*

School of Chemistry and Environment, Yunnan Minzu University, Kunming 650500, Yunnan, China

Corresponding author

Hongbin Wang, School of Chemistry and Environment, Yunnan Minzu University, Kunming 650500, Yunnan, P.R. China (E-mail: wanghb2152@126.com; Tel. +13708440749)

Fig. S1 SEM images of diatomite: A, the natural diatomite; B, the pickling diatomite; C, the

pickling and NaCl modified diatomite; D, the pickling, NaCl modified, and calcining diatomite.

Fig. S2(a) The elemental composition of the natural diatomite by use of EDS.

Fig. S2(b) The elemental composition of the U-D-Na by use of EDS.

Fig. S3(a) The phosphate adsorption isotherm by U-D-Na at 25 ℃.

Fig. S3(b) The linear langmuir isotherm equation for phosphate removal by U-D-Na at 25 ℃.

Table S1 The phosphate adsorption parameters fitted by Langmuir model.

Fig. S1. SEM images of diatomite: A, natural diatomite; B, pickling diatomite; C,

pickling and NaCl modified diatomite; D, pickling, NaCl modified and calcining

diatomite.

Fig. S2(a) The elemental composition of the natural diatomite by use of EDS

Fig. S2(b) The elemental composition of the U-D-Na by use of EDS

Fig. S3(a) The phosphate adsorption isotherm by U-D-Na at 25 ℃.

b

Fig. S3(b) The linear langmuir isotherm equation for phosphate removal by U-D-Na at 25 ℃.

| Langmuir model | Equation | KL | Qm | R |
| --- | --- | --- | --- | --- |
|  | Qe=0.8104Ce/(1+0.3138Ce) | 0.2543 | 3.1867 | 0.9626 |

Table S1 The phosphate adsorption parameters fitted by Langmuir model at 25 ℃.