Supplementary Information

Fluorine-induced d-band center shift of the Nb site boosts anodic formamide electrosynthesis

Mou et al.

Contents

Supplementary Figure 1. XRD pattern and SEM image of Nb3O7F and Nb2O5 	3

Supplementary Figure 2. XPS data of Nb2O5/CP catalyst 	4

Supplementary Figure 3. Optimization molar ratios of CH3OH/NH3 	5

Supplementary Figure 4. LSV curves and FEs of Nb2O5/CP 	6

Supplementary Figure 5. Chronoamperometry curves of different applied potentials 	7

Supplementary Figure 6. Calibration curves of formamide and H2O2 	8

Supplementary Figure 7. 1H NMR spectrum for the formamide	9

Supplementary Figure 8. Methanol and NH3 consumption	10

Supplementary Figure 9. XPS spectrum of F-Nb2O5/CP catalysts after stability test 	11

Supplementary Figure 10. XRD patterns and SEM image of F-Nb2O5/CP after stability test 	12

Supplementary Figure 11. CVs of F-Nb2O5/CP and Nb2O5/CP 	13

Supplementary Figure 12. Gibbs free energy diagram of formamide synthesis path 2	14

Supplementary Figure 13. Atomic configurations of intermediates on F-Nb2O5 (100) for path 1 	15

Supplementary Figure 14. Atomic configurations of intermediates on Nb2O5 (100) for path 1 	16

Supplementary Figure 15. Slow growth simulation data for C-N bond formation 	17

Supplementary Figure 16. Atomic configurations of intermediates on F-Nb2O5 (100) for path 2 	18

Supplementary Figure 17. Atomic configurations of intermediates on Nb2O5 (100) for path 2 	19

Supplementary Figure 18. Charge density difference analysis for F-Nb2O5 and Nb2O5 (100)	20

Supplementary Figure 19. COHP analysis of *CH2O on F-Nb2O5 (100) and Nb2O5 (100) surface 	21

Table S1. Comparison of anodic amide synthesis performance for F-Nb2O5/CP 	22

References 	22

Supplementary Figure 1 │  (a) XRD patterns of Nb2O5, (b) and (c) SEM image of Nb2O5 nanoparticles on carbon nanofiber paper (Nb2O5/CP). (d) XRD patterns of Nb3O7F. (e) and (f) SEM image of Nb3O7F nanosheets on carbon nanofiber paper (Nb3O7F/CP).

Supplementary Figure 2│(a) Survey XPS spectrum of Nb2O5/CP catalysts. High-resolution XPS spectra of (b) F 1s and (c) O 1s and (d) Nb 3d of Nb2O5/CP catalysts.

Supplementary Figure 3 │Faradaic efficiency and yield rate of HCONH2 with different CH3OH/NH3 molar ratios on F-Nb2O5/CP at 1.5 V versus Hg/HgO.

Supplementary Figure 4 │ (a) LSV curves of Nb2O5/CP in 0.5 M KHCO3 solution, with methanol and NH3. (b) FEs of oxidation products on Nb2O5/CP at different potentials.

Supplementary Figure 5│ The chronoamperometry curves of different applied potentials for (a) F-Nb2O5/CP and (b) Nb2O5/CP.

Supplementary Figure 6│ (a) Chromatograph curve of formamide and (b) External standard calibration curve used for calculation of formamide detected by HPLC. (c) Absorption spectra of H2O2 and (d) External standard calibration curve used for calculation of formamide detected by UV-Vis.

Supplementary Figure 7│ 1H nuclear magnetic resonance spectrum for the formamide product.

Supplementary Figure 8│ (a) The detection of methanol consumption using HS-GCMS, (b) The detection of NH3 consumption using ion chromatography.

Supplementary Figure 9│ (a) Survey XPS spectrum of F-Nb2O5/CP catalysts after stability test. High-resolution XPS spectra of (b) F 1s and (c) O 1s and (d)Nb 3d of F-Nb2O5/CP catalysts after stability test.

Supplementary Figure 10│ (a) XRD patterns of F-Nb2O5/CP before and after the stability test. (b) and (c) SEM image of the F-Nb2O5/CP after stability test.

Supplementary Figure 11│(a) CVs of a) F-Nb2O5/CP and (b) Nb2O5/CP with various scan rates (10–100 mV s–1) in the regions of 0.12 to 0.22 V vs. RHE.

Supplementary Figure 12│Gibbs free energy diagram of formamide synthesis path 2 on （a) F-Nb2O5 (100) surface and （b) Nb2O5 (100) surface.

Supplementary Figure 13│Atomic configurations of formamide synthesis intermediates on F-Nb2O5 (100) for path 1.

Supplementary Figure 14│Atomic configurations of formamide synthesis intermediates on Nb2O5 (100) for path 1.

Supplementary Figure 15│(a) Potential of mean force derived from slow growth simulation (blue line) and thermodynamic integrations (orange line) of *NH2+*CH2O→ *CH2ONH2 with a step size of 0.0005 Å, and (b)  corresponding C-N bond length change. (c)  Potential of mean force derived from slow growth simulation (dark blue line) and thermodynamic integrations (orange line) of *NH2+*CHO→ *CO + *NH3 with a step size of 0.0005 Å, and (d) corresponding C-N and N-H bond length change.

Supplementary Figure 16│Atomic configurations of formamide synthesis intermediates on F-Nb2O5 (100) for path 2.

Supplementary Figure 17│ Atomic configurations of formamide synthesis intermediates on Nb2O5 (100) for path 2.

Supplementary Figure 18│Charge density difference analysis for a) F-doped Nb2O5 (100) and b) Nb2O5 (100).

Supplementary Figure 19│ Crystal Orbital Hamilton Population (COHP) analysis of *CH2O on F-Nb2O5 (100) and Nb2O5 (100) surface.

Table S1│ Comparison of anodic amide synthesis performance for F-Nb2O5/CP with other anodic amide-producing electrocatalysts.

| Catalyst | Electrolyte |  | Reactants | Products | FE% | Potential | Current density | Stability | Yield | Ref. |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| F-Nb2O5/CP |  | 0.5 M KHCO3 | CH3OH NH3 | Formamide | 52.0 | 1.5 V v.s Hg/HgO | 20 mA cm-2 | 120 h | 252 μmol cm-2 h−1 | This work |  |
| Pt-Ti |  | 0.5 M NaHCO3 | CH3OH NH3 | Formamide | 40.39 | ∼1.6 V Cell potential | 100 mA cm-2 | 46 h | 305.4 μmol cm-2 h−1 | [1] |  |
| BDD |  | 0.5 M NaHCO3 | CH3OH NH3 | Formamide | 41.20 | 3.2 V v.s SCE[a] | 120 mA cm-2 | N/A | 461.39 μmol cm-2 h−1 | [2] |  |
| Pr-Doped MnO2 |  | 0.5 M NaHCO3 | CH3OH NH3 | Formamide | 22.63 | N/A | 100 mA cm-2 | 50 h | 211.32 μmol cm-2 h−1 | [3] |  |
| β-Ni(OH)2 |  | 1.0 M KOH | CH3OH NH3 | Acetamide | ∼32[b] | 0.65 V v.s Hg/HgO | ≈600 mA cm-2 | 16 h | ∼1 mmol cm−2h−1 | [4] |  |
| graphite flake |  | 0.7 M K2CO3 | TMA | DMF | 40.0 | 1.1 V v.s Hg/HgO | 40 mA cm-2 | 24 h | 7.63 μmol cm−2 h−1 | [5] |  |

[a] Retrieve data from LSV curves of BDD in electrolytes in supporting information. [b] Retrieve data from the FE and production rate of acetamide on β-Ni(OH)2 anode.

References

1	Meng, Nannan, et al. Electrosynthesis of formamide from methanol and ammonia under ambient conditions. Nat. Commun., 13, 5452, (2022).

2	Shao, Jiang, et al. Scalable Electrosynthesis of formamide through C− N coupling at the industrially relevant current density of 120 mA cm−2. Angew. Chem. Int. Ed. 61, e202213009, (2022).

3	Zhu, Jiewei, et al. Formamide Electrosynthesis from Methanol and Ammonia in Water over Pr-Doped MnO2. JACS Au 3, 2987-2992, (2023):

4	Lu, Yuxuan, et al. Anodic Electrosynthesis of Amide from Alcohol and Ammonia. CCS Chem. 6, 125-136, (2024).

5	Jin, Meng, et al. Electrosynthesis of N, N-dimethylformamide from market-surplus trimethylamine coupled with hydrogen production. Green Chem. 25, 5936-5944 (2023).