Table 1 The reported literature on natural polymers as metal corrosion inhibitors.

| Polymers | Metal/ Medium | The highest η% / Dosage | References |
| --- | --- | --- | --- |
| Starch |  |  |  |
| Tapioca starch | AA6061alloy/ seawater | 93.98% (1000 ppm) | Rosliza and Wan Nik (2010) |
| Cassava starch-acryl amide graft copolymer (CS-AAGC) | 1060 aluminum / 1.0 M H3PO4 | 90.6% (1 g/L) | Deng et al. (2021) |
| Activated and carboxymethylated starch cassava starch | XC 35 carbon steel/Alkaline 200 mg/L NaCl | -- | Bello et al. (2010) |
| Cellulose |  |  |  |
| Carboxymethyl cellulose | Mild steel/ 2 M H2SO4 | 64.8% (0.5 g/L) | Solomon et al. (2010) |
| Methyl hydroxyethyl cellulose | Copper/ 1M HCl | 90.29% (4 g/L) | Sobhi and Eid (2018) |
| Borated aminated cellulose citrate | A3 steel/ simulated cooling water | 88.33% (200 mg/L) | Gan et al. (2018) |
| Tetrazole cellulose | Carbon steel/ 1 M HCl | 94.2% (100 ppm) | Al Kiey et al. (2021) |
| Hydroxyethyl cellulose (HEC) (potassium iodide, KI) | Mild steel/ 0.5 M H2SO4 | 92.74% (2 g/L HEC+0.5 g/L KI) | Arukalam et al. (2014) |
| Methyl cellulose (MC) | Magnesium / 0.1 M HCl | -- | Hassan and Ibrahim (2021) |
| Hydroxyethyl cellulose | Carbon steel (1018 grade) / 3.5% NaCl | 96.7% (0.5 mM) | El-Haddad. (2014) |
| Chitosan |  |  |  |
| N-phenyl-O-benzylthiourea chitosan | Carbon steel / acidic solutions | 97.8% (150 mg/L) | Zhang et al. (2023) |
| Salicylaldehyde Schiff-base grafted chitosan | Mild steel/ 1 M HCl | 75.35% (1500 ppm) | Menaka and Subhashini (2016) |
| 5-hydroxymethylfurfural grafted chitosan | Mild steel/ 1 M HCl | 97.01% (200 mg/L) | Zhang et al. (2023) |
| 8-hydroxyquinoline functionalized chitosan | N80 steel/ 1 M HCl | 98.52% (800 mg/L) | Wu et al. (2023) |
| Vanillin Schiff base functionalized chitosan | Mild steel/ 1 M HCl | 91.1% (1500 ppm) | Ramanathan et al. (2022) |
| Triazole-modified chitosan | Carbon steel/ 1 M HCl | 90.81% (200 ppm) | Chauhan et al. (2019) |
| Sulfonated chitosan | Carbon steel/ 2 M HCl | 95.6% (5000 ppm) | Farhadian et al. (2020) |
| L-Arginine grafted chitosan | Mild steel/ 0.5 M HCl | 91.4% (500 ppm) | Dalhatu et al. (2023) |
| Pectin |  |  |  |
| Pectin extracted from fresh lemon peel | Mild steel/ 1 M HCl | 94.2% (2 g/L) | Fiori-Bimbi et al. (2015) |
| Pectin extracted from apple | X60 pipeline steel/ 0.5 M HCl | 78.7% (1000 ppm) | Umoren et al. (2015) |
| Pectin-g-polyacrylic acid | Mild steel/ 3.5% NaCl | 85.53% (800 ppm) | Geethanjali et al. (2014) |
| Sugar beet pectin | Mild steel/ 1 M HCl | 93.9% （1g/L） | Abou-Elseoud et al. (2021) |
| Pectin extracted from citrus peel | Mild steel/ 1 M H3PO4 | 70.26% (800 ppm) | Sushmitha and Rao (2020) |
| Sunflower head pectin（Mw = 4.50 kDa） | Mild steel/ 1 M HCl | 90.3% (2 g/L） | Ma et al. (2019) |
| Exudate gums |  |  |  |
| Phosphorylated xanthan gum (PXG) | Mild steel/ 200 ppm NaCl | 92.54% (150 ppm) | Vimal Kumar and Appa Rao (2019) |
| Gum Arabic (GA) | Carbon steel/ Synthetic brine | 94% (5 g/L) | Shen et al. (2019) |
| polysaccharide guar gum(GG) | Carbon steel/ CO2-saturated saline solution | 76.16% (0.4 g/L) | Palumbo et al. (2023) |
| Gum arabic | 09G2S steel / 0.1% NaCl | -- (2g/L) | Danyliak and Rizun (2022) |
| Moringa oleifera (G2) | Mild steel/ Diesel/saline water biphasic system | 95.75% (5000 ppm) | Palanisamy et al. (2023) |
| Tragacanth Gum-Ceftriaxone | Mild steel/ 1 M HCl | 98.1% (250 ppm) | Barrodi et al. (2023) |
| Plant polysaccharides |  |  |  |
| Lentinan | Q235 steel/ 1 M HCl | 92.66% (100 mg/L) | Liu et al. (2022) |
| Plantago polysaccharide | Carbon steel/ 1 M HCl | 93.54% (1000 ppm) | Mobin and Rizvi (2017) |
| Adlay seed hull polysaccharide (ASP) | Mild steel/ 1 M HCl | 94.7% (800 mg/L) | Chen et al. (2021) |
| Prickly pear nopales Pulp polysaccharide | Mild steel/ 1 M HCl | 93.22% (25 ppm) | Madaci et al. (2023) |
| Fucoidan | 304 stainless steel/ 3.5% NaCl | 81.7% (200 ppm) | Keshk et al. (2023) |

Table 2 The corrosion protection properties of some different types of polymeric surfactant corrosion inhibitors.

| Surfactant Type | Metal and electrolyte | Nature of adsorption | The highest η% | References |
| --- | --- | --- | --- | --- |
| Cationic |  |  |  |  |
|  | Mild Steel/ 1 M HCL | Langmuir | 80.05% (1000M) | Shaban et al. (2019) |
|  | 304L SS / 1 M HCL | Langmuir | 94.42% (50 ppm) | Goni et al. (2023) |
| Anionic |  |  |  |  |
|  | Steel / 1.0 M HCl | Langmuir | 92.62% (800 ppm) | Badr et al. (2020) |
| Non-ionic |  |  |  |  |
|  | Zinc/ 0.1 M Na2SO4 | -- | 60.12% (32 ppm) | Bawazeer et al. (2017) |
|  | Mild steel/ 5% HCl | Langmuir | 62.89% (20 ppm) | Attia and Abdel-Fatah (2019) |
|  | Mild steel / 0.5 M H2SO4 | Temkin | 71% (1000 ppm) | Umoren et al. (2015) |
| Zwitterionic |  |  |  |  |
|  | Carbon Steel / 0.5 M HCL | Langmuir | 93.36% (500 ppm) | Wang et al. (2020) |
|  | Mild steel / 1 M HCl | Langmuir | 94.7% (100 ppm) | Jafar Mazumder (2019) |

Table 3 The literature reports on polymeric ionic liquids as metal corrosion inhibitors.

| Polymers | Metal/ Medium | The highest η% / Dosage | References |
| --- | --- | --- | --- |
| The PIL inhibitors based on imidazolium |  |  |  |
| Vinylimidazolium poly(ionic liquid)s | API 5L X60 / 1 M H2SO4 | 75% (175 ppm) | Gómez-Sánchez et al. (2023) |
| Poly [3-butyl-1-vinylimidazolium bromide] | Mild Steel / 1M HCL | 96.4% (400 ppm) | Kamali Ardakani et al. (2020) |
| Polymeric imidazolates from alkylimidazolium | API 5L X52 / Production water | 80% (150 ppm) | Likhanova et al. (2022) |
| 6.Vinylalkylimidazolium-Based Polymeric Ionic Liquids | API 5L X60 / 1 M H2SO4 | 85% (175 ppm) | Atta et al. (2015b) |
| 9.Polymeric Ionic Liquids Based on Benzimidazole Derivatives | X-65 steel / 1 M HCl | 99.3% (250 ppm) | El Nagy et al. (2020) |
| Bisimidazole-based copoly(ionic liquid)s | Copper / 0.5 M H2SO4 | 96.5% (0.2 g/L) | Huang et al. (2019) |
| Poly(1-vinyl-3-alkyl-imidazolium Hexafluorophosphate) | AA6061 / 1 M H2SO4 | 61% (100 ppm) | Arellanes-Lozada et al. (2014) |
| The PIL inhibitors based on acrylamide |  |  |  |
| 5.Poly Ionic Liquid-Based on 2- Acrylamido-2-methyl Propane Sulfonic Acid | Steel / Acidic chloride solutions | 93.7% (25 ppm) | Atta et al. (2015b) |
| Novel acrylamide ionic liquids | X-65 Steel / 1 M HCL | 91.4% (250 ppm) | El Tamany et al. (2018) |
| 1-Butyl-3 Methylimidazolium Acrylate polymer | C1020 steel / 1 M HCl | 91.8% (200 ppm) | Gobara et al. (2019) |
| Poly(2-acrylamido-2-methylpropane sulfonic acid) | Steel / 1 M HCl | 85% (250 ppm) | Atta et al. (2015a) |
| The PIL inhibitors based on ammonium |  |  |  |
| Coumarate ionic liquid coupled with ammonium cation | AS1020 steel /0.01 M NaCl | 99.1% ( 8 mM) | Udabe et al. (2020) |
| The PIL inhibitors based on chitosan |  |  |  |
| Chitosan polymeric ionic liquids(CSPTA-lauric) | X-65 steel/ 1 M HCl | 98.6% (250 ppm) | Elsaeed et al. (2018) |

Table 4 β-CD-basedpolymers as metal corrosion inhibitors

| Molecular structural formula | Metal/ Medium | The highest η%/Dosage | References |
| --- | --- | --- | --- |
| Natural polymer-modified β-CD |  |  |  |
| β-cyclodextrin with xanthan gum | X80 steel/ 1M H2SO4 L80 steel/ 1 M HCl | 94.85% (150 mg/L) 94.74% (200 mg/L) | Cao et al. (2021) Cao et al. (2021) |
| β-cyclodextrin modified chitosan | Carbon steel/ 0.5 M HCl | 96.02% (230 mg/L) | Liu et al. (2015) |
| β-CD modified with synthetic polymers |  |  |  |
| β-cyclodextrin grafted polyacrylamide | X80 steel/ 1 M H2SO4 | 92.48% (200 mg/L) | Wang et al. (2021) |
| Polyaspartic acid graft copolymer | N80 carbon steel/ Simulate oilfield water | 94.6% (250 mg/L) | Fu et al. (2020) |
| β-cyclodextrin–polyethylene glycol | Steel/ produced-water in shale gas well | 89.1% (180 mg/L) | Liu et al. (2016) |
| β-Cyclodextrin-modified polyacrylamide | X70 steel/ 0.5 M H2SO4 | 84.9% (150 mg/L) | Yan et al. (2014) |
| Divinyl sulfone cross-linked β-cyclodextrin polymer | Zn anode/ 3.5 M KOH | 93.61% (250 ppm) | Abd El-Lateef and Elremaily (2016) |
| Hydroxypropyl-β-cyclodextrin/octadecylamine | Q235 steel/ Simulated condensate water | 95% (50 mg/L) | Fan et al. (2014) |
| β-CD-based supramolecular (host-guest) systems |  |  |  |
| Soluble cyclodextrin polymer (SCDP) | Mild steel/ 3.5 % NaCl | 92.2% (125 mg/L) | Ma et al. (2019) |
| Dibenzylthiourea with α and β forms of hydroxypropylated cyclodextrins | Carbon steel/ 1 M HCl | 91.3% (0.1 mM) | de Souza et al. (2016) |
| Carboxymethylated beta-cyclodextrin and an aniline trimer | Q235 steel/ 1 M HCl | 99.2% (250 mg/L) | Yang et al. (2019) |
| Beta-cyclodextrin-zinc acetylacetonate inclusion complex | Mild steel/ 3.5 % NaCl | 88% -- | Dehghani et al. (2020) |
| 5-mercapto-1-phenyl-tetrazole and β-CD | Bronze/ Acid rain | 98% (654 M−1) | Monticelli et al. (2019) |
| 2-mercapto-benzothiazole and β-CD | Zinc/ - M KCl | -- | Altin et al. (2018) |
| 2-Phosphonobutane-1,2,4-tricarboxylic acid with β-CD | Q235 steel/ 1 M H2SO4 | 90% (100 mg/L) | Zou et al. (2013) |

Table 5 Polymeric nanocomposites as metal corrosion inhibitors.

| Polymers | Metal/ Medium | The highest η%/ Dosage | References |
| --- | --- | --- | --- |
| L-proline nitrate and graphene oxide nanohybrid (IL-GO) | Mild steel/ 1 M HCl | 86.5% (250 ppm) | Mobin et al. (2022) |
| Conducting polyaniline–sulfonated naphthalene formaldehyde nanocomposites | 316L stainless steel/ 1 M HCl | 99.3% (50 ppm) | Packiaraj and Kumar (2021) |
| Polyaniline/V2O5 composites | Mild steel/ 5 M HCl | 94.256% (7.5 mg/L) | Maruthi et al. (2021) |
| Carboxymethyl cellulose/silver nanoparticles composite | St37 specimen/ 15% H2SO4 | 96.37% (1000 ppm) | Solomon et al. (2017) |
| Novel cellulose derivatives containing metal (Cu, Fe, Ni) oxide nanoparticles | C-steel/ 1 M HCl | 98.6% (250 mg/L) | Gouda and El-Lateef (2021) |
| Carboxymethyl cellulose/metal (Fe, Cu and Ni) nanocomposites | Carbon steel/ 2 N HCl | 98.4% (400 mg/L) | El-Lateef et al. (2020) |
| Poly[(2,6-dicarbonylpyridine)(2,5-dihydrazinyl-1,3,4-thiadiazole)] (AMTP) with α-Al(OH)3-gel | C1018-steel/ 1 M H2SO4 | 97.6% (100 mg/L) | Abd El-Lateef et al. (2022) |
| Poly 12-(3-amino phenoxy) dodecane-1-thiol surfactant self assembled on silver nanoparticles | Carbon steel/ 1 M HCl | 87.59% (375 ppm) | Azzam and Abd El-Aal (2013) |
| Poly para aminophenol (PpAP)/Al2O3 composite | Mild steel/ 1 M HCl | 97.4% (200 mg/L) | Thenmozhi et al. (2014) |
| Chitosan–CuO Nanocomposite | Carbon Steel/ 5% HCl | 90.35% (0.5% CHT1.0-CuO) | Umoren et al. (2022) |
| A chitosan/silver nanoparticles (AgNPs/chitosan) composite | St37 Steel/ 15% HCl | 97.09% (1000 ppm) | Solomon et al. (2016) |
| Chitosan based new nanocomposites | Mild steel/ 1 M HCl | 97% (400 mg/L) | Srivastava et al. (2019) |
| Chitosan Schiff base derivative (CVZ) doped with ZnO nanoparticles | Q235 steel/ 3.5 wt% NaCl | 99.6% (200 ppm) | Liu et al. (2022) |
| Water-soluble poly (N-vinyl imidazole) grafted carboxymethyl chitosan composite | X70 steel/ 1 M HCl | -- (500 ppm) | Eduok et al. (2018) |
| Polyaniline & Polyaminophenol Nanomaterials | Mild steel/ 1 M HCl | 94.66% (100 mg/L Tween80 50 mg/L) | Gao et al. (2019) |
| Spherical polydopamine (PDA) nanoparticles | Mild steel/ 1 M HCl | 86% (40 mol/L) | Yang et al. (2017) |
| Mussel-inspired bio-polymers based on Polydopamine Nanospheres | Mild steel/ 1 M HCl | 99% (5 mg/L) | Habibiyan et al. (2020) |
| Grape seed proanthocyanidins loaded Zein-NaCas composite nanoparticles | Q235 steel/ Seawater | 96.06% (200 mg/L) | Wang et al. (2022) |
| Addition of CeO2 nanoparticles to pectin | X60 steel/ 0.5 M HCl | 91.3% (500 ppm pectin + 5 mM CeO2) | Umoren and Madhankumar (2016) |