Supporting Material

Sodium Alginate Carboxymethyl Cellulose Composite Hydrogel beads for Oral Drug Delivery

Hidayatullaha, Muhmmad Akrama*, Haiqa Khanc, Muhammad Irfana, Ayaz Hassana.

a Interdisciplinary Research Centre in Biomedical Materials (IRCBM), COMSATS University Islamabad (CUI), Lahore Campus, Defence Road Off Raiwind Road, Lahore 54000, Pakistan.

b Office of Research, Innovation and Commercialization, Peshawar Medical College, Riphah International University, 46000, Islamabad, Pakistan.

Figure S1 Physical appearance of Sodium alginate (a) 1% w (w/v %) (b) 1.5% w (w/v %) and (c) composite hydrogel beads SA2% C2% % w (w/v %)

Table S1 Comparison of drug loading contents with different concentration of polymer

| Sample (n=20) | Average weight (g) | Dimension (mm) |
| --- | --- | --- |
| SA3% (low viscosity) | 0.031 | 2.72 |
| SA2% (low viscosity) | 0.021 | 1.91 |
| SA1.5% (low viscosity) | 0.019 | 1.86 |
| SA1% (low viscosity) | 0.015 | 1.40 |
| SA 2% (medium viscosity) | 0.052 | 2.61 |
| SA 1.5% (medium viscosity) | 0.024 | 1.83 |
| SA 1% (medium viscosity) | 0.016 | 1.52 |
| SA1% (low viscosity) C1% | 0.026 | 2.85 |
| SA1 % (low viscosity) C2% | 0.034 | 2.96 |
| SA1 % (low viscosity) C3% | 0.042 | 3.14 |
| SA1 % (low viscosity) C4% | 0.046 | 3.39 |
| SA2% (low viscosity) C1% | 0.031 | 3.13 |
| SA2% (low viscosity) C2% | 0.041 | 3.48 |
| SA2% (low viscosity) C3% | 0.057 | 3.82 |
| SA2% (low viscosity) C4% | 0.062 | 4.14 |

* Correspondence to Dr. Muhammad Akram, Email: drmakram@cuilahore.edu.pk.