Supplementary Information

Pyroelectrocatalytic CO2 reduction for methanol driven by temperature-variation

Lingbo Xiao1,†, Xiaoli Xu1,†, Yanmin Jia2,*, Ge Hu3, Jun Hu3,*, Biao Yuan,4 Yi Yu,4 Guifu Zou1,*

1College of Energy, Soochow Institute for Energy and Materials Innovations, and Key Laboratory of Advanced Carbon Materials and Wearable Energy Technologies of Jiangsu Province Soochow University, Suzhou 215006, China;

2School of Science, Xi’an University of Posts & Telecommunications, Xi’an, 710121, China;

3School of Physical Science and Technology & Jiangsu Key aboratory of Thin Films, Soochow University, Suzhou 215006;

4School of Physical Science and Technology, ShanghaiTech University, Shanghai, 201210, China.

*E-mail: jiayanmin@xupt.edu.cn (Y. Jia), jhu@suda.edu.cn (J. Hu) and zouguifu@suda.edu.cn (G. Zou).

† These authors contributed equally.

Fig. S1 The COMSOL simulation of pyro-potential of Bi2WO6 nanoplate, different colors represent different potentials. It can be seen potential difference occurs on the surfaces of the Bi2WO6 nanoplate.

Fig. S2 Photoelectric response of Bi2WO6 excited by xenon lamp.

Fig. S3 1H NMR spectra of the pyroelectrocatalytic reaction solution, the DMSO were added as internal standard reference

Fig. S4 Gas products by the pyroelectrocatalytic after 20 thermal cycles.

Fig. S5 Characterization of Bi2WO6 after pyroelectrocatalytic CO2 reduction. (a) XRD, (b) SEM.

Fig. S6 (a) pyroelectrocatalytic CO2 conversion without Bi2WO6 (b) pyroelectrocatalytic CO2 conversion at different stable temperature

Fig. S7 (a) The absorption spectra of RhB in aqueous dispersion systems after experiencing different temperature-variation cycles. The inset picture in (a) shows an intuitive diagram of RhB dye decomposition. (b) The pyro-electric catalytic decomposition efficiency of RhB with or without Bi2WO6 under different cycles.

Fig. S8 Slab model for the Bi2WO6(001) surface. (a) and (b) Side and top views of the Bi2WO6(001) surface. The red, cyan, purple and light grey spheres stand for O, W, Bi and H atoms, respectively. In (b), the surface O and W atoms are highlighted to distinguish them from the atoms underneath.

Fig. S9 Temperature variation between 15 oC-70 oC during the pyroelectrocatalytic CO2 reduction.