Journal name: Discover Nano

Supplementary Information

A novel transdermal drug delivery system: drug loaded ROS responsive ferrocene fibers for effective photoprotective and wound healing activity

Sangwoo Kim a,b, Yoon Kim c, Chaehyun Kim a,d, Won Il Choi a, Byoung Soo Kim a, Jinkee Hong b, Hoik Lee c,*, and Daekyung Sung a,*

aCenter for Bio-Healthcare Materials, Bio-Convergence Materials R&D Division, Korea Institute of Ceramic Engineering and Technology, 202 Osongsaengmyeong 1-ro, Osong-eup, Heungdeok-gu, Cheongju, 
bDepartment of Chemical and Biomolecular Engineering, Yonsei University, 50 Yonsei-ro, Seodaemun-gu, Seoul 03722, Republic of Korea

cKorea Institute of Industrial Technology (KITECH), 143 Hanggaulro, Sangnok-gu, Ansan-si, Gyeonggi-do 15588, Republic of Korea

dDepartment of Applied Bioengineering, Research Institute for Convergence Science, Seoul National University, Seoul 08826, Republic of Korea

* Corresponding authors:

Hoik Lee (hoik@kitech.re.kr)

Daekyung Sung (dksung@kicet.re.kr)

S.K. and Y.K. contributed equally to this work.

1. Supplementary Figures and Tables

Figure S1. 1H-NMR spectra of the synthesized ferrocene polymers with chemical structures and peak assignments. The proton chemical shifts are expressed in parts per million (ppm) as follows: δ = (1) 12.4 (br, 1H, COOH of MA), (2) 4.8 (br, 2H, CO2-CH2 of FMMA), (3,4) 4.4–4.1 (br, 9H of FMMA), 2.5 (DMSO‑d6), 2.0–1.7 (br, 15H), and 1.1–0.8 (br, 17H).

50 μm

Figure S2. Scanning electron microscopy image of the electrospun fiber with 43 w/v% of poly(FMMA-r-MA).

(a)

(b)

(c)

(d)

Figure S3. Scanning electron microscopy images of the electrospun fibers with (a) 0 wt%, (b) 20 wt%, (c) 45 wt%, and (d) 70 wt% AT relative to the poly(FMMA-r-MA) content.

| Name | Monomer feed (mol%) |  | Polymer feed (mol%) |  | Conversion (%) | Mn (g/mol) | Mw (g/mol) | Dm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | FMMA | MA | FMMA | MA | 99.77 | 3,217 | 5,150 | 1.601 |  |
| Ferrocene polymer | 16.7 | 83.3 | 16.0 | 84.0 |  |  |  |  |  |

Table S1. Monomer feed and ferrocene polymer compositions along with average molecular weight and polydispersity index of the synthesized ferrocene polymers