Supporting Information for

Monoclinic distortion and magnetic transitions in FeO under pressure and temperature

Xiang Li1*, Elena Bykova2,4, Denis Vasiukov3,5, Georgios Aprilis2,3, Stella Chariton2, Valerio Cerantola5, Maxim Bykov2, Susanne Müller5, Anna Pakhomova5, Fariia I. Akbar2,3, Elena Mukhina6, Innokenty Kantor7, Konstantin Glazyrin4, Davide Comboni5, Aleksandr I. Chumakov5, Catherine McCammon2, Leonid Dubrovinsky2, Carmen Sanchez-Valle1, Ilya Kupenko1,5*

1Institut für Mineralogie, Universität Münster, Corrensstraße 24, D-48149 Münster, Germany. 2Bayerisches Geoinstitut, Universität Bayreuth, 95447 Bayreuth, Germany; 3Material Physics and Technology at Extreme Conditions, Laboratory of Crystallography, Universität Bayreuth, 95440 Bayreuth, Germany; 4Deutsches Elektronen-Synchrotron (DESY), Notkestr. 85, 22607 Hamburg, Germany; 5 European Synchrotron Radiation Facility, 71, avenue des Martyrs CS 40220, 38043 Grenoble, France; 6KTH Royal Institute of Technology, 114 28, Stockholm, Sweden; 7Department of Physics,Technical University of Denmark, 2800 Kgs. Lyngby, Denmark.

*email: xli2@uni-muenster.de; ikupenko@esrf.fr

Contents of this file

Figures S1 to S6

Tables S1 to S4

Fig. S1. (a) Pressure dependence of the relative unit-cell parameters in the monoclinic phase (mC4-model) of FeO, determined by the single crystal X-ray diffraction studies. Pressure dependence of the Fe-O (b) and Fe-Fe (c) distances in the monoclinic phases (mC4-model and mP4). The Fe-OX and Fe-FeX in (b) and (c) show the different Fe-O and Fe-Fe distances in the structure the monoclinic phases (mC4-model and mP4) of FeO. (d) The distortion of Fe-O octahedron and Fe-Fe distance splitting in the monoclinic phases (mC4-model and mP4) at 78 GPa.

Fig. S2. Selected SMS spectra of FeO at indicated pressures and room temperature. The blue arrows show the broadening of the low-pressure doublet that indicates the onset of magnetic ordering at 15 GPa. The green arrow shows the shoulder of the minor charge transfer component from 21 to 73 GPa. The cyan box shows the low-spin singlet of FeO at 94 GPa. The percentage bars indicate the relative absorptions.

Fig. S3. Pressure evolution of the relative abundances of the Mössbauer spectral components of FeO at room temperature.

Fig. S4. Selected Mössbauer spectra of FeO measured at indicated pressure-temperature conditions. The percentage bars indicate the relative absorptions. FeO was heated by resistive heating at 26.5 GPa, and other pressures were heated by laser heating.

Fig. S5. The selected powder XRD pattern of the FeO sample after laser-heating at ~ 78.8 GPa and ~ 1300 K. Insets show portions

of azimuthally unwrapped (caked) 2D diffraction images. The pattern matches the mP4 phase identified by single-crystal XRD. The reflections that are too weak in the non-heated monoclinic phase (mC4 model) are indicated with asterisks. We also note a very tiny amount of reflections from novel iron oxide Fe25O32 (ref.2). The dash lines are guides for the eye.

Fig. S6. Temperature dependence of the hyperfine magnetic field Bhf in FeO high-pressure polymorphs at the indicated pressures. For the crystallographic description of the phases please refer to the main text.

Table S1 Refined unit-cell and crystal-chemical parameters of FeO for mC4 and mP4 model from single-crystal XRD data.

| P (GPa) | a (Å) | b (Å) | c (Å) | β (º) | V (Å3) | Z | V/Z | Vpoly (Å3) | d(Fe-O1) | d(Fe-O2) | d(Fe-Fe1) | d(Fe-Fe2) | model | R1_all | R1 | wR2 | GOOF |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 42.6 | 4.836(2) | 2.725(1) | 2.992(2) | 124.06(7)° | 32.64(3) | 2 | 16.34 | 10.8813 | 2.008(2) | 2.023(1) | 2.723(1) | 2.775(1) | mC4 | 0.0364 | 0.0364 | 0.1088 | 1.372 |
| 47.6 | 4.808(3) | 2.710(2) | 2.986(4) | 123.86(13)° | 32.31(7) | 2 | 16.16 | 10.7694 | 2.002(4) | 2.016(2) | 2.710(2) | 2.760(1) | mC4 | 0.0776 | 0.0777 | 0.2167 | 1.301 |
| 51.3 | 4.758(4) | 2.697(2) | 2.968(6) | 123.60(20)° | 31.71(10) | 2 | 15.85 | 10.5759 | 1.989(5) | 2.005(2) | 2.697(2) | 2.735(2) | mC4 | 0.0833 | 0.0812 | 0.2291 | 1.231 |
| 55.9 | 4.741(4) | 2.684(2) | 2.957(5) | 123.61(16)° | 31.34(8) | 2 | 15.67 | 10.4457 | 1.981(4) | 1.997(2) | 2.684(2) | 2.724(2) | mC4 | 0.0602 | 0.0592 | 0.1474 | 1.198 |
| 58.5 | 4.739(5) | 2.680(2) | 2.957(5) | 123.60(19)° | 31.28(10) | 2 | 15.64 | 10.4269 | 1.981(5) | 1.995(2) | 2.680(2) | 2.722(2) | mC4 | 0.065 | 0.0637 | 0.181 | 1.2 |
| 64.5 | 4.706(6) | 2.643(4) | 2.945(8) | 123.60(30)° | 30.50(14) | 2 | 15.25 | 10.1699 | 1.967(8) | 1.979(3) | 2.643(4) | 2.699(3) | mC4 | 0.0796 | 0.078 | 0.2086 | 1.218 |
| 67.1 | 4.691(5) | 2.641(4) | 2.939(7) | 123.60(20)° | 30.34(12) | 2 | 15.17 | 10.1092 | 1.961(6) | 1.976(3) | 2.641(4) | 2.692(2) | mC4 | 0.086 | 0.0819 | 0.2142 | 1.18 |
| 70.5 | 4.665(7) | 2.629(4) | 2.927(9) | 123.60(30)° | 29.90(15) | 2 | 14.95 | 9.9666 | 1.951(8) | 1.967(4) | 2.629(4) | 2.677(3) | mC4 | 0.0799 | 0.0799 | 0.2136 | 1.354 |
| 74.2 | 4.664(7) | 2.625(6) | 2.932(9) | 123.50(30)° | 29.94(17) | 2 | 14.97 | 9.9779 | 1.953(1) | 1.967(4) | 2.625(6) | 2.676(3) | mC4 | 0.0819 | 0.0762 | 0.1841 | 1.197 |
| 78 | 4.653(10) | 2.614(6) | 2.914(14) | 123.40(5)° | 29.60(20) | 2 | 14.80 | 9.8631 | 1.950(13) | 1.957(6) | 2.614(6) | 2.669(5) | mC4 | 0.0747 | 0.0665 | 0.1539 | 1.055 |

| P (GPa) | a (Å) | b (Å) | c (Å) | β (º) | V (Å3) | Z | V/Z | Vpoly (Å3) | d(Fe-O1) | d(Fe-O2) | d(Fe-O3) | d(Fe-O4) | d(Fe-Fe1) | d(Fe-Fe2) | d(Fe-Fe3) | model | R1_all | R1 | wR2 | GOOF |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 42.6 | 4.838(2) | 2.725(11) | 2.992(2) | 124.06(7)° | 32.68(4) | 2 | 16.34 | 10.892 | 2.005(3) | 2.015(3) | 2.021(2) | 2.027(2) | 2.715(1) | 2.725(1) | 2.838(1) | mP4 | 0.0579 | 0.0558 | 0.1624 | 1.113 |
| 47.6 | 4.805(3) | 2.708(2) | 2.984(4) | 123.84(13)° | 32.25(7) | 2 | 16.125 | 10.75 | 1.999(4) | 2.006(4) | 2.012(4) | 2.019(4) | 2.693(2) | 2.708(2) | 2.823(2) | mP4 | 0.0824 | 0.0791 | 0.2318 | 1.149 |
| 51.3 | 4.760(3) | 2.697(16) | 2.964(4) | 123.66(15)° | 31.67(8) | 2 | 15.835 | 10.558 | 1.979(6) | 1.998(6) | 1.995(5) | 2.013(5) | 2.662(2) | 2.697(2) | 2.810(3) | mP4 | 0.1052 | 0.1027 | 0.2804 | 1.174 |
| 55.9 | 4.747(4) | 2.686(3) | 2.954(5) | 123.59(17)° | 31.38(9) | 2 | 15.69 | 10.459 | 1.978(7) | 1.993(7) | 1.995(7) | 1.999(7) | 2.648(3) | 2.686(3) | 2.809(3) | mP4 | 0.1226 | 0.1212 | 0.3638 | 1.787 |
| 58.5 | 4.735(4) | 2.674(19) | 2.954(5) | 123.67(16)° | 31.13(8) | 2 | 15.565 | 10.376 | 1.969(6) | 1.988(6) | 1.988(7) | 1.997(8) | 2.637(3) | 2.674(2) | 2.803(3) | mP4 | 0.1129 | 0.1098 | 0.348 | 1.565 |
| 64.5 | 4.703(5) | 2.641(3) | 2.938(7) | 123.60(2)° | 30.41(11) | 2 | 15.205 | 10.132 | 1.948(13) | 1.985(13) | 1.961(19) | 1.961(19) | 2.613(5) | 2.641(3) | 2.782(5) | mP4 | 0.1255 | 0.1191 | 0.2695 | 1.249 |
| 67.1 | 4.699(5) | 2.646(3) | 2.941(7) | 123.60(2)° | 30.47(12) | 2 | 15.235 | 10.153 | 1.933(9) | 1.997(9) | 1.957(12) | 2.000(12) | 2.610(4) | 2.646(3) | 2.784(4) | mP4 | 0.1264 | 0.1137 | 0.3156 | 1.267 |
| 70.5 | 4.677(7) | 2.630(3) | 2.930(8) | 123.70(3)° | 29.97(14) | 2 | 14.985 | 9.995 | 1.915(11) | 1.992(11) | 1.939(16) | 1.999(17) | 2.594(5) | 2.630(3) | 2.774(5) | mP4 | 0.1051 | 0.0958 | 0.267 | 1.156 |
| 74.2 | 4.672(7) | 2.625(3) | 2.950(9) | 123.60(3)° | 30.13(15) | 2 | 15.065 | 9.985 | 1.904(17) | 2.001(17) | 1.938(24) | 1.999(24) | 2.599(7) | 2.624(4) | 2.763(7) | mP4 | 0.1292 | 0.1184 | 0.2212 | 1.209 |
| 78 | 4.675(11) | 2.613(4) | 2.934(14) | 123.60(5)° | 29.90(2) | 2 | 14.95 | 9.951 | 1.910(18) | 2.001(18) | 1.942(19) | 1.988(20) | 2.588(7) | 2.613(4) | 2.769(8) | mP4 | 0.1789 | 0.1396 | 0.3698 | 1.244 |
| 78-heated* | 4.670(60) | 2.646(2) | 2.953(16) | 123.70(12)° | 30.40(50) | 2 | 15.2 | 10.120 | 1.910(5) | 2.000(5) | 1.956(17) | 2.003(19) | 2.510(30) | 2.646(2) | 2.860(40) | mP4 | 0.1434 | 0.1265 | 0.3012 | 1.185 |

*presents the pattern collected after heating

| Phases | rB1-FeO | mC4 model-FeO | mC4 model-FeO | mP4-FeO |
| --- | --- | --- | --- | --- |
| Pressure (GPa) | 38.8 | 42.6 | 78 | 78 |
| Temperature (K) Mr | 297 71.85 | 297 71.85 | 297 71.85 | after laser heating at 1700 K 71.85 |
| Crystal system, space group | Rhombohedral, R-3m | Monoclinic, C2/m | Monoclinic, C2/m | Monoclinic, P21/m |
| Lattice parameter, a (Å) | 2.790(3) | 4.836(2) | 4.653(10) | 4.670(60) |
| Lattice parameter, b (Å) | 2.790(3) | 2.725(1) | 2.614(6) | 2.646(2) |
| Lattice parameter, c (Å) | 7.370(12) | 2.992(2) | 2.914(14) | 2.953(16) |
| β (°) | 90 | 124.06(7) | 123.40(50)° | 123.70(12)° |
| γ (°) | 120 | 90 | 90 | 90 |
| Unit cell volume, V (Å3) | 49.67(11) | 32.64(3) | 29.60(20) | 30.40(50) |
| Z | 3 | 2 | 2 | 2 |
| Radiation type | X-ray, λ = 0.2966 Å |  |  |  |
| No. of measured, independent and observed [I > 2σ(I)] reflections | 90, 40, 40 | 88,59,59 | 73, 47, 40 | 159, 92, 71 |
| Rint(F2) (sin θ/λ)max (Å−1) | 0.058 1.009 | 0.07 1.018 | 0.021 1.018 | 0.118 1.030 |
| R[F2 > 2σ(F2)], wR(F2), S | 0.077, 0.178, 1.27 | 0.036, 0.110, 1.37 | 0.067, 0.149, 1.055 | 0.1265, 0.301, 1.185 |
| data/parameters ratio | 40/5 | 60/10 | 44/6 | 92/13 |
| Δρmax, Δρmin (e Å−3) | 1.34, −1.78 | 0.97, −0.87 | 1.41, −0.92 | 1.60, −1.29 |

Table S2 Details of crystal structure refinements of FeO high-pressure phases

Table S3 Mössbauer hyperfine parameters of FeO at high pressure before and after heating.

| P (GPa) | Spectral components | CS (mm/s) | QS (mm/s) | Magnetic field (T) | Assignment |
| --- | --- | --- | --- | --- | --- |
| ES-212-before heating |  |  |  |  |  |
| 2 | Doublet | 0.96(1) | 0.29(1) | - | Fe2+ |
|  | Singlet | 0.21(6) | - | - | Fe3+ |
| 6.5 | Doublet | 0.94(1) | 0.27(1) | - | Fe2+ |
|  | Singlet | 0.17(1) | - | - | Fe3+ |
| 30 | Magnetic sextet | 0.87(1) | 0.18(1) | 40.51(5) | Fe2+ |
|  | Magnetic sextet | 0.72(3) | -0.22(4) | 41.29(40) | Fe2.5+ |
| ES-326-before heating |  |  |  |  |  |
| 1.5 | Doublet | 0.95(1) | 0.29 (1) | - | Fe2+ |
|  | Singlet | 0.26(6) | - | - | Fe3+ |
| 8.6 | Doublet | 0.95(1) | 0.25(2) | - | Fe2+ |
|  | Singlet | 0.22 (7) | - | - | Fe3+ |
| 15 | Doublet | 0.90(1) | 0.23(1) | - | Fe2+ |
|  | Singlet | 0.20(fixed) | - | - | Fe3+ |
| 20.5 | Magnetic sextet | 0.94(1) | 0.13(1) | 33.59(7) | Fe2+ |
| 28.4 | Magnetic sextet | 0.90(1) | 0.19(1) | 39.20(4) | Fe2+ |
|  | Magnetic sextet | 0.71(2) | -0.30(fixed) | 41.36(57) | Fe2.5+ |
| 34.5 | Magnetic sextet | 0.87(1) | 0.17(1) | 41.61(4) | Fe2+ |
|  | Magnetic sextet | 0.70(2) | -0.26(3) | 43.81(63) | Fe2.5+ |
| ES-565-before heating |  |  |  |  |  |
| 40.6 | Magnetic sextet | 0.85(1) | 0.15(1) | 43.29(5) | Fe2+ |
|  | Magnetic sextet | 0.66(1) | -0.15(5) | 44.77(54) | Fe2.5+ |
| ES-1071-before heating |  |  |  |  |  |
| 21 | Magnetic sextet | 0.94(2) | 0.29(2) | 33.85(5) | Fe2+ |
|  | Magnetic sextet | 0.68(3) | -0.24(3) | 34.01(33) | Fe2.5+ |
| 25 | Magnetic sextet | 0.90(1) | 0.18(1) | 38.05(2) | Fe2+ |
|  | Magnetic sextet | 0.67(3) | -0.30(3) | 39.26(19) | Fe2.5+ |
| 34.2 | Magnetic sextet | 0.87(1) | 0.17(1) | 40.75(3) | Fe2+ |
|  | Magnetic sextet | 0.65(2) | -0.32(3) | 41.85(19) | Fe2.5+ |
| 45.2 | Magnetic sextet | 0.82(1) | 0.16(2) | 43.57(1) | Fe2+ |
|  | Magnetic sextet | 0.61(2) | -0.28(5) | 43.89(7) | Fe2.5+ |
| 50.2 | Magnetic sextet | 0.81(1) | 0.19(1) | 44.42(1) | Fe2+ |
|  | Magnetic sextet | 0.60(2) | -0.21(8) | 44.63(4) | Fe2.5+ |
| 52.9 | Magnetic sextet | 0.81(1) | 0.14(1) | 44.49(2) | Fe2+ |
|  | Magnetic sextet | 0.75(7) | -0.40(7) | 47.42(13) | Fe2.5+ |
| 60.3 | Magnetic sextet | 0.77(1) | 0.11(1) | 45.69(2) | Fe2+ |
|  | Magnetic sextet | 0.53(7) | -0.32(5) | 46.14(8) | Fe2.5+ |
| 66.8 | Magnetic sextet | 0.75(1) | 0.09(1) | 46.26(1) | Fe2+ |
|  | Magnetic sextet | 0.53(5) | -0.37(5) | 46.98(9) | Fe2.5+ |
| 73 | Magnetic sextet | 0.73(2) | 0.15(1) | 46.73(3) | Fe2+ |
|  | Magnetic sextet | 0.49(5) | -0.37(fixed) | 47.59(10) | Fe2.5+ |
| 78 | Magnetic sextet | 0.72(1) | 0.03(1) | 47.07(1) | Fe2+ |
|  | Magnetic sextet | 0.42(1) | -0.38(fixed) | 48.77(15) | Fe2.5+ |
| 83 | Magnetic sextet | 0.70(1) | 0.04(3) | 46.83(2) | Fe2+ |
| 88.4 | Magnetic sextet | 0.68(1) | 0.03(2) | 46.87(6) | Fe2+ |
| 94 | Magnetic sextet | 0.68(1) | 0.02(2) | 46.75(4) | Fe2+ |
|  | Singlet | 0.60(7) | - | - | Fe2+-LS |
| ES-326-after heating |  |  |  |  |  |
| 26.5 | Magnetic sextet | 0.90(1) | 0.21(1) | 39.22(1) | Fe2+ |
|  | Magnetic sextet | 0.70(fixed) | -0.29(4) | 40.22(13) | Fe2.5+ |
| 35.6 | Magnetic sextet | 0.85(1) | 0.21(1) | 42.60(2) | Fe2+ |
|  | Magnetic sextet | 0.69(3) | -0.20(5) | 43.98(13) | Fe2.5+ |
| 40.2 | Magnetic sextet | 0.84(1) | 0.15(1) | 43.34(2) | Fe2+ |
| 48 | Magnetic sextet | 0.80(2) | 0.16(1) | 45.04(1) | Fe2+ |
| 48 | Magnetic sextet | 0.81(1) | 0.15(2) | 45.03(8) | Fe2+ |
| 48 | Magnetic sextet | 0.81(2) | 0.16(2) | 45.17(2) | Fe2+ |
| 67.4 | Magnetic sextet | 0.78(2) | 0.13(2) | 46.99(2) | Fe2+ |
|  | Singlet | 0.40(3) | - | - | Fe2+-LS |
| 67.4 | Magnetic sextet | 0.77(1) | 0.13(2) | 47.30(2) | Fe2+ |
|  | Singlet | 0.46(3) | - | - | Fe2+-LS |
| 70.4 | Magnetic sextet | 0.76(1) | 0.13(2) | 47.27(3) | Fe2+ |
|  | Singlet | 0.41(2) | - | - | Fe2+-LS |
| 70.4 | Magnetic sextet | 0.77(1) | 0.10(1) | 47.55(1) | Fe2+ |
|  | Singlet | 0.41(2) | - | - | Fe2+-LS |
| 77 | Magnetic sextet | 0.76(1) | 0.11(2) | 48.00(2) | Fe2+ |
|  | Singlet | 0.40(3) | - | - | Fe2+-LS |
| ES-565-after heating |  |  |  |  |  |
| 40.6 | Magnetic sextet | 0.85(1) | 0.13(2) | 42.95(2) | Fe2+ |
| 55 | Magnetic sextet | 0.80(1) | 0.13(7) | 45.17(2) | Fe2+ |
| 55 | Magnetic sextet | 0.78(1) | 0.14(1) | 45.49(2) | Fe2+ |
| 66.2 | Magnetic sextet | 0.77(1) | 0.12(2) | 46.53(2) | Fe2+ |
|  | Singlet | 0.49(4) | - | - | Fe2+-LS |
| 66.2 | Magnetic sextet | 0.77(1) | 0.13(1) | 46.56(3) | Fe2+ |
|  | Singlet | 0.42(4) | - | - | Fe2+-LS |
| 78.8 | Magnetic sextet | 0.74(1) | 0.10(4) | 47.76(3) | Fe2+ |
|  | Singlet | 0.45(3) | - | - | Fe2+-LS |
| 78.8 | Magnetic sextet | 0.75(1) | 0.12(3) | 48.35(3) | Fe2+ |
|  | Singlet | 0.45(4) | - | - | Fe2+-LS |

LS-Low Spin; ES-212, ES-326, ES-1071 and ES-565 are different experimental runs.

| Pressure (GPa) | GM1+ | GM3+ | GM5a+ | GM5b+ | X3- (As) | X3- (Ap) | X5- (As) | X5- (Ap) | model |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0a 11.1b | -0.00423 -0.02976 | 0.00378 - | 0.01124 - | -0.00618 - | - - | - - | - - | - - | mC4 B1 |
| 13.2b | -0.04062 | - | - | - | - | - | - | - | B1 |
| 16.2b | -0.04906 | - | - | - | - | - | - | - | B1 |
| 21.9b | -0.06230 | - | 0.06928 | - | - | - | - | - | rB1 |
| 25.9b | -0.07551 | - | 0.06654 | - | - | - | - | - | rB1 |
| 29.3b | -0.08318 | - | 0.06375 | - | - | - | - | - | rB1 |
| 33.5b | -0.09197 | - | 0.06176 | - | - | - | - | - | rB1 |
| 35.7b | -0.09716 | - | 0.06038 | - | - | - | - | - | rB1 |
| 37b | -0.09848 | - | 0.06012 | - | - | - | - | - | rB1 |
| 37.4b | -0.10099 | - | 0.05837 | - | - | - | - | - | rB1 |
| 35.2 | -0.09664 | - | - | - | - | - | - | - | rB1 |
| 38.8 | -0.10384 | - | - | - | - | - | - | - | rB1 |
| 42.6 | -0.11088 | -0.0050 | 0.04780 | -0.06198 | - | - | - | - | mC4 |
| 47.6 | -0.11626 | -0.00473 | 0.0518 | -0.0636 | - | - | - | - | mC4 |
| 51.3 | -0.12587 | -0.00585 | 0.05652 | -0.06225 | - | - | - | - | mC4 |
| 55.9 | -0.13247 | -0.00537 | 0.05614 | -0.06281 | - | - | - | - | mC4 |
| 58.5 | -0.13338 | -0.00504 | 0.05645 | -0.06373 | - | - | - | - | mC4 |
| 64.5 | -0.14631 | -0.00358 | 0.05759 | -0.06951 | - | - | - | - | mC4 |
| 67.1 | -0.14949 | -0.00483 | 0.05801 | -0.06857 | - | - | - | - | mC4 |
| 70.5 | -0.15692 | -0.00567 | 0.05845 | -0.06856 | - | - | - | - | mC4 |
| 74.2 | -0.15617 | -0.00494 | 0.06056 | -0.07061 | - | - | - | - | mC4 |
| 78 | -0.16232 | -0.00201 | 0.05954 | -0.06900 | - | - | - | - | mC4 |
| 42.6 | -0.11036 | -0.00484 | 0.04758 | -0.06165 | 0.04032 | 0.02851 | 0.06910 | 0.04886 | mP4 |
| 47.6 | -0.11723 | -0.00447 | 0.05198 | -0.06359 | 0.04203 | 0.02972 | 0.06223 | 0.04400 | mP4 |
| 51.3 | -0.12685 | -0.00563 | 0.05494 | -0.06137 | 0.04497 | 0.0318 | 0.06589 | 0.04659 | mP4 |
| 55.9 | -0.13189 | -0.00418 | 0.05524 | -0.06167 | 0.05094 | 0.03602 | 0.08101 | 0.05728 | mP4 |
| 58.5 | -0.13599 | -0.00514 | 0.05552 | -0.06445 | 0.05122 | 0.03622 | 0.08012 | 0.05665 | mP4 |
| 64.5 | -0.14838 | -0.00292 | 0.05664 | -0.06837 | 0.05663 | 0.04004 | 0.05999 | 0.04242 | mP4 |
| 67.1 | -0.14728 | -0.00455 | 0.05757 | -0.06789 | 0.05255 | 0.03716 | 0.06445 | 0.04557 | mP4 |
| 70.5 | -0.15549 | -0.00532 | 0.05668 | -0.06906 | 0.05261 | 0.0372 | 0.07159 | 0.05062 | mP4 |
| 74.2 | -0.15587 | -0.00542 | 0.05777 | -0.07160 | 0.05903 | 0.04174 | 0.08236 | 0.05824 | mP4 |
| 78 | -0.1575 | -0.00287 | 0.05871 | -0.0739 | 0.05999 | 0.04242 | 0.06728 | 0.04758 | mP4 |
| 78c | -0.14869 | -0.01130 | 0.06149 | -0.07054 | 0.10575 | 0.07478 | 0.14774 | 0.10447 | mP4 |

Table S4 The mode amplitudes for Fe-O polymorphs under pressure. As and Ap mean a standard supercell-normalized and a parent-cell-normalized amplitudes, respectively.

a the data are from Fjellvåg et al1 at 10 K for stoichiometric FeO.

b the parameters are from powder XRD data, and others are from single crystal XRD data.

c the data collected after heating.

Reference:

1	Fjellvåg et al., Monoclinic nearly stoichiometric wüstite at low temperatures. American Mineralogist (2002) 87 (2-3): 347–349.

2      Bykova, E. et al. Structural complexity of simple Fe2O3 at high pressures and temperatures. Nat. Commun. 7, 10661 (2016).