| n=24 | Mass before cleaning | Mass before cleaning | Mass before cleaning | Mean | SD | Mass after cleaning | Mass after cleaning | Mass after cleaning | Mean | SD | Mass loss during cleaning procedure (gram) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 33,0221 | 33,0214 | 33,0215 | 33,0217 | 0,0004 | 33,017 | 33,0152 | 33,019 | 33,0171 | 0,0019 | -0,0046 |
| 2 | 33,037 | 33,035 | 33,0345 | 33,0355 | 0,0013 | 32,9993 | 32,9989 | 32,996 | 32,9981 | 0,0018 | -0,0374 |
| 3 | 33,0382 | 33,0361 | 33,0346 | 33,0363 | 0,0018 | 32,9957 | 33,0009 | 33 | 32,9989 | 0,0028 | -0,0374 |
| 4 | 33,0243 | 33,0222 | 33,0201 | 33,0222 | 0,0021 | 32,9899 | 32,9879 | 32,9893 | 32,9890 | 0,0010 | -0,0332 |
| 5 | 32,9617 | 32,9616 | 32,9602 | 32,9612 | 0,0008 | 32,9499 | 32,9495 | 32,9497 | 32,9497 | 0,0002 | -0,0115 |
| 6 | 33,098 | 33,0967 | 33,0961 | 33,0969 | 0,0010 | 33,0835 | 33,0883 | 33,0872 | 33,0863 | 0,0025 | -0,0106 |
| 7 | 32,9923 | 32,9905 | 32,9897 | 32,9908 | 0,0013 | 32,9691 | 32,9702 | 32,9644 | 32,9679 | 0,0031 | -0,0229 |
| 8 | 33,0301 | 33,0316 | 33,0324 | 33,0314 | 0,0012 | 33,0211 | 33,0239 | 33,021 | 33,0220 | 0,0016 | -0,0094 |
| 9 | 33,0036 | 33,0001 | 32,9995 | 33,0011 | 0,0022 | 32,985 | 32,9882 | 32,9906 | 32,9879 | 0,0028 | -0,0131 |
| 10 | 33,0306 | 33,0292 | 33,0274 | 33,0291 | 0,0016 | 33,018 | 33,0203 | 33,0221 | 33,0201 | 0,0021 | -0,0089 |
| 11 | 33,0432 | 33,0337 | 33,0402 | 33,0390 | 0,0049 | 33,021 | 33,0173 | 33,0162 | 33,0182 | 0,0025 | -0,0209 |
| 12 | 33,0374 | 33,0337 | 33,0344 | 33,0352 | 0,0020 | 32,9997 | 32,9961 | 32,9985 | 32,9981 | 0,0018 | -0,0371 |
| 13 | 33,1125 | 33,1115 | 33,1112 | 33,1117 | 0,0007 | 33,1008 | 33,0987 | 33,0984 | 33,0993 | 0,0013 | -0,0124 |
| 14 | 33,1433 | 33,1421 | 33,1413 | 33,1422 | 0,0010 | 33,1282 | 33,1257 | 33,1259 | 33,1266 | 0,0014 | -0,0156 |
| 15 | 33,0952 | 33,0942 | 33,0923 | 33,0939 | 0,0015 | 33,071 | 33,0776 | 33,0731 | 33,0739 | 0,0034 | -0,0200 |
| 16 | 33,1127 | 33,1091 | 33,1086 | 33,1101 | 0,0022 | 33,0793 | 33,0817 | 33,0815 | 33,0808 | 0,0013 | -0,0293 |
| 17 | 32,9728 | 32,9767 | 32,9768 | 32,9754 | 0,0023 | 32,9452 | 32,9445 | 32,946 | 32,9452 | 0,0008 | -0,0302 |
| 18 | 33,0021 | 33,0022 | 33,0016 | 33,0020 | 0,0003 | 32,9978 | 32,9988 | 32,9975 | 32,9980 | 0,0007 | -0,0039 |
| 19 | 33,0505 | 33,0483 | 33,0458 | 33,0482 | 0,0024 | 33,0417 | 33,0452 | 33,0401 | 33,0423 | 0,0026 | -0,0059 |
| 20 | 33,0185 | 33,0159 | 33,0129 | 33,0158 | 0,0028 | 32,9758 | 32,9796 | 32,9795 | 32,9783 | 0,0022 | -0,0375 |
| 21 | 33,0329 | 33,0311 | 33,0301 | 33,0314 | 0,0014 | 32,9962 | 32,996 | 32,9984 | 32,9969 | 0,0013 | -0,0345 |
| 22 | 33,0866 | 33,0836 | 33,0839 | 33,0847 | 0,0017 | 33,0479 | 33,0499 | 33,0488 | 33,0489 | 0,0010 | -0,0358 |
| 23 | 33,0567 | 33,0531 | 33,0522 | 33,0540 | 0,0024 | 33,0242 | 33,0259 | 33,0293 | 33,0265 | 0,0026 | -0,0275 |
| 24 | 33,0861 | 33,0834 | 33,0817 | 33,0837 | 0,0022 | 33,0673 | 33,0656 | 33,0628 | 33,0652 | 0,0023 | -0,0185 |

Table S1. Mass loss of bottles (n=24) resulting from cleaning procedure applied.

Table S2. Mass loss of the bottles (n=43) resulting during their transport in rivers

| n = 43 | Mass before transport | Mass before transport | Mass before transport | Mean | SD | Distance travelled (m) | Mass after transport | Mass after transport | Mass after transport | Mean | SD | Mass loss occurring during transport (corrected by cleaning errror) (gram) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 33,375 | 33,376 | 33,378 | 33,376 | 0,001 | 8525 | 33,318 | 33,319 | 33,320 | 33,319 | 0,001 | 0,0228 |
| 2 | 33,458 | 33,456 | 33,455 | 33,456 | 0,001 | 1107 | 33,325 | 33,328 | 33,324 | 33,326 | 0,002 | 0,0237 |
| 3 | 33,448 | 33,450 | 33,452 | 33,450 | 0,002 | 3989 | 33,385 | 33,386 | 33,389 | 33,387 | 0,002 | 0,0236 |
| 4 | 33,418 | 33,417 | 33,416 | 33,417 | 0,001 | 7784 | 33,370 | 33,369 | 33,370 | 33,369 | 0,001 | 0,0225 |
| 5 | 33,378 | 33,377 | 33,376 | 33,377 | 0,001 | 2851 | 33,288 | 33,288 | 33,273 | 33,283 | 0,009 | 0,0304 |
| 6 | 33,413 | 33,412 | 33,411 | 33,412 | 0,001 | 5611 | 33,281 | 33,284 | 33,283 | 33,283 | 0,001 | 0,0230 |
| 7 | 33,461 | 33,462 | 33,463 | 33,462 | 0,001 | 3542 | 33,427 | 33,419 | 33,417 | 33,421 | 0,005 | 0,0268 |
| 8 | 33,423 | 33,420 | 33,418 | 33,420 | 0,002 | 861 | 33,375 | 33,369 | 33,371 | 33,372 | 0,003 | 0,0247 |
| 9 | 33,447 | 33,449 | 33,451 | 33,449 | 0,002 | 902 | 33,317 | 33,320 | 33,318 | 33,318 | 0,002 | 0,0231 |
| 10 | 33,438 | 33,437 | 33,435 | 33,437 | 0,001 | 386 | 33,287 | 33,288 | 33,292 | 33,289 | 0,003 | 0,0242 |
| 11 | 33,394 | 33,393 | 33,392 | 33,393 | 0,001 | 3681 | 33,298 | 33,294 | 33,296 | 33,296 | 0,002 | 0,0235 |
| 12 | 33,435 | 33,433 | 33,431 | 33,433 | 0,002 | 819 | 33,375 | 33,370 | 33,370 | 33,372 | 0,003 | 0,0248 |
| 13 | 33,457 | 33,455 | 33,453 | 33,455 | 0,002 | 3573 | 33,292 | 33,292 | 33,291 | 33,292 | 0,000 | 0,0218 |
| 14 | 33,430 | 33,429 | 33,428 | 33,429 | 0,001 | 408 | 33,357 | 33,370 | 33,370 | 33,365 | 0,007 | 0,0290 |
| 15 | 33,415 | 33,414 | 33,413 | 33,414 | 0,001 | 426 | 33,351 | 33,352 | 33,350 | 33,351 | 0,001 | 0,0227 |
| 16 | 33,425 | 33,428 | 33,431 | 33,428 | 0,003 | 10141 | 33,354 | 33,358 | 33,355 | 33,356 | 0,002 | 0,0235 |
| 17 | 33,479 | 33,477 | 33,479 | 33,478 | 0,002 | 10648 | 33,306 | 33,304 | 33,302 | 33,304 | 0,002 | 0,0233 |
| 18 | 33,472 | 33,471 | 33,470 | 33,471 | 0,001 | 408 | 33,410 | 33,418 | 33,411 | 33,413 | 0,004 | 0,0259 |
| 19 | 33,424 | 33,426 | 33,428 | 33,426 | 0,002 | 408 | 33,375 | 33,369 | 33,375 | 33,373 | 0,003 | 0,0249 |
| 20 | 33,426 | 33,428 | 33,430 | 33,428 | 0,002 | 398 | 33,295 | 33,293 | 33,295 | 33,294 | 0,001 | 0,0226 |
| 21 | 33,423 | 33,421 | 33,419 | 33,421 | 0,002 | 1066 | 33,305 | 33,304 | 33,301 | 33,303 | 0,002 | 0,0236 |
| 22 | 33,358 | 33,356 | 33,355 | 33,356 | 0,002 | 10151 | 33,264 | 33,266 | 33,269 | 33,266 | 0,002 | 0,0239 |
| 23 | 33,376 | 33,375 | 33,374 | 33,375 | 0,001 | 1707 | 33,323 | 33,325 | 33,324 | 33,324 | 0,001 | 0,0224 |
| 24 | 33,456 | 33,459 | 33,462 | 33,459 | 0,003 | 16256 | 33,314 | 33,316 | 33,321 | 33,317 | 0,003 | 0,0251 |
| 25 | 33,451 | 33,449 | 33,447 | 33,449 | 0,002 | 411 | 33,374 | 33,380 | 33,379 | 33,378 | 0,003 | 0,0248 |
| 26 | 33,453 | 33,452 | 33,451 | 33,452 | 0,001 | 399 | 33,411 | 33,405 | 33,410 | 33,409 | 0,003 | 0,0249 |
| 27 | 33,455 | 33,455 | 33,456 | 33,455 | 0,001 | 2079 | 33,402 | 33,403 | 33,399 | 33,401 | 0,002 | 0,0236 |
| 28 | 33,449 | 33,448 | 33,447 | 33,448 | 0,001 | 403 | 33,394 | 33,392 | 33,392 | 33,393 | 0,001 | 0,0228 |
| 29 | 33,425 | 33,423 | 33,422 | 33,423 | 0,002 | 12056 | 33,379 | 33,376 | 33,378 | 33,378 | 0,001 | 0,0230 |
| 30 | 33,423 | 33,422 | 33,421 | 33,422 | 0,001 | 1221 | 33,396 | 33,395 | 33,397 | 33,396 | 0,001 | 0,0226 |
| 31 | 33,426 | 33,425 | 33,424 | 33,425 | 0,001 | 6880 | 33,329 | 33,330 | 33,330 | 33,329 | 0,001 | 0,0224 |
| 32 | 33,381 | 33,380 | 33,379 | 33,380 | 0,001 | 10837 | 33,279 | 33,277 | 33,276 | 33,277 | 0,002 | 0,0231 |
| 33 | 33,449 | 33,450 | 33,451 | 33,450 | 0,001 | 1187 | 33,334 | 33,33,65 | 33,335 | 33,335 | 0,001 | 0,0223 |
| 34 | 33,353 | 33,351 | 33,349 | 33,351 | 0,002 | 1184 | 33,250 | 33,247 | 33,247 | 33,248 | 0,001 | 0,0230 |
| 35 | 33,418 | 33,417 | 33,416 | 33,417 | 0,001 | 349 | 33,366 | 33,361 | 33,365 | 33,364 | 0,003 | 0,0244 |
| 36 | 33,460 | 33,459 | 33,458 | 33,459 | 0,001 | 13197 | 33,420 | 33,421 | 33,425 | 33,422 | 0,003 | 0,0241 |
| 37 | 33,421 | 33,420 | 33,419 | 33,420 | 0,001 | 1834 | 33,360 | 33,360 | 33,388 | 33,369 | 0,016 | 0,0377 |
| 38 | 33,432 | 33,430 | 33,431 | 33,431 | 0,001 | 7107 | 33,388 | 33,388 | 33,388 | 33,388 | 0,000 | 0,0219 |
| 39 | 33,448 | 33,446 | 33,444 | 33,446 | 0,002 | 7216 | 33,379 | 33,377 | 33,380 | 33,378 | 0,001 | 0,0231 |
| 40 | 33,426 | 33,427 | 33,428 | 33,427 | 0,001 | 2687 | 33,387 | 33,385 | 33,386 | 33,386 | 0,001 | 0,0226 |
| 41 | 33,425 | 33,424 | 33,423 | 33,424 | 0,001 | 2079 | 33,271 | 33,271 | 33,271 | 33,271 | 0,000 | 0,0219 |
| 42 | 33,419 | 33,417 | 33,416 | 33,417 | 0,002 | 7142 | 33,330 | 33,329 | 33,330 | 33,330 | 0,000 | 0,0219 |
| 43 | 33,415 | 33,414 | 33,412 | 33,414 | 0,002 | 974 | 33,341 | 33,350 | 33,354 | 33,348 | 0,007 | 0,0285 |

Figure S1. Lack of statistically significant relation between mass loss of transported bottles and their travel distance (R2=0.004; p=0.56, n=43).