Table of contents entry

A novel architecture facilitating charge multiplication was developed for high detectivity in CQD-based IRPDs. Photogenerated electrons acquire electrokinetic energy as they pass through the CQD region with strong electric fields and subsequently transfer the excess energy to neighboring valence electrons, thereby inducing electrokinetically pumped charge multiplication. A thick CQD layer (>540 nm) promoted electron acceleration while suppressing electron tunneling. Moreover, a shorter dDtoD tended to increase electron hopping, which improved charge extraction but demanded a high Eth for impact ionization owing to the rise in Auger recombination. Our representative device exhibited a maximum multiplication gain of 85 and a peak D* of 1.4×1014 Jones at a wavelength of 940 nm.

Keywords: Colloidal quantum dots, infrared photodetector, charge multiplication, electron hopping, impact ionization, dot-to-dot distance.

[Authors]

Byeongsu Kim, Sang Yeon Lee, Hyunseok Ko, Jihyung Lee, Hyejeong Song, Sungjun Cho, Min-Ho Lee, and Jung-Yong Lee*

Title

Ultra-high gain colloidal quantum dot infrared photodetectors: Unraveling the potential of electro-kinetically pumped charge multiplication

ToC figure