Supplementary information

Engineering the catalyst interface enables high carbon efficiency in both cation-exchange and bipolar membrane electrolyzers

Huali Wu*1, Bonito Aristide Karamoko1, Wensen Wang1, Jiefeng Liu1, Eddy Petit1, Suming Li1, Chrystelle Salameh1, Damien Voiry*1

1 Institut Européen des Membranes, IEM, UMR 5635, Université Montpellier, ENSCM, CNRS, Montpellier 34000, France

Note S1. Mechanism of carbonate formation in anion-exchange membrane (AEM) during CO2 electroreduction	4

Figure S1. SEM image of spray-coated commercial Ag on gas diffusion layer(a), and the related electrochemical performance in BPM-based MEA electrolyzers with 1M CsOH anolyte under reversed bias(b) and forward bias(c).	5

Figure S2. Faradaic efficiency (a) and total current density, CO energy efficiency(b) over glass fiber-based buffering layer (3M CsHCO3) on Ag catalyst as a functional of cell voltages in BPM-based MEA electrolyzers with 1M CsOH anolyte.	5

Figure S3. SEM images of Ag/buffering electrodes with various PEI concentrations: 0.5%(a), 1.5%(b), 2.1%(c), and 3.4%(d), as well as 2.1% PEI on pure gas diffusion layer(e). Fourier transformed infrared (FTIR) spectra of the pristine Ag-GDL, Ag/0.5% PEI, Ag/1.5% PEI, Ag/2.1% PEI, and Ag/3.4% PEI electrodes (f).	6

Figure S4. BET measurements: N2 adsorption-desorption curves (a) and pore size distributions on 0.5% PEI, 1.5% PEI, 2.1% PEI, and 3.4% PEI hydrogels.	7

Figure S5. The air-contact angle of 0.5%(a), 1.5%(b), 3.4%(c)- PEI derived buffer layers. And the photo of measuring air-contact angle (d).	8

Figure S6. The performance of different loadings of PEI derived buffer layers: 0.5%(a), 1.5%(b), 2.1%(c) and 3.4%-3M CsHCO3(d) in BPM-MEA with 1 M CsOH anolyte.	9

Figure S7. The total current density of different loading of PEI derived buffer layer (0.5%, 1.5%, 2.1% and 3.4%-3M CsHCO3) in BPM-MEA with 1 M CsOH anolyte.	10

Figure S8. The comparison of carbon efficiency: SPU (a) and SPC(b), on different loading of PEI derived buffer layer (0.5%, 1.5%, 2.1% and 3.4%-3M CsHCO3) in BPM-MEA with 1 M CsOH anolyte.	11

Figure S9. Faradaic efficiency over Ag/2.1%-PEI catalysts as a function of applied cell voltages measured with different buffering catholyte: DI water(a), 3 M NaHCO3 (b), 3 M KHCO3 (c), and 3 M CsHCO3 (d). The total (e) and CO partial current density (f) comparison with different buffering catholyte in BPM-based MEA electrolyzers.	12

Figure S10. Faradaic efficiency and total current density over Ag/buffering catalysts as a function of applied cell voltages measured in H2SO4 with a pH value of 0.5.	13

Figure S11. Faradaic efficiency and CO partial current density over Ag/buffering catalysts as a function of applied cell voltages measured in different anolyte (0.5 M K2SO4 + H2SO4) with pH=1.0 (a), pH=0.5 (a), and pH=0.25 (c) in CEM-based MEA electrolyzers. The error bars represent standard deviation from three independent measurements.	14

Figure S12. The schematic of one dimensional COMSOL modelling in BPM-based MEA electrolyzers. GDL refers to gas diffusion layer.	15

Figure S13. The bicarbonate concentration profiles from finite-element numerical simulation results of the buffering layers with 3 M CsHCO3 and PEI concentration from 0.5 to 3.4% in BPM-based MEA configurations.	16

Figure S14. Finite-element numerical simulation results of 2.1% PEI- buffering layers in CEM-based MEA configuration with different 0.5 M K2SO4+ H2SO4 anolytes (pH=0.25, 0.5 and 1). (a) The pH profiles. (b) The bicarbonate concentration profiles.	17

Figure S15. The relationships among flow rate, current density and CO2 conversion efficiency in BPM-based MEA with an optimized Ag/buffer cathode(a), CEM-based MEA with an optimized Ag/buffer cathode (b) and AEM-based MEA electrolyzers with a pure Ag cathode (c)	18

Figure S16. The FE and full cell voltage for neutral MEA with Ag catalyst.	19

Table S1. Comparison of the CO2 Single-pass conversion rate (SPC, %), Single-pass utilization rate (SPU, %) in BPM/CEM-based MEA electrolyzers and this work.	20

Table S2. The chemical reactions at the catholyte region and the corresponding forward kf rate constants and reverse kr rate constants used in simulation7.	21

Table S3. The species diffusion coefficients used in simulation8-11.	22

Table S4. The sechenov coefficients used in simulation 12.	23

References:	23

## Note S1. Mechanism of carbonate formation in anion-exchange membrane (AEM) during CO2 electroreduction

To produce 1M CO by CO2RR, 2M OH- would be generated which will react with another 1M CO2 to form CO32-. Therefore, the total consumed CO2 are 2M.  If the CO FE is 100%, the CO2-to-CO single-pass conversion is limited to 50%.

## Figure S1. SEM image of spray-coated commercial Ag on gas diffusion layer(a), and the related electrochemical performance in BPM-based MEA electrolyzers with 1M CsOH anolyte under reversed bias(b) and forward bias(c).

## Figure S2. Faradaic efficiency (a) and total current density, CO energy efficiency(b) over glass fiber-based buffering layer (3M CsHCO3) on Ag catalyst as a functional of cell voltages in BPM-based MEA electrolyzers with 1M CsOH anolyte.

## Figure S3. SEM images of Ag/buffering electrodes with various PEI concentrations: 0.5%(a), 1.5%(b), 2.1%(c), and 3.4%(d), as well as 2.1% PEI on pure gas diffusion layer(e). Fourier transformed infrared (FTIR) spectra of the pristine Ag-GDL, Ag/0.5% PEI, Ag/1.5% PEI, Ag/2.1% PEI, and Ag/3.4% PEI electrodes (f).

## Figure S4. BET measurements: N2 adsorption-desorption curves (a) and pore size distributions on 0.5% PEI, 1.5% PEI, 2.1% PEI, and 3.4% PEI hydrogels.

## Figure S5. The air-contact angle of 0.5%(a), 1.5%(b), 3.4%(c)- PEI derived buffer layers. And the photo of measuring air-contact angle (d).

## Figure S6. The performance of different loadings of PEI derived buffer layers: 0.5%(a), 1.5%(b), 2.1%(c) and 3.4%-3M CsHCO3(d) in BPM-MEA with 1 M CsOH anolyte.

## Figure S7. The total current density of different loading of PEI derived buffer layer (0.5%, 1.5%, 2.1% and 3.4%-3M CsHCO3) in BPM-MEA with 1 M CsOH anolyte.

## Figure S8. The comparison of carbon efficiency: SPU (a) and SPC(b), on different loading of PEI derived buffer layer (0.5%, 1.5%, 2.1% and 3.4%-3M CsHCO3) in BPM-MEA with 1 M CsOH anolyte.

## Figure S9. Faradaic efficiency over Ag/2.1%-PEI catalysts as a function of applied cell voltages measured with different buffering catholyte: DI water(a), 3 M NaHCO3 (b), 3 M KHCO3 (c), and 3 M CsHCO3 (d). The total (e) and CO partial current density (f) comparison with different buffering catholyte in BPM-based MEA electrolyzers.

## Figure S10. Faradaic efficiency and total current density over Ag/buffering catalysts as a function of applied cell voltages measured in H2SO4 with a pH value of 0.5.

## Figure S11. Faradaic efficiency and CO partial current density over Ag/buffering catalysts as a function of applied cell voltages measured in different anolyte (0.5 M K2SO4 + H2SO4) with pH=1.0 (a), pH=0.5 (a), and pH=0.25 (c) in CEM-based MEA electrolyzers. The error bars represent standard deviation from three independent measurements.

## Figure S12. The schematic of one dimensional COMSOL modelling in BPM-based MEA electrolyzers. GDL refers to gas diffusion layer.

## Figure S13. The bicarbonate concentration profiles from finite-element numerical simulation results of the buffering layers with 3 M CsHCO3 and PEI concentration from 0.5 to 3.4% in BPM-based MEA configurations.

## Figure S14. Finite-element numerical simulation results of 2.1% PEI- buffering layers in CEM-based MEA configuration with different 0.5 M K2SO4+ H2SO4 anolytes (pH=0.25, 0.5 and 1). (a) The pH profiles. (b) The bicarbonate concentration profiles.

## Figure S15. The relationships among flow rate, current density and CO2 conversion efficiency in BPM-based MEA with an optimized Ag/buffer cathode(a), CEM-based MEA with an optimized Ag/buffer cathode (b) and AEM-based MEA electrolyzers with a pure Ag cathode (c)

## Figure S16. The FE and full cell voltage for neutral MEA with Ag catalyst.

## Table S1. Comparison of the CO2 Single-pass conversion rate (SPC, %), Single-pass utilization rate (SPU, %) in BPM/CEM-based MEA electrolyzers and this work.

| Membranes | Catalysts | jtotal (mA/cm2) | SPC (%) | SPU (%) | Note |
| --- | --- | --- | --- | --- | --- |
| BPM (Reversed bias) | Ag | 200 | 9 | 58 | Ref 1 |
|  | Cu/K2SO4 buffering | 200 | / | 78 | Ref 2 |
|  | Ag/CsHCO3 buffering | 375 | 20 | 80 | This work |
| CEM | Ni-N-C | 500 | / | 78 | Ref 3 |
|  | Ag | 60 | / | 88 | Ref 4 |
|  | Ag@C | 300 | 46 | / | Ref 5 |
|  | Cu/PCRL | 100 | / | 85 | Ref 6 |
|  | Ag/ CsHCO3 buffering | 375 | 18 | 77 | This work |

## Table S2. The chemical reactions at the catholyte region and the corresponding forward kf rate constants and reverse kr rate constants used in simulation7.

| Reaction | kf | kr |
| --- | --- | --- |
| CO2+H2O=H++HCO3- | 0.036 [s-1] | 7.83×104 [M-1s-1] |
| CO2+OH-=HCO3- | 2.23×103 [M-1s-1] | 4.85×10-5 [M-1s-1] |
| HCO3-=H++CO32- | 2.5 [s-1] | 5×1010 [M-1s-1] |
| HCO3-+OH-=CO32-+H2O | 6×109 [M-1s-1] | 1.2 [s-1] |
| HCO3-+H+ =CO2+H2O | 7.83×104 [M-1s-1] | 0.036 [s-1] |
| CsHCO3=Cs++HCO3- |  |  |
| K2SO4=2K++SO42- | 1×107 [s-1] | 7.96×107 [M-2s-1] |
| H2O=H++ OH- | 108 [s-1] | 1019 [M-1s-1] |

## Table S3. The species diffusion coefficients used in simulation8-11.

| Species | Diffusion coefficients Di(10-9 m2s-1) |
| --- | --- |
| CO2 | 1.91 |
| H2O | 2.57 |
| K2SO4 | 1.39 |
| KHCO3 | 1.20 |
| K+ | 1.98 |
| H+ | 9.31 |
| OH- | 5.26 |
| HCO3- | 1.185 |
| CO32- | 0.923 |
| SO42- | 1.07 |
| Cs+ | 2.06 |
| CsHCO3 | 1.503 |

## Table S4. The sechenov coefficients used in simulation 12.

| Species | Sechenov coefficients |
| --- | --- |
| hG,0,CO2 | -0.0172 |
| hT,CO2 | -0.000338 |
| hK | 0.0922 |
| hOH | 0.0839 |
| hHCO3 | 0.0967 |
| hCO3 | 0.1423 |
| hCs | 0.0759 |

## References:

- Yang K, Li M, Subramanian S, et al. Cation-driven increases of CO2 utilization in a bipolar membrane electrode assembly for CO2 electrolysis[J]. ACS Energy Letters, 2021, 6(12): 4291-4298.

- Xie K, Miao R K, Ozden A, et al. Bipolar membrane electrolyzers enable high single-pass CO2 electroreduction to multicarbon products[J]. Nature communications, 2022, 13(1): 3609.

- Li H, Li H, Wei P, et al. Tailoring acidic microenvironments for carbon-efficient CO2 electrolysis over a Ni–N–C catalyst in a membrane electrode assembly electrolyzer[J]. Energy & Environmental Science, 2023, 16(4): 1502-1510.

- Pan B, Fan J, Zhang J, et al. Close to 90% single-pass conversion efficiency for CO2 electroreduction in an acid-fed membrane electrode assembly[J]. ACS Energy Letters, 2022, 7(12): 4224-4231.

- Li X, Zhang P, Zhang L, et al. Confinement of an alkaline environment for electrocatalytic CO2 reduction in acidic electrolytes[J]. Chemical Science, 2023, 14(21): 5602-5607.

- O’Brien C P, Miao R K, Liu S, et al. Single pass CO2 conversion exceeding 85% in the electrosynthesis of multicarbon products via local CO2 regeneration[J]. ACS Energy Letters, 2021, 6(8): 2952-2959.

- Chen, Y., Lewis, N.S., and Xiang, C. (2020).  Modeling the Performance of A Flow-Through Gas Diffusion Electrode for Electrochemical Reduction of CO or CO2. J. Electrochem. Soc. 167, 114503.

- Petr Vany ́sek (1996). ionic conductiVity and diffusion at infinite dilution. CRC Handb. Chem. Phys 96, 5–98.

- Aqion Table of Diffusion Coefficients. https://www.aqion.de/site/diffusion-coefficients.

- Applin, K.R., and Lasaga, A.C. (1984). The determination of SO42-, NaSO4-, and MgSO40 tracer diffusion coefficients and their application to diagenetic flux calculations. Geochim. Cosmochim. Acta 48, 2151–2162.

- Sugisaki, M. (1975). Soret Coefficients and Heat of Transport of Polyvalent Electrolytes in an Aqueous Solution. Bull. Chem. Soc. Jpn., 2751.

- Weisenberger, S., and Schumpe, A. (1996). Estimation of Gas Solubilities in Salt Solutions at Temperatures from 273 K to 363 K. AIChE J. 42, 298–300.