Extended Data Figure Legends

Extended Data Fig. 1| Polarized PL of a CuI(Hda) single crystal. a, Diagram illustrating measurement geometry with the excitation source and detection polarized parallel and perpendicular to the crystallographic (100) face. b, Polarized emission spectra from (100) face of CuI(Hda) single crystal. c, Diagram illustrating measurement geometry with the excitation source and detection polarized parallel and perpendicular to the crystallographic (011) face. d, Polarized emission spectra from (011) face. e, Diagram illustrating measurement geometry with the excitation source and detection polarized parallel and perpendicular to the crystallographic (011) face. f, Polarized emission spectra from (011) face.

Extended Data Fig. 2| Angular-resolved C1s core level of PMMA thin films on CuI(Hda). a, ARXPS C1s spectra of a 500 rpm PMMA thin film (3.8 nm) on CuI(Hda). b, ARXPS C1s spectra of a 3000 rpm PMMA thin film (2.1 nm) on CuI(Hda). c, ARXPS C1s spectra of a 6000 rpm PMMA thin film (1.7 nm) on CuI(Hda).

Extended Data Fig. 3| Reference LED devices w/o PMMA capping layer using various HTL/ETL selection. a-c, Energy diagram, J-L-V curves and EQE-J curves of pristine and PMMA-capped ITO/NiOx/CuI(Hda)/Corannulene/LiF/Al blue LEDs. d-f, Energy diagram, J-L-V curves and EQE-J curves of pristine and PMMA-capped ITO/PEDOT:PSS/CuI(Hda)/Ca(acac)2/LiF/Al blue LEDs. g-i, Energy diagram, J-L-V curves and EQE-J curves of pristine and PMMA-capped ITO/NiOx/CuI(Hda)/TPBi/LiF/Al blue LEDs. j-l, Energy diagram, J-L-V curves and EQE-J curves of pristine and PMMA-capped ITO/PEDOT:PSS/CuI(Hda)/TPBi/LiF/Al blue LEDs.

Extended Data Fig. 4| Control CuI(Hda) LEDs with Non-H-bonded SAMs. a, UPS energy levels of 2PACz, Br2PACz and MeO2PACz-functionalized NiOx. b, Current density and luminance as a function of voltage for 2PACz, Br2PACz, and MeO2PACz functionalized deep-blue LEDs. c, EQE-J curves for 2PACz (bottom), Br2PACz (top), and MeO2PACz (middle) functionalized deep-blue LEDs.

Extended Data Fig. 1

Extended Data Fig. 2

Extended Data Fig. 3

Extended Data Fig.4