Supplementary Information for

Unconventional angular dependence of spin-orbit torque-induced harmonic Hall resistances in Pt/YIG bilayers

Takayuki Shiino1, Phuoc Cao Van2, Jong-Guk Choi1, Geunwoo Kim1, Jong-Ryul Jeong2, and Byong-Guk Park1*

1Department of Materials Science and Engineering, KAIST, Daejeon 34141, Republic of Korea

2Department of Material Science and Engineering, Chungnam National University, Daejeon 34134, Republic of Korea

CONTENTS

- Derivation of the equations of Rxy1ω and Rxy2ω

- A possible explanation for the even/odd-number nϕ symmetries in Rxy1ω/Rxy2ω

- X-ray diffraction data

- M-H curve

- Longitudinal harmonic resistances Rxx1ω and Rxx2ω

- Anomalous Hall effect in Pt/YIG

- Supplemental data for Figures 2

S1. Derivation of the equations of Rxy1ω and Rxy2ω

Rxy=RAHEmz+2RPHEmxmy+αSSEImx=RAHEcosθ+RPHEsin2θsin2ϕ+αSSEIsinθcosϕ.       S1

The first and second terms represent AHE and PHE, respectively. The third term represents SSE where αSSE is an SSE coefficient in the unit of Ω/A. Here we consider the magnetization vector m=mx,my,mz=cosϕsinθ,sinϕsinθ,cosθ that is aligned along an external static magnetic field direction (θ, ϕ) in the equilibrium state, where θ and ϕ are the polar and azimuthal angles of an external magnetic field. Current-induced SOTs cause the deviations (Δθ and Δϕ) of m with respect to θ and ϕ. We have performed a similar calculation as in ref. S1,2 and extended the equations to the higher-order terms [including Δθ2, Δθ3, Δθ4… and Δϕ2, Δϕ3, Δϕ4…]. By calculating the Taylor expansions with respect to θ and ϕ, we obtain the following equations:

Rxy=RAHEcosθ-sinθΔθ-12cosθΔθ2+16sinθΔθ3+124cosθΔθ4-1120sinθΔθ5+…+RPHEsin2ϕ+2cos2ϕΔϕ-2sin2ϕΔϕ2-43cos2ϕΔϕ3+23sin2ϕΔϕ4+…sin2θ+sin2θΔθ+cos2θΔθ2-23sin2θΔθ3-13cos2θΔθ4+…+αSSEIcosϕ-sinϕΔϕ-12cosϕΔϕ2+16sinϕΔϕ3+124cosϕΔϕ4+…sinθ+cosθΔθ-12sinθΔθ2-16cosθΔθ3+124sinθΔθ4+…,                S2

with

Δθ=-HDLcosϕHeff=-hDLIcosϕ,                 S3

Δϕ=HFLcosϕHa=hFLIcosϕ,              S4

where HDL and HFL are effective magnetic fields of DL and FL SOTs, respectively; Heff is the effective field including the applied field Ha and the demagnetization and anisotropy fields of the FM layer. Here we assume that the SOT effective fields (HDL and HFL) are proportional to I and define the normalized SOT effective fields hDL≡HDL/IHeff and hFL≡HFL/IHa. Note that hDL and hFL are independent of current I at constant Ha. In this study, we calculated up to the fifth order [Δθ5 and Δϕ5]. Here we consider the in-plane FM under an in-plane (θ=π/2) magnetic field with the azimuthal angle ϕ. The Hall resistance can be described as follows:

Rxy=RAHE-Δθ+16Δθ3-1120Δθ5+…+RPHEsin2ϕ+2cos2ϕΔϕ-2sin2ϕΔϕ2-43cos2ϕΔϕ3+23sin2ϕΔϕ4+…1-Δθ2+13Δθ4+…+αSSEIcosϕ-sinϕΔϕ-12cosϕΔϕ2+16sinϕΔϕ3+124cosϕΔϕ4+…1-12sinθΔθ2+124sinθΔθ4+….                S5

On the other hand, a (Hall) resistance can be generally described as follows:

R=R0+IdRdII=0+12I2d2RdI2I=0+16I3d3RdI3I=0+124I4d4RdI4I=0+…
=R0+IR1+I2R2+I3R3+I4R4+…,                     S6

where

R1≡dRdII=0, R2≡12d2RdI2I=0, R3≡16d3RdI3I=0, R4≡124d4RdI4I=0.           S7

Considering an AC current I=I0sinωt,

R=R0+3R2I024+…sinωt+R1I02+R3I032+…sin2ωt-π2+-R2I024+…sin3ωt+-R3I038+…sin4ωt-π2+….        S8

From this equation, in this study, we define the first and second harmonic resistances as follows:

R1ω≡R0+34I02R2+58I04R4+3564I06R6+OI08.       S9

R2ω≡12I0R1+12I03R3+1532I05R5+OI07.       S10

By substituting Eqs. S3 and S4 into Eq. S5 and comparing Eq. S5 and Eq. S6 with respect to the coefficients of the current-dependent terms, we obtain the expressions of Rp for the Hall resistances where p=1,2,…,8. By further substituting the obtained Rp (p=1,2,…,8) into Eqs. S9 and S10, we obtain Eqs. (1) and (2) (main text) with the following coefficients:

c2ϕ1ω=RPHE-I02RPHE38hDL2+34hFL2+38αSSEhFL+I04RPHE25384hDL4+2564hDL2hFL2+25192hFL4+…, S11

c4ϕ1ω=-I02RPHE316hDL2+38hFL2+I04RPHE596hDL4+516hDL2hFL2+548hFL4+αSSE5128hDL2hFL+5384hFL3+…, S12

c6ϕ1ω=I04RPHE5384hDL4+564hDL2hFL2+5192hFL4-I06RPHE351024hDL4hFL2+351024hDL2hFL4+αSSE3549152hDL4hFL+3524576hDL2hFL3+749152hFL5+…, S13

c8ϕ1ω=-I06RPHE356144hDL4hFL2+356144hDL2hFL4+I08RPHE72048hDL4hFL4+αSSE7262144hDL4hFL3+211310720hDL2hFL5+…, S14

c1ϕ2ω=I012RPHEhFL+12RAHEhDL+12αSSE-I03RPHE12hDL2hFL+13hFL3+116RAHEhDL3+αSSE316hDL2+316hFL2+I05RPHE75512hDL4hFL+75256hDL2hFL3+15256hFL5+52048RAHEhDL5+αSSE252048hDL4+751024hDL2hFL2+252048hFL4+…, S15

c3ϕ2ω=I012RPHEhFL-I03RPHE38hDL2hFL+14hFL3+148RAHEhDL3+αSSE116hDL2+116hFL2+I05RPHE55512hDL4hFL+55256hDL2hFL3+11256hFL5+54096RAHEhDL5+αSSE254096hDL4+752048hDL2hFL2+254096hFL4+…, S16

c5ϕ2ω=-I03RPHE18hDL2hFL+112hFL3+I05RPHE25512hDL4hFL+25256hDL2hFL3+5256hFL5+14096RAHEhDL5+αSSE54096hDL4+152048hDL2hFL2+54096hFL4+…, S17

c7ϕ2ω=I05RPHE5512hDL4hFL+5256hDL2hFL3+1256hFL5-I07RPHE494608hDL4hFL3+497680hDL2hFL5+αSSE749152hDL4hFL2+749152hDL2hFL4+…. S18

The SSE term (RxySSE) in Eq. (4) (in the main text) is defined as RxySSE=12αSSEI0. It is also noteworthy that the hybridization of the DL and FL SOTs (the product terms of hFL and hDL: e.g., hDL2hFL3) becomes significant in the nonlinear current-dependent terms. Note that one can read I0→J0 (with a multiplication of geometric factors) when discussing current density. From Eq. S17, the coefficients of c5ϕ2ω=-A1I03+A2I05+… mentioned in the main text can be expressed as follows:

A1=RPHE18hDL2hFL+112hFL3,

A2=RPHE25512hDL4hFL+25256hDL2hFL3+5256hFL5+14096RAHEhDL5+αSSE54096hDL4+152048hDL2hFL2+54096hFL4.

S2. A possible explanation for the even/odd-number nϕ symmetries in Rxy1ω/Rxy2ω

Here we consider the reason why Rxy1ωRxy2ω contains only even (odd) number (n) terms with respect to the angle nϕ. The harmonic resistance Rxy1ωRxy2ω is even (odd) with respect to I0 [see Eq. S9 (Eq. S10)]. Thus Rxy1ωRxy2ω is symmetric (antisymmetric) under the sign reversal of I0:

Rxy1ωI0=Rxy1ω-I0,     S19

Rxy2ωI0=-Rxy2ω-I0.      S20

As seen in the schematic illustration of Fig. S1, Eqs. S19 and S20 require the following constraints with respect to ϕ:

Rxy1ωϕ=Rxy1ωϕ+π,     S21

Rxy2ωϕ=-Rxy2ωϕ+π.      S22

Therefore, from Eqs. S21 and S22, only n = even (odd) number sin/cos(nϕ) terms can exist in Rxy1ωRxy2ω.

Figure S1 | Schematic illustration for the sign reversal of I0.

Schematics for current flow at time t under (a) I=I0sinωt and (b) I=-I0sinωt.

S3. X-ray diffraction data

Figure S2 shows the X-ray diffraction pattern of the YIG(30)/GGG, the main sample used for magnetoresistance measurements in this study. A peak corresponding to single-crystal GGG(444) is evident, and the additional peak adjacent to the GGG peak is attributed to YIG(444), which has a small difference in lattice constants. The presence of Laue oscillation fringes indicates layer-by-layer growth and the high crystallinity of the YIG film3.

Figure S2 | X-ray diffraction pattern of 30 nm thick YIG film grown on a GGG(111) substrate.

S4. M-H curve

Figure S3 shows the in-plane magnetization (M) vs an applied external field (Ha) curves of the YIG(30)/GGG sample. A magnetic field was swept along 112 (red) and 110 (green), which are orthogonal to each other. The in-plane M-H curves do not indicate any significant in-plane anisotropic behavior in the present YIG sample.

Figure S3 | In-plane M-H curves of the YIG sample used in this study.

S5. Longitudinal harmonic resistances Rxx1ω and Rxx2ω

We show the longitudinal harmonic resistances (Rxx1ω and Rxx2ω) of the Pt-YIG sample corresponding to SMR and magnonic unidirectional SMR (USMR)4. We observe typical cos2ϕ behavior of longitudinal SMR in Rxx1ω measured at J0=4.1×1010 A/m2 (Fig. S4a). The observed SMR ratio RSMR/Rxx1ωϕ=0 is 0.036% where RSMR≡Rxx1ωϕ=0-Rxx1ωϕ=π/2. Figure S4b shows the angular dependence of Rxx2ω measured at J0=4.1×1010 A/m2. The ϕ dependence of Rxx2ω of the present system can be expressed as follows:4

Rxx2ω=RxxSSE+RxxUSMRsinϕ-2RSMRHFL+HOeHasinϕcos2ϕ,

where HFL and HOe indicate the effective fields of the current-induced field-like (FL) SOT and current-induced Oersted fields, respectively. By fitting with Rsinϕ2ω≡RxxSSE+RxxUSMR and Rsinϕcos2ϕ2ω≡-2RSMRHFL+HOe/Ha as the fitting parameters, we decompose sinϕ and sinϕcos2ϕ contributions. The value of  Rsinϕ2ω is plotted as a function of Ha in Fig. S4c. The USMR component (RxxUSMR), which is indicated by the decreasing behavior of Rsinϕ2ω with Ha, becomes absent above ~ 1000 Oe, where only the SSE (RxxSSE) contribution remains. The USMR ratio defined as RxxUSMR/Rxx1ωϕ=0 is 2.3×10-4 % at J0=1×1011 A/m2 and Ha=25 Oe.

Figure S4 | Longitudinal MR signals in Pt/YIG

a, b, Angular dependences of Rxx1ω (a) and Rxx2ω (b) measured at room temperature (T ≈ 300 K). The longitudinal SMR curve Rxx1ω (a) was obtained at Ha=25 Oe. Note that the constant offsets are subtracted in the Rxx2ω plot (b). c, Plot of Rsinϕ2ω=RxxSSE+RxxUSMR as a function of Ha. All the data here were obtained at J0=4.1×1010 A/m2.

S6. Anomalous Hall effect in Pt/YIG

Figure S5 shows the anomalous Hall effect (AHE) measurement result of our Pt/YIG sample. Note that the contribution from the ordinary Hall effect (which is linear in the field Ha applied in the out-of-plane direction) and a constant offset value are subtracted. The obtained value is RAHE=2.7 mΩ. The seemingly unusual AHE behavior in the low-field region is attributed to the planar Hall effect (i.e., transverse SMR), which is significantly larger than the AHE in the present Pt/YIG system. Note that a similar behavior has been observed previously5.

Figure S5 | Anomalous Hall effect measurement result.

S7. Supplemental data for Figures 2

Figure S6 shows the measured Rxy1ω and Rxy2ω at different fields (25 Oe≤Ha≤10 kOe) and currents (0.5×1011≤J0≤2.2×1011 A/m2), for magnetic fields (Ha = 25, 100 and 2600 Oe) and current densities.

Figure S6 | Angle-dependent PHE curves for various values of magnetic fields and current density.

a, b, Angular dependences of Rxy1ω (a) and Rxy2ω (b) for various values of current density at Ha = 25 Oe, 200 Oe, and 2600 Oe.

References

S1. Han, B. et al. Determination of the Spin-Orbit Torques in Ferromagnetic-Heavy-Metal Bilayers Using Harmonic Longitudinal Voltage Measurements. Phys Rev Appl 13, 014065 (2020).

S2. Cheng, Y. et al. Third harmonic characterization of antiferromagnetic heterostructures. Nature Communications 13, 1–6 (2022).

S3. Cao Van, P. et al. Effect of annealing temperature on surface morphology and ultralow ferromagnetic resonance linewidth of yttrium iron garnet thin film grown by rf sputtering. Appl Surf Sci 435, 377–383 (2018).

S4. Liu, G. et al. Magnonic Unidirectional Spin Hall Magnetoresistance in a Heavy-Metal-Ferromagnetic-Insulator Bilayer. Phys Rev Lett 127, 207206 (2021).

S5. Avci, C. O. et al. Nonlocal Detection of Out-of-Plane Magnetization in a Magnetic Insulator by Thermal Spin Drag. Phys Rev Lett 124, 027701 (2020).