Table 1. Physical properties of ACWCF and ACWP obtained from the N2 adsorption-desorption isotherms.

| Physical properties | ACWCF | ACWP |
| --- | --- | --- |
| Specific surface (BET) (m2.g-1) | 1110.99 | 298.59 |
| Total pore volume (cm3.g-1) at P/Po = 0.99205 | 0.082468 | 0.056205 |
| Average pore diameter (Å) | 26.949 | 21.34 |

Table 2. Chemical identification of surface groups and Zeta potential of ACWCF and ACWP adsorbents

| Adsorbent | Acidic groups, mmol g-1 |  |  |  | Basic groups mmol g-1 | pHpzc | Interpretation |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Carboxylic | Lactonic | Phenolic | Total acidic groups |  |  |  |
| ACWCF | 2.4 | 0 | 0 | 2.4 | 8.8 | 7.1 | Basic |
| ACWP | 0 | 0 | 30.4 | 30.4 | 6.4 | 6.92 | Acid |

Table 3. Adsorption rate constants of the Fe(II) ions for ACWCF and ACWP adsorbents

| Adsorbent | Co (mg/L) | qe,exp. (mg/g) | Pseudo-first-order |  |  | Pseudo-second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | qe1, cal. (mg/g) | K110-2(1/min) | R2 | qe2, cal. (mg/g) | K210-2 (g/mg-min) | R2 |
| ACWCF | 25 | 31.87 | 4.468 | 2.76 | 0.988 | 35.71 | 0.130 | 0.997 |
| ACWP | 25 | 20.47 | 3.799 | 1.84 | 0.948 | 25.64 | 0.077 | 0.995 |

Table 4. Langmuir, Freundlich and Dubinin- Radushkevich parameters for adsorption of Fe(II) ion onto ACWCF and ACWP adsorbents

| Adsorbent | T (K) | qe,exp. (mg/g) |  | Langmuir |  |  |  |  | Freundlich |  |  |  |  | Dubinin-R |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | qm, (mg/g) | KL (L/mg) |  | R2 |  | Kf, (mg/g) (L/mg)1/n | n | R2 |  | qs, mg/g | KD-R (mol2 KJ-2) | E (kJ mol-1) | R2 |
| ACWCF | 298 | 55 |  | 62.5 | 1.454 |  | 0.995 |  | 29.814 | 2.624 | 0.835 |  | 54.217 | 10-7 | 2.236 | 0.995 |
|  | 313 | 56.6 |  | 62.5 | 2 |  | 0.999 |  | 33.284 | 2.923 | 0.860 |  | 54.434 | 7 x10-8 | 2.672 | 0.992 |
|  | 328 | 59.6 |  | 66.666 | 2.142 |  | 0.997 |  | 36.488 | 3.039 | 0.789 |  | 58.615 | 7 x10-8 | 2.672 | 0.917 |
| ACWP | 298 | 35.8 |  | 38.474 | 0.141 |  | 0.820 |  | 7.964 | 1.543 | 0.835 |  | 15.910 | 10-6 | 0.707 | 0.991 |
|  | 313 | 63.9 |  | 40.165 | 0.080 |  | 0.444 |  | 8.723 | 1.6 | 0.860 |  | 16.793 | 10-6 | 0.707 | 0.992 |
|  | 328 | 37.9 |  | 41.679 | 0.195 |  | 0.848 |  | 10.034 | 1.7 | 0.789 |  | 19.125 | 10-6 | 0.707 | 0.987 |

Table 5.  Comparison of the Fe(II) adsorption capacity of onto ACWCF and ACWP adsorbents with other activated carbon adsorbents

| Adsorbent | Kinetic/Isotherm models | Endo/Exothermic process | Specific surface (BET) (m2.g-1) | qm(mg/g) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Activated carbon prepared from olive stone waste | PSO/ Langmuir | - | 886.72 | 57.47 | [55] |
| Activated carbon prepared from pomegranate peel | PFO/ Langmuir | Exothermic | - | 18.52 | [56] |
| Activated carbon derived from Pecan shell | PSO/ Temkin | Endothermic | 1500 | 41.66 | [57] |
| Activated carbon derived from Walnut shell | PSO/ Sips | Endothermic | 1223 | 39.250 | [58] |
| Activated carbon derived from ombretum quadrangulare Kurz. | PSO/ Langmuir | Endothermic | 374.2 | 15 | [59] |
| Activated carbon derived from Rice husk ash | PSO/ Fraundlich | - | - | 6.210 | [60] |
| ACWCF | PSO/ Fraundlich | Endothermic | 1110.9 | 66.666 | This study |
| ACWP | PSO/ Dubinin- Radushkevich | Endothermic | 298.59 | 41.679 | This study |

Table 6. Thermodynamic parameters for adsorption of Fe(II) on ACWCF and ACWP adsorbents

| Adsorbent | Temperature (K) | ΔG° (kJ mol-1) | ΔH° (kJ mol-1) | ΔS° (J mol-1 K-1) |
| --- | --- | --- | --- | --- |
| ACWCF | 298 | -21.740 | 20.03 | 0.139 |
|  | 313 | -23.060 |  |  |
|  | 328 | -25.920 |  |  |
| ACWP | 298 | -19.395 | 2.768 | 0.074 |
|  | 313 | -20.510 |  |  |
|  | 328 | -21.626 |  |  |