Supporting Information

Fig. S1. TGA curves of DG-CC, EG-CC and DW-CC

Fig. S2. XPS spectra of DG-CC, EG-CC and DW-CC: (a-c) Survey spectra, and (d-f) High-resolution spectra of Co 2p, respectively.

Fig. S3. (a) Nitrogen adsorption and desorption curves of DG-CC, EG-CC and DW-CC and their (b) Pore size distribution plots.

Fig. S4. XRD patterns of the intermediates during solvothermal process with different solvents: (a) DG, (b) EG and (c) DW, respectively.

Fig. S5. CV curves of (a) DG-CC, (b) EG-CC and (c) DW-CC from 2.5 to 3.0 V in charging process.

Table S1. Comparison of the long cycle performances of our CoCO3 samples with other previous cobalt carbonate anodes.

| Type | Electrode materials | Specific capacity/(mAh /g) | Current density/(A /g) | Cycles | Initial Coulombic efficiency |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Bare CoCO3 | DG-CC | 690.7 | 1 | 1000 | 71.32% | this work |  |
|  | EG-CC | 382.8 | 1 | 1000 | 66.84% | this work |  |
|  | DW-CC | 295.0 | 1 | 1000 | 73.82% | this work |  |
|  | CoCO3 after ball-milling | 231.4 | 0.05 | 20 | 46.72% | 1 |  |
|  | CC | 361.2 | 0.1 | 100 | 68.03% | 2 |  |
|  | CoCO3 microspindles | 469 | 0.5 | 40 | 60.53% | 3 |  |
|  | Micro-spherical CoCO3 | 330 | 0.2 | 100 | 65.88% | 4 |  |
|  | CoCO3 rhombohdra | 480 | 1 | 500 | 76.84% | 5 |  |
|  | CoCO3 dumbbells | 821 | 1 | 500 | 75.94% | 5 |  |
|  | CoCO3 spheres | ~400 | 0.1 | 50 | 72.1% | 6 |  |
|  | CCSMSs | 1475 | 0.5 | 500 | 75.23% | 7 |  |
| CoCO3 composite | CoCO3/GNS | 680 | 0.5 | 40 | 66.52% | 8 |  |
|  | CC–PPy | 458.6 | 5 | 560 | 60.11% | 2 |  |
|  | CoCO3/CNT | ~600 | 0.1 | 50 | not mentioned | 6 |  |
|  | S-CoCO3 | 500 | 1 | 100 | 78.19% | 9 |  |
|  | T-CoCO3 | ~250 | 1 | 100 | 73.76% | 9 |  |
|  | spindle-CoCO3/CNF | 666 | 1 | 100 | not mentioned | 10 |  |
|  | CoCO3/RGO | 343.1 | 0.2 | 200 | 81.9% | 11 |  |
| bicomponent CoCO3 | Zn0.12Co0.88CO3 | ~600 | 0.1 | 50 | 71% | 6 |  |
| bicomponent CoCO3 composite | Zn0.12Co0.88CO3/CNT | ~800 | 0.1 | 50 | 74% | 6 |  |

Table S2. The specific capacity contribution of DG-CC, EG-CC and DW-CC in different regions in the 20th and 1000th cycle.

| Region | Specific capacity of the 20th cycle (mAh/g) |  |  | Specific capacity of the 100th cycle (mAh/g) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | DG-CC | EG-CC | DW-CC | DG-CC | EG-CC | DW-CC |
| 1 | 281.2 | 275.0 | 192.9 | 283.9 | 124.2 | 97.4 |
| 2 | 214.5 | 223.9 | 184.2 | 182 | 101.6 | 77.2 |
| 3 | 251.4 | 232.0 | 200.2 | 224.8 | 157.0 | 121.0 |
| Total | 747.1 | 730.9 | 577.3 | 690.7 | 382.8 | 295.6 |

Table S3. The values of Rs and Rct in the 1st cycles of DG-CC, EG-CC and DW-CC fitting by Zview.

|  | DG-CC 1st cycle | EG-CC 1st cycle | DW-CC 1st cycle |
| --- | --- | --- | --- |
| Rs/(Ohm) | 3.515 | 3.508 | 3.5 |
| Rct/(Ohm) | 28.80 | 37.55 | 56.64 |

Table S4. The values of Rs, RSEI and Rct in different cycles of DG-CC fitting by Zview.

|  | 30th | 90th | 120th | 200th |
| --- | --- | --- | --- | --- |
| Rs/(Ohm) | 3.634 | 4.346 | 4.521 | 5.554 |
| RSEI/(Ohm) | 99.68 | 163.3 | 123.4 | 39.44 |
| Rct/(Ohm) | 269.8 | 484.4 | 168.9 | 66.76 |

References

[1] S. Zhao, Z. Wang, Y. He, H. Jiang, Y.W. Harn, X. Liu, C. Su, H. Jin, Y. Li, S. Wang, Q. Shen, Z. Lin, A Robust Route to Co2(OH)2CO3 Ultrathin Nanosheets with Superior Lithium Storage Capability Templated by Aspartic Acid‐Functionalized Graphene Oxide, Adv. Energy Mater 9 (2019) 1901093. https://doi.org/10.1002/aenm.201901093.

[2] Z. Ding, B. Yao, J. Feng, J. Zhang, Enhanced Rate Performance and Cycling Stability of a CoCO3-Polypyrrole Composite for Lithium Ion Battery Anodes, J. Mater. Chem. A 1 (2013) 11200−11209. https://doi.org/10.1039/C3TA12227A.

[3] L. Wang, W. Tang, Y. Jing, L. Su, Z. Zhou, Do Transition Metal Carbonates Have Greater Lithium Storage Capability Than Oxides? A Case Study of Monodisperse CoCO3 and CoO Microspindles, ACS Appl. Mater. Interfaces 6 (2014) 12346−12352. https://doi.org/10.1021/am5021233.

[4] G. Huang, S. Xu, Y. Yang, H. Sun, Z. Li, Q. Chen, S. Lu, Micro-Spherical CoCO3 Anode for Lithium-Ion Batteries, Mater Lett 131 (2014) 236–239. https://doi.org/ 10.1016/j.matlet.2014.05.208.

[5] S. Zhao, S. Wei, R. Liu, Y. Wang, Y. Yu, Q. Shen, Cobalt Carbonate Dumbbells for High-Capacity Lithium Storage: A Slight Doping of Ascorbic Acid and an Enhancement in Electrochemical Performances, J. Power Sources 284 (2015) 154–161. https://doi.org/10.1016/j.jpowsour.2015.03.016.

[6] J. Yin, Z. Ding, D. Lei, L. Tan, J. Deng, B Li, Y. B. He, Zn-Substituted CoCO3 Embedded in Carbon Nanotubes Network as High Performance Anode for Lithium-Ion Batteries, J. Alloy Compd 712 (2017) 605–612. https://doi.org/10.1016/j.jallcom. 2017.04.055.

[7] Z. Zhao, Z. Wan, D.K. Deni, X. Su, J. Zhan, L. Hou, X. Zhang, C. Yuan, Intrinsic Lithium Storage Mechanisms and Superior Electrochemical Behaviors of Monodispersed Hierarchical CoCO3 Sub-Microspheroids as a Competitive Anode towards Li-Ion Batteries, Electrochim. Acta 307 (2019) 20−29. https://doi.org/10.1016/ j.electacta. 2019.03.171.

[8] L. Su, Z. Zhou, X. Qin, Q. Tang, D. Wu, P. Shen, CoCO3 Submicrocube/Graphene Composites with High Lithium Storage Capability, Nano Energy 2 (2013) 276–282. https://doi.org/10.1016/j.nanoen.2012.09.012.

[9] S. Shi, M. Zhang, Y. Liu, X. Hua, H. Guo, G. Yang, Efficient Construction of a CoCO3/Graphene Composite Anode Material for Lithium-Ion Batteries by Stirring Solvothermal Reaction, Ceram. Int 44 (2018) 3718–3725. https://doi.org/10.1016/ j.ceramint.2017.11.152.

[10] Z. Lu, H. Wang, T. Zhou, C. Ma, F. Yin, X. Jiang, G. Yang, CoCO3 Micrometer Particles Stabilized by Carbon Nanofibers Networks as Composite Electrode for Enhanced Rate and Cyclic Performance of Lithium-Ion Batteries, Electrochim. Acta 270 (2018) 22–29. https://doi.org/10.1016/j.electacta.2018.03.081.

[11] T. Zeng, C, Zhang, Facile-Synthesized Amorphous CoCO3 for High-Capacity Lithium-Ion Battery Anode, Ionics 25 (2019) 4149–4159. https://doi.org/10.1007/ s11581-019-03006-4.