Supporting information for

Research on carbon black and Cerium co-doped Ti4O7-CB-Ce electrocatalytic oxidation of tetracycline-based antibiotics

Junxia Chen a, Xinyi He a, Chongtian Lei a, Weigang Li a, Zhenzhen Yang a, Qing Zhou a*.

a State Key Laboratory of Pollution Control and Resource Reuse, School of Environment, Nanjing University, Nanjing210023, China.

State Key Laboratory of Pollution Control and Resource Reuse, School of Environment, Nanjing University, Nanjing210023, China.

*Corresponding author:

zhouqing@nju.edu.cn

Page S3 Figure S1

Page S4 Figure S2

Page S5 Figure S3

Page S6 Figure S4

Page S7 Figure S5

Page S8 Figure S6

Page S9 Table S1

Page S10 Table S2

Page S11 Table S3

Page S12 Table S4

Page S13 Table S5

Figure S1 EDS elemental analysis of (a) Ti4O7, (b) Ti4O7-CB, (c) Ti4O7-Ce, (d) Ti4O7-CB-Ce.

Figure S2 TOC removal of MNC degradation. (a) Ce doping, (b) Ce and CB co-doping.

Figure S3 Mineralization current efficiency at different current densities.

Figure S4. Electrical power at different electrolyte concentrations.

Figure S5. (a) raw MNC mass spectra; (b) MNC mass spectra at 10 min of reaction.

Figure S6. Degradation profile of MNC under the interference of inorganic anions (HCO3-, Cl- and NO3-).

Table S1 Electrochemical characterization information for Ti4O7, Ti4O7-CB, Ti4O7-Ce and Ti4O7-CB-Ce, OEP: oxygen precipitation potential; AP: anodic potential; j0: current density; RΩ: internal resistance; Rct: charge transfer resistance

| Anode | OEP (V vs SHE) | AP at j0 = 6 mA/cm2 (V vs SHE) | RΩ/Ω | Rct/Ω |
| --- | --- | --- | --- | --- |
| Ti/Ti4O7 | 1.76 | 2.42 | 9.65 | 1.76 |
| Ti/Ti4O7-Ce | 1.90 | 2.37 | 9.55 | 2.04 |
| Ti/Ti4O7-CB | 1.68 | 2.30 | 8.30 | 1.28 |
| Ti/Ti4O7-CB-Ce | 2.10 | 2.15 | 7.25 | 1.05 |

Table S2 Kinetic parameters of the MNC degradation fitting curve

| Doping condition | K（min-1） | R2 |
| --- | --- | --- |
| None | 0.0711 | 0.8693 |
| 1% Ce | 0.1202 | 0.9567 |
| 5% Ce | 0.2867 | 0.9694 |
| 10% Ce | 0.3870 | 0.9896 |
| 15% Ce | 0.2414 | 0.9540 |
| 10% Ce+1% CB | 0.4236 | 0.9678 |
| 10% Ce+3% CB | 0.4623 | 0.9723 |
| 10% Ce+5% CB | 0.3633 | 0.9933 |
| 10% Ce+10% CB | 0.3005 | 0.9748 |

Table S3 EE/O and related parameters in the electrocatalytic oxidation of MNC by Ti/Ti4O7-CB-Ce at different current densities (at 50% MNC removal rate)

| current densities mA/cm2 | Volt V | Current A | T min | Volume L | C0/C | EE/O KWh·m-3 |
| --- | --- | --- | --- | --- | --- | --- |
| 10 | 8 | 0.08 | 5 | 0.15 | 2 | 1.181 |
| 20 | 13 | 0.16 | 3.75 | 0.15 | 2 | 2.879 |
| 30 | 16 | 0.24 | 3.3 | 0.15 | 2 | 4.677 |
| 40 | 25 | 0.32 | 2.5 | 0.15 | 2 | 7.382 |

Table S4 Endpoint pH of the reaction and its variation under different initial pH conditions

| Initial pH | End pH | Difference |
| --- | --- | --- |
| 3 | 2.9 | 0.1 |
| 5 | 4.1 | 0.9 |
| 7 | 4.3 | 2.7 |
| 9 | 4.5 | 4.5 |
| 11 | 6.4 | 4.6 |

Table S5 Pharmaceutical wastewater quality indicators

| quality indicators | unit |  |
| --- | --- | --- |
| pH | - | 5.47 |
| COD | mg/L | 5850 |
| BOD5 | mg/L | 1460 |
| NH3-N | mg/L | 56 |
| TN | mg/L | 145 |
| conductivity | mS/cm | 5.78 |