Porous carbon nanosheets from coal tar pitch for zinc ion hybrid capacitor

Feng Weia*, Qingyun Liua, Jiadong Zhanga, Ziquan Rena, Linlin Zhangb,*

Fig. S1 O1s spectra of (a) PCNS1 and (b) PCNS3.

Fig. S2 (a) Capacitive contribution ratio, (e) capacitive contribution at 2 mV s−1 and (f) 100 mV s−1 of Zn‖PCNS2 ZHC at 1.6 V.

Table S1 The contents of C, O elements in PCNSs.

| Samples | C1s (at.%) | O1s (at.%) | O1s (at.%) |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | C=O | C-O | -OH |
| PCNS1 | 95.24 | 4.76 | 1.15 | 1.66 | 1.95 |
| PCNS2 | 93.72 | 6.28 | 1.13 | 3.53 | 1.62 |
| PCNS3 | 96.84 | 3.16 | 0.74 | 1.20 | 1.22 |

*Corresponding author. E-mail address: fengw@chzu.edu.cn (F. Wei); 1061701412@qq.com (L.L. Zhang).