Table 2: Mean (SD, n=10) of enamel variables analyzed according to the toothpaste experimental after in situ cariogenic challenge

| Analysis | Toothpaste Experimental |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Placebo | 1100F |  | 1100F-CPP-ACP |  | 1100F-TMP |  | 1100F-CPP-ACP-TMP |  |
| %SH (KHN) | -72.6a (3.9) | -47.2b (2.2) |  | -45.1c (2.3) |  | -39.0d (2.8) |  | -27.5e (3.2) |  |
| KHN (KHN µm) | 7,258.1a (722.5) | 5,000.4b (688.8) |  | 5,044.7b (598.1) |  | 4,395.1c (682.6) |  | 3,205.4d (398.1) |  |
| Enamel (µg/mm3) |  |  |  |  |  |  |  |  |  |  |
| F | 1.6a (0.6) | 2.5b (0.6) |  | 2.6b (0.7) |  | 2.7b (0.8) |  | 3.4c (0.6) |  |
| Ca | 378.3a (88.3) | 695.3b (91.5) |  | 790.3c (72.4) |  | 912.1d (62.4) |  | 1244.3e (70.4) |  |
| P | 396.6a (88.2) | 586.8b (75.6) |  | 735.2c (79.3) |  | 788.4c (92.5) |  | 954.1d (72.6) |  |

Different lowercase letters indicate significant differences among the treatments for each variable separately. One-way ANOVA, repeated measures followed Student–Newman–Keuls’ test (n = 10, p < 0.001). Values represent means (standard deviations). %SH: percentage of surface hardness loss. ΔKHN: integrated subsurface hardness loss. F: fluoride in enamel. Ca: calcium in enamel. P: phosphor in enamel.