| Toothpaste Experimental |  | Composition |  |
| --- | --- | --- | --- |
| Placebo | Titanium dioxide, carboxymethylcellulose, sodium methyl-p-hydroxybenzoate, saccharin, mint oil, glycerin, abrasive silica, sodium lauryl sulfate, and water. |  |  |
| 1100F | Titanium dioxide, carboxymethylcellulose, sodium methyl-p-hydroxybenzoate, saccharin, mint oil, glycerin, abrasive silica, sodium lauryl sulfate, sodium fluoride (NaF: 1100 ppm F) and water. |  |  |
| 1100F-CPP-ACP | Titanium dioxide, carboxymethylcellulose, sodium methyl-p-hydroxybenzoate, saccharin, mint oil, glycerin, abrasive silica, sodium lauryl sulfate, sodium fluoride (NaF: 1100 ppm F), casein phosphopeptide-amorphous calcium phosphate (CPP-ACP: 10%) and water. |  |  |
| 1100F-TMP | Titanium dioxide, carboxymethylcellulose, sodium methyl-p-hydroxybenzoate, saccharin, mint oil, glycerin, abrasive silica, sodium lauryl sulfate, sodium fluoride (NaF: 1100 ppm F), sodium trimetaphosphate (TMP: 3%) and water. |  |  |
| 1100F-CPP-ACP-TMP | Titanium dioxide, carboxymethylcellulose, sodium methyl-p-hydroxybenzoate, saccharin, mint oil, glycerin, abrasive silica, sodium lauryl sulfate, sodium fluoride (NaF: 1100 ppm F), casein phosphopeptide-amorphous calcium phosphate (CPP-ACP: 10%), ), sodium trimetaphosphate (TMP: 3%) and water. |  |  |

Table 1: Toothpaste experimental composition