Supporting Information

Catalytic Dehydration of Lactic Acid to Acrylic Acid over Phosphorus Promoted and Alkali Modified ZSM-5

Ainur Syeitkhajy*, Ismail Boz, Mehtap Safak Boroglu

Faculty of Engineering, Chemical Engineering Department, Istanbul University-Cerrahpasa, 34320 Istanbul, Turkey.

Table S1 Coded independent variables and levels of the reaction conditions

factor; name; units; minimum; maximum. X1; flow rate; ml/h; 2; 7.2. X2; temperature; °C; 340; 360. X3; feed concentration; %; 20; 30.

Table S2 Experimental design matrix and results

run; X1; X2; X3; selectivity (%); LA conv. (%). AA; AcH; others. 1; 4.6; 350; 30; 69; 14; 17; 94. 2; 4.6; 360; 25; 70; 16; 14; 97. 3; 4.6; 350; 25; 72; 15; 13; 95. 4; 7.2; 340; 20; 52; 30; 18; 100. 5; 4.6; 350; 25; 68; 17; 15; 95. 6; 2; 340; 30; 41; 11; 48; 96. 7; 2; 360; 30; 51; 13; 36; 99. 8; 7.2; 360; 20; 73; 21; 6; 100. 9; 2; 350; 25; 56; 12; 32; 97. 10; 2; 340; 20; 51; 9; 40; 99. 11; 7.2; 340; 30; 45; 26; 29; 93. 12; 4.6; 340; 25; 51; 16; 33; 95. 13; 4.6; 350; 20; 83; 13; 4; 98. 14; 7.2; 360; 30; 75; 21; 4; 96. 15; 7.2; 350; 25; 68; 19; 13; 96. 16; 4.6; 350; 25; 75; 16; 9; 95. 17; 2; 360; 20; 50; 10; 40; 100. 18; 4.6; 350; 25; 76; 15; 9; 95. AA: acrylic acid; AcH: acetaldehyde; LA: lactic acid; others: propionic acid, 2,3-pentanedione, carbon deposits and gaseous products.

Table S3 Analysis of variance test for the AA selectivity of the ZSM-5/P-Na catalyst

source; sum of square; df; mean square; F-value; p-value; R2. model; 11.09; 9; 1.23; 34.74; < 0.0001; 0.9751. X1-flow rate; 0.8924; 1; 0.8924; 25.16; 0.001. X2-temperature; 2.15; 1; 2.15; 60.74; < 0.0001. X3-feed conc.; 0.0375; 1; 0.0375; 1.06; 0.3339. X1X2; 0.8561; 1; 0.8561; 24.13; 0.0012. X1X3; 0.0099; 1; 0.0099; 0.2788; 0.6118. X2X3; 0.2548; 1; 0.2548; 7.18; 0.0279. X1²; 1.07; 1; 1.07; 30.25; 0.0006. X2²; 1.48; 1; 1.48; 41.83; 0.0002. X3²; 0.1247; 1; 0.1247; 3.51; 0.0977. residual; 0.2838; 8; 0.0355. lack of fit; 0.1491; 5; 0.0298; 0.6637; 0.6793. pure error; 0.1347; 3; 0.0449. cor total; 11.38; 17.

Table S4 Analysis of variance test for the LA conversion of the ZSM-5/P-Na catalyst

| source | sum of squares | df | mean square | F-value | p-value | R2 |
| --- | --- | --- | --- | --- | --- | --- |
| model | 0.2179 | 9 | 0.0242 | 153.14 | < 0.0001 | 0.9942 |
| X1-flow rate | 0.0252 | 1 | 0.0252 | 159.16 | < 0.0001 |  |
| X2-temperature | 0.0269 | 1 | 0.0269 | 170.4 | < 0.0001 |  |
| X3-feed conc. | 0.0009 | 1 | 0.0009 | 5.99 | 0.0401 |  |
| X1X2 | 0.0003 | 1 | 0.0003 | 1.8 | 0.2164 |  |
| X1X3 | 0.0159 | 1 | 0.0159 | 100.4 | < 0.0001 |  |
| X2X3 | 0.0082 | 1 | 0.0082 | 51.86 | < 0.0001 |  |
| X1² | 0.0129 | 1 | 0.0129 | 81.82 | < 0.0001 |  |
| X2² | 0.0051 | 1 | 0.0051 | 32.45 | 0.0005 |  |
| X3² | 0.0025 | 1 | 0.0025 | 15.63 | 0.0042 |  |
| residual | 0.0013 | 8 | 0.0002 |  |  |  |
| lack of fit | 0.0013 | 5 | 0.0003 |  |  |  |
| pure error | 0 | 3 | 0 |  |  |  |
| cor total | 0.2191 | 17 |  |  |  |  |