Fluorescent enhancement of CNDs from Cinnamon bark with L-Arginine doping for Yeast cell Imaging

Urvi M. Lada, Dhruti J. Daveb, Bhumi N. Desaib, Devesh H. Sutharb, Chetan K. Modia,*

aApplied Chemistry Department, Faculty of Technology & Engineering, The Maharaja Sayajirao University of Baroda, Vadodara, Gujarat-390001, India

bDepartment of Biochemistry, Faculty of Science, The Maharaja Sayajirao University of Baroda, Vadodara, Gujarat-390001, India

- Materials and method

Scheme. S1 Synthetic route for the preparation of Cinnamon bark wood-derived carbon nanodots (CNDs) (upper) and L-Arginine-doped CNDs (lower) by hydrothermal reaction.

- Results and Discussion

  - Dynamic Light Scattering (DLS)

Fig. S1 DLS measurement graph of synthesized  CNDs.

FT-IR Spectroscopy

Fig. S2 FT-IR spectra of raw Cinnamon bark wood powder.

In fig. S2, the peak at 1626 cm−1 is attributed to the stretching vibration of an aldehyde carbonyl C═O, which corresponds to aldehydes such as coumarin [1, 2] associated the appearance of these peaks with cinnamaldehyde and other aldehydes founded in high levels in cinnamon bark.

The peak at 1536  cm-1 corresponds to the skeleton vibration C═C of an aromatic ring, normally associated with eugenol, a phenol present in cinnamon oil. The peak at 1450 cm−1 is described by the bending vibration absorption of an alcohol C–OH. On the other hand, in the region 3500-2800 cm−1 (C–H and O–H region) the peak in 2920 cm−1 can be assigned to symmetric C–H stretching vibrations that are caused by cinnamon lipids (essential oil) and the peaks at 3300 cm−1 are O–H stretching vibration absorption peaks. These are due to the presence of various alcohols including eugenol, with both carbonyl and hydroxy function groups and small quantities of proteins present in the sample. On the other hand, in the region 3500-2800 cm−1 (C–H and O–H region) the peak in 2920 cm−1 can be assigned to symmetric C–H stretching vibrations that are caused by cinnamon lipids (essential oil) and the peaks at 3300 cm−1 are O–H stretching vibration absorption peaks.

Fig. S3. FT-IR spectra of pristine L-Arginine

In the FT-IR spectrum of pure L-arginine (fig. S3), the observed peaks are indicative of specific functional groups. The region of 3300-3500 cm-1 exhibits stretching vibrations attributed to O-H (notably at 3470 cm-1) and N-H in the amino groups (particularly at 3197 cm-1). Additionally, peaks at 3019 cm-1 and 2890 cm-1 are associated with C-H stretching vibrations in the aliphatic region. The peak at 1700 cm-1 signifies C=O stretching vibrations of the carbonyl group within the side chain, while 1638 cm-1 is likely associated with the amide I band, primarily linked to C=O stretching vibrations in the peptide bond. Furthermore, the peak at 1515 cm-1 is attributed to N-H bending vibrations in the amino group. Lastly, values at 1326 cm-1 and 1070 cm-1 correspond to C-N stretching vibrations, possibly associated with the peptide bond, and C-N stretching vibrations in the amino group, respectively.

References

1. 	Li Y, Kong D, Wu H (2013) Analysis and evaluation of essential oil components of cinnamon barks using GC–MS and FTIR spectroscopy. Ind Crops Prod 41:269–278. https://doi.org/10.1016/j.indcrop.2012.04.056

2. 	Lin R-C, Mohamed M, Chen T, Kuo S-W (2017) Coumarin- and Carboxyl-Functionalized Supramolecular Polybenzoxazines Form Miscible Blends with Polyvinylpyrrolidone. Polymers (Basel) 9:146. https://doi.org/10.3390/polym9040146