Ultrasensitive determination of quercetin using electrochemical sensor based on nickel-doping Zinc-based zeolite imidazole frame with a four-point star morphology

- Jianxia Gu*a, Yankun Weia, Yongxia Lia, Tingting Weia, Zhanbin Jina

- aDepartment of chemistry, Xinzhou Normal University, Xinzhou, Shanxi, China

Corresponding Authors

E-mail: 1583229616@qq.com (Jianxia Gu)

Fig. S1. Nyquist plot (EIS) of Star ZIF-8-R/GCE, GCE and Ni-ZIF-8-S/GCE in 0.1 M KCl solution containing 5 mM Fe (CN)63-/4- with frequency range of 0.1-100 KHz.

Fig. S2. (A) XPS spectra of prepared ZIF-8-R and Ni-ZIF-8-S. (B) Ni2p signal deconvolution.

Table S1 Effect of interferences on the oxidation peak current changes for quercetin determination on the Ni-ZIF-8-S.

| Interferences | Concentration (μM) | Signal change (%) |
| --- | --- | --- |
| Na+ | 1500 | 0.87 |
| K+ | 1500 | 0.43 |
| Ca2+ | 1500 | 0.52 |
| Mg2+ | 1500 | 0.90 |
| Ascorbic acid | 10 | 0.33 |
| Uric acid | 10 | 0.64 |
| Glucose | 10 | -0.12 |
| Rutin | 5 | 0.59 |
| Luteolin | 5 | 0.56 |

Table S2 DPV determination of quercetin on electrochemical sensor based on Ni-ZIF-8-S in the real sample of urine.

| Samples | Amount added (nM) | Amount found (nM) | Recovery (%) | RSD (n=3, %) |
| --- | --- | --- | --- | --- |
| 1 | 10 | 9.8 | 98.0 | 1.56 |
|  | 10 | 9.9 | 99.0 |  |
|  | 10 | 9.6 | 96.0 |  |
| 2 | 50 | 48.5 | 97.0 | 2.06 |
|  | 50 | 48.4 | 96.8 |  |
|  | 50 | 50.2 | 100.4 |  |
| 3 | 100 | 100.3 | 100.3 | 1.95 |
|  | 100 | 101.1 | 101.1 |  |
|  | 100 | 97.4 | 97.4 |  |