Supplementary material appendix 1:

Plasma-engineered sugarcane bagasse: A novel strategy for efficient mercury removal from aqueous solutions

Angie Paola Santacruz-Salasa, Maria Lúcia Pereira Antunesa, Elidiane Cipriano Rangela, Cláudia Hitomi Watanabea, André Henrique Rosaa*.

a São Paulo State University (Unesp), Institue of Science and Technology, Av. 3 de março 511, 18087-315, Sorocaba-SP, Brazil

*Corresponding Author

E-mail address: andre.rosa@unesp.br

Experimental

Mercury Adsorption Study

The adsorption capacity of the adsorbents was calculated from the Equation 1:

| Qe=v*(Ci-Cf)/m | (1) |
| --- | --- |

Where:

Qe: amount adsorbed (mg/g) at equilibrium (mg/g).

Ci: initial Hg concentration (mg/l)

Cf: final concentration of Hg (mg/l)

v: volume of the solution (l)

m: mass of the adsorbent (g)

The removal efficiency was calculated with the Equation 2 presented below

| ER%=(Ci-Cf)/Ci*100 | (2) |
| --- | --- |

Where:

ER: percentage of adsorbed Hg

Ci: initial concentration (mg/l)

Cf: final concentration (mg/l)

Adsorption Kinetics

Lagergren's Pseudo-First Order kinetics stands out as the most frequently utilized model for liquid-solid adsorption systems. This model characterizes the adsorption kinetics of a species on an adsorbent particle through the following non-linear equation (BENJELLOUN et al., 2021):

| Qt= Qe (1- exp -Klt) | (3) |
| --- | --- |

Where

K1: the equilibrium rate constant in the pseudo–first-order model (L/min).

Qe: amount adsorbed at equilibrium (mg/g)

Qt: amount adsorbed as a function of time (mg/g)

t: time (min) for each of the aliquots

In the Pseudo-Second Order kinetic model, adsorption takes place on two surface sites. This model, proposed by Blanchard in 1984, can be represented by the following non-linear equation (BENJELLOUN et al., 2021; GÓMEZ-HERRERA, 2021):

| Qt= (Qe2K2t)/(1+Qe2K2t) | (4) |
| --- | --- |

Where

K2: the equilibrium rate constant of the pseudo–second-order model (g/mg min)

Qe: amount adsorbed at equilibrium (mg/g)

Qt: amount adsorbed as a function of time (mg/g)

t: time (min) for each of the aliquots

Adsorption isotherms

The Langmuir adsorption isotherm is based on the assumption of a homogeneous adsorbent surface, and its corresponding expression can be formulated as follows:

| Qe= (qmaxKLCe)/1 + KLCe | (5) |
| --- | --- |

Where

KL: Langmuir adsorption constant

Qe: amount of solute adsorbed per unit mass of material at equilibrium (mg/g)

qmaxt: maximum adsorption capacity in the monolayer (mg/g)

Ce: concentration at equilibrium (mg/L)

The linear form of the Langmuir isotherm equation may be written as:

| Ce/Qe=(1/KLqmax)+(Ce/qmax) | (6) |
| --- | --- |

The Freundlich isotherm is an equation that best describes a heterogeneous adsorbent surface. It may be written as:

| Qe= KfCe1/n | (7) |
| --- | --- |

Where

Kf: Freundlich adsorption constant

Qe: amount of solute adsorbed per unit mass of material at equilibrium (mg/g)

1/n: represents the heterogeneity factor.

Ce: concentration at equilibrium (mg/L)

The linear form of the Freundlich isotherm equation may be written as:

| Log Qe = Log Kf*(1/n)logCe | (8) |
| --- | --- |

Results and discussion

Figure A1 - FTIR spectra of the of the as-received and the modified SB under various time intervals and pressures: (a) 80 W (b) 190 W and c) 300 W

A

B

C