Novel Fe/Ca oxide co-coated biochar enables efficient phosphorus recovery

Anqi Hu a,c†, Yongcan Jiang a,b† *, Jiaqi An c, Xiaodian Huang a, Abdelbaky Hossam Elgarhy c,d, Huafen Cao c, Guanglong Liu c

Affiliation

a PowerChina Huadong Engineering Corporation Ltd., Hangzhou 311122, Zhejiang Province, China;

b Institute of Soil and Water Resources and Environmental Science, College of Environmental and Resource Sciences, Zhejiang University, Hangzhou 310058, Zhejiang Province, China;

c State Environmental Protection Key Laboratory of Soil Health and Green Remediation, College of Resources and Environment, Huazhong Agricultural University, Wuhan 430070, China;

d Central Laboratory for Environmental Quality Monitoring (CLEQM), National Water Research Center (NWRC), Qalyobia, 13621, Egypt.

*Corresponding author:

Mr. Yongcan Jiang. E-mail: jiangyc6@zju.edu.cn. Tel:+86-130-1592-2119

† Contributed equally to this work.

CONTENTS:

Table S1 Surface area and pore structure of BC and FCBC

Table S2 Parameters for adsorption isotherm of P on FCBC

Table S3 Comparison of the maximum adsorption capacity of different biochar adsorbents for P

Table S4 Parameters for adsorption kinetics of P on FCBC

Fig. S1 Element mapping of BC(a) and FCBC(b)

Fig. S2 C 1s (a) and O 1s (b) XPS spectra of BC

Fig. S3 Phosphorus adsorption capacity of FCBC at different pyrolysis temperatures

Fig. S4 The abundance ratio of phosphates in solutions of varying pH

Fig. S5 Determination of the point of zero charge of FCBC

Table S1 Surface area and pore structure of BC and FCBC

|  | SBET (m2/g) | Pore volume (cm3/g) | Pore size (nm) |
| --- | --- | --- | --- |
| BC | 291.2934 | 0.218585 | 4.2745 |
| FCBC | 441.5189 | 0.263961 | 3.3788 |

Table S2 Parameters for adsorption isotherm of P on FCBC

| Models | Parameter 1 | Parameter 2 | R2 |
| --- | --- | --- | --- |
| Langmuir | KL=0.01623 L/mg | Qm=53.3131 mg P/g | R2=0.9982 |
| Freundlich | KF=4.1684 mg1-1/n·g-1·L1/n | 1/n=0.4168 | R2=0.9631 |

Table S3 Comparison of the maximum adsorption capacity of different biochar adsorbents for P

| Adsorpant | Isotherm | Kinetics | Qmax (mg/g) | References |
| --- | --- | --- | --- | --- |
| MgO-modified biochar | F | S | 18.98 | (Wu et al. 2019) |
| Palm waste biochar | L | S | 26.90 | (Fseha et al. 2021) |
| Lime sludge modified biochar | R-P | S | 15 | (Yang et al. 2021) |
| Hydrocotyle vulgaris derived novel biochar beads | L | S | 20.32 | (Fu et al. 2022) |
| Fe/Mg-Biochar Nanocomposites | L-F | S | 6.95 | (Tao et al. 2020) |
| Lanthanum-ammonia-modified hydrothermal biochar | L | S | 43.1 | (Shang et al. 2022) |
| ZrO2 nanoparticles embedded in biochar modified with layered double oxides nanosheets | L | S | 20.36 | (Song et al. 2024) |
| FCBC | L | S | 53.31 | This study |

F, L, R-P, and S represent Freundlich, Langmuir, Redlich-Peterson, and Pseudo-second-order, respectively.

Table S4 Parameters for adsorption kinetics of P on FCBC

| Models | Parameter 1 | Parameter 2 | R2 |
| --- | --- | --- | --- |
| Pseudo-first-order | k1=0.0049 | Qe=18.1213 mg P/L | R2=0.9844 |
| Pseudo-second-order | k2=0.0002 | Qe=22.2797 mg P/L | R2=0.9939 |
| Intraparticle diffusion | ki1=0.8783 | C1=-1.0271 | R2=0.9961 |
|  | ki2=0.6253 | C2=2.4845 | R2=0.9921 |
|  | ki3=0.0701 | C3=16.4141 | R2=0.9911 |

Table S5 Physical and chemical properties of water samples

| Parameters | Samples |  |  |
| --- | --- | --- | --- |
|  | Ponds | Farmlands | Ditches |
| pH | 8.14±0.064 | 8.79±0.089 | 8.02±0.042 |
| DOC (mg/L) | 10.3±0.505 | 11.5±0.156 | 15.8±0.459 |
| TP (mg/L) | 0.34±0.004 | 0.53±0.005 | 0.11±0.002 |
| DOP (mg/L) | 0.21±0.002 | 0.37±0.003 | 0.084±0.001 |
| TN (mg/L) | 0.92±0.014 | 1.13±0.014 | 0.89±0.014 |
| NO3--N (mg/L) | 0.150±0.001 | 0.140±0.001 | 0.525±0.002 |
| NO2--N (mg/L) | 0.009±0.002 | 0.010±0.001 | 0.072±0.002 |

Fig. S1 Element mapping of BC(a) and FCBC(b)

Fig. S2a demonstrated that the C1s XPS spectra of BC can be categorized into five distinct peaks, which corresponded to C-C/C-H (284.8 eV), C-O (286.1 eV), C=O (287.8 eV), O-C=O* (289.3 eV), and CO32- (290.3 eV). The O1s spectra of BC (Fig. S2b) exhibited three distinct peaks corresponding to C-O-C/C-O-H (532.5 eV), O=C-O* (533.9 eV), and C=O/CO32- (531.1 eV).

Fig. S2 C 1s (a) and O 1s (b) XPS spectra of BC

Fig. S3 Phosphorus adsorption capacity of FCBC at different pyrolysis temperatures

Fig. S4 The abundance ratio of phosphates in solutions of varying pH (Yin et al. 2018)

Fig. S5 Determination of the point of zero charge of FCBC

References

Fseha YH, Sizirici B, Yildiz I (2021) The potential of date palm waste biochar for single and simultaneous removal of ammonium and phosphate from aqueous solutions. J Environ Chem Eng 9. https://doi.org/10.1016/j.jece.2021.106598

Fu XX, Wang P, Wu JD, Zheng PY, Wang TT, Li XX, Ren MZ (2022) Hydrocotyle vulgaris derived novel biochar beads for phosphorus removal: static and dynamic adsorption assessment.  J Environ Chem Eng 10. https://doi.org/10.1016/j.jece.2022.108177

Shang ZX, Wang YR, Wang SQ, Jin FL, Hu Z (2022) Enhanced phosphorus removal of constructed wetland modified with novel Lanthanum-ammonia-modified hydrothermal biochar: Performance and mechanism. Chem Eng J 449. https://doi.org/10.1016/j.cej.2022.137818

Song X, Chen X, Chen WQ, Ao TQ (2024) ZrO2 nanoparticles embedded in biochar modified with layered double oxides nanosheets for phosphorus removal by capacitive deionization. Sep Purif Technol 328. https://doi.org/10.1016/j.seppur.2023.125117

Tao XF, Huang T, Lv B (2020) Synthesis of Fe/Mg-Biochar Nanocomposites for Phosphate Removal. Materials (Basel) 13. https://doi.org/10.3390/ma13040816

Wu LP, Wei CB, Zhang SR, Wang YD, Kuzyakov Y, Ding XD (2019) MgO-modified biochar increases phosphate retention and rice yields in saline-alkaline soil. J Cleaner Prod 235:901-9. https://doi.org/10.1016/j.jclepro.2019.07.043

Yang SM, Katuwal S, Zheng W, Sharma B, Cooke R (2021) Capture and recover dissolved phosphorous from aqueous solutions by a designer biochar: Mechanism and performance insights. Chemosphere 274:129717. https://doi.org/10.1016/j.chemosphere.2021.129717

Yin QQ, Ren HP, Wang RK, Zhao ZH (2018) Evaluation of nitrate and phosphate adsorption on Al-modified biochar: Influence of Al content. Sci Total Environ 631-632:895-903. https://doi.org/10.1016/j.scitotenv.2018.03.091