Supporting Information

The interlayer twist effectively regulates interlayer excitons in InSe/Sb van der Waals heterostructure

Anqi Shi1, Ruilin Guan1, Zifan Niu1, Wenxia Zhang2, Xiuyun Zhang 3, Shiyan Wang1, Bing Wang4*, Jin Lv5* and Xianghong Niu1*

1 State Key Laboratory of Organic Electronics and Information Displays & Institute of Advanced Materials (IAM), School of Science and College of Electronic and Optical Engineering, Nanjing University of Posts & Telecommunications, Nanjing

210023, China

2 School of Optoelectronic Engineering, Chongqing University of Posts and Telecommunications, Chongqing 400065, P. R. China

3 College of Physics Science and Technology, Yangzhou University, Yangzhou 225002, China

4 Institute for Computational Materials Science, Joint Center for Theoretical Physics (JCTP),

School of Physics and Electronics, Henan University, Kaifeng, 475004, China

5 Key Laboratory of Magnetic Molecules, Magnetic Information Materials Ministry of Education, School of Chemical and Material Science, Shanxi Normal University, Taiyuan030031, China.

Email: wb@henu.edu.cn; lvjin_sxnu@163.com; and xhniu@njupt.edu.cn

Methods

Density functional theory (DFT) were conducted within the projected-augmented wave (PAW) potentials1 in the Vienna ab initio simulation package (VASP).2, 3 The electron exchange and correlation functionals were described by Perdew-Burke-Ernzerhof generalized gradient approximation (PBE-GGA)4. The energy cutoff was set to 500 eV. A Γ-centered 4×4×1Monkhorst-Pack k-point grid was adopted for the heterostructure with different twist angle. vdW interactions were described by Grimme et al. (DFT-D3).5 Dipole correction was considered to cancel the errors of total energy, atomic force and electrostatic potential caused by periodic boundary condition.6

The dynamics of photogenerated carriers were obtained based on the ab initio NAMD within time domain DFT using Hefei-NAMD code.7-10 for the optimized heterostructures, we heated to 300 K for 2 ps using the repeated velocity rescaling method, and then obtained a 10 ps microcanonical trajectory with a time step of 1fs via ab initio molecular dynamics (ABMD).11 By selecting 100 different initial geometries from the first 2 ps, we sampled 2×104 trajectories for the next 8 ps. The decoherence induced surface hopping method was employed to provide a probability for hopping between interacting states.12

To explore optical properties, we employ the energy-dependent dielectric functions to investigate the optical absorption of isolate InSe, Sb layer, and InSe/Sb heterostructure with different twist angle. The dielectric matrix is determined by the following equation, 13, 14

(1)

Where  is the volume of the primitive cell, q is the electron momentum operator, v and c are the valence and conduction band states, respectively, k is the k point weight, εck, εvk and ck, vk are the eigenvalues and wave-functions at the k point, respectively, and eα, eβ are the unit vectors for the three Cartesian directions.

The geometric structure

2D Sb monolayer is made up of two Sb atomic sublayer in wrinkle pattern, and 2D InSe monolayer is composed of two outer Se atomic sublayers wrapping two inner In atomic sublayers.

For InSe/Sb heterostructures with 0° twist angle structure, the Sb atoms of interface are just below the center of the three Se atoms of interface. The Se atoms of interface are located above the center of the three Sb atoms of interface (overlapping the above of Sb atoms of outer surface).

References

(1)	Kresse, G.; Joubert, D., From Ultrasoft Pseudopotentials to the Projector Augmented-Wave Method. Phys. Rev. B 1999, 59, 1758-1775.

(2)	Kresse, G.; Furthmüller, J., Efficient Iterative Schemes for Ab Initio Total-Energy Calculations Using a Plane-Wave Basis Set. Phys. Rev. B 1996, 54, 11169-11186.

(3)	Kresse, G.; Furthmüller, J., Efficiency of Ab-Initio Total Energy Calculations for Metals and Semiconductors Using a Plane-Wave Basis Set Comput. Mater. Sci. 1996, 6, 15-50.

(4)	Perdew, J. P.; Burke, K.; Ernzerhof, M., Generalized Gradient Approximation Made Simple. Phys. Rev. Lett. 1996, 77, 3865-3868.

(5)	Grimme, S., Semiempirical Gga-Type Density Functional Constructed with a Long-Range Dispersion Correction. J. Comput. Chem. 2006, 27, 1787-1799.

(6)	Bengtsson, L., Dipole Correction for Surface Supercell Calculations. Phys. Rev. B 1998, 59, 12301-12304.

(7)	Craig, C. F.; Duncan, W. R.; Prezhdo, O. V., Trajectory Surface Hopping in the Time-Dependent Kohn-Sham Approach for Electron-Nuclear Dynamics. Phys. Rev. Lett. 2005, 95, 163001.

(8)	Akimov, A. V.; Prezhdo, O. V., The Pyxaid Program for Non-Adiabatic Molecular Dynamics in Condensed Matter Systems. J. Chem. Theory Comput. 2013, 9, 4959-4972.

(9)	Akimov, A. V.; Prezhdo, O. V., Advanced Capabilities of the Pyxaid Program: Integration Schemes, Decoherence Effects, Multiexcitonic States, and Field-Matter Interaction. J. Chem. Theory Comput. 2014, 10, 789-804.

(10)	Zheng, Q.; Chu, W.; Zhao, C.; Zhang, L.; Guo, H.; Wang, Y.; Jiang, X.; Zhao, J., Ab Initio Nonadiabatic Molecular Dynamics Investigations on the Excited Carriers in Condensed Matter Systems. WIRES Comput. Mol. Sci. 2019, 9, e1411.

(11)	Niu, X.; Li, Y.; Zhang, Y.; Zheng, Q.; Zhao, J.; Wang, J., Highly Efficient Photogenerated Electron Transfer at a Black Phosphorus/Indium Selenide Heterostructure Interface from Ultrafast Dynamics. J. Mater. Chem. C 2019, 7, 1864-1870.

(12)	Jaeger, H. M.; Fischer, S.; Prezhdo, O. V., Decoherence-Induced Surface Hopping. J. Chem. Phys. 2012, 137, 22A545.

(13)	Lalitha, S.; Karazhanov, S. Z.; Ravindran, P.; Senthilarasu, S.; Sathyamoorthy, R.; Janabergenov, J., Electronic Structure, Structural and Optical Properties of Thermally Evaporated Cdte Thin Films. Physica B 2007, 387, 227-238.

(14)	Gajdoš, M.; Hummer, K.; Kresse, G.; Furthmüller, J.; Bechstedt, F., Linear Optical Properties in the Projector-Augmented Wave Methodology. Phys. Rev. B 2006, 73, 045112.

Figure S1 The top and side view for supercell structure of InSe/Sb heterostructure with 0° twist angle. The grey, orange and purple balls represent the In, Se and Sb atoms, respectively.

Figure S2 Schematic diagram of the twist supercell in hexagonal lattice with different rotation angles. The lattice vector is (na1+ma2), and the twist angle can be expressed as θ=tan-13m2n+m, the formed twisted bilayer has the rotation angle of θ=θ2-θ1.

Figure S3 The top and side view for supercell structure of InSe/Sb heterostructure with 10.9° twist angle. The grey, orange and purple balls represent the In, Se and Sb atoms, respectively.

Figure S4 The top and side view for supercell structure of InSe/Sb heterostructure with 19.1° twist angle. The grey, orange and purple balls represent the In, Se and Sb atoms, respectively.

Figure S5 The top and side view for supercell structure of InSe/Sb heterostructure with 30.0° twist angle. The grey, orange and purple balls represent the In, Se and Sb atoms, respectively.

Figure S6 The top and side view for supercell structure of InSe/Sb heterostructure with 40.9° twist angle. The grey, orange and purple balls represent the In, Se and Sb atoms, respectively.

Figure S7 The top and side view for supercell structure of InSe/Sb heterostructure with 49.1° twist angle. The grey, orange and purple balls represent the In, Se and Sb atoms, respectively.

Figure S8 The top and side view for supercell structure of InSe/Sb heterostructure with 60.0° twist angle. The grey, orange and purple balls represent the In, Se and Sb atoms, respectively.

Figure S9 The charge density difference of InSe/Sb heterostructure with 0° twist angle. The yellow and cyan regions refer to distribution of positive and negative charges, respectively. To clear exhibit the distribution of charge density difference at the two internal interfaces of InSe and Sb sublayers, the top view of the section is exhibited. The unit of the color scale is the e bohr-3.

Figure S10 The charge density difference of InSe/Sb heterostructure with 10.9° twist angle. The yellow and cyan regions refer to distribution of positive and negative charges, respectively. To clear exhibit the distribution of charge density difference at the two internal interfaces of InSe and Sb sublayers, the top view of the section is exhibited. The unit of the color scale is the e bohr-3.

Figure S11 The charge density difference of InSe/Sb heterostructure with 19.1° twist angle. The yellow and cyan regions refer to distribution of positive and negative charges, respectively. To clear exhibit the distribution of charge density difference at the two internal interfaces of InSe and Sb sublayers, the top view of the section is exhibited. The unit of the color scale is the e bohr-3.

Figure S12 The charge density difference of InSe/Sb heterostructure with 30.0° twist angle. The yellow and cyan regions refer to distribution of positive and negative charges, respectively. To clear exhibit the distribution of charge density difference at the two internal interfaces of InSe and Sb sublayers, the top view of the section is exhibited. The unit of the color scale is the e bohr-3.

Figure S13 The charge density difference of InSe/Sb heterostructure with 40.9° twist angle. The yellow and cyan regions refer to distribution of positive and negative charges, respectively. To clear exhibit the distribution of charge density difference at the two internal interfaces of InSe and Sb sublayers, the top view of the section is exhibited. The unit of the color scale is the e bohr-3.

Figure S14 The charge density difference of InSe/Sb heterostructure with 49.1° twist angle. The yellow and cyan regions refer to distribution of positive and negative charges, respectively. To clear exhibit the distribution of charge density difference at the two internal interfaces of InSe and Sb sublayers, the top view of the section is exhibited. The unit of the color scale is the e bohr-3.

Figure S15 The charge density difference of InSe/Sb heterostructure with 60.0° twist angle. The yellow and cyan regions refer to distribution of positive and negative charges, respectively. To clear exhibit the distribution of charge density difference at the two internal interfaces of InSe and Sb sublayers, the top view of the section is exhibited. The unit of the color scale is the e bohr-3.