Tables

Table 1 Prepared samples ratio in grams and weight percentage.

| S.no | Sample code | The ratio of IC:AG: LiClO4 weight percentage with 0.75ml Ethylene glycol | Ratio in grams |
| --- | --- | --- | --- |
| 1 | IAB | 60:40:00 | 0.9366:0.0634:0.0000 |
| 2 | IAO05 | 57:38:05 | 0.9316:0.0600:0.0080 |
| 3 | IAO10 | 54:36:10 | 0.9205:0.0622:0.0172 |
| 4 | IAO15 | 51:34:15 | 0.9126:0.0618:0.0256 |
| 5 | IAO20 | 50:30:20 | 0.9048:0.0612:0.0338 |

Table 2 FTIR peak assignments for all the prepared SPEs.

| Assignments | Wavenumber (cm-1) |
| --- | --- |
| O−H Stretching | 3348 |
| C−H Stretching | 2934 |
| H−O−H (Water deformation band) | 1645 |
| –COO−symmetrical and asymmetrical Stretching | 1460 |
| S–O sulfate stretching | 1232 |
| C–O stretching of 3-6 anhydro galactose stretching | 1067 |
| CH2 asymmetric stretching | 1032 |
| C–O–C of 3-6 anhydro galactose stretching | 926 |
| –O–SO3 stretching at D-galactose-4-sulphate | 848 |
| Sulfate C−4 galactose | 736 |
| ClO4¯ Stretching | 693 |

Table 3 Measured conductivity and activation energy values of all samples.

| Sample code | AC Conductivity (Scm-1) | DC Conductivity (Scm-1) | Activation energy (eV) |
| --- | --- | --- | --- |
| IAB | 2.96×10-4 | 3.98 ×10-4 | 0.071 |
| IAO05 | 5.02×10-4 | 5.13 ×10-4 | 0.066 |
| IAO10 | 1.33×10-3 | 1.08 ×10-3 | 0.062 |
| IAO15 | 2.02×10-2 | 1.99 ×10-2 | 0.022 |
| IAO20 | 1.22×10-4 | 1.16×10-4 | 0.075 |

Table 4 Observed tangent spectra parameters.

| Sample code | Relaxation time (τ) in s |
| --- | --- |
| IAB | 6.72 × 10−7 |
| IAO05 | 7.74× 10−7 |
| IAO10 | 7.05× 10−7 |
| IAO15 | 5.54× 10−7 |
| IAO20 | 1.04× 10−6 |

Table 5 Mobility and diffusion coefficient of prepared solid polymer electrolyte.

| Wt.% of LiClO4 | No. of charge carriers (n) in cm-3 | Transference Number |  | Diffusion co-efficient in cm2/s |  |  | Mobility (μ) in cm2/Vs |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Tion | Tele | D | D+ | D- | µ | µ+ | µ- |
| 5 | 5.16×1019 | 0.9758 | 0.0241 | 1.59 ×10-6 | 1.44 ×10-6 | 1.54 ×10-7 | 6.08 ×10-5 | 5.49 ×10-5 | 5.89 ×10-6 |
| 10 | 1.03×1020 | 0.9844 | 0.0155 | 2.11 ×10-6 | 2.01 ×10-6 | 9.79 ×10-8 | 8.05 ×10-5 | 7.68 ×10-5 | 3.75 ×10-6 |
| 15 | 1.55×1020 | 0.9950 | 0.0004 | 2.13 ×10-5 | 2.12 ×10-5 | 1.07 ×10-8 | 8.16 ×10-4 | 8.15 ×10-4 | 4.08 ×10-7 |
| 20 | 2.06×1020 | 0.9613 | 0.038 | 9.66 ×10-8 | 9.54 ×10-8 | 1.18 ×10-9 | 3.69 ×10-6 | 3.65 ×10-6 | 4.51 ×10-8 |

Table 6 The calculated device's, specific capacitance, power density, energy density, and area.

| Cyclic Voltametric | Galvanostatic Charge-Discharge (GCD) |  |  |  |
| --- | --- | --- | --- | --- |
| Cs (F/g) | Current density (A/g) | Cs (F/g) | Power density (W/kg) | Energy density (Wh/kg) |
| 367 | 2.4 | 292 | 1380 | 54 |
| 464 | 2.8 | 275 | 5796 | 182 |
| 577 | 3.2 | 261 | 6624 | 173 |
| 761 | 3.6 | 250 | 7452 | 166 |
| 901 | 16(1st cycle) | 75 | 8000 | 12 |