Artificial fingerprints engraved through block-copolymers as nanoscale physical unclonable functions for authentication and identification - Supplementary Information

Irdi Murataj1,‡, Chiara Magosso1,2,‡, Stefano Carignano3, Matteo Fretto1, Federico Ferrarese Lupi1*, Gianluca Milano1*

1Advanced Materials Metrology and Life Sciences Division, INRiM (Istituto Nazionale di Ricerca Metrologica), 10135 Turin, Italy.

2Department of Electronics and Telecommunications, Politecnico di Torino, 10129 Turin, Italy.

3Barcelona Supercomputing center, 08034, Barcelona, Spain.

‡ these authors contributed equally to this work

*e-mails: f.ferrareselupi@inrim.it, g.milano@inrim.it

Supplementary Figure S1 | Raw SEM image of the nanopattern. Raw SEM image exploited as example in Fig. 2c to compare conventional binarization techniques with fingerprint enhancement algorithm. Scale bar is set to 100 nm.

Supplementary Figure S2 | Detailed comparison of pattern extraction from different binarization techniques. Details on the comparison of conventional binarization techniques with fingerprint enhancement algorithms. As can be observed, fingerprint enhancement allows obtaining a binarized image of the nanopattern with reduced noise and with a reduced number of artifacts. All scale bars are set to 100 nm.

Supplementary Figure S3 | Successful binarization of low-quality SEM images by fingerprint enhancement algorithm. Example of a successful binarization of a low-quality SEM image by exploiting the fingerprint enhancement algorithm. Scale bar is set to 500 nm.

Supplementary Figure S4 | Details on the influence of the binarization technique on defect identification. Example of overestimation and improper attribution of a positive phase dot defect depicted in the raw SEM image due to improper binarization by different thresholding techniques, compared to fingerprint enhancement algorithm. Otsu, Bernstein, Mean and MidGrey thresholding methods improperly attribute a positive phase dot defect to two positive terminal points. Whereas Median thresholding attributes the same defect to one positive and three negative phase terminal points along with another improper attribution to other three positive phase 3-way junctions. All scale bars are set to 50 nm.

Supplementary Figure S5 | Relationship between fractional intra-HD and unit entropy of binary code matrices. This graph was obtained by considering fractional HD values and entropy at different pixel sizes during the assignment of the binary code matrix from the nanopattern (analyzed pixel sizes are the one reported in Fig. 3c, note that the entropy was not evaluated for pixel sizes of 595 and 476 nm since in this case was observed a not null probability of having all 1-bit values across the matrix). Results were obtained by considering 200 binary code matrices obtained from SEM images with an area of 2.38 × 2.38µm2 acquired on different areas of the patterned sample. Note that the fractional inter-HD between different binary code matrices tends to the ideal value of 0.5 when entropy of binary code matrices tends to the ideal value of 1.

Supplementary Figure S6 | Bit uniformity of binary code matrices. The bit uniformity was evaluated on 200 SEM images of different nanopatterns, for a fixed pixel size of the binary code matrix of 238 nm.

Supplementary Figure S7 | Unit entropy of binary code matrices. a. Unit entropy for 200 nanopatterns and b. corresponding unit entropy distribution for a fixed pixel size of the binary code matrix of 238 nm.

Supplementary Figure S8 | Tuning correlation length of nanopatterns depending on the self-assembly process parameters. SEM images of the lamellar structures obtained with the same polymers under different processing conditions. For a processing time of 300 s, annealing temperatures of 210°C and 230°C result in nanopatterns with correlation length of ~173 and ~328 nm, respectively. Scale bar is set to 200 nm.

Supplementary Figure S9 | Analog version of binary code matrices based on defect density. Analog version of the binary code matrix reported in Fig. 3b, where the color intensity here represents the number of defects in the pixel area.

Supplementary Figure S10 | Analog version of binary code matrices based on defect types. Analog version of the binary code matrix reported in Fig. 3b where the color intensity represents the number of a. positive phase dot defects, b. positive phase point defects and c. positive phase 3-way junction defects in the corresponding pixel area.

Supplementary Figure S11 | Bit flips in slightly shifted/rotated images of the same pattern. Raw images, corresponding binarized images through fingerprint enhancement and corresponding binary code matrices. As can be observed, even slight shifts and rotations of different images of the same pattern can result in strongly different binary code matrices. In this case, slightly shifted/rotated image 1 and 2 results in 47% and 55% of bit flips in the corresponding binary matrix with respect to the binary code matrix obtained from the reference image. Scale bars are set to 500 nm.

Supplementary Figure S12 | PUF device based on block-copolymer templated SiO2 substrate. SEM image of a PUF device, where the nanopattern area of interest for authentication/identification is identified thanks to an Au frame. Scale bar is 1 µm.

Supplementary Figure S13 | Bit uniformity and unit entropy of binarized lamellar patterns of PUF devices. a. Bit uniformity of the 100 binarized PUF nanopatterns and b. corresponding bit uniformity distribution. c. Unit entropy of the 100 binarized PUF nanopatterns and d. corresponding unit entropy distribution. Note that bit uniformity and unit entropy are here calculated on the whole image, without encoding the pattern into a binary code matrix, by considering images of 100 PUF nanopatterns from the database set of images. A total of 987 x 708 or 996 x 717 pixels is here considered.

Supplementary Figure S14 | Example of the resulting homographic transformation of a test image when compared with the database image of the same PUF nanopattern. The image represents the homographic transformation of the test image, obtained by comparing the test image with the database image reported in Fig. 4a. As can be observed, the homographic transformation enables the adjustment of the shift/rotation of the acquired test image for a correct overlapping of the test image on the database one.

Supplementary Figure S15 | Example of the resulting homographic transformation of a test image when compared with the database image of a different PUF nanopattern. The image represents the homographic transformation of the test image, obtained by comparing the test image with the database image reported in Fig. 4b. The homographic transformation of a test image with an image database of a different nanopattern results in a deformation of the test image.

Supplementary Figure S16 | Evaluation of the decision threshold. a. Gaussian distributions of fractional intra-HD and inter-HD obtained by interpolating experimental distribution reported in Fig. 4d, where the test set is compared with the database test, and b. detail of the intersection between intra-HD and inter-HD distributions chosen as the decision threshold (the decision threshold is here represented by the dashed line).

Supplementary Figure S17 | PUF device imaging with different equipment. Example of SEM images of the same nano identifier acquired by two different SEM systems. Images from SEM 1 have been acquired through a FEI Inspect-F, while image SEM 2 have been acquired through FEI Quanta 3D (details in Methods). Scale bars are to 1µm.

Supplementary Figure S18 | Authentication/Identification through images acquired by a different user operating with a different SEM equipment. a. Heat-map matrix representing the fractional HD between images from a test set of images acquired by a different user operating with a different SEM equipment (SEM FEI Quanta 3D) and images from the database (acquired with a SEM FEI Inspect-F), and b. corresponding fractional intra-HD and inter-HD distributions. This test was performed on a subset of 30 PUF patterns.

Supplementary Figure S19 | 3D morphology of the nanopattern. Close-up of an AFM micrograph of an engraved nanopattern on a SiO2 substrate. The image represents a zoom version of the pattern of an acquisition with measurement field 2 µm x 2 µm, acquired in tapping mode.

Supplementary Table 1. Details on fractional intra and inter-HD mean values and standard deviations evaluated for each authentication/identification test vs the database. Results are obtained from Gaussian fitting of experimental results.

|  | Intra-HD | Inter-HD |
| --- | --- | --- |
| Test Set vs Database | 0.14 ± 0.04 | 0.500 ± 0.003 |
| Different user/Different SEM (restricted test set) | 0.16 ± 0.04 | 0.500 ± 0.003 |
| Aging Stability | 0.15 ± 0.03 | 0.500 ± 0.003 |
| Thermal Stability | 0.16 ± 0.04 | 0.500 ± 0.003 |

Supplementary Note 1:

BCPs are constituted by two or more different and chemically incompatible homopolymer chains (one hydrophilic and one hydrophobic) that are covalently linked together. Due to the amphiphilic nature of BCPs, even small structural differences of the constituent blocks determine an increase of the free energy resulting in a microphase separation under specific annealing conditions. However, unlike homopolymer blends, the covalent bond linking the two different blocks counterbalances the thermodynamic forces involved in the phase separation. This leads therefore to the in-parallel self-registration of periodic nanostructures in the range of 10 – 100 nm, that is the so-called self-assembly. The main factors that influence the self-assembly process are the polymerization degree (N), which represents the number of monomeric units in a polymer; Flory-Huggins interaction parameter (χ), that describes the excess of free energy of mixing and estimates the immiscibility of the constituent blocks; volume fractions (fα and fβ) of each homopolymer.1 Changes in volume fraction affect the morphology and packing symmetry of the resulting phase-separated nanostructures. BCPs with two constituent blocks can self-assemble into four thermodynamically stable phases. Highly asymmetric BCPs with a ratio above 80:20 self-organize in zero-dimensional spheres arranged in a body-centered cubic (BCC) lattice of polymer B embedded in a polymer A matrix. Hexagonally packed (HP) cylinders of the minority component are formed for BCPs with ratio 70:30. Double gyroids are formed for a very narrow compositional ratio interval and two-dimensional lamellae are formed by highly symmetric (ratio 50:50) BCPs.2 On the other hand, the periodicity (L0) and the typical dimensions of the resulting nanostructures is determined by the total molecular weight (Mn), given by the multiplication of N with the molecular weight of the monomeric units (M0) of the BCP.3

References

1.	Bates, F. S. & Fredrickson, G. H. Block Copolymer Thermodynamics: Theory and Experiment. Annu Rev Phys Chem 41, 525–557 (1990).

2.	Matsen, M. W. & Schick, M. Stable and unstable phases of a diblock copolymer melt. Phys Rev Lett 72, 2660–2663 (1994).

3.	Ferrarese Lupi, F. et al. Fine Tuning of Lithographic Masks through Thin Films of PS-b-PMMA with Different Molar Mass by Rapid Thermal Processing. ACS Appl Mater Interfaces 6, 7180–7188 (2014).