Supporting Information

Optimizing the coordination environment of Cu single-atom catalyst for efficient electroreduction of CO2 to CH3OH

Guodong Sun*1, Yanan Cao2, Deqing Li3, Yingfei Ma1, Mengchen Sun2

*1 A. Prof G. Sun, Materials and packaging engineering, Fujian Polytechnic Normal University, Fuzhou, Fujian Province, 350330, the People's Republic of China, Email: sunguodong20@mails.ucas.ac.cn.

2 School of Chemical Sciences, National Engineering Laboratory for VOCs Pollution Control Material & Technology, University of Chinese Academy of Sciences, Beijing, 100049, the People's Republic of China.

3 School of Vehicle and Mobility, Tsinghua University, Beijing, 100049, the People's Republic of China.

Supplementary Index

Fig. S1 HAADF-STEM images of (a) CuN3-C and (b) CuN4-C catalysts.

Fig. S2 High-resolution X-ray photoelectron spectroscopy (XPS) of (a) CuN3-C and (b) CuN4-C catalysts.

Fig. S3 Deconvoluted N 1s spectra of (a) CuN3-C and (b) CuN4-C catalysts.

Fig. S4 Fourier transforms of the Cu K-edge EXAFS oscillations in the k space of simulated (a) CuN3-C and (b) CuN4-C catalysts.

Fig. S5 TEM images of (a) CuN3-C and (b) CuN4-C catalysts.

Fig. S6 HAADF-STEM images of (a) N-C and (b) C samples.

Fig. S7 Deconvoluted N 1s spectra of (a) N-C and (b) C samples.

Fig. S8 Amperage curves of CO2 reduction catalyzed by CuN3-C in first 300 seconds at different potentials.

Fig. S9 LSV and Faradaic efficiency distributions of CO2RR on (a) N-C and (b) C samples.

Fig. S10 HAADF-STEM images of CuN3-C catalyst after test.

Fig. S11 Structure and morphology of catalysts after the CO2RR electrolysis.

Fig. S12 EXAFS spectra of CuN3-C catalyst after the CO2RR electrolysis

Fig. S13 Model of CuN3-C catalyst.

Fig. S14 Model of CuN4-C catalyst.

Table S1. EXAFS fitting parameters at the Cu K-edge for various samples（Ѕ02=0.90 from Cu-foil）

Table. S2 The Onset potential and current density of catalysts reacting with different gases.

Table. S3 The Onset potential and Current density of catalysts reacting with different gases.

Table.S4 Faradaic efficiency distributions of CO2RR over Cu4N-C

Table. S5 Faradaic efficiency distributions of CO2RR over CuN3-C

Table S6 Comparison of the FE of CH3OH in aqueous conditions from this work and previous representative reports.

Table S7 Comparison of the rate of CH3OH in aqueous conditions from this work and previous representative reports.

Table S8 The Onset potential and Current density of C and N-C reacting with different gases.

Table S9 Faradaic efficiency distributions of CO2RR over C and N-C

Table S10 Nyquist plot of catalysts over the frequency from 0.1 MHz to 0.1 Hz

Table 11. EXAFS fitting parameters at the Cu K-edge for various samples（Ѕ02=0.90 from Cu-

Table 12 Energy of the CH3OH pathway on CuN3-C catalyst

Table 13 D-band center of catalysts

Fig. S1 HAADF-STEM images of (a) CuN3-C and (b) CuN4-C catalysts.

Fig. S2 High-resolution X-ray photoelectron spectroscopy (XPS) of (a) CuN3-C and (b) CuN4-C catalysts.

Fig. S3 Deconvoluted N 1s spectra of (a) CuN3-C and (b) CuN4-C catalysts.

Fig. S4 Fourier transforms of the Cu K-edge EXAFS oscillations in the k space of simulated (a) CuN3-C and (b) CuN4-C catalysts.

Fig. S5 TEM images of (a) CuN3-C and (b) CuN4-C catalysts.

Fig. S6 HAADF-STEM images of (a) N-C and (b) C samples.

Fig. S7 Deconvoluted N 1s spectra of (a) N-C and (b) C samples.

Fig. S8 Amperage curves of CO2 reduction catalyzed by CuN3-C in first 300 seconds at different potentials.

Fig. S9 LSV and Faradaic efficiency distributions of CO2RR on (a) N-C and (b) C samples.

Fig. S10 HAADF-STEM images of CuN3-C catalyst after test.

Fig. S11 Structure and morphology of catalysts after the CO2RR electrolysis.

Fig. S12 EXAFS spectra of CuN3-C catalyst after the CO2RR electrolysis

Fig. S13 Model of CuN3-C catalyst.

Fig. S14 Model of CuN4-C catalyst.

Table S1. EXAFS fitting parameters at the Cu K-edge for various samples（Ѕ02=0.90 from Cu-foil）

| Sample | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | S02 | R factor |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CuN3-C | Cu-N | 3.1±0.1 | 1.95 | 0.005 | 4.8±0.7 | 0.7000(set) | 0.007 |
| CuN4-C | Cu-N | 4.0±0.1 | 1.95 | 0.008 | 4.2±0.3 | 0.7000(set) | 0.003 |

aCN: coordination numbers; bR: bond distance; cσ2: Debye-Waller factors; d ΔE0: the inner potential correction. R factor: goodness of fit. Error bounds that characterize the structural parameters obtained by EXAFS spectroscopy were estimated as CN±20%; R ± 1%; σ2 ± 20%.

Table. S2 The Onset potential and current density of catalysts reacting with different gases.

| Sample | Gaseous atmosphere | Onset potential (V, Current density = −20 mA cm2) | Current density (mA cm2, at-1.1 V) |
| --- | --- | --- | --- |
| CuN3-C | Ar | −0.61 | −316 |
| CuN3-C | CO2 | −0.45 | −560 |
| CuN4-C | Ar | −0.71 | −301 |
| CuN4-C | CO2 | −0.65 | −471 |

Table. S3 The Onset potential and Current density of catalysts reacting with different gases.

| Potential (V) | FE (%, over CuN3-C) |  |  |
| --- | --- | --- | --- |
|  | CO | CH3OH | H2 |
| −0.6 | 58.88 | 25.63 | 13.86 |
| −0.7 | 47.16 | 40.12 | 11.17 |
| −0.8 | 39.41 | 53.49 | 8.62 |
| −0.9 | 29.10 | 61.45 | 5.79 |
| −1.0 | 11.54 | 80.15 | 3.86 |
| −1.1 | 20.37 | 65.22 | 9.18 |

Table.S4 Faradaic efficiency distributions of CO2RR over CuN4-C

| Potential (V) | FE (%, over CuN4-C) |  |  |
| --- | --- | --- | --- |
|  | CO | CH3OH | H2 |
| −0.6 | 78.9 | 0 | 20.86 |
| −0.7 | 74.16 | 2.58 | 23.17 |
| −0.8 | 65.18 | 4.77 | 28.21 |
| −0.9 | 53.5 | 8.12 | 32.96 |
| −1.0 | 47.17 | 16.11 | 34.02 |
| −1.1 | 39.66 | 30.99 | 27.11 |

Table. S5 Faradaic efficiency distributions of CO2RR over CuN3-C

| Potential (V) | FE (%) | Partial current density (mA cm2) |
| --- | --- | --- |
| −0.6 | −25.63 | −11.53 |
| −0.7 | −40.12 | −34.90 |
| −0.8 | −53.49 | −86.65 |
| −0.9 | −61.45 | −164.07 |
| −1.0 | −80.15 | −332.33 |
| −1.1 | −65.22 | −363.92 |

Table S6 Comparison of the FE of CH3OH in aqueous conditions from this work and previous representative reports.

| Catalysts | FECH3OH (%) | REF |
| --- | --- | --- |
| CuSAs/TCNFs | 44 | 1 |
| CoO/CN/Ni | 45 | 2 |
| CuN4-C | 45.1 | This work |
| Cu-3(HHTQ) | 53.6 | 3 |
| Ti3(Al1−xCux)C2 | 59.1 | 4 |
| Ag,S-Cu2O/Cu | 67.4 | 5 |
| Cu2NCN | 70 | 6 |
| CoO/CN/Ni | 70.7 | 2 |
| Co3O4/N-RGO | 74.8 | 7 |
| Cu2−xSe | 77 | 8 |
| CuN3-C | 78 | This work |

Table S7 Comparison of the rate of CH3OH in aqueous conditions from this work and previous representative reports.

| Catalysts | CH3OH production rate | REF |
| --- | --- | --- |
| CuPc | 3.8 | 9 |
| CuSAs/TCNFs | 737.133 | 1 |
| CoO/CN/Ni | 178.7565 | 2 |
| CoPc/CNT | 200 | 10 |
| Cu-3(HHTQ) | 18.51468 | 3 |
| Ti3(Al1−xCux)C2 | 217.4145 | 4 |
| Ag,S-Cu2O/Cu | 1428.321 | 5 |
| Cu2NCN | 1115.889 | 6 |
| CoO/CN/Ni | 129.4335 | 2 |
| Pd/SnO2 | 2 | 11 |
| Co3O4/N-RGO | 51.6753 | 7 |
| CuN3-C | 5321.244 | This work |
| Cu2−xSe | 556.2004 | 8 |
| Pd83Cu17 | 439.3782 | 12 |
| Sn1 /Vo -CuO-x | 1025.25 | 13 |

计算方法

Table S8 The Onset potential and Current density of C and N-C reacting with different gases.

| Sample | Onset potential (V, Current density = −10 mA cm2) | Current density (mA cm2, at −1.1 V) |
| --- | --- | --- |
| C | −1.01 | −16.82 |
| N-C | −0.98 | −19.76 |

Table S9 Faradaic efficiency distributions of CO2RR over C and N-C

| Potential (V) | FE (%, over C) |  |  | FE (%, over N-C) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | CO | CH3OH | H2 | CO | CH3OH | H2 |
| -0.6 | 0 | 0 | 99.12 | 71.55 | 0 | 27.46 |
| -0.7 | 0 | 0 | 99.43 | 62.16 | 0 | 35.88 |
| -0.8 | 0 | 0 | 99.19 | 58.81 | 0 | 40.16 |
| -0.9 | 1.24 | 0 | 97.22 | 50.68 | 0 | 48.34 |
| -1.0 | 2.37 | 0 | 96.77 | 44.73 | 0 | 52.17 |
| -1.1 | 2.88 | 0 | 96.28 | 41.75 | 0 | 56.21 |

Table S10 Nyquist plot of catalysts over the frequency from 0.1 MHz to 0.1 Hz

| Sample | Charge-transfer resistance （Ω） |
| --- | --- |
| CuN3-C | 6.2 |
| CuN4-C | 8.4 |

Table 11. EXAFS fitting parameters at the Cu K-edge for various samples（Ѕ02=0.90 from Cu-foil）

| Sample | Shell | CNa | R(Å)b | σ2(Å2)c | ΔE0(eV)d | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| CuN3-C | Cu-N | 3.1±0.1 | 1.95 | 0.00084 | 6.2±0.7 | 0.0019 |

aCN: coordination numbers; bR: bond distance; cσ2: Debye-Waller factors; d ΔE0: the inner potential correction. R factor: goodness of fit. Error bounds that characterize the structural parameters obtained by EXAFS spectroscopy were estimated as CN±20%; R ± 1%; σ2 ± 20%.

Table 12 Energy of the CH3OH pathway on CuN3-C catalyst

| Intermediates | Energy (eV) | Energy (eV) |
| --- | --- | --- |
| *+CO2 | 0 | 0 |
| *COOH | -0.65 | -0.45 |
| *CO | 0.9 | -1.29 |
| *CHO | -0.56 | -0.15 |
| *CHOH | 1.87 | -0.41 |
| *CH2OH | -1.3 | -0.82 |

Table 13 D-band center of catalysts

| Cu 3d | d-band center (eV) |
| --- | --- |
| CuN3-C | -1.58 |
| CuN4-C | -3.12 |

1	Yang, H. et al. Scalable Production of Efficient Single-Atom Copper Decorated Carbon Membranes for CO2 Electroreduction to Methanol. Journal of the American Chemical Society 141, 12717-12723, doi:10.1021/jacs.9b04907 (2019).

2	Wang, L. et al. Ternary heterostructural CoO/CN/Ni catalyst for promoted CO2 electroreduction to methanol. Journal of Catalysis 393, 83-91, doi:10.1016/j.jcat.2020.11.012 (2021).

3	Liu, J. et al. Tricycloquinazoline‐Based 2D Conductive Metal–Organic Frameworks as Promising Electrocatalysts for CO2Reduction. Angewandte Chemie International Edition 60, 14473-14479, doi:10.1002/anie.202103398 (2021).

4	Zhao, Q. et al. Selective Etching Quaternary MAX Phase toward Single Atom Copper Immobilized MXene (Ti3C2Clx) for Efficient CO2 Electroreduction to Methanol. ACS Nano 15, 4927-4936, doi:10.1021/acsnano.0c09755 (2021).

5	Li, P. et al. In situ dual doping for constructing efficient CO2-to-methanol electrocatalysts. Nature Communications 13, doi:10.1038/s41467-022-29698-3 (2022).

6	Kong, S. et al. Delocalization state-induced selective bond breaking for efficient methanol electrosynthesis from CO2. Nature Catalysis 6, 6-15, doi:10.1038/s41929-022-00887-z (2022).

7	Bharath, G. et al. Self-Assembled Co3O4 Nanospheres on N-Doped Reduced Graphene Oxide (Co3O4/N-RGO) Bifunctional Electrocatalysts for Cathodic Reduction of CO2 and Anodic Oxidation of Organic Pollutants. ACS Applied Energy Materials 4, 11408-11418, doi:10.1021/acsaem.1c02196 (2021).

8	Yang, D. et al. Selective electroreduction of carbon dioxide to methanol on copper selenide nanocatalysts. Nature Communications 10, doi:10.1038/s41467-019-08653-9 (2019).

9	Kusama, S., Saito, T., Hashiba, H., Sakai, A. & Yotsuhashi, S. Crystalline Copper(II) Phthalocyanine Catalysts for Electrochemical Reduction of Carbon Dioxide in Aqueous Media. ACS Catalysis 7, 8382-8385, doi:10.1021/acscatal.7b02220 (2017).

10	Guo, T. et al. Enhancing effect of cobalt phthalocyanine dispersion on electrocatalytic reduction of CO2 towards methanol. Environmental Science and Pollution Research 30, 122755-122773, doi:10.1007/s11356-023-30883-0 (2023).

11	Zhang, W. et al. Electrochemical Reduction of Carbon Dioxide to Methanol on Hierarchical Pd/SnO2 Nanosheets with Abundant Pd–O–Sn Interfaces. Angewandte Chemie International Edition 57, 9475-9479, doi:10.1002/anie.201804142 (2018).

12	Lu, L. et al. Highly Efficient Electroreduction of CO2 to Methanol on Palladium–Copper Bimetallic Aerogels. Angewandte Chemie International Edition 57, 14149-14153, doi:10.1002/anie.201808964 (2018).

13	Guo, W. et al. Highly Efficient CO2 Electroreduction to Methanol through Atomically Dispersed Sn Coupled with Defective CuO Catalysts. Angewandte Chemie International Edition 60, 21979-21987, doi:10.1002/anie.202108635 (2021).