Results

Model comparison and analysis

| Property | DenseGNN | ALIGNN | Schnet(kgcnn) | M3GNet(kgcnn) | MODNet | coGN | coNGN |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Jdft2d | 32.5425±7.0394 | 43.4240±8.949 | 42.6637±13.7201 | 50.1719±11.90 | 33.192±7.343 | 37.1652±13.683 | 36.170±11.597 |
| Phonons | 24.8470±1.7783 | 29.5390±2.115 | 38.9636±1.9760 | 34.1606±4.500 | 34.2751±2.0781 | 29.7117±1.997 | 28.887±3.284 |
| Dielectric | 0.2837±0.0633 | 0.3449±0.0871 | 0.3277±0.0829 | 0.3120±0.063 | 0.2711±0.0714 | 0.3088±0.0859 | 0.3142±0.074 |
| Perovskites | 0.0268±0.0007 | 0.0288±0.0009 | 0.0342±0.0005 | 0.0330±0.0001 | 0.0908±0.0028 | 0.0269±0.0008 | 0.0290±0.0011 |
| Log gvrh | 0.0668±0.0011 | 0.0715±0.0006 | 0.0796±0.0022 | 0.0860±0.002 | 0.0731±0.0007 | 0.0689±0.0009 | 0.0670±0.0006 |
| Log kvrh | 0.0512±0.0014 | 0.0568±0.0028 | 0.0590±0.0022 | 0.0580±0.003 | 0.0548±0.0025 | 0.0535±0.0028 | 0.0491±0.0026 |
| Band gap | 0.1551±0.0031 | 0.1861±0.0030 | 0.2352±0.0034 | 0.1830±0.0050 | 0.2199±0.0059 | 0.1559±0.0017 | 0.1697±0.0035 |
| Formation enthapy | 0.0170±0.0002 | 0.0215±0.0005 | 0.0218±0.0004 | 0.01950±0.0002 | 0.0448±0.0039 | 0.0170±0.0003 | 0.1780±0.0004 |

TableS1 presents the test mean absolute error(MAE) for multiple tasks of the MatBench. The models compared include ALIGNN, SchNet, M3GNet, MODNet, coGN, and coNGN. Standard deviations for all test results are also provided.

| OC22/model | DenseGNN | coGN | GemNet-dT | PAiNN | DimeNetPP | Schnet |
| --- | --- | --- | --- | --- | --- | --- |
| MAE(ID) | 1.6001 | 1.6183 | 1.6771 | 1.7160 | 1.960 | 2.0012 |
| MAE(OOD) | 2.7986 | 2.8058 | 3.0837 | 3.6835 | 3.5186 | 4.8468 |
| Average | 2.19935 | 2.2121 | 2.3804 | 2.6997 | 2.7393 | 3.4240 |

Table S2 presents the test MAE for multiple tasks of the OC22 benchmark dataset. Models for comparison are coGN, GemNet-dT, PAiNN, DimeNetPP and Schnet. The best results are indicated in bold font.

| Molecules/Models | DenseGNN | AttentiveFP | HamNet | PAiNN | DMPNN | GIN | GAT | INorp | DimeNetPP | Schnet |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Lipop | 0.3807 | 0.4836 | 0.4543 | 0.4419 | 0.3718 | 0.4632 | 0.4844 | 0.4671 | 0.4495 | 0.4899 |
| FreeSolv | 0.5589 | 0.6037 | 0.6789 | 0.5341 | 0.5190 | 0.6638 | 0.6299 | 0.6991 | 0.5838 | 0.6333 |
| ESOL | 0.3857 | 0.4223 | 0.5204 | - | 0.4340 | 0.4862 | 0.4569 | 0.5069 | 0.5213 | 0.4473 |

Table S3 presents the test MAE for multiple tasks of the Lipop, FreeSolv and ESOL benchmark datasets. Models for comparison are AttentiveFP, HamNet, PAiNN, DMPNN, GIN, GAT, INorp, DimeNetPP and Schnet. The best results are indicated in bold font.

Ablation study

| Property | DenseGNN | Model1 | Model2 | Model3 | Model4 | DeeperDenseGNN |
| --- | --- | --- | --- | --- | --- | --- |
| Jdft2d | 32.5425 | 33.2371 | 37.7566 | 35.6381 | 38.5513 | 31.8750 |
| Phonons | 24.8470 | 26.9417 | 32.1046 | 29.2872 | 30.4843 | 23.1206 |
| Dielectric | 0.2837 | 0.3022 | 0.3342 | 0.3040 | 0.3082 | 0.3032 |
| Perovskites | 0.0268 | 0.0279 | 0.0311 | 0.0348 | 0.0313 | 0.0257 |
| Log gvrh | 0.0668 | 0.0706 | 0.0797 | 0.0730 | 0.0751 | 0.0661 |
| Log kvrh | 0.0512 | 0.0552 | 0.0632 | 0.0548 | 0.0571 | 0.0490 |

Table S4 presents the MAE results of ablation experiments on all models for jdft2d - exfoliation energy (meV/atom); phonons - phonon DOS peak frequency; dielectric - refractive index (unitless); perovskites - perovskite formation energy, in eV per atom; log gvrh - base 10 logarithm of the DFT Voigt-Reuss-Hill average shear moduli in GPa; log kvrh - base 10 logarithm of the DFT Voigt-Reuss-Hill average bulk moduli in GPa.

Our DCN and LOPE strategy improve GNN models in different fields

Figure S1, the MAE comparison of representative models in three specific domains (materials, molecular, and computer science) on 6 Matbench datasets before and after fusing the DCN strategy is shown.

Optimizing Edge Connectivity for Efficient Enhancements

| Schnet / Radius | 4.0 | 5.0 | 6.0 | 8.0 |
| --- | --- | --- | --- | --- |
| Jdft2d | 52.9513 | 47.2116 | 43.8966 | 45.6324 |
| Phonons | 48.7089 | 42.155 | 40.1608 | 40.7092 |
| Dielectric | 0.3231 | 0.3140 | 0.3168 | 0.3018 |
| Perovskites | 0.0408 | 0.0386 | 0.0349 | 0.0388 |
| Log gvrh | 0.0864 | 0.0824 | 0.0792 | 0.0789 |
| Log kvrh | 0.0644 | 0.0619 | 0.0601 | 0.0604 |

| CGCNN/ Radius | 4.0 | 5.0 | 6.0 | 8.0 |
| --- | --- | --- | --- | --- |
| Jdft2d | 45.0284 | 42.1485 | 41.9138 | 39.8461 |
| Phonons | 40.6583 | 40.4221 | 39.8657 | 40.6511 |
| Dielectric | 0.3615 | 0.3485 | 0.3381 | 0.3423 |
| Perovskites | 0.0380 | 0.0382 | 0.0374 | 0.0383 |
| Log gvrh | 0.0828 | 0.0806 | 0.0805 | 0.0826 |
| Log kvrh | 0.0626 | 0.0613 | 0.0604 | 0.0609 |

| MEGNet / Radius | 4.0 | 5.0 | 6.0 | 8.0 |
| --- | --- | --- | --- | --- |
| Jdft2d | 57.861 | 54.1602 | 53.2526 | 54.830 |
| Phonons | 30.1969 | 30.2264 | 30.1585 | 36.1921 |
| Dielectric | 0.3279 | 0.3312 | 0.3298 | 0.3402 |
| Perovskites | 0.0428 | 0.0421 | 0.0419 | 0.0409 |
| Log gvrh | 0.0871 | 0.0852 | 0.0846 | 0.0867 |
| Log kvrh | 0.0638 | 0.0634 | 0.0618 | 0.0634 |

| DenseGNN/KNN | 6 | 12 | 18 | 24 |
| --- | --- | --- | --- | --- |
| Jdft2d | 37.6720 | 32.5425 | 33.2046 | 33.3927 |
| Phonons | 26.0533 | 24.8470 | 25.2097 | 26.0858 |
| Dielectric | 0.3213 | 0.2837 | 0.3100 | 0.3015 |
| Perovskites | 0.0268 | 0.0287 | 0.0282 | 0.0282 |
| Log gvrh | 0.0717 | 0.0668 | 0.0688 | 0.0695 |
| Log kvrh | 0.0553 | 0.0512 | 0.0524 | 0.0536 |

| Edges numbers | DenseGNN | CGCNN | Schnet | MEGNet | coGN |
| --- | --- | --- | --- | --- | --- |
| Jdft2d | 56040 | 126676 | 126676 | 126676 | 56971 |
| Phonons | 119003 | 452302 | 452302 | 452302 | 113959 |
| Dielectric | 982466 | 4867630 | 4867630 | 4867630 | 777655 |
| Perovskites | 1196573 | 6099290 | 6099290 | 6099290 | 2167618 |
| Log gvrh | 1186890 | 5417274 | 5417274 | 5417274 | 1083580 |
| Log kvrh | 1186890 | 5417274 | 5417274 | 5417274 | 1083580 |

| Nodes numbers | DenseGNN | CGCNN | Schnet | MEGNet | coGN |
| --- | --- | --- | --- | --- | --- |
| Jdft2d | 4575 | 4575 | 4575 | 4575 | 2296 |
| Phonons | 9521 | 9521 | 9521 | 9521 | 4342 |
| Dielectric | 80487 | 80487 | 80487 | 80487 | 31521 |
| Perovskites | 94640 | 94640 | 94640 | 94640 | 85648 |
| Log gvrh | 94777 | 94777 | 94777 | 94777 | 41305 |
| Log kvrh | 94777 | 94777 | 94777 | 94777 | 41305 |

Table S5, Summary of MAE comparisons for different GNN Models on the Matbench Dataset.

1. Schnet (radius-based approach for crystal graphs) at different radii;

2. CGCNN (radius-based approach for crystal graphs) at different radii;

3. MEGNet (radius-based approach for crystal graphs) at different radii;

4. DenseGNN (k-nearest-neighbors approach for crystal graphs) at various k values;

5. Comparison of all edges and nodes for DenseGNN, Schnet, CGCNN, MEGNet, and coGN on the Matbench dataset.