A homochiral hexagadolinium phosphonate cluster with a large magnetocaloric effect

Qing-Qing Qiana, Jian-Huangb,c, Jia-Ge Jiaa,b*, Wu Qionga*, Min Renb, Li-Min Zhengb

aMagnetism Key Laboratory of Zhejiang Province, College of Materials and Chemistry, China Jiliang University, Hangzhou, 310018, P. R. China. *Corresponding author. E-mail: jgjia322@cjlu.edu.cn

bState Key Laboratory of Coordination Chemistry, School of Chemistry and Chemical Engineering, Collaborative Innovation Center of Advanced Microstructures, Nanjing University, Nan Jing, 210023, P. R. China.

c Nantong Customs Comprehensive Technology Center, Nantong, 226006, P. R. China.

| Table S1. Crystal data and structure reﬁnement parameters for compound R-1 |  |
| --- | --- |
| Empirical formula | C56H96Gd6N10O95P8 |
| Formula weight | 3691.36 |
| Temperature | 296 |
| Crystal system | monoclinic |
| space group | P21 |
| a/[Å] | 14.8793(6) |
| b/[Å] | 23.7170(10) |
| c/[Å] | 20.0088(9) |
| β[o] | 109.0150(10) |
| Z | 2 |
| Volume/[Å3] | 6675.7(5) |
| Calculated density/[ g·cm-3] | 1.836 |
| μ/[mm-1] | 3.148 |
| F(000) | 3688.0 |
| Crystal size | 0.36 × 0.15 × 0.13 |
| Flack parameter | 0.015(6) |
| Limiting indices | -12<=h<=19, -30<=k<=30, -26<=l<=16 |
| Reflections collected | 28987 |
| Independent reflections | [Rint = 0.0149] Rsigma = 0.0422] |
| Goodness-of-fit on F2 | 1.002 |
| R1, wR2[a] [I>2(I)] (all data) | R1 = 0.0239, wR2 = 0.0574 |
|  | R1 = 0.0251, wR2 = 0.0578 |
| Largest diff. peak and hole/[ e·Å-3] | 1.60, -0.95 |
| aR1 = Σ¦¦Fo¦ - ¦Fc¦¦/Σ¦Fo¦, wR2 = [Σw(Fo2 - Fc2)2/Σw(Fo2)2]1/2 |  |

| Table S2 Part bond length (Å) and bond angle (°) of compound R-1 |  |  |  |
| --- | --- | --- | --- |
| Bonds | Length/Å | Bonds | Length/Å |
| Gd1-O19 | 2.2585(4) | Gd4-O14 | 2.311(4) |
| Gd1-O24 | 2.319(4) | Gd4-O39 | 2.324(4) |
| Gd1-O21 | 2.363(4) | Gd4-O11 | 2.372(4) |
| Gd1-O16 | 2.403(4) | Gd4-O36 | 2.382(4) |
| Gd1-O1 | 2.403(4) | Gd4-O31 | 2.418(4) |
| Gd1-O36 | 2.434(4) | Gd4-O16 | 2.425(4) |
| Gd1-O37 | 2.448(4) | Gd4-O17 | 2.460(4) |
| Gd1-O2 | 2.509(4) | Gd4-O32 | 2.500(4) |
| Gd2-O29 | 2.284(4) | Gd5-O13 | 2.327(4) |
| Gd2-O4 | 2.360(4) | Gd5-O3 | 2.329(4) |
| Gd2-O1 | 2.4282(1) | Gd5-O8 | 2.334(4) |
| Gd2-O26 | 2.390(4) | Gd5-O18 | 2.350(4) |
| Gd2-O21 | 2.405(4) | Gd5-O1W | 2.436(4) |
| Gd2-O6 | 2.430(4) | Gd5-O2W | 2.448(4) |
| Gd2-O7 | 2.453(4) | Gd5-O3W | 2.464(4) |
| Gd2-O22 | 2.505(4) | Gd5-O4W | 2.469(4) |
| Gd3-O9 | 2.298(4) | Gd6-O23 | 2.326(4) |
| Gd3-O34 | 2.300(4) | Gd6-O38 | 2.327(4) |
| Gd3-O31 | 2.373(4) | Gd6-O33 | 2.333(4) |
| Gd3-O6 | 2.386(4) | Gd6-O28 | 2.345(4) |
| Gd3-O26 | 2.420(4) | Gd6-O8W | 2.443(4) |
| Gd3-O11 | 2.420(4) | Gd6-O7W | 2.443(4) |
| Gd3-O27 | 2.481(4) | Gd6-O6W | 2.455(4) |
| Gd3-O12 | 2.504(4) | Gd6-O5W | 2.458(4) |

Table S3 The theoretical calculation of the shape of Gd3 and Gd6 polyhedral geometrical configuration

| Label | Shape | Gd3 | Gd6 |
| --- | --- | --- | --- |
| OP-8 | Octagon | 30.381 | 28.858 |
| HPY-8 | Heptagonal pyramid | 23.351 | 23.642 |
| HBPY-8 | Hexagonal bipyramid | 12.496 | 14.748 |
| CU-8 | Cube | 8.636 | 7.445 |
| SAPR-8 | Square antiprism | 4.343 | 0.515 |
| TDD-8 | Triangular dodecahedron | 1.904 | 1.620 |
| JGBF-8 | Johnson - Gyrobifastigium | 11.691 | 15.542 |
| JETBPY-8 | Johnson - Elongated triangular bipyramid | 23.915 | 28.495 |
| JBTPR-8 | Johnson Biaugmented trigonal prism | 2.848 | 2.659 |
| BTPR-8 | Biaugmented trigonal prism | 2.443 | 2.067 |
| JSD-8 | Snub disphenoid | 4.581 | 4.766 |
| TT-8 | Triakis tetrahedron | 9.370 | 8.322 |
| ETBPY-8 | Elongated trigonal bipyramid | 20.296 | 23.271 |

Figure S1. Packing arrangement of polyanions of 1 viewed along the a-axis.

Figure S2. PXRD pattern of R, S-1.

Figure S3. IR spectra (KBr pellets) of R, S-1

Figure S4.  The TGA curves of R, S-1.

Figure S5. The plots of χM-1 versus T for R-1. The red curve means the best fitting of the plot of χM-1 vs. T above 50 K to the Curie–Weiss law.

Figure S6. The isothermal field dependence of magnetization for R-1 at different temperature.