List of Tables

Table 1 Surface and pore characteristics of SBA-15 support and SBA-15 supported catalysts with different metal loadings

| Catalyst | Total surface area (m2/g)a | Micropore area (m2/g)b | External surface area (m2/g)b | Micropore volume (cm3/g)b | Total pore volume (cm3/g)c | Average pore size (Å)c |
| --- | --- | --- | --- | --- | --- | --- |
| SBA-15 | 678 | 248 | 429 | 0.1249 | 0.5970 | 51.47 |
| 5Ce1-xZrxO2/SBA-15 | 529 | 233 | 296 | 0.1179 | 0.4313 | 48.23 |
| 10Ce1-xZrxO2/SBA-15 | 503 | 184 | 276 | 0.0938 | 0.4068 | 51.33 |
| 20Ce1-xZrxO2/SBA-15 | 419 | 161 | 258 | 0.0821 | 0.3569 | 50.94 |
| 30Ce1-xZrxO2/SBA-15 | 355 | 148 | 207 | 0.0756 | 0.2843 | 45.48 |
| 40Ce1-xZrxO2/SBA-15 | 297 | 131 | 166 | 0.0671 | 0.2301 | 45.13 |
| a from BET desorption method; b from t-plot method; c from BJH desorption method. |  |  |  |  |  |  |

Table 2 Elemental composition of SBA-15 support and SBA-15 supported catalysts at varying metal loadings

| Catalyst | Elemental composition (wt.%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | O | Si | Ce | Zr |
| SBA-15 | 76.61 | 23.39 | 0 | 0 |
| 5Ce1-xZrxO2/SBA-15 | 70.66 | 23.32 | 6.02 | 0 |
| 10Ce1-xZrxO2/SBA-15 | 71.32 | 20.32 | 7.42 | 0.94 |
| 20Ce1-xZrxO2/SBA-15 | 64.5 | 24.66 | 9.44 | 1.4 |
| 30Ce1-xZrxO2/SBA-15 | 68.36 | 20.11 | 9.95 | 1.58 |
| 40Ce1-xZrxO2/SBA-15 | 66.49 | 21.91 | 9.56 | 2.04 |

Table 3 The estimated rate constant values at different temperatures

| Temperature (⁰C) | Estimated specific rate constant, ks (1/M.hr) |
| --- | --- |
| 240 | 0.0953 |
| 250 | 0.2151 |
| 260 | 0.6129 |
| 270 | 0.7192 |