Supporting Information

Effect of material composition on the performance for ZnO@C/Bi as Zn anode

Ziyuan Wang a,b, Chun Guo a,b, Zheng Li a,b, Zhifan Hua a,b, Yifan Li a,b, Zhongliang Tian a,b and Ke Peng a*

a School of Metallurgy and Environment, Central South University, Changsha 410083, PR China

bEngineering Research Centre of Advanced Battery Materials, Ministry of Education, Changsha, China

*Email: pengke_msg@csu.edu.cn

ORCID: 0009-0002-2407-690X

Figure S1. The device picture of the Zn-Ni battery. (a) main view, and (b) side view.

Figure S2. TEM images of ZnO@C/Bi composites with different carbon layer thicknesses at 50nm scale. (a) C-1, (b) C-2, (c) C-3, and (d) C-4.

Table S1. Tafel parameters for ZnO@C/Bi composites with different Bi contents.

| Sample | Corrosion potential/V | Corrosion current density/mA cm-2 |
| --- | --- | --- |
| 4.14% | -1.436 | 20.55 |
| 5.66% | -1.422 | 15.13 |
| 8.01% | -1.427 | 17.22 |

Table S2. CV curves parameters for ZnO@C/Bi composites with different Bi contents.

| Sample | Oxidation peak position/V | Oxidation peak height/A | Reduction peak position/V | Reduction peak height/A | Redox peak difference/V |
| --- | --- | --- | --- | --- | --- |
| 0.10 g | -1.308 | 0.1417 | -1.565 | -0.1776 | 0.257 |
| 0.15 g | -1.285 | 0.1655 | -1.548 | -0.1131 | 0.263 |
| 0.20 g | -1.251 | 0.2112 | -1.526 | -0.0913 | 0.275 |

Table S3. Pore volume, specific surface area and pore size of ZnO@C/Bi composites with different carbon layer thicknesses.

| Sample | Carbon layer thickness /nm | Va tot/ cm3 g-1 | Vb micro/ cm3 g-1 | V micro/ Vtot | Average pore size/nm | Specific surface area /m2 g-1 |
| --- | --- | --- | --- | --- | --- | --- |
| C-1 | 2.28 | 0.0169 | 0.006 | 36.41% | 3.1086 | 22.97 |
| C-2 | 5.48 | 0.0285 | 0.0178 | 62.56% | 2.1759 | 54.63 |
| C-3 | 14.26 | 0.0497 | 0.0307 | 61.89% | 2.1326 | 96.48 |
| C-4 | 20.38 | 0.0505 | 0.0344 | 68.10% | 2.0175 | 103.97 |

Table S4. Tafel parameters for ZnO@C/Bi composites with different carbon layer thicknesses.

| Sample | Corrosion potential/V | Corrosion current density/mA cm-2 |
| --- | --- | --- |
| C-1 | -1.449 | 15.20 |
| C-2 | -1.426 | 15.13 |
| C-3 | -1.421 | 14.75 |
| C-4 | -1.412 | 19.05 |

Table S5. CV curves parameters for ZnO@C/Bi composites with different carbon layer thicknesses.

| Sample | Oxidation peak position/V | Oxidation peak height/A | Reduction peak position/V | Reduction peak height/A | Redox peak difference/V |
| --- | --- | --- | --- | --- | --- |
| C-1 | -1.278 | 0.09693 | -1.555 | -0.09589 | 0.277 |
| C-2 | -1.262 | 0.1081 | -1.561 | -0.08851 | 0.299 |
| C-3 | -1.260 | 0.119 | -1.535 | -0.07973 | 0.275 |
| C-4 | -1.231 | 0.1475 | -1.528 | -0.06729 | 0.297 |