2D g-GaN as Interphase Anode Layer in Mg Battery for Capturing Passivation Species (MgO, Mg(OH)2, Mg(CO3)  – A First-Principles Study

Nandhini Panjulingam, Senthilkumar Lakshmipathi*

Department of Physics, Bharathiar University, Coimbatore 641 046, Tamil

Nadu, India

[*] Corresponding author: Senthilkumar Lakshmipathi

Email: lsenthilkumar@buc.edu.in

Table S1 Bond Distance (Å) for passivation species after adsorption at different sites (room temperture)

| Species | Sites | Interactions | R(Å) |
| --- | --- | --- | --- |
| MgO | S1 | Mg-O | 1.95 |
|  | S2 |  | 1.80 |
|  | S3 |  | 1.80 |
|  | S4 |  | 1.84 |
| Mg(OH)2 | S1 | OH1-Mg | 2.01 |
|  |  | Mg-OH2 | 2.18 |
|  | S2 | OH1-Mg | 1.96 |
|  |  | Mg-OH2 | 2.01 |
|  | S3 | OH1-Mg | 2.17 |
|  |  | Mg-OH2 | 2.12 |
|  | S4 | OH1-Mg | 1.95 |
|  |  | Mg-OH2 | 1.96 |
| Mg(CO3) | S1 | Mg-O2 | 2.03 |
|  |  | Mg-O3 | 2.08 |
|  |  | Mg-C | 2.34 |
|  | S2 | Mg-O2 | 1.95 |
|  |  | Mg-O3 | 1.94 |
|  |  | Mg-C | 2.26 |
|  | S3 | Mg-O2 | 2.02 |
|  |  | Mg-O3 | 2.05 |
|  |  | Mg-C | 2.34 |
|  | S4 | Mg-O2 | 2.00 |
|  |  | Mg-O3 | 2.01 |
|  |  | Mg-C | 2.31 |

Table S2  The bond interactions, electron density (), and Laplacian of electron density (2) in atomic units corresponding to the bond critical points (BCPs) between before and after adsorption of passivation species.

| Passivation Species | (a.u) 2 (a.u) | Bond interactions | Bare | After adsorption of passivation species |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Sites |  |  |  |
|  |  |  |  | S1 | S2 | S3 | S4 |
| MgO |  | Mg-O | 0.013 | 0.0067 | 0.013 | 0.013 | 0.011 |
|  | 2 |  | 0.72 | 0.334 | 0.780 | 0.780 | 0.515 |
| Mg(OH)2 |  | Mg-O1 | 0.015 | 0.0075 | 0.015 | 0.001 | 0.008 |
|  |  | Mg-O2 | 0.015 | 0.0021 | 0.016 | 0.003 | 0.001 |
|  | 2 | Mg-O1 | 0.85 | 0.310 | 0.610 | 0.166 | 0.303 |
|  |  | Mg-O2 | 0.85 | 0.160 | 0.663 | 0.201 | 0.145 |
| Mg(CO3) |  | Mg-O1 | 0.009 | 0.000 | 0.002 | 0.001 | 0.010 |
|  |  | Mg-O2 | 0.008 | 0.001 | 0.006 | 0.002 | 0.010 |
|  |  | Mg-C1 | 0.0004 | 0.000 | 0.001 | 0.000 | 0.002 |
|  | 2 | Mg-O1 | 0.434 | 0.161 | 0.214 | 0.170 | 0.465 |
|  |  | Mg-O2 | 0.396 | 0.201 | 0.318 | 0.221 | 0.439 |
|  |  | Mg-C1 | 0.227 | 0.132 | 0.169 | 0.136 | 0.284 |

Table S3 The charge transfer value for Ga, Mg, O, and C atoms for pristine and complexes            systems.

| Passivation species | Atoms | Charge transfer value for various sites at different atoms (e) |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | S1 | S2 | S3 | S4 |
| MgO | Ga(1.74)* | 0.83 | 0.33 | 0.83 | 0.00 |
|  | Mg(0.36)* | 1.09 | 1.33 | 1.05 | 1.30 |
|  | O(7.63)* | 8.04 | 8.32 | 8.05 | 8.26 |
| Mg(OH)2 | Ga1 | 1.73(1.78)* | 0.05(1.74)* | 0.00(1.74)* | 0.11(1.81)* |
|  | Ga2 | 0.05(0.02)* | 0.00(0.18)* | 2.04(0.12)* | 2.19(0.18)* |
|  | Mg(0.03)* | 0.01 | 0.63 | 0.01 | 0.02 |
|  | O1(7.98)* | 8.06 | 8.21 | 8.04 | 8.05 |
|  | O2(7.98)* | 8.24 | 8.20 | 8.20 | 8.21 |
| Mg(CO3) | Ga | 0.04(0.02)* | 0.00(0.04)* | 0.05(1.74)* | 0.70(0.02)* |
|  | Mg(0.15)* | 0.80 | 0.95 | 0.62 | 0.87 |
|  | C(0.00)* | 0.00 | 0.00 | 0.00 | 0.00 |
|  | O1(8.03)* | 8.04 | 8.07 | 8.02 | 8.09 |
|  | O2(7.97)* | 8.04 | 8.06 | 8.04 | 8.03 |
|  | O3(7.84)* | 8.02 | 8.06 | 8.02 | 8.00 |

⁎ Denotes charge transfer value for pristine atoms

Figure S1. Charge density plot of g-GaN@Mg+passivation molecules. (a-d) Mg(OH)2+surface and (e-h) Mg(CO3) +surface.

Figure S2. (a) AIMD calculations were conducted on the surface of g-GaN@Mg in the

presence of Mg(CO)2 at 500 K (A snapshot of various time scales). (b-c) depict the

bond distance and the free energy fluctuations of Mg(CO)2 +g-GaN@Mg during the 10 ps

AIMD simulation at 500 K.

Figure S3. (a) AIMD calculations were conducted on the surface of g-GaN@Mg in the presence of Mg(OH)2 at 500 K (A snapshot of various time scales). (b-c) depict the bond distance and the free energy fluctuations of Mg(OH)2 +g-GaN@Mg during the 10 ps AIMD simulation at 500 K.