Rational Electrolytes Design for Li-Metal Batteries Operated Under Extreme Conditions: A Combined DFT, COSMO-RS, and Machine Learning Study

Liang-Ting Wu,1 Yu-Ting Zhan,1 Zhong-Lun Li,1 Po-Ting Chen,1 Bing Joe Hwang,1,2 and Jyh-Chiang Jiang1*

1 Department of Chemical Engineering, National Taiwan University of Science and Technology, Taipei 106, Taiwan; Sustainable Electrochemical Energy Development Center (SEED Center), National Taiwan University of Science and Technology, Taipei 106, Taiwan

2 National Synchrotron Radiation Research Center (NSRRC), Hsinchu 30076, Taiwan

Corresponding Author

*Jyh-Chiang Jiang. Email: jcjiang@mail.ntust.edu.tw

Figure S1. Optimized structures of 20 solvents, 3 diluents (TTE, BTFE, TFEO), and a lithium salt (LiTFSI). The common organic solvents include cyclic carbonates (EC, PC, FEC, VC), linear carbonate (DMC, DEC, EMC, FEMC), cyclic ester (GBL), linear ester (MA, EA, MP), cyclic ether (DOL, THF), linear ether (DME, DEE, FDMB), sulfone (TMS), sultone (PES), and amide (DMAC).

Table S1. The melting point (mp in K), boiling point (bp in K), and enthalpy of fusion (ΔHf in kJ mol-1) of 20 common organic solvents. a From Sigma-Aldrich; b From indagoochem; c Predicted from QSPR in AMS.

| Solvents | Melting Point (K) | Boiling Point (K) | Enthalpy of fusion (kJ mol-1) |
| --- | --- | --- | --- |
| EC | 309.48 1 | 519.15 1 | 13.02 2 |
| PC | 224.35 1 | 514.75 1 | 8.96 2 |
| FEC | 290.45 3 | 485.15 4 | 15.95 c |
| VC | 293.65 a | 435.15 a | 15.79 c |
| DMC | 272.15 1 | 363.26 1 | 11.58 2 |
| DEC | 230.15 1 | 399.05 1 | 9.24 2 |
| EMC | 259.15 1 | 380.65 1 | 11.24 2 |
| FEMC | 229.00 5 | 363.00 5 | 16.64 c |
| GBL | 229.79 1 | 477.75 1 | 9.57 1 |
| MA | 174.90 1 | 329.85 1 | 7.49 1 |
| EA | 189.35 1 | 350.25 1 | 10.48 1 |
| MP | 185.65 1 | 351.75 1 | 17.02 c |
| DOL | 175.94 1 | 348.45 1 | 6.57 1 |
| THF | 164.77 1 | 339.15 1 | 8.54 1 |
| DME | 204.15 1 | 358.15 1 | 14.01 c |
| DEE | 199.15 a | 394.15 a | 15.44 c |
| FDMB | 224.15 c | 405.82 c | 21.17 c |
| TMS | 301.60 1 | 559.15 1 | 1.372 6 |
| PES | 355.65 b | 529.75 b | 16.95 c |
| DMAC | 254.15 1 | 439.05 1 | 15.78 c |

Table S2. The calculated Li+ binding energy (EB, Li in eV), and TFSI- binding energy (EB, TFSI in eV) of 20 solvents and 3 diluents.

| Compounds | EB, Li | EB, TFSI |
| --- | --- | --- |
| EC | -0.712 | -0.259 |
| PC | -0.722 | -0.295 |
| FEC | -0.608 | -0.289 |
| VC | -0.636 | -0.238 |
| DMC | -0.695 | -0.140 |
| DEC | -0.715 | -0.149 |
| EMC | -0.704 | -0.150 |
| FEMC | -0.593 | -0.250 |
| GBL | -0.780 | -0.186 |
| MA | -0.743 | -0.140 |
| EA | -0.756 | -0.140 |
| MP | -0.780 | -0.131 |
| DOL | -0.713 | -0.212 |
| THF | -0.847 | -0.146 |
| DME | -0.712 | -0.143 |
| DEE | -0.753 | -0.148 |
| FDMB | -0.754 | -0.213 |
| TMS | -0.779 | -0.203 |
| PES | -0.580 | -0.248 |
| DMAC | -1.012 | -0.135 |
| TTE | -0.460 | -0.297 |
| BTFE | -0.582 | -0.274 |
| TFEO | -0.724 | -0.380 |

Table S3. Mean values and standard deviations of the predicted Li+ binding energy (eV), and TFSI- binding energy (eV) of 20 solvents and 3 diluents.

| Compounds | EB, Li, Mean | EB, Li, STD | EB, TFSI, Mean | EB, TFSI, STD |
| --- | --- | --- | --- | --- |
| EC | -0.7279 | 0.0084 | -0.2446 | 0.0087 |
| PC | -0.7608 | 0.0077 | -0.2358 | 0.0105 |
| FEC | -0.5634 | 0.0437 | -0.2935 | 0.0048 |
| VC | -0.6431 | 0.0082 | -0.2095 | 0.0189 |
| DMC | -0.6435 | 0.0139 | -0.1635 | 0.0054 |
| DEC | -0.6814 | 0.0129 | -0.1415 | 0.0045 |
| EMC | -0.6633 | 0.0071 | -0.1536 | 0.0025 |
| FEMC | -0.6478 | 0.0097 | -0.2469 | 0.0044 |
| GBL | -0.763 | 0.004 | -0.2138 | 0.0053 |
| MA | -0.7008 | 0.0091 | -0.1629 | 0.0046 |
| EA | -0.73 | 0.0074 | -0.1553 | 0.0045 |
| MP | -0.7961 | 0.0049 | -0.1431 | 0.0021 |
| DOL | -0.7354 | 0.0107 | -0.1725 | 0.0036 |
| THF | -0.8212 | 0.0037 | -0.1319 | 0.0041 |
| DME | -0.7626 | 0.0058 | -0.1401 | 0.0034 |
| DEE | -0.8385 | 0.0054 | -0.1348 | 0.0038 |
| FDMB | -0.7708 | 0.0077 | -0.2074 | 0.0012 |
| TMS | -0.7659 | 0.0058 | -0.2324 | 0.0051 |
| PES | -0.626 | 0.0063 | -0.2449 | 0.0053 |
| DMAC | -0.9348 | 0.0047 | -0.1566 | 0.0032 |
| TTE | -0.4597 | 0 | -0.2971 | 0 |
| BTFE | -0.648 | 0.0094 | -0.3126 | 0.0056 |
| TFEO | -0.6468 | 0.0043 | -0.3638 | 0.0016 |

References

1	CRC handbook of chemistry and physics.  (1977).

2	Ding, M. S. Liquid−Solid Phase Equilibria and Thermodynamic Modeling for Binary Organic Carbonates. J. Chem. Eng. Data 49, 276-282, doi:10.1021/je034134e (2004).

3	Jänes, A., Thomberg, T., Eskusson, J. & Lust, E. Fluoroethylene Carbonate as Co-Solvent for Propylene Carbonate Based Electrical Double Layer Capacitors. J. Electrochem. Soc. 160, A1025, doi:10.1149/2.016308jes (2013).

4	Zhang, Q.-K., Zhang, X.-Q., Yuan, H. & Huang, J.-Q. Thermally Stable and Nonflammable Electrolytes for Lithium Metal Batteries: Progress and Perspectives. Small Sci. 1, 2100058, doi:10.1002/smsc.202100058 (2021).

5	Naejus, R., Damas, C., Lemordant, D., Coudert, R. & Willmann, P. Excess thermodynamic properties of the ethylene carbonate–trifluoroethyl methyl carbonate and propylene carbonate–trifluoroethyl methyl carbonate systems at T= (298.15 or 315.15) K. J. Chem. Thermodynamics 34, 795-806, doi:10.1006/jcht.2001.0877 (2002).

6	Ahlers, J., Lohmann, J. & Gmehling, J. Binary Solid−Liquid Equilibria of Organic Systems Containing Different Amides and Sulfolane. J. Chem. Eng. Data 44, 727-730, doi:10.1021/je9802975 (1999).