Supporting Information

Regulating the Double-Way Traffic of Cations and Anions in Ambipolar Polymer Cathodes for Sustainable Aluminum Dual-Ion Batteries

Lian-Wei Luoa, Chong Zhanga*, Wenyan Maa, Changzhi Hana,b, Xuan Aia, Yu Chena, Yunhua Xuc, Xiulei Jid* and Jia-Xing Jianga,b*

aSchool of Materials Science and Engineering, Shaanxi Normal University, Xi’an, Shaanxi 710062, P. R. China.

bKey Laboratory of Optoelectronic Chemical Materials and Devices (Ministry of Education), School of Optoelectronic Materials & Technology, Jianghan University, Wuhan 430056, P. R. China.

cSchool of Materials Science and Engineering, Tianjin University, Tianjin, 300072, P. R. China.

dDepartment of Chemistry, Oregon State University, Corvallis, Oregon 97331-4003, United States.

E-mail: chongzhangabc@snnu.edu.cn; jiaxing@jhun.edu.cn; david.ji@oregonstate.edu

Experimental Procedures

Materials

2,6-dibromoanthraquinone, bis(pinacolato)diboron, anhydrous N,N-dimethylformamide (DMF), 10-phenyl-10H-phenothiazine, N-bromosuccinimide, p-Toluenesulfonic acid monohydrate (TsOH·H2O), 1,4-dioxane, 2,7-dibromo-9,10-phenanthrenedione, tris(4-bromophenyl)amine, ethylene glycol, tris(4-(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)phenyl)amine, 1,3,6,8-tetrabromopyrene, 2,7-dibromopyrene-4,5,9,10-tetraone, 1,3,5-Tribromobenzene, [1,1’bis(diphenylphosphino)ferrocene]dichloropalladium(II) (Pd(dppf)Cl2), tetrakis-(triphenylphosphine)palladium(0) (Pd(PPh3)4), propylamine, and acetic acid were purchased from TCI, Acros, Alfa, J&K and Yanshen Technology Co., Ltd.. Potassium acetate, potassium carbonate, bromine, dichloromethane, acetic acid, ethyl acetate, petroleum ether, dichloromethane, acetone, toluene, tetrahydrofuran (THF) and methanol were purchased from Sinopharm Chemical Reagent Co. Ltd. All reagents were used as received. Aluminium chloride/1-ethyl-3-methylimidazolium chloride (EMImCl) ionic liquid (AlCl3/EMImCl=1.3) was purchased from DoDoChem.

Synthesis

Synthesis of 2,6-bis(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)-9,10-anthracenedione: Under N2 atmosphere, 2,6-dibromoanthraquinone (3.66 g, 10 mmol) was added into a solution of bis(pinacolato)diboron (6.47 g, 25.5 mmol), Pd(dppf)Cl2 (0.11 g, 1.3 mmol) and potassium acetate (3.0 g, 30.5 mmol) in 1,4-dioxane (100 mL). The reaction solution was heated to 90 oC and stirred for 24 hours. After cooling to room temperature, the reaction was quenched by water (50 mL). Then, the mixture was extracted by dichloromethane for three times. The combined organic layer was dried over by MgSO4 and then evaporated to give a yellow powder. The crude product was purified by column chromatography on silica gel (petroleum ether/dichloromethane = 5:1) to give a light yellow product (yield: 64.5%). 1H NMR (400 MHz, CDCl3): δ 8.73 (s, 2H), 8.29 (d, J = 7.6 Hz, 2H), 8.19 (dd, J = 7.7, 1.1 Hz, 2H), 1.38 (d, J = 6.1 Hz, 24H).

Synthesis of 3,7-dibromo-10-(4-bromophenyl)-10H-phenothiazine: N-Bromo-succinimide (10.69 g, 60.08 mmol) was added in five times to a solution of 10-Phenyl-10H-phenothiazine (5.0 g, 18.2 mmol) in THF (100 mL) and then stirred for 6 hours at 0-5 ℃. The mixture solution was poured into ice water and then filtered. Before drying under vacuum, the obtained residue was washed with water. The collected crude product was purified by column chromatography (petroleum ether/dichloromethane = 3/1) to obtain the target product (yield: 42.6%) as a white solid. 1H-NMR (400 MHz, CDCl3) δ 7.80-7.66 (m, 2H), 7.26-7.16 (m, 2H), 7.11 (d, J = 2.3 Hz, 2H), 6.94 (dd, J = 8.8, 2.3 Hz, 2H), 6.02 (d, J = 8.8 Hz, 2H).

Synthesis of 3,7-bis(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)-10-(4-(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)phenyl)-10H-phenothiazine: Under N2 atmosphere, the mixture of  3,7-dibromo-10-(4-bromophenyl)-10H-phenothiazine (2.56 g, 5 mmol), bis(pinacolato)diboron (4.57 g, 18 mmol), potassium acetate (3.54 g, 36 mmol) and Pd(dppf)Cl2 (0.27 g, 0.37 mmol) in dry 1,4-dioxane (50 mL) was stirred for 48 hours at 90 oC. After cooling down to room temperature, the resulting suspension was extracted three times with ethyl acetate. The organic layers were combined, washed with saturated brine, dried with anhydrous Na2SO4 and filtered. A crude product was obtained after removing all the solvent by rotary evaporation, and further purified by quick chromatography using petroleum ether /EtOAc (15:1 v/v) as eluent (yield: 67.4%). 1H NMR (400 MHz, CDCl3) δ 8.04 (d, 1H), 7.44 – 7.31 (m, 2H), 7.18 (d, 1H), 6.04 (d, 1H), 1.40 (s, 6H), 1.28 (d, 12H).

Synthesis of PPTZ: Under the N2 atmosphere, aqueous potassium carbonate solution (2.0 M, 4 mL) was added to a solution of 3,7-dibromo-10-(4-bromophenyl)-10H-phenothiazine (1.0 mmol, 512 mg), 3,7-bis(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)-10-(4-(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)phenyl)-10H-phenothiazine (1.0 mmol, 653 mg) and tetrakis-(triphenylphosphine) palladium (0) (16 mg, 14 μmol) in DMF (20 mL). The mixture was heated to 150 oC and stirred for 48 hours. After the reaction solution was cooled to ambient temperature and filtrated, the residue was washed with deionized water, methanol, dichloromethane and THF, respectively. The obtained polymer was further purified by Soxhlet extraction with tetrahydrofuran for 48 hours. Then the polymer was dried in a vacuum for 24 hours at 80 oC to give a yellow-green powder (yield: 89.6%).

Synthesis of the Polymer PAQ: Under the N2 atmosphere, aqueous potassium carbonate solution (2.0 M, 4 mL) was added to a solution of 2,6-dibromoanthraquinone (1.0 mmol, 366 mg), 2,6-bis(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)-9,10-anthracenedione (1.0 mmol, 460 mg) and tetrakis-(triphenylphosphine) palladium (0) (16 mg, 14 μmol) in dimethylformamide (DMF, 20 mL). The mixture was heated to 150 oC and stirred for 48 hours. After the reaction solution was cooled to ambient temperature and filtrated, the residue was washed with deionized water and methanol, dichloromethane and THF, respectively. The resulting polymer was dried in a vacuum for 24 hours at 80 oC to give a pale yellow powder (yield: 70.6%).

Synthesis of the Polymer PPTZ-AQ: Under the N2 atmosphere, aqueous potassium carbonate solution (2.0 M, 4 mL) was added to a solution of 2,6-bis(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)-9,10-anthracenedione (0.9 mmol, 414 mg), 3,7-dibromo-10-(4-bromophenyl)-10H-phenothiazine (0.6 mmol, 307.2 mg) and tetrakis-(triphenylphosphine) palladium (0) (16 mg, 14 μmol) in DMF (20 mL). The mixture was heated to 150 oC and stirred for 48 hours. After the reaction solution was cooled to ambient temperature and filtrated, the residue was washed with deionized water, methanol, dichloromethane and THF, respectively. The obtained polymer was further purified by Soxhlet extraction with tetrahydrofuran for 48 hours. The resulting polymer was dried in a vacuum for 24 hours at 80 oC to give a red powder (yield: 91%).

Synthesis of the Polymer PBAQ: Under the N2 atmosphere, aqueous potassium carbonate solution (2.0 M, 4 mL) was added to a solution of 2,6-dibromoanthraquinone (1.5 mmol, 549 mg), benzene-1,3,5-triyltriboronic acid (1.0 mmol, 210 mg) and tetrakis-(triphenylphosphine) palladium (0) (16 mg, 14 μmol) in DMF (20 mL). The mixture was heated to 150 oC and stirred for 48 hours. After the reaction solution was cooled to ambient temperature and filtrated, the residue was washed with deionized water, methanol, dichloromethane and THF, respectively. The obtained polymer was further purified by Soxhlet extraction with tetrahydrofuran for 48 hours. Then the resulting polymer was dried in a vacuum for 24 hours at 80 oC to give a pale green powder (yield: 90.2%).

Synthesis of the Polymer PPy-AQ: Under the N2 atmosphere, aqueous potassium carbonate solution (2.0 M, 4 mL) was added to a solution of 1,3,6,8-tetrabromopyrene (1 mmol, 517.8 mg), 2,2',2''-(8-(4,4,5,5-tetramethyl-1,3-dioxolan-2-yl)pyrene-1,3,6-triyl)tris(4,4,5,5-tetramethyl-1,3,2-dioxaborolane) (1 mmol, 708.3 mg) and tetrakis-(triphenylphosphine) palladium (0) (16 mg, 14 μmol) in DMF (20 mL). The mixture was heated to 150 oC and stirred for 48 hours. After the reaction solution was cooled to ambient temperature and filtrated, the residue was washed with deionized water, methanol, dichloromethane and THF, respectively, and then purified by Soxhlet extraction with tetrahydrofuran for 48 hours. The resulting polymer was dried in a vacuum for 24 hours at 80 oC to give a black powder (yield: 87.5%).

Synthesis of the Polymer PTPA-AQ: Under the N2 atmosphere, aqueous potassium carbonate solution (2.0 M, 4 mL) was added to a solution of 2,6-bis(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)-9,10-anthracenedione (0.9 mmol, 414 mg), tris(4-bromophenyl)amine (0.6 mmol, 289.2 mg) and tetrakis-(triphenylphosphine) palladium (0) (16 mg, 14 μmol) in DMF (20 mL). The mixture was heated to 150 oC and stirred for 48 hours. After the reaction solution was cooled to ambient temperature and filtrated, the residue was washed with deionized water, methanol, dichloromethane and THF, respectively. The obtained polymer was further purified by Soxhlet extraction with tetrahydrofuran for 48 hours. The resulting polymer was dried in a vacuum for 24 hours at 80 oC to give a red powder (yield: 84%).

Synthesis of the Polymer PPy: Under the N2 atmosphere, aqueous potassium carbonate solution (2.0 M, 4 mL) was added to a solution of 1,3,6,8-tetrabromopyrene (1 mmol, 517.8 mg), 2,2',2''-(8-(4,4,5,5-tetramethyl-1,3-dioxolan-2-yl)pyrene-1,3,6-triyl)tris(4,4,5,5-tetramethyl-1,3,2-dioxaborolane) (1 mmol, 708.3 mg) and tetrakis-(triphenylphosphine) palladium (0) (16 mg, 14 μmol) in DMF (20 mL). The mixture was heated to 150 oC and stirred for 48 hours. After the reaction solution was cooled to ambient temperature and filtrated, the residue was washed with deionized water, methanol, dichloromethane and THF, respectively, and then purified by Soxhlet extraction with tetrahydrofuran for 48 hours. The resulting polymer was dried in a vacuum for 24 hours at 80 oC to give a black powder (yield: 89.5%).

Synthesis of the Polymer PTPA: Under the N2 atmosphere, aqueous potassium carbonate solution (2.0 M, 4 mL) was added to a solution of tris(4-(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)phenyl)amine (1 mmol, 623 mg), tris(4-bromophenyl)amine (1 mmol, 482 mg) and tetrakis-(triphenylphosphine) palladium (0) (16 mg, 14 μmol) in DMF (20 mL). The mixture was heated to 150 oC and stirred for 48 hours. After the reaction solution was cooled to ambient temperature and filtrated, the residue was washed with deionized water, methanol, dichloromethane and THF, respectively. The obtained polymer was further purified by Soxhlet extraction with tetrahydrofuran for 48 hours. The resulting polymer was dried in a vacuum for 24 hours at 80 oC to give a red powder (yield: 86%).

Characterizations

The thermal stability of all the polymers was evaluated by a thermogravimetric analysis (Q1000DSC+LNCS+FACS Q600DT) with the temperature range from 20 to 800 oC under N2 atmosphere. Fourier transform infrared (FT-IR) spectra were collected on transmission on a Tensor 27 FT-IR spectrometer (Bruker). The solid state 13C CP/MAS NMR spectra were collected on a JEOL RESONRNCE ECZ 400R NMR spectrometer with a MAS frequency of 12 kHz. The morphology of the polymers was obtained by a field emission scanning electron microscope (SEM) (SU8020, Hitachi). The specific surface area and pore size distributions were analyzed by an ASAP 2420-4 (micromeritics) volumetric adsorption analyze at 77.3 K. The surface area was calculated in the relative pressure (P/Po) range from 0.05 to 0.20. The pore size distribution data was calculated by NL-DFT utilizing the adsorption branch isotherm. The sample was degassed under vacuum (10−5 bar) at 120 oC for 12 hours before N2 sorption analysis. Powder X-ray diffraction (PXRD) measurement was carried out on a X-ray diffractometer (D/Max-3c). X-ray photoelectron spectroscopy (XPS) measurement was performed on a ESCALAB Xi+ spectrometer (Thermo Fisher Scientific). The UV-vis reflection spectra were obtained on an UV-vis spectrophotometer (UV-Lambda 950, PerkinElmer, US) equipped with an integrating sphere assembly, using BaSO4 as a reflectance background. For the ex situ XPS, and EDX measurements, the cells at different states of charge were disassembled in an argon-filled glove box and then the cathodes were washed by dried tetrahydrofuran several times for removing the residual electrolytes; Afterwards, the cathodes were dried under vacuum before the measurements. In the process of transferring the cathodes into the equipment, all samples were exposed to air within 5 s. For the ex situ FTIR measurement, the cells at different states of charge were disassembled in an argon-filled glove box, and the residual electrolytes on the surface of the cathodes were carefully wiped out, without using a washing process by solvents.

Figure S1. The CV curves of D type (a) PTPA (b) Py, (c) TT and (d) PTZ units at 0.5 mV s-1. Since the small molecule of triphenylamine (TPA) is not redox-active in the AlCl3-based ionic liquid electrolytes, the electrochemical reaction of TPA unit was tested using the polymer poly(triphenylamine) (PTPA) synthesized through Suzuki coupling reaction as the active material in the cathode.

Figure S2. The CV curves of A type units (a) AQ, (b) PQ, (c) NQ, (d) PTO and (e) HATN at 0.5 mV s-1.

Figure S3. The characterizations of PAQ, PPTZ and PPTZ-AQ. (a) FT-IR spectra. (b) Thermogravimetric analysis under N2 atmosphere. (c) Solid state 13C nuclear magnetic resonance spectra. (d) X-ray diffraction patterns.

Figure S4. The SEM images of PAQ, PPTZ and PPTZ-AQ.

Figure S5. The GCD plots of PPTZ-AQ cathode containing 30 wt% conductive agent and PPTZ-AQ-811 cathode containing 10 wt% conductive agent at 0.05 A g−1.

The specific capacities of PPTZ-AQ cathode and PPTZ-AQ-811 cathode are 205 and 196 mAh g−1, respectively. The capacity loss of 9 mAh g−1 from PPTZ-AQ cathode to PPTZ-AQ-811 cathode can be imputed to two factors: one is the decreased capacity contribution from the reduced content of carbon black; another is the weakened redox activity of the polymer due to the decreased electronic conductivity of the electrode. To get the highest value of the specific capacity (Cca) of conductive agent in the PPTZ-AQ -based cathodes, we assumed that the decreased capacity of 9 mAh g−1 just originated from the decreased capacity contribution from the reduced content of conductive agent, thus the equation of 3Cca/6 − Cca/8 =9 mAh g−1 could be built. After solving this equation, the calculated highest value of Cca is 24 mAh g−1. In this research, we use the highest value of 24 mAh g−1 as the real Cca, thus the capacity contribution from conductive agent in PPTZ-AQ cathode and PPTZ-AQ-811 cathode are 12 mAh g−1 and 3 mAh g−1, respectively.

Figure S6. The GCD plots of PAQ and PPTZ at different currents.

Figure S7. The structure and characterizations for PBAQ. (a) The notional polymer structure. (b) The FTIR spectrum. (c) The N2 adsorption (solid)-desorption (hollow) isotherms. (d) The PSD curves calculated by NL-DFT based on the N2 adsorption isotherm.

Figure S8. (a) The rate performance of PBAQ. (b) The GCD profiles of PBAQ at different current rates. characterizations for PBAQ.

Figure S9. The voltage hysteresis between charge and discharge voltages of PAQ, PPTZ and PPTZ-AQ at different currents from 0.05 to 15 A g-1.

Figure S10. The energy efficiency of PPTZ-AQ at 0.1 A g-1.

Figure S11. The ex situ FT-IR spectra of the PAQ cathode at different states of charge.

Figure S12. The ex situ FT-IR spectra of the PPTZ cathode at different states of charge.

Figure S13. The ex situ XPS spectra of the PPTZ-AQ cathode at different states of charge.

Figure S14. The EDX data of PPTZ cathode at the charged state.

Figure S15. The EDX data of the PPTZ-AQ cathode at fully (a) discharged and (b) charged states.

Figure S16. The EDX data of PAQ cathode at the discharged state.

Figure S17. (a) The band structures of PTZ unit and its positively charged state (PTZ+) with one charge. (b) The band structures of AQ unit and its negatively charged state (AQ−) with one and two charges. (c) The band structures of a model segment [PTZ-AQ]’ and its positively charged state ([PTZ-AQ]’+) with one charge, the segment [PTZ-AQ]’ comprises one PTZ unit and one AQ unit.

Figure S18. The GITT response of PAQ, PPTZ and PPTZ-AQ.

Figure S19. The calculated binding energies between the ion pairs of PTZ+ with one AlCl4−, PTZ2+ with two AlCl4−, AQ− with one AlCl2+, and AQ2− with two AlCl2+ (the insets are the optimized structures for the charged building blocks with their counter ions).

Figure S20. The electrochemical impedance spectroscopy (EIS) of the batteries adopting PAQ, PPTZ, and PPTZ-AQ cathodes at different states of charge.

Figure S21. (a) The GCD plots of the PPTZ-AQ cathode with different active mass loadings of 1.5 mg cm−2 at 0.05 A g−1, 13.2 mg cm−2 at 0.05 A g−1, 25.6 mg cm−2 at 0.05 A g−1, 39.4 mg cm−2 at 0.05 A g−1, 72.3 mg cm−2 at 0.03 A g−1 and 100 mg cm−2 at 0.02 A g−1. The cycling performance of the PPTZ-AQ cathode with different active mass loadings of (b) 39.4 mg cm−2 at 0.05 A g−1, (c) 72.3 mg cm−2 at 0.03 A g−1.

Figure S22. The GCD plots of PPTZ-AQ cathode with an active mass loading of 13.1 mg cm−2.

Figure S23. The GCD plots at different cycles of PPTZ-AQ cathode with an active mass loading of 25.6 mg cm−2 at 1.28 mA cm−2.

Figure S24. The (a) synthetic route of PPy-AQ and its (b) FT-IR spectrum and (c) SEM image.

Figure S25. The (a) synthetic route of PTPA-AQ and its (b) FT-IR spectrum and (c) SEM image.

Figure S26. The (a) band structures and (b) N2 sorption isotherms of PPy-AQ and PTPA-AQ.

Figure S27. The GCD curves of (a) PPy-AQ and (b) PTPA-AQ at different current rates. (c) The comparison of rate performance for PPTZ-AQ, PPy-AQ, and PTPA-AQ.

Figure 28. The GITT response of (a) PPy-AQ and (b) PTPA-AQ. (c) The comparison of diffusion rates for PPTZ-AQ, PPy-AQ, and PTPA-AQ.

Figure S28. (a) The GCD curves of the PPTZ-AQ cathode with an active mass loading of 72.3 mg cm−2 at 0.03 A g−1, the PPy-AQ cathode with an active mass loading of 49.7 mg cm−2 at 0.05 A g−1, the PTPA-AQ cathode with an active mass loading of 56.9 mg cm−2 at 0.05 A g−1. (b) The GCD curves of PTPA with an active mass loading of 57.3 mg cm−2 and PPy with an active mass loading of 48.1 mg cm−2 at 0.05 A−1.

Note 1.

Since the chloroaluminate ions (AlCl4−, AlCl2+ etc.) typically serve as the charge carriers in organic cathodes of rechargeable aluminum batteries and the electrolyte is the only source of Cl, the dosage of electrolyte should provide enough charge carriers to fulfil the redox reactions of cathode materials. Additionally, it should be noted that the molar ratio of AlCl3 to 1-ethyl-3-methylimidazolium chloride ([EMIm]Cl) changes with the charge/discharge processes due to the consumption of AlCl3. The upper limit of the molar ratio (r) of AlCl3 to [EMIm]Cl for ionic liquid state electrolyte is around 2, and reversible Al plating on the anode surface only can be achieved when r >1. As a result, we assume that r is 2 in the initial electrolyte and it decreases to 1 after the completely charge process of all the three polymers of PPTZ, PAQ and PPTZ-AQ. For the p-type doing reaction with AlCl4− as the charge carrier, the reaction of the electrolyte is:

43AlCl3+e-=AlCl4-+ 13Al                                                    (1)

Therefore, the required electrolyte dosage of p-type doping reaction can be represented as below:

mep=np×83MAlCl3+ 43MEMImClmep=np×83MAlCl3+ 43MEMImCl=551.7 g/mol×np                          (2)

Where mep is the required electrolyte dosage (g) of p-type doping reaction with AlCl4− as the charge carrier, np is the number (mol) of the transferred electrons of the repeating unit during its p-type doping reaction, MAlCl3 is the molecular weight (g/mol) of AlCl3, M[EMIm]Cl is the molecular weight (g/mol) of [EMIm]Cl.

For the n-type doing reaction with AlCl2+ as the charge carrier, the reaction of the electrolyte is:

AlCl3 +2Al- 6e-= 3AlCl2+                                                       (3)

Therefore, the required electrolyte dosage of n-type doping reaction can be represented as below:

men1=nn1×13MAlCl3+ 16MEMImCl+ 13MAl=77.8 g/mol×nn1   men1=nn1×13MAlCl3+ 16MEMImCl+ 13MAl         men1=nn1×13MAlCl3+ 16MEMImCl+ 13MAl=77.8nn1     (4)

Where men1 is the required electrolyte dosage (g) of n-type doping reaction with AlCl2+ as the charge carrier, nn1 is the number (mol) of the transferred electrons of the repeating unit during its n-type doping reaction, MAlCl3 is the molecular weight (g/mol) of AlCl3, M[EMIm]Cl is the molecular weight (g/mol) of [EMIm]Cl, MAl is the molecular weight (g/mol) of Al metal.

For the n-type doing reaction with AlCl2+ as the charge carrier, the reaction of the electrolyte is:

2AlCl3 +Al- 3e-= 3AlCl2+                                                          (5)

Therefore, the required electrolyte dosage of n-type doping reaction can be represented as below:

men2=nn2×43MAlCl3+ 23MEMImCl+ 13MAl=284.5 g/mol×nn2men2=nn2×43MAlCl3+ 23MEMImCl+ 13MAl=284.53 g/mol×nn2men2=nn2×43MAlCl3+ 23MEMImCl+ 13MAl             men2=nn2×43MAlCl3+ 23MEMImCl+ 13MAl=284.53nn2    (6)

Where men2 is the required electrolyte dosage (g) of n-type doping reaction with AlCl2+ as the charge carrier, nn2 is the number (mol) of the transferred electrons of the repeating unit during its n-type doping reaction, MAlCl3 is the molecular weight (g/mol) of AlCl3, M[EMIm]Cl is the molecular weight (g/mol) of [EMIm]Cl, MAl is the molecular weight (g/mol) of Al metal.

According to the stoichiometric ratio (1.5) of AQ to PTZ in PPTZ-AQ, the repeating unit of PPTZ-AQ contains one PTZ unit with one and half AQ units. Therefore, the redox reaction of 1 mol repeating units in PPTZ-AQ transfer 5 mol electrons that is the sum of 3 mol electrons for n-type doping reaction and 2 mol electrons for p-type doping reaction. Since mep is around 7 times higher than that of men1 and the n-type doping reaction potential of AQ units is located between the two-step p-type doping reaction potential of PTZ units, the required electrolyte dosage for the p-type doping reaction of PTZ units could cover that for the n-type doping reaction of AQ units. This indicates that the required electrolyte dosage for the redox reaction of 1 mol repeating units with 5 mol electron transfer in PPTZ-AQ is 2 mol × 551.7 g/mol = 1103.4 g. While, the required electrolyte dosage for the redox reaction of 2.5 mol repeating units with 5 mol electron transfer in PPTZ is 5 mol × 551.7 g/mol = 2758.5 g. Therefore, the theoretically required electrolyte dosage per transferred electron for fulfilling the electrochemical reactions of PPTZ-AQ is only around 40% of that of PPTZ. The required electrolyte dosage for the redox reaction of 2.5 mol repeating units with 5 mol electron transfer in PAQ is 5 mol × 284.5 g/mol = 1442.5 g. Hence, the theoretically required electrolyte dosage per transferred electron for fulfilling the electrochemical reactions of PPTZ-AQ is only around 76% of that of PAQ.

Table S1. The comparison of electrochemical performances of PPTZ-AQ with most organic cathodes in rechargeable aluminum batteries (RABs) in recent investigations.

| Samples | Charge Carriers | Specific capacity (mAh/g) (current) | Rate capability (mAh/g) (current) | Cycle number (current) | Refs |
| --- | --- | --- | --- | --- | --- |
| PPTZ-AQ | AlCl4-AlCl2+ | 205 (0.05 A/g) | 160 (15 A/g) | 800 (0.1 A/g) 60000 (5 A/g) | This work |
| TPB | AlCl2(urea)2+ | 180 (0.1 A/g) | 50 (1 A/g) | 250 (0.1 A/g) | 1 |
| COFJLU2 | AlCl4- | 90 (2 A/g) | - | 30000 (5 A/g) | 2 |
| TCNQ | AlCl2+ | 120 (0.2 A/g) | 100 (0.5 A/g) | 2000 (0.5 A/g) | 3 |
| PAQS/MWCNTs | AlCl2+ | 165 (0.1125 A/g) | 133 (4.5 A/g) | - | 4 |
| H2TPP | AlCl2+ | 101.2 (0.1 A/g) | 74 (0.5 A/g) | 5000 (0.2 A/g) | 5 |
| poly(nitropyrene-co-pyrene) | AlCl4- | 100 (0.2 A/g) | 48 (2 A/g) | 1000 (0.2 A/g) | 6 |
| PyPz | AlCl4- | 231 (0.1 A/g) | 116 (30 A/g) | 1000 (0.2 A/g) 100000 (10 A/g) | 7 |
| 2D Cu-based MOF@rGO | AlCl2+ AlCl4- | 184 (0.05 A/g) | 65 (0.5 A/g) | 1000 (0.2 A/g) | 8 |
| PI@CNT | Al3+ | 130 (0.15 A/g) | - | 100 (0.15 A/g) | 9 |
| PHATN | AlCl2+ | 145 (0.05 A/g) | - | 100 (0.05 A/g) | 10 |
| anthracene | AlCl4- | 157 (0.1 A/g) | 82 (0.5 A/g) | 800 (0.1 A/g) | 11 |
| PANI(H+)@SWCNTs | AlCl2+ | 200 (1 A/g) | 75 (40 A/g) | 8000 (10 A/g) | 12 |
| PyTQ-CNT | AlCl2+ | 208 (0.2 A/g) | 85 (2 A/g) | 4000 (1 A/g) | 13 |
| N4 | AlCl4- | 136 (0.05 A/g) | 116 (2 A/g) | 4000 (1 A/g) | 14 |
| PVBPX | AlCl4- | 133 (0.2 A/g) | 60 (10 A/g) | 50000 (5 A/g) | 15 |
| β-PT | AlCl4- | 190 (2 A/g) | 127 (5 A/g) | 100000 (10 A/g) | 16 |
| MXene@BDTO | Al3+ | 229.8 (0.5 A/g) | - | 500 (0.5 A/g) | 17 |
| TpBpy-COF | AlCl4- | 307 (0.1 A/g) | 113 (5 A/g) | 3000 (2 A/g) | 18 |
| PAQS/MWCNT | AlCl2+ | 160 (0.5 C) | 130 (10 C) | 500 (0.5 C) | 19 |
| X-PVMPT | AlCl4- | 167 (0.5 C) | 64 (100 C) | 5000 (10 C) | 20 |
| PANI/OMC | AlCl4- | 140 (0.1 A/g) | 118 (2 A/g) | 5000 (1 A/g)) | 21 |
| AQ | Al3+ | 215 (0.1 A/g) | 166 (0.5 A/g) | 200 (0.1 A/g) | 22 |
| TPBQ | AlCl2+ | 177 (0.02 A/g) | 122 (1 A/g) | 3000 (1 A/g) | 23 |
| PI/MOFs | AlCl2+ | 83 (1 A/g) | 40 (10 A/g) | 1800 (1 A/g) | 24 |
| PQ-Δ-HY | AlCl2+ AlCl4- | 130 (0.1 A/g) | 92 (2 A/g) | 500 (0.2 A/g) | 25 |
| G-PANI-8 | AlCl4- | 180 (1 A/g) | 155 (2 A/g) | 4000 (1 A/g) | 26 |
| TDK | AlCl2+ | 185 (0.1 A/g) | 66 (2 A/g) | 8000 (1 A/g) | 27 |
| PTh/MWCNT | AlCl4- | 216 (0.0325 A/g) | - | 300 (0.13 A/g) | 28 |
| PTCDA-SP | Al3+ | 110 (0.1 A/g) | 72 (1000 A/g) | 1200 (0.1 A/g) | 29 |
| PNA | AlCl2+ | 178.2 (0.05 A/g) | 31.5 (10 A/g) | 10000 (2 A/g) | 30 |
| PTh/G | AlCl4- | 152.5 (0.5 A/g) | 113.5 (1 A/g) | 500 (5 A/g) | 31 |
| PPP | AlCl4- AlCl2+ | 92 (0.1 A/g) | 70 (10 A/g) | 30000 (10 A/g) | 32 |
| PTh@GO | AlCl4- | 130 (1 A/g) | 86 (5 A/g) | 4000 (1 A/g) | 33 |

Table S2. The comparison of electrochemical performances between PPTZ-AQ and the reported organic cathodes with high active mass loadings in rechargeable aluminum batteries.

| Samples | Mass Loading (mg/cm2)/Areal capacity (mAh/cm2) | Areal capacity (mAh/cm2)/Cylcle number | Refs |
| --- | --- | --- | --- |
| PPTZ-AQ | 72.3/14.24 100/17.20 | 5.1/580 | This work |
| PyPz | 7.5/1.40 28.7/4.56 | 2.4/2000 | 7 |
| N4 | 6/0.77 12.9/1.61 | 0.768/50 1.61/50 | 14 |
| AQ | 12-16/2.58~3.44 | 2.58-3.44/200 | 22 |
| TBPQ | 5/0.71 9/1.09 | 0.71/200 1.09/200 | 23 |
| PQ-Δ-HY | 9/0.99 | 0.99/100 | 25 |
| PPP | 4/0.31 8/0.58 | 0.31/200 0.58/200 | 32 |

Reference

1. Kao, Y.-T. et al. A quinone-based electrode for high-performance rechargeable aluminum-ion batteries with a low-cost AlCl3/urea ionic liquid electrolyte. ACS Appl. Mater. Interfaces 12, 25853-25860 (2020).

2. Zhang, Q. et al. Accessible COF-based functional materials for potassium-ion batteries and aluminum batteries. ACS Appl. Mater. Interfaces 11, 44352-44359 (2019).

3. Guo, F. et al. Active cyano groups to coordinate AlCl2+ cation for rechargeable aluminum batteries. Energy Storage Mater. 33, 250-257 (2020).

4. Bitenc, J. et al. Concept and electrochemical mechanism of an Al metal anode‒organic cathode battery. Energy Storage Mater. 24, 379-383 (2020).

5. Han, X. et al. Stable high-capacity organic aluminum–porphyrin batteries. Adv. Energy Mater. 11, 2101446 (2021).

6. Walter, M.; Kravchyk, K. V.; Böfer, C.; Widmer, R. & Kovalenko, M. V. Polypyrenes as high-performance cathode materials for aluminum batteries. Adv. Mater. 30, 1705644 (2018).

7. Ma, W. Y. et al. Dihydrophenazine-based conjugated microporous polymer cathodes with enhanced electronic and ionic conductivities for high-performance aluminum dual-ion batteries. Adv. Energy Mater. 13, 2203253 (2023).

8. Guo, Y.; Wang, W.; Lei, H.; Wang, M. & Jiao, S. Q. Alternate storage of opposite charges in multisites for high-energy-density Al–MOF batteries. Adv. Mater. 34, 2110109 (2022).

9. Fan, X. et al. A universal organic cathode for ultrafast lithium and multivalent metal batteries. Angew. Chem. Int. Ed. 57, 7146-7150 (2018).

10. Mao, M. et al. A pyrazine-based polymer for fast-charge batteries. Angew. Chem. Int. Ed. 58, 17820-17826 (2019).

11. Kong, D. et al. Polycyclic aromatic hydrocarbons as a new class of promising cathode materials for aluminum-ion batteries. Angew. Chem. Int. Ed. 61, e202114681 (2022).

12. Wang, S.; Huang, S.; Yao, M.; Zhang, Y. & Niu, Z. Q. Engineering active sites of polyaniline for AlCl2+ storage in an aluminum-ion battery. Angew. Chem. Int. Ed. 59, 11800-11807 (2020).

13. Peng, X. et al. Heterocyclic conjugated polymer nanoarchitectonics with synergistic redox-active sites for high-performance aluminium organic batteries. Angew. Chem. Int. Ed. 61, e202203646 (2022).

14. Wang, G. et al. An efficient rechargeable aluminium–amine battery working under quaternization chemistry. Angew. Chem. Int. Ed. 61, e202116194 (2022).

15. Yang, Z. et al. Phenoxazine polymer-based p-type positive electrode for aluminum-ion batteries with ultra-long cycle life. Angew. Chem. Int. Ed. 62, e202216797 (2023).

16. Zhang, J. et al. Self-adaptive re-organization enables polythiophene as an extraordinary cathode material for aluminum-ion batteries with a cycle life of 100 000 cycles. Angew. Chem. Int. Ed. 62, e202215408 (2023).

17. Wu, G. et al. Anthraquinone derivatives supported by Ti3C2(MXene) as cathode materials for aluminum-organic batteries. J. Energy Chem. 74, 174-183 (2022).

18. Lu, H. et al. Two-dimensional covalent organic frameworks with enhanced aluminum storage properties. ChemSusChem 13, 3447-3454 (2020).

19. Lindahl, N.; Bitenc, J.; Dominko, R. & Johansson, P. Aluminum metal–organic batteries with integrated 3D thin film anodes. Adv. Funct. Mater. 30, 2004573 (2020).

20. Studer, G. et al. On a high-capacity aluminium battery with a two-electron phenothiazine redox polymer as a positive electrode. Energy Environ. Sci. 16, 3760-3769 (2023).

21. Liao, Y. et al. High performance aluminum ion battery using polyaniline/ordered mesoporous carbon composite. J. Power Sources 477, 228702 (2020).

22. Zhou, L. et al. High-capacity and small-polarization aluminum organic batteries based on sustainable quinone-based cathodes with Al3+ insertion. Cell Reports Phys. Sci. 2, 100354 (2021).

23. Mao, M. et al. Simplifying and accelerating kinetics enabling fast-charge Al batteries. J. Mater. Chem. A 8, 23834-23843 (2020).

24. Zhou, J.; Yu, X.; Zhou, J. & Lu, B. Polyimide/metal-organic framework hybrid for high performance Al - Organic battery. Energy Storage Mater. 31, 58-63 (2020).

25. Kim, D. J. et al. Rechargeable aluminium organic batteries. Nat. Energy 4, 51-59 (2019).

26. Wang, D. et al. High-performance aluminum-polyaniline battery based on the interaction between aluminum ion and -NH groups. Sci. China Mater. 64, 318-328 (2021).

27. Yoo, D.-J.; Heeney, M.; Glöcklhofer, F. & Choi, J. W. Tetradiketone macrocycle for divalent aluminium ion batteries. Nat. Commun. 12, 2386 (2021).

28. Raju, V.; Rani, J. V. & Basak, P. Self-arranged polythiophene on multi-walled carbon nanotube templated composites: synthesis and application in rechargeable aluminium battery. Electrochim. Acta 361, 137097 (2020).

29. Fang, L. et al. Sulfur-linked carbonyl polymer as a robust organic cathode for rapid and durable aluminum batteries. J. Energy Chem. 63, 320-327 (2021).

30. Qin, K. et al. Synergy of carbonyl and azo chemistries for wide-temperature-range rechargeable aluminum organic batteries. Nano Energy 101, 107554 (2022).

31. Zhao, S.; Chen, H.; Li, J. & Zhang, J. Synthesis of polythiophene/graphite composites and their enhanced electrochemical performance for aluminum ion batteries. New J. Chem. 43, 15014-15022 (2019).

32. Li, T. et al. Ultrafast and long-cycle stable aluminum polyphenylene batteries. ACS Appl. Mater. Interfaces 14, 30927-30936 (2022).

33. Kong, D. et al. β-hydrogen of polythiophene induced aluminum ion storage for high-performance Al-polythiophene batteries. ACS Appl. Mater. Interfaces 12, 46065-46072 (2020).