Surface Alterations on Agro-Waste Filler and their Effect on the Properties of Biodegradable Polybutylene adipate-co-terephthalate (PBAT)

Niresha Perumal1, Srimala Sreekantan1*, Zuratul Ain Abdul Hamid1, Kesaven Bhubalan2,3, Muhammad Fadhirul Izwan Abdul Malik4, Anwar Iqbal5

1School of Materials and Mineral Resources Engineering, Engineering Campus, Universiti Sains Malaysia, 14300 Nibong Tebal, Penang, Malaysia

2Faculty of Science and Marine Environment, Universiti Malaysia Terengganu, Kuala Nerus 21030, Malaysia

3Institute of Marine Biotechnology, Universiti Malaysia Terengganu, Kuala Nerus 21030, Malaysia

4Science and Engineering Research Centre (SERC), Engineering Campus, Universiti Sains Malaysia, 14300 Nibong Tebal, Penang, Malaysia

5School of Chemical Science, Universiti Sains Malaysia, 11800 Penang, Malaysia

*Corresponding author. E-mail address: srimala@usm.my (SS)

Supplementary Materials

Table 1	Summary of Various Chemical Treatments of Fillers in Polymer Composites.

| Author | Composites | Ratio | Treatment on fillers | Tensile strength (MPa) | Young Modulus (MPa) | Elongation at break (%) | Soil Burial test (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Hu et al. (2007) | PLA/Hemp fiber | 70/30 60/40 50/50 70/30 60/40 50/50 | - - - Alkali (6% solution of NaOH) | 41.14 44.63 43.73 39.29 54.60 41.77 | 5652.5 7399.5 7030.8 7631.0 8489.6 7012.3 | N/A | N/A | [24] |
| Fávaro et al. (2010) | rHDPE/RH | 95/5 90/10 95/5 90/10 | - - Acetylation (acetic acid, acetic anhydride, and 0.1% sulphuric acid) | 20.0 19.5 19.5 19.4 | 470 570 495 525 | N/A | N/A | [25] |
| Ragunathan et al. (2011) | PP/NBRr/RHP | 70/30/5 70/30/10 70/30/15 70/30/30 70/30/5 70/30/10 70/30/15 70/30/30 | - - - - Silane (3 wt% of γ- aminopropyltrimethoxysilane) | 13 12.9 12.3 10.5 17.6 16.8 15.9 13.5 | 1070 1075 1120 1140 1315 1350 1348 1430 | 6.2 5.5 4.4 4.3 4.6 5.0 3.7 3.3 | N/A | [26] |
| Yeh et al. (2015) | PP/RH | 50/50 50/50 50/50 | - Alkali (10 wt% NaOH) Silane (3 wt% of 3-aminopropyltriethoxysilane) | 17.76 18.68 17.74 | 2134 2124 2110 | N/A | N/A | [27] |
| Yeh et al. (2015) | PP/RH/PP-g-MA | 50/50/2 50/50/2 50/50/2 | - Alkali (10 wt% NaOH) Silane (3 wt% of 3-aminopropyltriethoxysilane) | 24.46 22.47 21.92 | 2135 2362 2284 | N/A | N/A | [27] |
| Zahari et al. (2015) | PP/ijuk fiber | 100/0 90/10 80/20 70/30 90/10 80/20 70/30 | - - - - Silane (vinyltrimethoxysilane) | 17.45 17.57 18.36 19.71 20.21 20.27 23.00 | 298.14 361.32 720.24 1052.40 1051.84 1066.30 1098.51 | 0.106 mm 0.079 mm 0.059 mm 0.052 mm 0.084 mm 0.065 mm 0.051mm | N/A | [28] |
| Moustafa et al. (2017) | PBAT/CG | 100/0 90/10 80/20 70/30 90/10 80/20 70/30 | - - - - Torrefaction at 270°C | 14.3 ± 21.2 11.1 ± 1.6 7.4 ± 2.1 6.8 ± 1.7 18.2 ± 1.4 12.9 ± 1.6 8.7 ± 2.2 | N/A | 1545 ± 63 340 ± 4.2 220 ± 5.1 98 ± 7.4 1150 ± 7.9 910 ± 5.9 580 ± 8.4 | N/A | [29] |
| Moura et al. (2018) | PHB/RH | 100/0 90/10 80/20 90/10 80/20 | - - - Hot water treatment | 9.5 ± 3.11 14.0 ± 1.63 13.2 ± 2.17 11.1 ± 3.43 16.1 ± 5.08 | 732 ±104 844 ± 43 760 ± 59 759 ± 54 754 ± 40 | 5.67 ± 0.46 7.00 ± 0.53 5.57 ± 0.40 6.69 ± 0.42 6.95 ± 0.62 | N/A | [30] |
| Royan et al. (2018) | rHDPE/RH | 70/30 70/30 70/30 70/30 | - Alkali (0.5 M NaOH) Acid (3:1 (v/v) ratio of sulphuric and nitric acids) UV/O3 | 17.8 17.9 17.7 18.3 | 175 220 218 210 | N/A | N/A | [22] |
| Sumrith et al. (2020) | Bio-based epoxy/WHF | 100/0 70/30 70/30 70/30 | - - Alkali (5% solution of NaOH) Silane (1% solution of 3-Aminopropyltriethoxysilane) | 64.6 61.4 64 65.3 | 1868.9 1844.5 2105.8 2162.2 | N/A | N/A | [31] |
| Xiong et al. (2020) | PBAT/lignin | 100/0 60/40 50/50 40/60 60/40 50/50 40/60 | - - - - Methylation | 23.70± 1.51 14.41 ± 0.66 13.33 ± 0.58 12.78 ± 0.36 19.48 ± 0.71 13.89 ± 0.86 13.73 ± 0.53 | N/A | 816.49 ± 52.95 378.94 ± 10.21 55.12 ± 8.75 37.81 ± 5.91 545.08 ± 56.78 308.21 ± 42.68 144.12 ± 49.25 | N/A | [32] |
| Jaya et al. (2020) | LDPE/RH | 100/0 95/5 90/10 85/15 | - Alkali (5 wt% NaOH) | 7.8 9.0 9.8 10.2 | 50 64 77 82 | 148 68 52 50 | N/A | [33] |
| Azam et al. (2020) | rHDPE/RH | 50/50 50/50 50/50 50/50 | - Alkali (0.5M NaOH) Acid (3:1 (v/v) ratio of sulphuric and nitric acids) UV/O3 | 5.8 10.83 6.0 7.0 | 418 858 485 530 | N/A | N/A | [34] |
| Nanni et al. (2021) | PBS/GS | 90/10 90/10 90/10 | - Acetylation (1:10 (v/v) ratio of pyridine and acetic anhydride) Silane (1 wt% of MPTMS) | 25.4 ± 1 26.8 ± 1 26.3 ± 1 | 722 ± 2 732 ± 6 724 ± 5 | 168 ± 109 274 ± 32 153 ± 98 | N/A | [35] |
| Zaman et al. (2021) | PP/BBF | 100/0 90/10 80/20 70/30 60/40 50/50 | - Alkali (5% solution NaOH) | 28.9 32 34 36 38 37 | 575.7 590 800 920 1150 1050 | N/A | N/A | [36] |
| Zaman et al. (2021) | PP/BBF | 100/0 90/10 80/20 70/30 60/40 50/50 | - Acetylation (toluene, acetic anhydride, 60% perchloric acid) | 28.9 33 35 39 43 41 | 575.7 675 825 1015 1475 1235 | N/A | N/A | [36] |
| Yang et al. (2023) | PLA/WFs | 75/25 75/25 75/25 75/25 | 2wt% KH550 4wt% KH550 6wt% KH550 8wt% KH550 | 26.5 23.5 28 27.5 | 765 780 790 795 | 5.7 4.6 4.8 5.0 | N/A | [37] |
| Yang et al. (2023) | PLA/WFs | 75/25 75/25 75/25 75/25 | 2wt% KH560 4wt% KH560 6wt% KH560 8wt% KH560 | 26.0 29.0 26.5 25.0 | 835 825 830 820 | 4.7 4.9 4.8 5.1 | N/A | [37] |
| Yang et al. (2023) | PLA/WFs | 75/25 75/25 75/25 75/25 | 2wt% KH570 4wt% KH570 6wt% KH570 8wt% KH570 | 26.5 27.0 26.5 25.4 | 820 820 805 795 | 5.1 5.3 5.1 5.2 | N/A | [37] |
| Perumal et al. (2023) | PBAT/CS | 100/0 60/40 60/40 | - - Acetylation (acetic anhydride and 50% sodium hydroxide) | 28 8.4 7.28 | 22 95 101.01 | 2500 975 107.5 | N/A | [9] |
| Perumal et al. (2023) | PBAT/CS/MAH | 60/40/2 | Acetylation (acetic anhydride and 50% sodium hydroxide) | 15.47 | 95.30 | 170.81 | N/A | [9] |
| Yang et al. (2024) | PVC/Wheat straw | 50/50 50/50 50/50 | - Alkali (3% NaOH) Alkali (6% NaOH) | 26.8 28 27 | N/A | N/A | N/A | [38] |
|  | PBAT/RH | 100/0 70/30 70/30 70/30 70/30 | - - Acetylation (acetic anhydride and 2% sulfuric acid) Alkali (4 wt% NaOH) Silane (2 wt% of 3-aminopropyltriethoxysilane) | 23.29 ± 1.15 10.59 ± 0.76 15.08 ± 0.33 13.49 ± 0.92 18.83 ± 0.23 | 29.80 ± 3.00 84.68 ± 1.37 157.79±7.42 114.93±3.83 188.24±3.11 | 983.05 ± 111.67 61.04 ± 10.67 86.41 ± 8.66 34.62 ± 1.78 40.12 ± 0.04 | 1.7 96.4 95.2 94.6 95.2 | This work |
|  | PBAT/RH/MAH | 69/29/2 69/29/2 69/29/2 | Acetylation (acetic anhydride and 2% sulfuric acid) Alkali (4 wt% NaOH) Silane (2 wt% of 3-aminopropyltriethoxysilane) | 20.65 ± 1.35 14.97 ± 0.19 22.49 ± 0.85 | 165.06±6.15 97.16±5.85 187.60±1.93 | 88.41±7.69 34.89±2.65 41.83±4.52 | 93.1 92.6 92.1 | This work |

Abbreviation:  PLA, polylactic acid; rHDPE, recycled high-density polyethylene; NBRr, recycled acrylonitrile butadiene rubber; RHP, rice husk powder; PP, polypropylene; PP-g-MA, polypropylene-grafted maleic anhydride; CG, coffee grounds; PHB, polyhydroxybutyrate; WHF, water hyacinth fibers; LDPE,  low-density polyethylene; PBS, polybutylene succinate; GS, grape stalks; BBF, banana bunch fiber; WFs, waste corrugated paper fibers; CS, corn starch; PVC, polyvinyl chloride; NaOH, sodium hydroxide; MPTMS, 3-trimethoxysilylpropyl 2-methylprop-2-enoate; KH550, 3-aminopropyltriethoxysilane; KH560, 3-glycidoxypropyltrimethoxysilane; KH570, 3-trimethoxysilylpropyl methacrylate.