Supporting Information

Low-threshold distributed feedback laser based on holographic polymer dispersed liquid crystals through the oriented organic semiconductor films

Lijuan Liu,1,4, Minzhe Liu,2 Qidong Wang,3 Hanmin Hu,1 Feng Zhang1 and Xiaobo Kong 1 *

1 College of Electrical and Information Engineering, Quzhou University, Quzhou 324000, China

2 Laser Institute, Qilu University of Technology (Shandong Academy of Sciences), Qingdao 266000, China

3 State Key Laboratory of Applied Optics, Changchun Institute of Optics, Fine Mechanics and Physics, Chinese Academy of Sciences, Changchun 130033, China

4School of Physics and Physical Engineering, Shandong Provincial Key Laboratory of Laser Polarization and Information Technology, Qufu Normal University, Qufu 273165, China

Experimental Section

1.1 Materials

The HPDLC pre-polymer syrup was formed by mixing the following components: bifunctionality monomer phthalic diglycol diacrylate (PDDA, Sigma-Aldrich, 60 wt%), nematic LC TEB30A (= 1.692, Slichem, 28 wt%), chain extender N-vinylpyrrolidone (NVP, Sigma-Aldrich, 10 wt%), co-initiator N-phenylglycine (NPG, Sigma-Aldrich, 1.5 wt%), and photo-initiator Rose Bengal (RB, Sigma-Aldrich, 0.5 wt%). The syrup was subsequently injected into the cell through capillary action and positioned within the holographic optical field to generate the HPDLCs.

1.2 Light loss and diffraction efficiency measurements

To calculate the light loss, during the fabrication process, a circularly polarized He-Ne laser (laser-1) was directed onto the sample at normal direction after a polarizer (polarizer-1). Through rotating the polarizer-1, the light loss (L’) at s or p polarization state is derived by L'=(It-Id)It. Here is the intensity of He-Ne laser-1 passing through the sample before grating being fabricated and  is the intensity of He-Ne laser-1 detected by detector-1 in real time.

The diffraction efficiency of each sample was measured by another He-Ne laser. The laser beam from He-Ne laser-2 was incident onto the sample at the exact Bragg angle and the first order diffracted beam was measured by the detector-2. The diffraction efficiency is defined as the diffracted light intensity in the first order divided by the incident light intensity. By rotating the polarizer-2, we can get diffraction efficiency at s polarization state () or p polarization state ().

Fig. S1 Optical setup for light loss and diffraction efficiency measurements of the HPDLC grating layer.