Supplementary information

Novel precise separation technology will significantly improve the circulation of critical materials in automotive Lithium-ion batteries

Yi Dou1, Aya Heiho2, Chiharu Tokoro3, Yasunori Kikuchi1,4,5

1 Institute for Future Initiatives, The University of Tokyo, 7-3-1 Hongo Bunkyo-ku, Tokyo 113-8654, Japan

2 Faculty of Environmental Studies, Tokyo City University, 3-3-1 Ushikubo-Nishi, Tsuzuki-Ku, Yokohama, Kanagawa 224-8551 ,Japan

3 Department of Resources and Environmental Engineering, Faculty of Science and Engineering, Waseda University, 3-4-1 Okubo Shinjuku-ku, Tokyo 169-8555, Japan

4 Presidential Endowed Chair for “Platinum Society”, Organization for Interdisciplinary Research Project, The University of Tokyo, 7-3-1 Hongo, Bunkyo-ku, Tokyo 113-8656, Japan

5 Department of Chemical System Engineering, The University of Tokyo, 7-3-1 Hongo, Bunkyo-ku, Tokyo 113-8654, Japan

Contents

Acronyms and abbreviations	3

Supplementary Fig. S1 Positioning of a precise separation technology in recycling spent automotive LIBs.	4

Supplementary Fig. S2 Image of a pilot equipment using high-voltage pulsed discharge.	5

Supplementary Fig. S3 Projection of population and the number of people per household in Japan (2020-2050).	6

Supplementary Fig. S4 The ownership of various vehicles in Japan (1970-2020)(AIRIA, 2021).	7

Supplementary Fig. S5 The ownership of passenger vehicles in Japan (1970-2020) and its projection (2020-2050).	8

Supplementary Fig. S6 The past records and future prediction on the sharing of each type of passenger vehicles in Japanese new passenger cars sales market.	9

Supplementary Fig. S7 The past records and future projection of passenger car market and the share of EVs in Japan.	10

Supplementary Fig. S8 Market sharing of different Li-ion batteries in annual new battery sales in the future.	11

Supplementary Fig. S9 Actual survival rate of passenger cars in Japan (2019) and its fitted curve by Weibull distribution.	12

Supplementary Fig. S10 Actual passenger car ownership (1993-2019) and the comparison to the calculation result backwards from 2019.	13

Supplementary Fig. S11 The past records (1993-2020) and future prediction (2021-2050) on the number of registration cancellations and new car sales in Japan.	14

Supplementary Fig. S12 Capacity of the LIBs in use in the EVs and spent LIBs in secondary usage as stationary energy storage.	15

Supplementary Fig. S13 Sensitivity analysis: the annual stocks and flows of critical metals relating to automotive LIBs in Japan.	16

Supplementary Fig. S14 Sensitivity analysis: life cycle GHG emissions in cases.	17

Supplementary Fig. S15 Sensitivity analysis: life cycle RCP in cases.	18

Supplementary Table S1 Statistical data collected from national statistics and reports of Japan	19

Supplementary Table S2 Parameters setting regarding the future socio-economic changes of Japan	20

Supplementary Table S3 Target setting regarding the sales market share of each type of passenger vehicles according to the Carbon Neutral Target declared in Japan (METIJ, 2020)	21

Supplementary Table S4 Survival rate of passenger vehicles (vehicle fleets in the year 2019)	22

Supplementary Table S5 Calculation of sales-weighted average capacity of BEVs and PHEVs.	23

Supplementary Table S6 Lifetime parameters setting for LIBs.	24

Supplementary Table S7 Parameters setting: sales-weighted average battery wight and critical metals included (unit: kg).	25

Supplementary Table S8 The changes of GHG emission factors and resource consumption potential by years according to the decarbonization target in electricity supply.	26

Supplementary Table S9 Sensitivity analysis: life cycle GHG emissions in cases.	27

Supplementary Table S10 Sensitivity analysis: life cycle RCP in cases.	28

Reference:	29

Acronyms and abbreviations

| EV | Electric vehicle |
| --- | --- |
| HEV | Hybrid electric vehicle |
| BEV | Battery electric vehicle |
| PHEV | Plug-in hybrid electric vehicle |
| ICEV | Internal-combustion engine vehicle |
| FCV | Fuel cell vehicle |
| LIB | Lithium-ion battery |
| LFP | Lithium iron phosphate |
| NCA | Lithium Nickel Cobalt Aluminum Oxide |
| NCM | Lithium Nickel Manganese Cobalt Oxide |
| LMO | Lithium manganese oxide |
| Li-S | Lithium-sulfur battery |
| Li-Air | Lithium-air battery |
| MFA | Material flow analysis |
| LCA | Life-cycle assessment |
| GHG | Greenhouse Gas |
| RCP | Resource consumption potential |
| PE | Positive electrode |
| PEAM | Positive electrode active materials |

Supplementary Fig. S1 Positioning of a precise separation technology in recycling spent automotive LIBs.

A precise separation technique is firstly developed to pretreat the dismantled battery cells for the following metals recovery by hydrometallurgy, but it has potential to directly recycle the PEAMs if the separation is “precise enough” to extract and remain the properties of recovered PEAMs.

a                                    b

Supplementary Fig. S2 Diagram of the experimental circuit for a wire explosion caused by a high-voltage pulsed discharge in case of separating PEAMs from the cathode (a), and a picture of the pilot equipment (b).

The similar application to spent solar panels can refer to Lim et al., 20211.

Supplementary Fig. S3 Projection of population and the number of people per household in Japan (2020-2050).

The population of Japan was predicted to keep decreasing from 2020 2, while the number of people per household appeared the same tendency of a long-term decrement 3.

Supplementary Fig. S4 The ownership of various vehicles in Japan (1970-2020)4.

Our study took the passenger cars into consideration, where shared-ride cars (e.g., buses), cargo vehicles, and the others were excluded. Cargo vehicles possess a part of the whole car ownership, but may adopt hydrogen fuels because of the longer transport distance supported by hydrogen fuels.

Supplementary Fig. S5 The ownership of passenger vehicles in Japan (1970-2020) and its projection (2020-2050).

Based on the ownership of passenger vehicles in the past years 4, our study predicted the future ownership of passenger vehicles using the formula supported by 5. Additionally, we improved the formula by adding the effect of car-sharing to the car ownership 6. Here, ECOMO 7 reported that the car-sharing service will decrease the rate of car ownership by 62% among car-sharing members.

Supplementary Fig. S6 The past records and future prediction on the sharing of each type of passenger vehicles in Japanese new passenger cars sales market.

According to the ambitious targets carried out by the Japanese government and automobile associations, the sales of ICEs will be stopped in domestic by the early of 2030s while the transport sector should be decarbonized by 20508. Thus, we assumed that the ICEs will gradually quit the new sales market by 2035 and the HEVs will gradually quit the new sales market by 2050.

Supplementary Fig. S7 The past records and future projection of passenger car market and the share of EVs in Japan.

The past records are referred to 9, and future projection is the simulation result of this study.

Supplementary Fig. S8 Market sharing of different Li-ion batteries in annual new battery sales in the future.

Xu, et al. 10 set three scenarios to simulate the model changes of LIBs in the future, including (1) LFP remains the major in a long term due to its advantage in cost and technical maturity; (2) NCM gradually becomes the major in the market share because of its relatively low cost and high energy density; (3) Li-S, Li-Air are penetrated and fast diffused in the future due to the lower resource dependence. The scenario (2) has the highest probability to become the truth, thus we adopted the same scenario in our simulation.

Supplementary Fig. S9 Actual survival rate of passenger cars in Japan (2019) and its fitted curve by Weibull distribution.

According to the survey on survival rate of passenger cars in Japan in 201911, we fitted a curve by Weibull distribution to predict the number of abandoned passenger cars in the future.

Supplementary Fig. S10 Actual passenger car ownership (1993-2019) and the comparison to the calculation result backwards from 2019.

Because of the data lack on the cars’ years in service, we firstly used the calibrated Weibull distribution to calculate backwards from 2019, but found it underestimated than the actual data. Thus, we adjusted the underestimated number to the actual data in proportion before the following material flow analysis.

Supplementary Fig. S11 The past records (1993-2020) and future prediction (2021-2050) on the number of registration cancellations and new car sales in Japan.

Generally, the number of abandoned passenger cars (cancelled the registration, including the second-hand cars exported to the overseas) increased from 1993 to 2020, but will decrease gradually while the new car sales are becoming less in the future (estimated in this study).

| a | b |
| --- | --- |

Supplementary Fig. S12 Capacity of the LIBs in use in the EVs and spent LIBs in secondary usage as stationary energy storage.

a: assumed that the capacity of the spent LIBs in secondary usage as stationary energy storage will not over 25% of it of the LIBs in use in the EVs, referred to 12. b: assumed that the capacity of the spent LIBs in secondary usage as stationary energy storage will not have limit.

Supplementary Fig. S13 Sensitivity analysis: the annual stocks and flows of critical metals relating to automotive LIBs in Japan.

a, b, c: critical metals in use, d, e, f: critical metals recycled and input in LIB manufacture, g, h, i: critical metals newly input in LIB manufacture. Upper figures belong to the case of immediately recycling with unlimited stationary energy storage market to accept the spent LIBs, medium figures belong to the case of recycling after secondary use with unlimited stationary energy storage market to accept the spent LIBs, lower figures belong to the case of immediately recycling with no stationary energy storage market to accept the spent LIBs.

| - Immediately recycling | - Recycling after secondary use |
| --- | --- |

Supplementary Fig. S14 Sensitivity analysis: life cycle GHG emissions in cases.

Collection ratio of spent LIBs =100% ±10%, capacity of spent LIBs in secondary use <= 25% capacity of automotive LIBs in use in EVs.

| - Immediately recycling | - Recycling after secondary use |
| --- | --- |
| Supplementary Fig. S9 Sensitivity analysis on resource consumption potential of all cases (collection ratio of spent LIBs =100% ±10%) |  |

Supplementary Fig. S15 Sensitivity analysis: life cycle RCP in cases.

Collection ratio of spent LIBs =100% ±10%, capacity of spent LIBs in secondary use <= 25% capacity of automotive LIBs in use in EVs.

Supplementary Table S1 Statistical data collected from national statistics and reports of Japan

| Statistics | Period | Reference | Status |
| --- | --- | --- | --- |
| Ownership of passenger vehicles | 1966-2020 | Automobile Inspection & Registration Information Association 4 | Statistic value |
| Population; Number of households | 1970-2020 | National census of Japan 13 | Statistic value |
| Average household income | 2005‐2018 | Comprehensive Survey of Living Conditions 14 | Statistic value |
| Average purchase price of passenger vehicles | 2005-2019 | Current Survey of Production 15 | Statistic value |
| Number of car-sharing members | 2002‐2020 | Survey by Foundation for Promoting Personal Mobility and Ecological Transportation 6 | Statistic value |
| Fleet composition of passenger vehicles | 2019.3 | Automobile Inspection & Registration Information Association 9 | Statistic value |
| Prospects of number of households | 2021-2040 | “Future prospection of number of households in Japan” by National Institute of Population and Social Security Research 3 | Estimated value |
| Prospects of population | 2021-2065 | “Future prospection of population in Japan” by National Institute of Population and Social Security Research 2 | Estimated value |

Supplementary Table S2 Parameters setting regarding the future socio-economic changes of Japan

| Socio-economic prospection | Period | Value | Reference | Status |
| --- | --- | --- | --- | --- |
| Ownership reduce due to car sharing | Constant | 62% | “Report on the environmental load reduction due to car-sharing” by Foundation for Promoting Personal Mobility and Ecological Transportation 7 | Referential value |
| Annual increase rate of car-sharing members | Constant | 0.19% | Average increase rate during period 2014-2019 6 | Referential value |
| Average purchase price of passenger vehicles | 2021-50 | - | Assume to follow the changes of CPI 16 | Referential value |
| Annual increase of employees' income | 2021-30 | 1.6% | “Initiative of Future Society 2050” by Mitsubishi Research Institute 16 | Referential value |
|  | 2031-40 | 1% |  |  |
|  | 2041-50 | 0.9% |  |  |
| Consumer Price Index | 2021-30 | 1.6% |  | Referential value |
|  | 2031-40 | 1.7% |  |  |
|  | 2041-50 | 1.9% |  |  |

Supplementary Table S3 Target setting regarding the sales market share of each type of passenger vehicles according to the Carbon Neutral Target declared in Japan 17

| Vehicle type | Year | Value | Reference | Status |
| --- | --- | --- | --- | --- |
| ICEV | 2035 | 0% | Green Growth Strategy by the cabinet office of Japan | Target value |
|  | 2050 | 0% | Must for achieving Carbon Neutral Declaration by 2050 | Target value |
| HEV | 2035 | 0% | Must for achieving Carbon Neutral Declaration by 2050 | Assumption |
|  | 2050 | 0% | Must for achieving Carbon Neutral Declaration by 2050 | Assumption |
| PHEV | 2030 | 3% | Next-generation vehicle strategy by Ministry of Economy, Trade and Industry of Japan (2010) | Target value |
|  | 2050 | 0% | Possible target for achieving Carbon Neutral Declaration by 2050 | Assumption |
| BEV | 2030 | 22% | Next-generation vehicle strategy by Ministry of Economy, Trade and Industry of Japan (2010) | Target value |
|  | 2050 | 90% | Possible target for achieving Carbon Neutral Declaration by 2050 | Assumption |
| FCV | 2030 | 3% | Next-generation vehicle strategy by Ministry of Economy, Trade and Industry of Japan (2010) | Target value |
|  | 2050 | 10% | Possible target for achieving Carbon Neutral Declaration by 2050 | Assumption |
| Others | 2030 | 0% | Possible target for achieving Carbon Neutral Declaration by 2050 | Assumption |
|  | 2050 | 0% | Possible target for achieving Carbon Neutral Declaration by 2050 | Assumption |

Supplementary Table S4 Survival rate of passenger vehicles (vehicle fleets in the year 2019)

| Years in service | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Survival ratio (%) | 98.75 | 98.23 | 96.58 | 92.93 | 91.57 | 89.16 | 88.40 | 83.59 | 80.77 | 77.55 |
| Years in service | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 |
| Survival ratio (%) | 70.31 | 61.90 | 57.54 | 47.54 | 41.10 | 30.78 | 24.74 | 17.05 | 14.55 | 11.04 |
| Years in service | 21 | 22 | 23 | 24 | 25 | 26 | 27 | 28 | 29 |  |
| Survival ratio (%) | 9.05 | 7.17 | 6.19 | 5.22 | 4.56 | 4.28 | 3.61 | 3.66 | 2.93 |  |

Supplementary Table S5 Calculation of sales-weighted average capacity of BEVs and PHEVs.

| BEVs | Sales maeket share | Required battery capacity (kWh) | Sales-weighted average capacity (kWh) | PHEVs | Sales maeket share | Required battery capacity (kWh) | Sales-weighted average capacity (kWh) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Small BEV | 19% | 33 | 72 | Small PHEV | 23% | 17 | 11 |
| Mid-size BEV | 48% | 66 |  | Mid-size PHEV | 45% | 8 |  |
| Large BEV | 34% | 100 |  | Large PHEV | 32% | 12 |  |

Parameters of various type of EVs are referred from Xu, et al. 10. The authors calculate the average capacity per vehicle in the simulation.

Supplementary Table S6 Lifetime parameters setting for LIBs.

| Li-ion battery lifetime | Years |
| --- | --- |
| Primary use in EVs | 8 |
| Secondary use in stationary energy storage | 10 |

Parameters are set referred to Xu, et al. 10, Zeng, et al. 18.

Supplementary Table S7 Parameters setting: sales-weighted average battery wight and critical metals included (unit: kg).

|  | LFP | NCA | NCM111 | NCM523 | NCM622 | NCM622-Graphite (Si) | NCM811-Graphite (Si) | NCM955-Graphite (Si) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Pack level |  |  |  |  |  |  |  |  |
| BEV average | 558.90 | 405.74 | 450.24 | 442.30 | 415.87 | 387.32 | 374.37 | 356.81 |
| PHEV average | 138.42 | 92.36 | 101.04 | 99.45 | 93.55 | 88.88 | 86.75 | 83.95 |
| BEV average |  |  |  |  |  |  |  |  |
| Li | 7.14 | 7.38 | 10.16 | 9.86 | 8.56 | 8.69 | 8.08 | 7.24 |
| Ni | 0.00 | 47.72 | 24.99 | 36.35 | 37.74 | 38.52 | 47.72 | 47.99 |
| Co | 0.00 | 8.98 | 25.09 | 14.60 | 12.63 | 12.89 | 5.99 | 2.82 |
| Mn | 0.00 | 0.00 | 23.39 | 20.41 | 11.77 | 12.02 | 5.58 | 2.50 |
| Al | 116.74 | 91.23 | 96.07 | 94.96 | 92.04 | 87.97 | 86.42 | 84.38 |
| Cu | 63.47 | 55.03 | 56.08 | 55.45 | 54.48 | 54.96 | 54.28 | 53.65 |
| Steel | 4.20 | 2.73 | 2.98 | 2.95 | 2.80 | 2.51 | 2.43 | 2.32 |
| Graphite | 85.08 | 76.58 | 78.57 | 77.59 | 75.83 | 51.16 | 50.26 | 49.19 |
| Electrolyte | 98.44 | 46.75 | 52.04 | 51.08 | 48.01 | 42.23 | 40.73 | 38.71 |
| Separator | 6.45 | 5.79 | 5.83 | 5.77 | 5.69 | 5.83 | 5.76 | 5.71 |
| Si | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 5.06 | 4.97 | 4.86 |
| PHEVs average |  |  |  |  |  |  |  |  |
| Li | 1.15 | 1.18 | 1.62 | 1.57 | 1.36 | 1.38 | 1.29 | 1.16 |
| Ni | 0.00 | 7.58 | 3.97 | 5.77 | 5.99 | 6.11 | 7.57 | 7.62 |
| Co | 0.00 | 1.43 | 3.98 | 2.32 | 2.01 | 2.05 | 0.95 | 0.45 |
| Mn | 0.00 | 0.00 | 3.71 | 3.24 | 1.87 | 1.91 | 0.89 | 0.40 |
| Al | 29.88 | 18.15 | 19.97 | 19.72 | 18.20 | 16.69 | 16.45 | 16.19 |
| Cu | 35.73 | 24.31 | 24.85 | 24.56 | 23.95 | 24.70 | 24.54 | 24.41 |
| Steel | 1.07 | 0.64 | 0.70 | 0.69 | 0.66 | 0.61 | 0.59 | 0.57 |
| Graphite | 13.44 | 12.17 | 12.48 | 12.33 | 12.05 | 8.13 | 7.98 | 7.81 |
| Electrolyte | 18.17 | 8.22 | 9.15 | 8.97 | 8.40 | 7.55 | 7.31 | 7.00 |
| Separator | 2.90 | 1.49 | 1.57 | 1.54 | 1.46 | 1.53 | 1.52 | 1.52 |
| Si | 0.00 | 0.00 | 0.00 | 0.00 | 0.00 | 0.80 | 0.79 | 0.77 |

Parameters are set based on Xu, et al. 10. The authors calculate the average value due to the market share of small, medium, and large EVs and their individual components’ weight.

Supplementary Table S8 The changes of GHG emission factors and resource consumption potential by years according to the decarbonization target in electricity supply.

| Scenario | Year | 2025 | 2030 | 2035 | 2040 | 2045 | 2050 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Reference value |  |  |  |  |  |  |  |
| All | GHG emissions factor (electricity) | 0.366 | 0.250 | 0.188 | 0.125 | 0.063 | 0.000 |
| LIB manufacture |  |  |  |  |  |  |  |
| All | GHG unit (kg-CO2 eq/kg-PE sheet) | 16.09 | 11.00 | 8.25 | 5.50 | 2.75 | 0.00 |
| All | RCP unit (kg-Sb eq/kg-PE sheet) | 0.149 | 0.149 | 0.149 | 0.149 | 0.149 | 0.149 |
| LIB remanufacture |  |  |  |  |  |  |  |
| a-1, b-2 | GHG unit (kg-CO2 eq/kg-PE sheet) | 16.09 | 11.00 | 8.25 | 5.50 | 2.75 | 0.00 |
| a-2, b-2 |  | 7.48 | 5.12 | 3.84 | 2.56 | 1.28 | 0.00 |
| a-3, b-3 |  | 7.74 | 5.29 | 3.97 | 2.65 | 1.32 | 0.00 |
| a-4, b-4 |  | 3.61 | 2.47 | 1.85 | 1.23 | 0.62 | 0.00 |
| a-1, b-1 | RCP unit (kg-Sb eq/kg-PE sheet) | 0.149 | 0.149 | 0.149 | 0.149 | 0.149 | 0.149 |
| a-2, b-2 |  | 0.078 | 0.078 | 0.078 | 0.078 | 0.078 | 0.078 |
| a-3, b-3 |  | 0.063 | 0.063 | 0.063 | 0.063 | 0.063 | 0.063 |
| a-4, b-4 |  | 0.008 | 0.008 | 0.008 | 0.008 | 0.008 | 0.008 |
| LIB recycling |  |  |  |  |  |  |  |
| a-1, b-2 | GHG unit (kg-CO2 eq/kg-PE sheet) | 13.84 | 11.58 | 10.35 | 9.13 | 7.91 | 6.68 |
| a-2, b-2 |  | 6.28 | 4.30 | 3.22 | 2.15 | 1.07 | 0.00 |
| a-3, b-3 |  | 2.41 | 1.65 | 1.23 | 0.82 | 0.41 | 0.00 |
| a-4, b-4 |  | 0.60 | 0.41 | 0.31 | 0.20 | 0.10 | 0.00 |
| a-1, b-1 | RCP unit (kg-Sb eq/kg-PE sheet) | 4.5.E-05 | 4.5.E-05 | 4.5.E-05 | 4.5.E-05 | 4.5.E-05 | 4.5.E-05 |
| a-2, b-2 |  | 8.6.E-03 | 8.6.E-03 | 8.6.E-03 | 8.6.E-03 | 8.6.E-03 | 8.6.E-03 |
| a-3, b-3 |  | 7.9.E-03 | 7.9.E-03 | 7.9.E-03 | 7.9.E-03 | 7.9.E-03 | 7.9.E-03 |
| a-4, b-4 |  | 2.7.E-05 | 2.7.E-05 | 2.7.E-05 | 2.7.E-05 | 2.7.E-05 | 2.7.E-05 |

Supplementary Table S9 Sensitivity analysis: life cycle GHG emissions in cases.

| Scenario | Secondary use | Collection ratio | 2025 | 2030 | 2035 | 2040 | 2045 | 2050 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| a-1 | No | 90% | 1860.47 | 3317.15 | 5372.72 | 6589.37 | 6526.48 | 4852.88 |
| a-1 | No | 100% | 1873.93 | 3394.97 | 5546.37 | 6856.38 | 6859.87 | 5220.76 |
| a-1 | No | 110% | 1887.40 | 3472.78 | 5720.01 | 7123.39 | 7193.26 | 5588.65 |
| a-2 | No | 90% | 1718.96 | 2513.22 | 3527.89 | 3432.54 | 2261.64 | 0.00 |
| a-2 | No | 100% | 1716.70 | 2501.72 | 3506.35 | 3407.50 | 2243.59 | 0.00 |
| a-2 | No | 110% | 1714.45 | 2490.21 | 3484.81 | 3382.47 | 2225.55 | 0.00 |
| a-3 | No | 90% | 1687.26 | 2367.82 | 3242.13 | 3052.66 | 1954.22 | 0.00 |
| a-3 | No | 100% | 1681.48 | 2340.15 | 3190.35 | 2992.48 | 1910.84 | 0.00 |
| a-3 | No | 110% | 1675.70 | 2312.48 | 3138.58 | 2932.31 | 1867.46 | 0.00 |
| a-4 | No | 90% | 1635.25 | 2125.34 | 2765.62 | 2419.21 | 1441.59 | 0.00 |
| a-4 | No | 100% | 1623.69 | 2070.74 | 2663.43 | 2300.43 | 1355.97 | 0.00 |
| a-4 | No | 110% | 1612.14 | 2016.13 | 2561.24 | 2181.66 | 1270.36 | 0.00 |
| b-1 | Yes | 90% | 1739.29 | 2167.23 | 2857.17 | 3143.39 | 2829.76 | 1759.47 |
| b-1 | Yes | 100% | 1739.29 | 2167.23 | 2867.25 | 3204.77 | 2962.39 | 1954.97 |
| b-1 | Yes | 110% | 1739.29 | 2167.23 | 2877.32 | 3266.14 | 3095.02 | 2150.47 |
| b-2 | Yes | 90% | 1739.29 | 2167.23 | 2755.27 | 2539.20 | 1571.45 | 0.00 |
| b-2 | Yes | 100% | 1739.29 | 2167.23 | 2754.02 | 2533.45 | 1564.27 | 0.00 |
| b-2 | Yes | 110% | 1739.29 | 2167.23 | 2752.77 | 2527.69 | 1557.09 | 0.00 |
| b-3 | Yes | 90% | 1739.29 | 2167.23 | 2739.48 | 2466.50 | 1480.74 | 0.00 |
| b-3 | Yes | 100% | 1739.29 | 2167.23 | 2736.48 | 2452.66 | 1463.49 | 0.00 |
| b-3 | Yes | 110% | 1739.29 | 2167.23 | 2733.47 | 2438.83 | 1446.23 | 0.00 |
| b-4 | Yes | 90% | 1739.29 | 2167.23 | 2713.16 | 2345.26 | 1329.50 | 0.00 |
| b-4 | Yes | 100% | 1739.29 | 2167.23 | 2707.23 | 2317.96 | 1295.44 | 0.00 |
| b-4 | Yes | 110% | 1739.29 | 2167.23 | 2701.30 | 2290.65 | 1261.37 | 0.00 |

Collection ratio of spent LIBs =100% ±10%, capacity of spent LIBs in secondary use <= 25% capacity of automotive LIBs in use in EVs.

Supplementary Table S10 Sensitivity analysis: life cycle RCP in cases.

| Scenario | Secondary use | Collection ratio | 2025 | 2030 | 2035 | 2040 | 2045 | 2050 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| a-1 | No | 90% | 16.13 | 35.49 | 67.48 | 100.45 | 134.59 | 165.26 |
| a-1 | No | 100% | 16.13 | 35.49 | 67.48 | 100.46 | 134.59 | 165.26 |
| a-1 | No | 110% | 16.13 | 35.49 | 67.48 | 100.46 | 134.59 | 165.27 |
| a-2 | No | 90% | 15.58 | 31.70 | 57.54 | 80.64 | 102.52 | 119.76 |
| a-2 | No | 100% | 15.52 | 31.28 | 56.49 | 78.81 | 99.88 | 116.32 |
| a-2 | No | 110% | 15.46 | 30.86 | 55.44 | 76.98 | 97.24 | 112.87 |
| a-3 | No | 90% | 15.44 | 30.72 | 54.98 | 75.54 | 94.26 | 108.04 |
| a-3 | No | 100% | 15.36 | 30.19 | 53.66 | 73.23 | 90.93 | 103.70 |
| a-3 | No | 110% | 15.28 | 29.66 | 52.34 | 70.93 | 87.61 | 99.37 |
| a-4 | No | 90% | 14.89 | 26.92 | 45.03 | 55.69 | 62.14 | 62.47 |
| a-4 | No | 100% | 14.75 | 25.97 | 42.66 | 51.55 | 56.17 | 54.68 |
| a-4 | No | 110% | 14.61 | 25.02 | 40.28 | 47.41 | 50.21 | 46.89 |
| b-1 | Yes | 90% | 16.13 | 29.39 | 50.02 | 70.28 | 88.76 | 103.02 |
| b-1 | Yes | 100% | 16.13 | 29.39 | 50.02 | 70.28 | 88.76 | 103.02 |
| b-1 | Yes | 110% | 16.13 | 29.39 | 50.02 | 70.28 | 88.76 | 103.02 |
| b-2 | Yes | 90% | 16.13 | 29.39 | 49.48 | 66.49 | 79.30 | 86.52 |
| b-2 | Yes | 100% | 16.13 | 29.39 | 49.41 | 66.07 | 78.25 | 84.69 |
| b-2 | Yes | 110% | 16.13 | 29.39 | 49.35 | 65.64 | 77.19 | 82.86 |
| b-3 | Yes | 90% | 16.13 | 29.39 | 49.33 | 65.51 | 76.86 | 82.27 |
| b-3 | Yes | 100% | 16.13 | 29.39 | 49.26 | 64.98 | 75.54 | 79.97 |
| b-3 | Yes | 110% | 16.13 | 29.39 | 49.18 | 64.45 | 74.21 | 77.66 |
| b-4 | Yes | 90% | 16.13 | 29.39 | 48.78 | 61.71 | 67.38 | 65.75 |
| b-4 | Yes | 100% | 16.13 | 29.39 | 48.65 | 60.76 | 65.01 | 61.61 |
| b-4 | Yes | 110% | 16.13 | 29.39 | 48.51 | 59.81 | 62.63 | 57.47 |

Collection ratio of spent LIBs =100% ±10%, capacity of spent LIBs in secondary use <= 25% capacity of automotive LIBs in use in EVs.

Reference:

1	Lim, S. et al. Recovery of Silver From Waste Crystalline Silicon Photovoltaic Cells by Wire Explosion. Ieee T Plasma Sci 49, 2857-2865 (2021). https://doi.org:10.1109/TPS.2021.3106307

2	IPSS. Population Projections for Japan (2021-2070). (National Institute of Population and Social Security Research (IPSS), Tokyo, 2023).

3	IPSS. Household Projection for Japan : 2015-2050. (National Institute of Population and Social Security Research, Tokyo, 2018).

4	AIRIA. The ownership of automobiles in Japan (1966-2020). (Automobile Inspection & Registration Information Association (AIRIA), Tokyo, 2021).

5	Nakamura, K., Kato, H. & Hayashi, Y. Forecast of Motorization Progress Considering Railway Improvement Timing In Asian Developing Mega-Cities. Journal of Japan Society of Civil Engineers, Ser. D3 (Infrastructure Planning and Management) 68, I_823-I_830 (2012). https://doi.org:10.2208/jscejipm.68.I_823

6	ECOMO. Number of car-sharing members in Japan (2002-2020). (Foundation for Promoting Personal Mobility and Ecological Transportation (ECOMO), Tokyo, 2021).

7	ECOMO. Verification of the eco effects brought about from car-sharing. (Foundation for Promoting Personal Mobility and Ecological Transportation (ECOMO), Tokyo, 2013).

8	METI. Green Growth Strategy Through Achieving Carbon Neutrality in 2050. (The Ministry of Economy, Trade and Industry (METI), Tokyo, 2021).

9	AIRIA. Fleet composition of the passenger vehicles in Japan. (Automobile Inspection & Registration Information Association, Tokyo, 2019).

10	Xu, C. J. et al. Future material demand for automotive lithium-based batteries. Commun Mater 1 (2020). https://doi.org:10.1038/s43246-020-00095-x

11	AIRIA. Survey on vehicles average age by the end of fiscal year 2018. (Automobile Inspection & Registration Information Association (AIRIA), Tokyo, 2019).

12	IRENA. Global Renewables Outlook: Energy transformation 2050. (The International Renewable Energy Agency (IRENA), Abu Dhabi, 2020).

13	SBJ. 2020 Population Census. (Statistics Bureau of Japan (SBJ), Tokyo, 2021).

14	MHLWJ. Comprehensive Survey of Living Conditions (2005-2018). (Ministry of Health, Labour and Welfare of Japan (MHLWJ), Tokyo, 2019).

15	METI. Current Survey of Production 2005-2019. (Ministry of Economy, Trade and Industry of Japan (METI), Tokyo, 2020).

16	MRI. Social and Economic Impacts of Carbon Neutrality in 2050. (Mitsubishi Research Institute (MRI), Tokyo, 2022).

17	METIJ. Japan’s Roadmap to “Beyond-Zero” Carbon. (Ministry of Economy, Trade and Industry (METI) of Japan, Tokyo, 2020).

18	Zeng, A. et al. Battery technology and recycling alone will not save the electric mobility transition from future cobalt shortages. Nature Communications 13, 1341 (2022). https://doi.org:10.1038/s41467-022-29022-z