Supplementary Information for

High-density asymmetric iron dual-atom sites for efficient and ultra-stable electrochemical water oxidation

Zhang etal.

Methods

Chemicals. Melamine (> 99%, Aladdin), 2-benzimidazolethiol (> 99%, Aladdin), trimesic acid (> 98%, Aladdin), iron (III) chloride (> 99%, Sigma-Aldrich), dicyandiamide (> 99%, Sigma-Aldrich), potassium hydroxide (95%, Aladdin), commercial Pt/C (20 wt% metal, Aladdin ltd), ruthenium (IV) oxide (99.9 %, Aladdin), nafion117 solution (~5% in a mixture of lower aliphatic alcohols and water, Aladdin), carbon cloth (CC, type: WOS1009, thickness: 0.33 mm), ethanol (> 99.5 %, Aladdin). All chemical reagents were utilized as received. The distilled water with a resistivity of 18.2 MΩ cm−1 was used in all experiments.

Preparation of SNC and NC. In a typical synthesis of S, N co-doped carbon nanosheets, the mixture of melamine and 2-benzimidazolethiol with certain mass ratios (7:1) were firstly ground into a homogenous precursor and then subjected to thermal polymerization and carbonization in the flowing N2 atmosphere, which was performed in a horizontally tubular quartz tube with the heating rate of 2 oC min-1 to 1000 oC maintaining for 2 h. The final synthesized sample products were designed as SNC. The NC support was obtained from the same process as SNC, except that the S source (2-benzimidazolethiol) was not added.

Preparation of Fe2N6/NC, and Fe1N4/NC. To prepare the Fe2N6/NC, the obtained NC nanosheet support was ultrasound dispersion in 10 mL of ethanol, then 40 mg iron (III) chloride, 1.0 g dicyandiamide, and 0.1 g trimesic acid were added into the above suspension and stirred vigorously for 30 minutes. The suspension was then evaporated to dry the solvent in a rotary evaporator to obtain a grey powder. The grey powder was annealed at different temperatures 900 1000 oC with a heating rate of 2 oC min-1 and maintained for 2 h under the N2 atmosphere. After naturally cooling to room temperature, the black Fe2-NC nanosheets were obtained. To obtain Fe1N4/NC, directly add 40 mg of iron (III) chloride, 1.0 g dicyandiamide and 0.1 g trimesic acid to 15 mL of ethanol and vigorously stir for 30 minutes. The suspension was then evaporated to dry the solvent in a rotary evaporator to obtain a grey powder. The grey powder was annealed at 900 oC with a heating rate of 2 oC min-1 and maintained for 2 h under the N2 atmosphere. After naturally cooling to room temperature, the black Fe1N4/NC was obtained.

Characterizations. X-ray diffraction (XRD, D8 Bruker AXS, scan range of 10-80°) test was performed to identify the crystallinity and phase of samples. Raman (Lab RAM HR Evolution spectrometer, excitation line of 532 nm) was analyzed to record the stretching and bond vibration modes. X-ray photoelectron spectroscopy (XPS, Escalab 250Xi, Mg Kα line excitation source) was carried out to explore the elemental compositions. Scanning electron microscopy (SEM, Ultra 55Zeiss) information was acquired to observe the morphology. Transmission electron microscopy (TEM, FEI Talos F200S, acceleration voltage 200 kV) results were performed to confirm structure and morphology. HAADF-STEM was obtained from aberration-corrected TEM (Hitachi HF5000) and JEOL Triple-C TEM. The N2 adsorption and desorption isotherm (collected from Quantachrone Autosorb iQ-MP-C) was obtained to derive the surface areas and the pore size distribution of the catalysts. ICP-OES (Thermo Fisher Scientific, IRIS Intrepid II XSP spectrometer) was used to determine the contents of Fe species in the samples.

Ex-situ XAFS measurements. The X-ray absorption fine structure spectra data were collected at BL14W1 station in Shanghai Synchrotron Radiation Facility (SSRF, operated at 3.5 GeV with a maximum current of 250 mA), respectively. The data were collected at room temperature (Fe K-edge in fluorescence excitation mode using a Lytle detector). All samples were pelletized as disks of 13 mm diameter with 1mm thickness using graphite powder as a binder.

In-situ synchrotron radiation XAFS measurements. A catalyst-modified carbon paper was used as the working electrode, graphite rod as the counter electrode and Ag/AgCl (KCl-saturated) electrode as the reference electrode. A home-made electrochemical cell was used for in-situ XAFS measurements. The experiments were performed at the BL14W1 station in SSRF.

Electrochemical measurements for ORR. The Oxygen reduction reaction measurements were performed in a three-electrode cell using an electrochemical workstation (CHI 760E) setup with a rotating disk electrode (RRDE-3A). A glassy carbon (GC: 4 mm inner diameter), platinum wire, and saturated calomel electrode (SCE) were used as the working, counter, and reference electrodes, respectively. The catalyst suspension was prepared by dispersing 2 mg catalyst into 250 μL ethanol/Nafion (5 wt%) mixed solution, followed by ultrasonication for 30 min to form a homogenous ink. Afterward, 10 μL ink was dropped onto the freshly polished GC electrode and naturally dried in air for all the catalysts. Before the ORR test, the electrolyte was purged with O2 to form the O2 saturated 0.1 M KOH solution. Cyclic voltammograms (CVs) were recorded at 50 mV s-1 in O2 saturated 0.1 M KOH. Linear sweep voltammetry (LSV) polarization curves for ORR were obtained at a rotating rate of 1,600 rpm, without iR compensation at 5 mV s-1. Durability tests were performed by cycling between 0.6-1.0 V versus RHE for 30,000 cycles at room temperature.

Zinc-air battery measurements. The A-Fe2S1N5/SNC ink was uniformly dispersed onto teflon-coated carbon fiber paper with the loading of 1.0 mg cm-2, then dried at 60 °C. For comparison, Pt/C electrode with the same catalyst loading was also prepared. The polished commercial Zn foil with a thickness of 0.2 mm was used as anode. Both electrodes were constructed into a home-made Zn–air device in 6 M KOH and 0.2 M zinc acetate electrolyte saturated with O2.

Supplementary Fig. 1. TEM images of SNC at (a) 500 nm and (b) 50 nm scale bar showing the two-dimensional folded sheet-like structure. (c-f) Corresponding EDS mapping images of SNC. Highly wrinkled SNC nanosheets with numerous tortuous edges can be observed in the transmission electron microscope (TEM) image, which provides a considerable number of active sites for trapping and anchoring metal atoms.

Supplementary Fig. 2. Controllable expansion preparation of SNC nanosheets. (a) Before and (b) after pyrolysis.

Supplementary Fig. 3. AFM image and corresponding height profile of A-Fe2S1N5/SNC.

Supplementary Fig. 4. High magnification SEM image of A-Fe2S1N5/SNC.

Supplementary Fig. 5. (a-f) EELS mapping of Fe, S, N, and C for A-Fe2S1N5/SNC.

Supplementary Fig. 6. HAADF-STEM images of A-Fe2S1N5/SNC.

Supplementary Fig. 7. TEM images of Fe2N6/NC at (a) 100 nm and (b) 20 nm scale bar showing the two-dimensional wrinkle sheet-like structure. (c-f) Corresponding EDS mapping images of Fe2N6/NC showing the Fe, N, and C elements are uniformly distributed throughout the entire Fe2N6/NC.

Supplementary Fig. 8. TEM images of Fe1N4/NC at (a) 200 nm and (b) 20 nm scale bar showing the two-dimensional sheet-like structure. (c, d) Corresponding EDS mapping images of Fe1N4/NC.

Supplementary Fig. 9. The diagram for the percentages of single metal atom catalysts and dual-metal atom catalysts. According to the statistical data, the proportion of diatoms Fe reaches ~81.7 %, and the proportion of single atoms Fe is ~18.3%.

Supplementary Fig. 10. (a) Aberration-corrected HAADF-STEM of the Fe2N6/NC. (b) corresponding intensity profile in Region A of (a). The diatomic Fe pair circled with the red dashed line. (c) Distance between two adjacent Fe atoms in Region A and Region B.

Supplementary Fig. 11. XRD patterns of A-Fe2S1N5/SNC, Fe1N4/NC, Fe2N6/NC, and SNC. The broad peaks at 20-30°and 40-50°are assigned to the (002) and (101) plane of graphite, respectively.

Supplementary Fig. 12. Raman patterns of A-Fe2S1N5/SNC, Fe1N4/NC, Fe2N6/NC, and SNC. The results showed that ID/IG was slightly elevated for the A-Fe2S1N5/SNC compared with the Fe1N4/NC and Fe2N6/NC, indicating a much higher percentage of carbon atoms at the defects/edges of the A-Fe2S1N5/SNC thin sheet, which were regarded as potential active sites for catalysis.

Supplementary Fig. 13. Characterization of Fe oxidation state from XANES. (a-b) The Fe K-edge XANES spectra of the references (Fe foil, Fe3O4, FePc, FeS2, Fe1N4/NC, and Fe2N6/NC).

Supplementary Fig. 14. (a) First-derivative XANES curves of Fe foil, Fe3O4, and A-Fe2S1N5/SNC. (b) Correlation between the Fe oxidation state and the energy position of the XANES spectrum, determined as the first maximum of the first derivative spectrum of A-Fe2S1N5/SNC and different Fe reference compounds.

Supplementary Fig. 15. FT-EXAFS fitting curves of A-Fe2S1N5/SNC, Fe2N6/NC, and Fe1N4/NC.

Supplementary Fig. 16. WT-EXAFS plots of (a) Fe foil, (b) FePc, (c) Fe2O3, (d) FeS2, (e) A-Fe2S1N5/SNC, (f) Fe2N6/NC, and (g) Fe1N4/NC.

Supplementary Fig. 17. EXAFS fitting curves of Fe foil (a) the FT-EXAFS fitting curve of Fe foil at Fe K-edge, (b) k space fitting curve and (c) q space fitting curve.

Supplementary Fig. 18. EXAFS fitting of A-Fe2S1N5/SNC. (a) the EXAFS fitting curve of A-Fe2S1N5/SNC at Fe K-edge. We carried out EXAFS curve-fitting for the first coordination shell of Fe by considering two backscattering paths, including Fe-N and Fe-S. (b) q space fitting curve at Fe K-edge of A-Fe2S1N5/SNC. The best-fit structural parameters are listed in Supplementary Table 2.

Supplementary Fig. 19. Atomic coordination environment of Fe1N4/NC. (a) FT k3-weighted EXAFS spectra of Fe1N4/NC and the reference samples. (b) FT-EXAFS fitting curves of Fe1N4/NC and the corresponding Fe K-edge EXAFS fitting curves. (c) q space fitting curve at Fe K-edge. (d) Atomic interface structure model of Fe1N4/NC. The best-fit structural parameters are listed in Supplementary Table 2. The gray, blue, and orange spheres represent the C, N, and Fe elements, respectively.

Supplementary Fig. 20. Atomic coordination environment of Fe2N6/NC. (a) FT k3-weighted EXAFS spectra of Fe2N6/NC and the reference samples. (b) FT-EXAFS fitting curves of Fe2N6/NC and the corresponding Fe K-edge EXAFS fitting curves. (c) q space fitting curve at Fe K-edge. (d) Atomic interface structure model of Fe2N6/NC. The best-fit structural parameters are listed in Supplementary Table 2. The gray, blue, and orange spheres represent the C, N, and Fe elements, respectively.

Supplementary Fig. 21. Comparison between the experimental Fe K-edge XANES spectrum of A-Fe2S1N5/SNC and the theoretical spectra calculated with the depicted structures based different Fe-S or C-S positions.

Supplementary Fig. 22. (a) The Fe 2p, (b) N 1s, (c) C 1s, and (d) S 2p XPS spectrum of A-Fe2S1N5/SNC. It was obvious from the Fe 2p spectra that the two peaks at the binding energies of 709.3 eV and 722.3 eV were generally attributed to the Fe (II) species in A-Fe2S1N5/SNC, and the other two peaks at 712.4 eV and 724.4 eV were the characteristic peaks of Fe (III). The Fe3+/Fe2+ ratio was 1.51 for A-Fe2S1N5/SNC. The coexistence of Fe (Ⅱ) and Fe (Ⅲ) species, suggested partial charge transfer from SNC to Fe3+ centers.

Supplementary Fig. 23. XPS spectrum of Fe2N6/NC (a) survey spectrum, (b) The Fe 2p, (c) N 1s, and (d) C 1s.

Supplementary Fig. 24. XPS spectrum of Fe1N4/NC (a) survey spectrum, (b) The Fe 2p, (c) N 1s, and (d) C 1s.

Supplementary Fig. 25. XPS spectrum of SNC (a) C 1s, (b) N 1s, and (c) S 2p.

Supplementary Fig. 26. (a) Fe L-edge XANES spectra. (b) C K-edge and (c) N K-edge XANES spectra of the A-Fe2S1N5/SNC, Fe2N6/NC, and Fe1N4/NC. (d) S L-edge XANES spectra of the A-Fe2S1N5/SNC. The S L-edge features result from the electronic transitions of 2p electrons to partially filled or empty molecular orbitals.

Supplementary Fig. 27. Tafel slope of A-Fe2S1N5/SNC, Fe2N6/NC, Fe1N4/NC, and RuO2.

Supplementary Fig. 28. (a) Comparison of overpotential and Tafel slope values at a current density of 10 mA cm−2. (b) Comparison of overpotential and Tafel slope values with other catalysts Supplementary Table 2 at a current density of 10 mA cm−2.

Supplementary Fig. 29. CV plots at various sweep rates of (a) A-Fe2S1N5/SNC, (b) Fe2N6/NC, (c) Fe1N4/NC, and (d) SNC for OER.

Supplementary Fig. 30. Calculated Cdl values of of A-Fe2S1N5/SNC, Fe2N6/NC, Fe1N4/NC, and SNC.

Supplementary Fig. 31. (a) ECSA normalized LSV curves. (b) EIS curves of A-Fe2S1N5/SNC, Fe2N6/NC, Fe1N4/NC, and SNC at an overpotential of 10 mV.

Supplementary Fig. 32. (a) TOFs of the measured catalysts calculated on the basis of the loaded Fe atoms at different overpotentials. (b) Mass activity of the measured catalysts calculated on the basis of the loaded Fe atoms at different overpotentials.

Supplementary Fig. 33. The detail of the in-situ X-ray absorption spectroscopy measurement. The device is set up at 14W1 beam line with the support from SSRF, where the X-ray induced fluorescence model is applied. CE, counter electrode; WE, working electrode; RE, reference electrode.

Supplementary Fig. 34. (a) Corresponding first-derivative XANES curves at the Fe K-edge for OER. (b) Oxidation state of A-Fe2S1N5/SNC at Fe K-edge for OER derived from (a).

Supplementary Fig. 35. EXAFS fitting curves of A-Fe2S1N5/SNC-in situ at 1.31 V. (a) The FT-EXAFS fitting curve at Fe K-edge, (b) k space fitting curve and (c) q space fitting curve.

Supplementary Fig. 36. EXAFS fitting curves of A-Fe2S1N5/SNC-in situ at 1.42 V. (a) The FT-EXAFS fitting curve at Fe K-edge, (b) k space fitting curve and (c) q space fitting curve.

Supplementary Fig. 37. LSV curves before and after 50000 CV stability test.

Supplementary Fig. 38. Summary of the long-term durability in water electrolysis for A-Fe2S1N5/SNC and other reported electrocatalysts (Supplementary Table 2).

Supplementary Fig. 39. A-Fe2S1N5/SNC after the 50000 cycles CV tests. (a-c) TEM, (d) Aberration-corrected HAADF-STEM, (e-h) EDS mapping images of Fe, S, N, and C.

Supplementary Fig. 40. Structural characterization of A-Fe2S1N5/SNC after the OER 50000 cycles CV test. (a) XRD pattern. (b) Raman pattern. XPS spectra for (c) Fe 2p, (d) N 1s, (e) C 1s, and (f) S 2p.

Supplementary Fig. 41. (a) XRD and (b) XPS survey spectrum of A-Co2S1N5/SNC, A-Cu2S1N5/SNC, A-Ni2S1N5/SNC, and A-Mn2S1N5/SNC.

Supplementary Fig. 42. Morphology characterizations of A-Co2S1N5/SNC. (a, b) TEM. (c) HAADF-STEM. (d, f) Aberration-corrected HAADF-STEM. (e) EDS mapping images of Co, S, N, and C. (g) statistical Co-Co distance in the observed diatomic pairs in region B of figure f.

Supplementary Fig. 43. Morphology characterizations of A-Cu2S1N5/SNC. (a, b) TEM. (c) HAADF-STEM. (d, f) Aberration-corrected HAADF-STEM. (e) EDS mapping images of Cu, S, N, and C. (g) statistical Cu-Cu distance in the observed diatomic pairs in region B of figure f.

Supplementary Fig. 44. Morphology characterizations of A-Ni2S1N5/SNC. (a, b) TEM. (c) HAADF-STEM. (d, f) Aberration-corrected HAADF-STEM. (e) EDS mapping images of Ni, S, N, and C. (g) statistical Ni-Ni distance in the observed diatomic pairs in region B of figure f.

Supplementary Fig. 45. Morphology characterizations of A-Mn2S1N5/SNC. (a, b) TEM. (c) HAADF-STEM. (d, f) Aberration-corrected HAADF-STEM. (e) EDS mapping images of Mn, S, N, and C. (g) statistical Mn-Mn distance in the observed diatomic pairs in region B of figure f.

Supplementary Fig. 46. (a) XANES spectra at the Co k-edge of A-Co2S1N5/SNC, Co3O4, and Co foil. (b) Fourier transform (FT) at the Co k-edge of A-Co2S1N5/SNC, Co3O4, and Co foil.

Supplementary Fig. 47. (a) XANES spectra at the Cu k-edge of A-Cu2S1N5/SNC, CuO, and Cu foil. (b) Fourier transform (FT) at the Cu k-edge of A-Cu2S1N5/SNC, CuO, and Cu foil.

Supplementary Fig. 48. (a) XANES spectra at the Ni k-edge of A-Ni2S1N5/SNC, NiO, and Ni foil. (b) Fourier transform (FT) at the Ni k-edge of A-Ni2S1N5/SNC, NiO, and Ni foil.

Supplementary Fig. 49. (a) XANES spectra at the Mn k-edge of A-Mn2S1N5/SNC, MnO2, and Mn foil. (b) Fourier transform (FT) at the Mn k-edge of A-Mn2S1N5/SNC, MnO2, and Mn foil.

Supplementary Fig. 50. The FT-EXAFS fitting curve of A-Co2S1N5/SNC, A-Cu2S1N5/SNC, A-Ni2S1N5/SNC, and A-Mn2S1N5/SNC.

Supplementary Fig. 51. The k space fitting curve of A-Co2S1N5/SNC, A-Cu2S1N5/SNC, A-Ni2S1N5/SNC, and A-Mn2S1N5/SNC.

Supplementary Fig. 52. The q space fitting curve of A-Co2S1N5/SNC, A-Cu2S1N5/SNC, A-Ni2S1N5/SNC, and A-Mn2S1N5/SNC.

Supplementary Fig. 53. OER performance of A-Co2S1N5/SNC, A-Cu2S1N5/SNC, A-Mn2S1N5/SNC, and A-Ni2S1N5/SNC. (a) LSV curves, (b) Tafel slope.

Supplementary Fig. 54. The optimized configuration of (a) Fe2N6/NC and (b) A-Fe 2S1N5/SNC structures. Purple, blue, and gray ball marks Fe, N, and C atom, respectively. Two Fe sites was named as Fe-1 and Fe-2.

Supplementary Fig. 55. Optimized configurations with different H, OH, and O coverages on the A-Fe2S1N5/SNC system. Purple, red, gray, blue, and white ball marks Fe, O, C, N, and H atom, respectively.

Supplementary Fig. 56. Optimized configurations with different H, OH, and O coverages on the Fe2N6/NC system. Purple, red, gray, blue, and white ball marks Fe, O, C, N, and H atom, respectively.

Supplementary Fig. 57. Free energy of a series of coverage fraction surfaces sampled for the Fe2N6/NC catalysts.

Supplementary Fig. 58. The optimized models of (a) OH, (b) O, and (c) OOH intermediates on the Fe-1 site of 1.5 O-Fe2S1N5/SNC system. Purple, red, gray, blue, and white ball marks Fe, O, C, N, and H atom, respectively.

Supplementary Fig. 59. The optimized models of (a) OH, (b) O, and (c) OOH intermediates on the Fe-2 site of 1.5 O-Fe2S1N5/SNC system, Purple, red, gray, blue, and white ball marks Fe, O, C, N, and H atom, respectively.

Supplementary Fig. 60. The optimized models of (a) OH, (b) O, and (c) OOH intermediates on the Fe-1 site of 1.5 O-Fe2N6/NC system, Purple, red, gray, blue, and white ball marks Fe, O, C, N, and H atom, respectively.

Supplementary Fig. 61. The optimized models of (a) OH, (b) O, and (c) OOH intermediates on the Fe-2 site of 1.5 O-Fe2N6/NC system, Purple, red, gray, blue, and white ball marks Fe, O, C, N, and H atom, respectively.

Supplementary Fig. 62. Free energy change of ORR mechanism on the Fe-2 site of (a) 1.5 O-Fe2S1N5/SNC (a) and (b) 1.5 O-Fe2N6/NC catalyst under the electrode potential of 0 V, 1.23 V, and limiting-determined potential.

Supplementary Fig. 63. The free energy change of (a) OER and (b) ORR on the Fe-1 site of 1.5 O-Fe2S1N5/SNC model under the electrode potential of 0 V, 1.23 V, and the limiting-determined potential.

Supplementary Fig. 64. The free energy change of (a) OER and (b) ORR on the Fe-1 site of 1.5 O-Fe2N6/NC model under the electrode potential of 0 V, 1.23 V, and the limiting-determined potential.

Supplementary Fig. 65. Differential charge density diagram of (a) bare-Fe2N6/NC and (b) A-Fe2S1N5/SNC. The yellow and cyan contour with the isosurface value of 0.008 e/bohr3 marks augmented and reduced charge density, respectively. Purple, gray, blue, and white ball marks Fe, C, N, and H atom, respectively. The red number indicates the charge transfer number of Fe atoms.

Supplementary Fig. 66. Differential charge density diagram of (a) 1.5 O-Fe2N6/NC and (b) 1.5 O-Fe2S1N5/SNC. The yellow and cyan contour with the isosurface value of 0.008 e/bohr3 marks augmented and reduced charge density, respectively. Purple, red, gray, blue, and white ball marks Fe, O, C, N, and H atom, respectively. The red number indicates the charge transfer number of Fe atoms.

Supplementary Fig. 67. CV test at different atmosphere. (a) CV curves of A-Fe2S1N5/SNC in O2- and N2-saturated 0.1 M KOH electrolyte at a scan rate of 50 mV/s.

Supplementary Fig. 68. ORR electrochemical activity in 0.1 M KOH. (a) Linear sweep voltammetry curves (LSV) and (b) the corresponding Tafel plots of the different catalysts at 1600 rpm. (c) Kinetic current density (Jk) at 0.85 V versus reversible hydrogen electrode (versus RHE) and half-wave potentials of A-Fe2S1N5/SNC, Fe2N6/NC, Fe1N4/NC, SNC, and Pt/C catalysts. (d) Calculated Cdl values from corresponding samples. As shown in Supplementary Fig. 68a, A-Fe2S1N5/SNC displayed superior ORR activity as evidenced by a high onset potential (Eonset) of 0.98 V, close to that of Pt/C (0.99 V). However, Fe2N6/NC, Fe1N4/NC, and SNC exhibited lower electrocatalytic performance with Eonset values of 0.83, 0.89, and 0.79 V, respectively. Linear sweep voltammetry (LSV) curves of these catalysts indicated the best activity of A-Fe2S1N5/SNC with aspect to its highest halfwave potential (E1/2). Specifically, E1/2 of A-Fe2S1N5/SNC, Fe2N6/NC, Fe1N4/NC, SNC, and Pt/C was 0.91, 0.82, 0.79, 0.70, and 0.85 V vs. RHE, respectively. The lowest Tafel slope of A-Fe2S1N5/SNC (87 mV dec-1) among those of Fe2N6/NC (91 mV dec-1), Fe1N4/NC (109 mV dec-1), SNC (110 mV dec-1), and Pt/C (101 mV dec-1) also supported the superior ORR kinetics of A-Fe2S1N5/SNC (Supplementary Fig. 68b). Moreover, A-Fe2S1N5/SNC exhibited a remarkable kinetic current density (Jk) of 12.6 mA cm-2 at 0.85 V vs. RHE, about 4 times and 7 times higher than that of Fe2N6/NC (3.5 mA cm-2) and Fe1N4/NC (1.8 mA cm-2), respectively (Supplementary Fig. 68c).

Supplementary Fig. 69. CV plots at various sweep rates of (a) A-Fe2S1N5/SNC, (b) Fe2N6/NC, (c) Fe1N4/NC, and (d) SNC for ORR.

Supplementary Fig. 70. (a) LSV curves of A-Fe2S1N5/SNC at various rotation rates. (b) The K-L plots for A-Fe2S1N5/SNC. (c) Electron transfer number (n, bottom) and H2O2 yield (top) versus potential for A-Fe2S1N5/SNC. (d) Stability test of A-Fe2S1N5/SNC. To further analyze the ORR reaction mechanism of the A-Fe2S1N5/SNC catalyst, Koutecky-Levich plots at various applied potentials (Supplementary Fig. 70a) were collected to determine the electron transfer number (n) based on the LSV curves at various rotating speeds ranging from 400 rpm to 2025 rpm. Linear plots comply with the first-order reaction kinetic of the dissolved oxygen concentration and the n. According to the Koutecky-Levich equation, the n was calculated to be ≈ 4, signifying a high 4e– selectivity for ORR (Supplementary Fig. 70b). Durability was another important evaluation indicator of the electrocatalyst. In addition, the catalyst could still maintain high electrochemical durability after 40000 s of continuous operation under a constant voltage (Supplementary Fig. 70d).

Supplementary Fig. 71. Cyclic voltammetry (CV) data for A-Fe2S1N5/SNC in O2-saturated 0.1 M KOH without and with 0.5 M CH3OH. There was no obvious change in the current density for the A-Fe2S1N5/SNC catalyst after methanol injecting.

Supplementary Fig. 72. Rechargeable Zn-air battery performance. A-Fe2S1N5/SNC -based battery shows a maximum peak power density of 182.1 mW cm−2, significantly higher than that of Pt/C+RuO2 (103.6 mW cm−2) based batteries. Importantly, the A-Fe2S1N5/SNC-based battery delivered exceptional performance and outperformed most reported results. In Supplementary Fig. 72d, the specific capacity of A-Fe2S1N5/SNC-based battery at discharge currents of 10 mA cm−2 was determined to be 815.7 mA h g−1, and the corresponding Zn utilization ratios were calculated to be 95.7%. The cyclability of ZAB was evaluated under continuous galvanostatic discharge/charge at a current density of 10 mA cm−2 with a duration of 30 min per cycle (Supplementary Fig. 72e). Compared with Pt/C+RuO2-based battery, A-Fe2S1N5/SNC demonstrated negligible voltage decay within 300 h (600 discharge/charge cycles), revealing superior long-term durability. More importantly, the zinc–air battery assembled with A-Fe2S1N5/SNC exhibited superior performance than other benchmarking counterparts in terms of peak power density, specific capacity, and cycling stability. The highly exposed active sites and unique electronic structure in SACs obtained by different synthesis methods contribute to the excellent bifunctional ORR and OER performance in rechargeable zinc–air batteries. Taken together, these results strongly support the superiority of A-Fe2S1N5/SNC as a potential material in the zinc-air battery.

XAFS measurements

The X-ray absorption fine structure spectra data were collected at BL1W1B station in Beijing Synchrotron Radiation Facility (BSRF) respectively. The data of the samples were collected at room temperature (Fe K-edge in fluorescence excitation mode using a Lytle detector). All samples were pelletized as disks of 13 mm diameter with 1mm thickness using PVDF powder as a binder.

The EXAFS spectra were obtained by subtracting the post-edge background from the overall absorption and then normalizing with respect to the edge-jump step. Subsequently, the χ(k) data of were Fourier transformed to real (R) space using a hanning windows (dk = 1.0 Å-1) to separate the EXAFS contributions from different coordination shells. To obtain the quantitative structural parameters around central atoms, least-squares curve parameter fitting was performed using the ARTEMIS module of IFEFFIT software packages.

The following EXAFS equation was used:

S02 is the amplitude reduction factor, Fj(k) is the effective curved-wave backscattering amplitude, Nj is the number of neighbors in the jth atomic shell, Rj is the distance between the X-ray absorbing central atom and the atoms in the jth atomic shell (backscatterer), λ is the mean free path in Å, ϕ j(k) is the phase shift (including the phase shift for each shell and the total central atom phase shift), σj is the Debye-Waller parameter of the jth atomic shell (variation of distances around the average Rj). The functions Fj(k), λ and ϕ j(k) were calculated with the ab initio code FEFF8.2. The additional details for EXAFS simulations are given below.

The coordination numbers of model samples were fixed as the nominal values. The obtained S02 was fixed in the subsequent fitting. While the internal atomic distances R, Debye-Waller factor σ2, and the edge-energy shift ΔE0 were allowed to run freely.

Supplementary Table 1 Structural parameters extracted from the Fe K-edge EXAFS fitting. (S02=0.87)

| sample | Scattering pair | CN | R(Å) | σ2(10-3Å2) | ΔE0(eV) | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Fe foil | Fe-Fe1 | 8 | 2.47 | 6.5 | 1.5 | 0.008 |
|  | Fe-Fe2 | 6 | 2.84 | 7.3 |  |  |
| Fe1N4/NC | Fe-N | 4.0 | 1.95 | 6.7 | 1.0 | 0.005 |
| Fe2N6/NC | Fe-N | 3.1 | 1.92 | 5.4 | 2.0 | 0.008 |
|  | Fe-Fe | 1.0 | 2.52 | 5.9 |  |  |
| A-Fe2S1N5/SNC | Fe-N | 2.5 | 1.90 | 4.1 | 2.0 | 0.006 |
|  | Fe-S | 0.5 | 2.30 | 4.6 |  |  |
|  | Fe-Fe | 1.0 | 2.56 | 6.9 |  |  |

S02 is the amplitude reduction factor; CN is the coordination number; R is interatomic distance (the bond length between central atoms and surrounding coordination atoms); σ2 is Debye-Waller factor (a measure of thermal and static disorder in absorber-scatterer distances); ΔE0 is edge-energy shift (the difference between the zero kinetic energy value of the sample and that of the theoretical model). R factor is used to value the goodness of the fitting.

Supplementary Table 2 Comparison of OER performance with other catalysts.

| Catalyst | Tafel slope (mV dec-1) | η10 (mV) | Durability (h) | reference |
| --- | --- | --- | --- | --- |
| A-Fe2S1N5/SNC | 61 | 193a | >2000 50000 CV | This work |
| Ni-NHGF | 63 | 331a | 20 | [1] Nature Catalysis 2018, 63-72 |
| WCx-FeNi | 44 | 237a | 1000 | [2] Nature Materials 2021, 20, 1240-1247 |
| Ir1/Ni LDH-T | 41 | 228a | 12 | [3] Nat. Commun. 2024, 152:559 |
| Ni/Fe-CNG | 74 | 270b | 72 | [4] Nat. Commun. 2021, 12, 5589 |
| NiFe-DASC | 45 | 310a | 30 | [5] Nat. Commun. 2021, 12:4088 |
| EA-FCCN (FeCoCrNi MCA) | 38.7 | 221a | 20 | [6] Nat. Commun. 2020, 11:4066 |
| Ru/CoFe-LDHs | 39 | 198a | 24 | [7] Nat. Commun. 2019, 10:1711 |
| S¦NiNx-PC | 45 | 280a | 10 | [8] Nat. Commun. 2019, 10:1392 |
| Ni3Fe1-xVx/CFP | 39 | 264a | 60 | [9] Nat. Commun. 2018, 9:2885 |
| Au-NiFeOOH | 36 | 237a | 20 | [10] J. Am. Chem. Soc. 2018, 140, 3876-3879 |
| Fe-Co-Ni MOF | 53.1 | 254a | 48 | [11] J. Am. Chem. Soc. 2022, 144, 3411-3428 |
| Co-Fe-N-C | 37 | 309a | 16 | [12] J. Am. Chem. Soc. 2019, 141, 14190–14199 |
| FeNiP/NCH | 69 | 250a | 72 | [13] J. Am. Chem. Soc. 2019, 141, 7906-7916 |
| P/Fe-N-C | 65 | 304b | 10 | [14] J. Am. Chem. Soc. 2023, 145, 3647-3655 |
| Co-SeMON | 57.4 | 265a | 50 | [15] J. Am. Chem. Soc. 2023, 145, 2, 1144-1154 |
| Co2Fe1@NC | 141.6 | 420b | 6 | [16] J. Am. Chem. Soc. 2020, 142, 7116-7127 |
| Fe2/Co1-GNCL | 70 | 350a | 200 | [17] Angew. Chem. Int. Ed. 2023, 62, e202314303 |
| Mg/Fe-N-C | 52 | 224b | 15 | [18] Angew. Chem. Int. Ed. 2019, 58, 13565-13572 |
| S, N-Fe/N/C-CNT | 82 | 370b | 11 | [19] Angew. Chem. Int. Ed. 2016, 55, 1-6 |
| a-NiCo/NC | 49 | 252a | 150 | [20] Angew. Chem. Int. Ed. 2022, 61, e202207537 |
| (Ni,Fe)P(S,Se)3 | 34 | 210a | 50 | [21] Angew. Chem. Int. Ed. 2023, e202214570 |
| ZnCo2O4/CNTs | 59.2 | 350b | 14 | [22] Angew. Chem. Int. Ed. 2023, 62, e202301408 |
| Fe-UNT | 36.6 | 270a | 10 | [23] Angew. Chem. Int. Ed. 2020, 59, 2313-2317 |
| Ir1@Co/NC | 119 | 315a | 5 | [24] Angew. Chem. Int. Ed. 2019, 19, 11868-11873 |
| Fe-N4 SAs/NPC | 95 | 430a | 20 | [25] Angew. Chem. Int. Ed. 2018, 57, 8614-8618 |
| CoFe/N-GCT | 106 | 310b | 10 | [26] Angew. Chem. Int. Ed. 2018, 57, 16166-16170 |
| Ni-BDC-1 | 89 | 225a | 100 | [27] Angew. Chem. 2022, 134, e202214794 |
| Ni SAs@S/N-FCS | 56.5 | 249a | 166 | [28] Angew. Chem. Int. Ed. 2022, 61, e202212542 |
| S/N-CMF@FexCoyNi1-x-y-MOF | 53.5 | 296a | 100 | [29] Adv. Mater. 2023, 35, 2207888 |
| Fe/N-G-SAC | 73 | 370b | 2000 CV | [30] Adv. Mater. 2020, 2004900 |
| Fe SAs/NC | 55.5 | 320b | 25 | [31] Adv. Mater. 2022, 2209644 |
| HCM@Ni-N | 76 | 304a | 12 | [32] Adv. Mater. 2019, 31, 1904548 |
| CoNi-SAs/NC | 58.7 | 340a | 10 | [33] Adv. Mater. 2019, 31, 1905622 |
| Mo1-NiFeOxHy | 32.33 | 193a | 30 | [34] Adv. Mater. 2022, 34, 2202523 |
| Ni SAs@S/N-CMF | 50.8 | 285a | 60 | [35] Adv. Mater. 2022, 34, 2203442 |
| Fe-NiMo-NH3/H2 | 28 | 192a | 18 | [36] Adv. Energy Mater. 2020, 2002285 |
| Pt1@Fe-N-C | 62 | 310b | 5 | [37] Adv. Energy Mater. 2018, 8, 1701345 |
| SCoNC | 74 | 310b | 56 | [38] Adv. Energy Mater. 2019, 1900149 |
| FePc¦¦CNTs¦¦NiCo/CP | 50 | 358b | 5000 CV | [39] Adv. Energy Mater. 2022, 12, 2202984 |
| Fe0.55Co0.45BPO | 26 | 270a | 50 | [40] Adv. Energy Mater. 2023, 2203886 |
| FeNi SAs/NC | 54.68 | 270a | 35 | [41] Adv. Energy Mater. 2021, 11, 2101242 |
| S-Fe-Co-N5 | 59.2 | 260b(𝜂50) | 20 | [42] Adv. Energy Mater. 2023, 13, 2301547 |
| NiFeLDH/Fe1-N-C | 41 | 320a | 12 | [43] Adv. Energy Mater. 2023, 2203609 |
| Mn/Fe-HIB-MOF | 45 | 280b | 100 | [44] Energy Environ. Sci., 2019, 12, 727-738 |
| Co/Fe-SNC800 | 47.92 | 240a | 26 | [45] Energy Environ. Sci., 2023, 16, 1685–1696 |
| Mn/Fe-HIB-MOF | 45 | 280b | 100 | [46] Energy Environ. Sci., 2019, 12, 727-738 |
| A-Ni@DG | 47 | 270a | 10 | [47] Chem 2018, 4, 285-297 |
| planar-Fe-Co DSC | 33.6 | 190a | 160 | [48] PNAS 2024, 121, e2317247121 |
| Cu,Co/NSC3 | 85.4 | 339a | 25 | [49] Adv. Funct. Mater. 2024, 34, 2311664 |
| Fe3Co7-NC | 69 | 343b | 60 | [50] Adv. Funct. Mater. 2023, 33, 2212299 |
| SS-Co-SAC NSAs | 94.2 | 348b | 80 | [51] Adv. Funct. Mater. 2019, 29, 1906477 |
| Ni0.5Fe0.5-THQ | 47.9 | 272b | 40 | [52] Adv. Funct. Mater. 2024, 34, 2310902 |
| Co1/TaS2-3 | 70 | 330a | 121 | [53] ACS Nano 2021, 15, 7105-7113 |
| NiSO4-GF | 80 | 300a | 20 | [54] ACS Nano 2020, 14, 11662-11669 |
| S-R-NiFe-CPs | 30.8 | 245a(𝜂20) | 25 | [55] ACS Nano 2022, 16, 15318-15327 |
| Fe,Co,N-C | 76 | 410b | 20 | [56] ACS Nano 2022, 16, 5, 7890-7903 |
| FePc-GO | 112 | 420b | 17 | [57] ACS Nano 2020, 14, 13279–13293 |
| Fe-N/S-CNT-GR | 78 | 370a | 12 | [58] ACS Catal. 2022, 12, 7994-8006 |
| Fe1Co3-NC-1100 | 99.93 | 349b | 5000 CV | [59] ACS Catal. 2022, 12, 1216-1227 |
| Fe1(OH)x/P-C | 41 | 320a | 20 | [60] Nano Lett. 2021, 21, 4795-4801 |
| NiFe-DG | 76 | 358a | 12 | [61] Nano Energy 2021, 90, 106488 |
| CoFe-N-C | 68 | 360b | 25 | [62] Nano Lett. 2022, 22, 3392−3399 |
| Fe–NiNC-50 | 54 | 340b | 5000 CV | [63] Nano Energy, 2020, 71, 104597 |
| FeCo/Se-CNT | 74.2 | 340b | 9 | [64] Nano Lett. 2021, 21, 2255-2264 |
| Ni-O-G SACs | 42 | 224a | 50 | [65] Adv. Sci. 2020, 7, 1903089 |
| FeCoDACys | 67 | 320b | 12 | [66] Chem. Commun. 2022, 58, 1934 |
| Fe-N-NDC-900 | 66.3 | 350b | 12 | [67] J. Mater. Chem. A 2021, 9, 5556-5565 |
| NiFe@g-C3N4/CNT | 67 | 326a | 16 | [68] J. Mater. Chem. A 2018, 6, 6840–6846 |
| Fe-NC | 114 | 450b | 3000 CV | [69] J. Mater. Chem. A, 2020, 8, 9981-9990 |
| Ni-O-G SACs | 42 | 224a | 50 | [70] Adv. Sci. 2020, 7, 1903089 |
| H-Co@FeCo/N/C | 96 | 378b | 12 | [71] Applied Catalysis B: Environmental. 2020, 278, 119259 |

a in 1.0 M KOH electrolyte. b in 0.1 M KOH electrolyte.

Supplementary Table 3 Structural parameters extracted from the Fe K-edge EXAFS fitting. (S02=0.87)

| sample | Scattering pair | CN | R(Å) | σ2(10-3Å2) | ΔE0(eV) | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| A-Fe2S1N5/SNC-in situ-1.31V | Fe-N | 2.4 | 1.88 | 3.7 | 3.0 | 0.007 |
|  | Fe-O | 1.1 | 2.01 | 5.6 |  |  |
|  | Fe-S | 0.5 | 2.29 | 4.9 |  |  |
|  | Fe-Fe | 1.0 | 2.53 | 6.5 |  |  |
| A-Fe2S1N5/SNC-in situ-1.42V | Fe-N | 2.3 | 1.85 | 6.5 | 2.0 | 0.009 |
|  | Fe-O | 1.4 | 2.01 | 5.8 |  |  |
|  | Fe-S | 0.4 | 2.27 | 5.9 |  |  |
|  | Fe-Fe | 1.1 | 2.49 | 7.0 |  |  |

S02 is the amplitude reduction factor; CN is the coordination number; R is interatomic distance (the bond length between central atoms and surrounding coordination atoms); σ2 is Debye-Waller factor (a measure of thermal and static disorder in absorber-scatterer distances); ΔE0 is edge-energy shift (the difference between the zero kinetic energy value of the sample and that of the theoretical model). R factor is used to value the goodness of the fitting.

Supplementary Table 4 Structural parameters extracted from the Mn, Cu, Co and Ni K-edge EXAFS fitting. (S02=0.86)

| sample | Scattering pair | CN | R(Å) | σ2(10-3Å2) | ΔE0(eV) | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| A-Mn2S1N5/SNC | Mn-N | 2.3 | 1.91 | 4.1 | 4.8 | 0.008 |
|  | Mn-S | 0.6 | 2.34 | 2.5 |  |  |
| A-Cu2S1N5/SNC | Cu-N | 2.4 | 2.02 | 3.2 | 5.9 | 0.005 |
|  | Cu-S | 0.5 | 2.31 | 6.8 |  |  |
| A-Co2S1N5/SNC | Co-N | 2.6 | 1.95 | 4.6 | 2.5 | 0.008 |
|  | Co-S | 0.4 | 2.33 | 7.3 |  |  |
| A-Ni2S1N5/SNC | Ni-N | 2.5 | 1.93 | 5.3 | 3.7 | 0.007 |
|  | Ni-S | 0.6 | 2.32 | 6.4 |  |  |

Supplementary Table 5 The total energy and free energy correction of free-state molecule and adsorbed intermediates. Gcorr = ZPE + H (0 → 2981.5 K)  ̶  TS

| Species | E | ZPE | H (0→298.15 K) (eV) | TS (eV) | Gcorr (eV) |
| --- | --- | --- | --- | --- | --- |
| H2O | -14.22 | 0.56 | 0.10 | 0.67 | -0.01 |
| H2 | -6.77 | 0.26 | 0.09 | 0.40 | -0.06 |
| *OH | / | 0.37 | 0.04 | 0.07 | 0.34 |
| *O | / | 0.08 | 0.02 | 0.04 | 0.06 |
| *H | / | 0.32 | 0.32 | 0 | 0.32 |

Supplementary Table 6 The adsorption free energy of various intermediates on the A-Fe2S1N5/SNC catalysts. MM represents total magnetic moment. G=Gcorr+E

| Species | MM | E | Gcorr | G |
| --- | --- | --- | --- | --- |
| *H | 4.22 | -1.38 | 0.35 | -1.03 |
| *O | 3.44 | -0.12 | 0.01 | -0.11 |
| *OH | 5.89 | -0.93 | 0.32 | -0.61 |
| 2*O | 1.00 | 0.17 | -0.01 | 0.16 |
| 2*OH | 6.96 | -0.80 | 0.53 | -0.27 |
| 3*O | 0.99 | 1.89 | 0.03 | 1.92 |
| 3*OH | -0.08 | -0.54 | 0.95 | 0.41 |

Supplementary Table 7 The adsorption free energy of various intermediates on the Fe2N6/NC catalysts. MM represents total magnetic moment.

| Species | MM | E | Gcorr | G |
| --- | --- | --- | --- | --- |
| *H | 3.22 | -0.55 | 0.33 | -0.22 |
| *O | 4.22 | -0.11 | 0.01 | -0.10 |
| *OH | 5.22 | -0.68 | 0.30 | -0.38 |
| 2*O | 6.01 | 1.17 | 0.02 | 1.19 |
| 2*OH | 8.22 | -0.63 | 0.60 | -0.03 |
| 3*O | 6.00 | 3.05 | 0.03 | 3.08 |
| 3*OH | -1.68 | -0.45 | 0.89 | 0.44 |

Supplementary Table 8 The adsorption free energy of intermediates for OER/ORR in 1.5O-Fe2S1N5/SNC model.

| site | Species | MM | E | Gcorr | G |
| --- | --- | --- | --- | --- | --- |
| Fe-1 | *O | -0.66 | 2.44 | -0.01 | 2.43 |
|  | *OH | 0 | 0.77 | 0.29 | 1.06 |
|  | *OOH | 0 | 3.70 | 0.27 | 3.98 |
| Fe-2 | *O | 1.00 | 2.32 | -0.01 | 2.32 |
|  | *OH | 0.02 | 0.69 | 0.29 | 0.98 |
|  | *OOH | 0.01 | 3.62 | 0.27 | 3.89 |

Supplementary Table 9 The adsorption free energy of intermediates for OER/ORR in 1.5O-Fe2N6/NC model.

| site | Species | MM | E | Gcorr | G |
| --- | --- | --- | --- | --- | --- |
| Fe-1 | *O | -0.30 | 2.33 | 0.00 | 2.33 |
|  | *OH | -1 | 0.70 | 0.31 | 1.01 |
|  | *OOH | -1.08 | 3.73 | 0.27 | 4.00 |
| Fe-2 | *O | -0.31 | 2.33 | 0.00 | 2.33 |
|  | *OH | 1 | 0.70 | 0.31 | 1.01 |
|  | *OOH | -1.13 | 3.71 | 0.27 | 3.99 |