Supplementary Information for “Approaching the adiabatic infimum of topological pumps on thin-film lithium niobate waveguides”

Shengjie Wu, Wange Song*, Jiacheng Sun, Jian Li, Zhiyuan Lin, Xuanyu Liu, Shining Zhu, and Tao Li*

National Laboratory of Solid State Microstructures, Key Laboratory of Intelligent Optical Sensing and Manipulation, Jiangsu Key Laboratory of Artificial Functional Materials, College of Engineering and Applied Sciences, Nanjing University, Nanjing 210093, China

and Collaborative Innovation Center of Advanced Microstructures, Nanjing 210093, China

*Corresponding author. songwange@nju.edu.cn, taoli@nju.edu.cn

Section I – Topological nature of periodically modulated RM model

Section II – Adiabatic theorem in topological pumps

Section III – Effective Berry connection between edge mode and other states

Section IV – Loop deformation

Section V – Waveguide parameter matching

Section VI – Broadband topological pump at adiabatic infimum

Section I – Topological nature of periodically modulated RM model

The periodically modulated RM model under periodic boundary conditions (PBC) can be described with the following Hamiltonian:

(S1)

where k corresponds to the Bloch wavevector. The band spectrum with respect to θ=2πz/P and k is shown in Figure S1, and the corresponding Chern number of each band is labeled.

Fig. S1 Band spectrum of the RM model under PBC. The Chern number of the valence/conduction band is -1/+1 respectively.

Section II – Adiabatic theorem in topological pumps

We would like to go through the rigorous derivation of the adiabatic theorem for a topological pumping process. This proof has been reported1,2, and is provided here for completeness of this work. Consider a time-dependent system with Hamiltonian H(t), whose wavefunction Ψ(t) satisfies the Schrödinger equation:

(S2)

The instantaneous eigenvalues En(t) and eigenfunctions ψn(t) of H(t) satisfy:

(S3)

The eigenfunction ψn(t) forms a complete orthonormal basis

(S4)

and Ψ(t) can be expressed as a linear superposition of ψn(t)

(S5)

where cn(t) is the superposition coefficient, and

(S6)

Substituting Eq. (S5) into Eq. (S2) gives

(S7)

which can be simplified to

(S8)

We multiply ψ*m on both sides of Eq. (S8) and then obtain

(S9)

Eq. (S9) describes how the wavefunction Ψ(t) evolves in the basis of instant eigenfunctions ψn(t). The first term on the right-hand-side  gives rise to the famous Berry phase in an adiabatic process, and the second term  denotes the transition coefficient between instant eigenstates induced by time-varying modulation, which is exactly the numerator of the adiabatic criterion provided in the main text.

In our work, we input the edge state |edge1> into the lattice and expect the state to pin on the |edge1> during the whole pump process. Therefore, the transition between |edge1> and all other modes |m> (|m>≠|edge1>) need to be minimized. Based on this, we minimize the Aδt eff=max{Aδt eff(m)} for (|m>≠|edge1>) between edge state |edge1> and all other modes.

Section III – Effective Berry connection between edge mode and other states

Follow the line in Section II, we analyze the effective berry connection between the edge state |edge1> and all other states, and the results are shown in Figure S2. It is clear that δβ modulation only tends to introduce transition between two edge states (see the 4th figure in the first row in Fig. S2), while δt modulation induces complex transitions between |edge1> and other states (the second row). The transition induced by δβ modulation can be minimized very easily by bypassing the center region in the parameter space, while the transition induced by δt modulation is hard to be minimized with conventional method. Therefore, we mainly focus on the Aδt eff value in the parameter space.

Figure S3 shows the Aδβ eff=max{Aδβ eff(m)} for |m>≠|edge1> and the corresponding conventional (blue) and INFI (red) loop in the δβ-δt space. It clearly shows that both the two loops bypass the high Aδβ eff region.

Fig. S2 Component of effective Berry connection between |edge1> and all other states in parameter space.

Fig. S3 Aδβ eff=max{Aδβ eff(m)} for |m>≠|edge1>.

Section IV – Loop deformation

We define the loop ρ(θ,α) as

(S10)

where α is the deforming factor. The conventional loop corresponds to ρ(θ,0) and the INFI loop corresponds to ρ(θ,1), and varying α leads to the continuous deformation of the loop. In Figure S4, we show some examples of the loop with α=0 (blue, the convention loop), α=0.5 (purple), α=1 (red, the INFI loop) and α=1.5 (gray) in the δβ-δt space, and the green arrow indicates the direction with increasing α.

Fig. S4 Loop deformation. a, b Four loops with α=0 (blue), 0.5 (purple), 1 (red) and 1.5 (gray) with background color indicating Aδβ eff (a) and Aδt eff (b).

Section V – Waveguide parameter matching

Figure S5 shows the dependence of effective refractive index neff and coupling c of LNOI waveguide on geometric parameters. The waveguide width wA,B=w0±δw and the gap between adjacent intra/inter-cell waveguides gintra/inter=g0±δg are modulated along the z-direction according to the chosen loop. The center waveguide width w0 is chosen as 500nm, so that β0=1.85k0 (see Fig. S5 a), and g0 is set as 520nm with t0=0.02k0. The coupling with respect to the waveguide gap for waveguides with w=w0 is shown in Fig. S5 b. The inset in Fig. S5 a shows Ex component of the fundamental TE0 mode in the waveguide with w=500nm. The geometric parameters of the waveguide lattice in experiment are obtained by mapping β and c to waveguide width and gap, respectively.

Fig. S5 Mapping to waveguide parameters. a Effective refractive index neff with varying waveguide width. b Coupling strength between adjacent waveguides with w=500nm with respect to varying waveguide gap.

Section VI – Broadband topological pump at adiabatic infimum

The characterization of the broadband response of our samples with L=400μm is shown in Fig. S6. The pump process is protected by the adiabatic process, and as a result, the output signal locates on the edge over 1500nm~1650nm for INFI lattice (red line). As a contrast, output signal spreads along the lattice within this band in the conventional lattice (blue line), indicating the nonadiabatic field evolution at this waveguide length. Insets display corresponding output signals captured in experiments for the INFI lattice (red box) and conventional lattice (blue box).

Fig. S6 Broadband response. Experimental results depicting the broadband topological edge state pump for INFI lattice (red) and conventional lattice (blue) with L=400μm. Insets show CCD-captured output signals at corresponding wavelengths for INFI (red box) and conventional (blue box) samples.

References

- Born, M. & Fock, V. Beweis des Adiabatensatzes. Z Med. Phys. 51, 165 (1928).

- Schiff, L. I. Quantum Mechanics (McGraw-Hill, New York, 1981).