Repurposing disposed surgical face masks into activated carbon for efficient sorption of bio recalcitrant malathion pesticide.

Robert O. Gemboa,b, Sebusi Odisitsea, Titus AM. Msagatib, and Cecil. K. King’ondua.⁕,

a Department of Chemical and Forensic Sciences, Botswana International University of Science and Technology, Palapye, Botswana.

b Institute for Nanotechnology and Water Sustainability, College of Science, Engineering and Technology, University of South Africa, Florida 1709, Roodepoort, Johannesburg, South Africa.

* Corresponding author: Cecil K. King’ondu. Email address: kingonduc@biust.ac.bw.

Optimization

Figure 1S illustrates a desirability profile generated from 17 optimal points through numerical optimization within the software. Among the 100 solutions in the response surface variations, the best local maximum was determined at pH 5.16, an adsorbent dose of 26.56 mg, and an initial concentration of 369.24 mg/L. Table 1S shows the constraints used to achieve the optimal conditions.

Figure 1S. RAMP plots for optimization procedure.

Table 1S. Constraints.

| Parameter | Goal | Lower Limit | Upper Limit | Lower Weight | Upper Weight | Importance |
| --- | --- | --- | --- | --- | --- | --- |
| Adsorbent dosage | is in range | 20 | 40 | 1 | 1 | 3 |
| Initial concentration | is in range | 200 | 400 | 1 | 1 | 3 |
| pH | is in range | 2 | 9 | 1 | 1 | 3 |
| Adsorption capacity | maximize | 248.32 | 500.17 | 1 | 1 | 3 |