Supporting Information

Biodegradation of ethylene vinyl acetate using Klebsiella aerogenes isolated from Effective Microorganisms

Amarbayasgalan Maidarjav1, Indra Nyamjav1, Hong Rae Kim2, Dong-Eun Suh2, Sukkyoo Lee1*

1Department of Brain Sciences, Graduate School, Daegu Gyeongbuk Institute of Science and Technology (DGIST), Daegu 42988, Republic of Korea

2Department of Research and Development, Repla Inc., Suwon 16679, Republic of Korea

*Corresponding author(s). E-mail(s): slee2012@dgist.ac.kr

Table S1. Elemental changes on surfaces of controls and treated EVA samples.

| Element | Untreated control | Treated control | K. aerogenes |
| --- | --- | --- | --- |
|  | Wt (%) | Wt (%) | Wt (%) |
| C | 96.4±0.32 | 96.63±0.37 | 91.79±0.54** |
| O | 3.61±0.32 | 3.38±0.37 | 8.22±0.54** |

Mean value and standard deviation (±SD), n=2, * p < 0.05, ** p < 0.01

Table S2. Elemental changes on surfaces of controls and treated EVA samples.

| Samples | C1s peak area, % |  |  |
| --- | --- | --- | --- |
|  | C-C, C=C | C-O, C-O-C | C=O, C-O=C |  |
| Untreated control | 82.9±0.6 | 13.4±0.6 | 3.7±0.004 |  |
| Treated control | 81.6±2.6 | 12.1±0.6 | 6.3±2 |  |
| K. aerogenes | 67.1±1.5* | 15.8±2.2 | 17.2±0.7* |  |

Mean value and standard deviation (±SD), n=2, * p < 0.05

Table S3. Changes of mass decomposition temperature in EVA samples.

| Sample | Deacetylation process in the vinyl acetate fraction |  | Decomposition of the residual main chain |  | Temperature of peak degradation rate, ℃ |
| --- | --- | --- | --- | --- | --- |
|  | 1st stage |  | 2nd stage |  |  |
|  | Decomposition T, ℃ | Weight loss, % | Decomposition T, ℃ | Weight loss, % |  |
| Untreated control | 360.7 | 9.6±0.4 | 478.7 | 90.7±0.4 | 466.7 |
| Treated control | 360 | 9.4±0.2 | 478.8 | 90.8±0.4 | 466.9 |
| K. aerogenes | 360 | 11.8±0.1 | 471.8 | 87.8±0.1 | 456.5 |

Mean value and standard deviation (±SD), n=2.