Supporting Information

Photocatalytic upcycling of polylactic acid into alanine by sulfur vacancies rich cadmium sulfide

Yue Wua,b‡, Phuc T.T. Nguyena,c,‡ Tianyong Zhang b and Ning Yana,c,d*

aDepartment of Chemical and Biomolecular Engineering, National University of Singapore, 4 Engineering Drive 4, 117585, Singapore

bTianjin Key Laboratory of Applied Catalysis Science and Technology, School of Chemical Engineering and Technology, Tianjin University, Tianjin 300354, People’s Republic of China

cJoint School of National University of Singapore and Tianjin University, Fuzhou 350207, Fujian, China

dCentre for Hydrogen Innovations, National University of Singapore, Singapore 117580, Singapore.

‡Both authors contributed equally to this work.

*Corresponding author: ning.yan@nus.edu.sg

Number of pages: 11

Number of tables: 3

Number of figures: 9

Table S1. The amount and speed of dropping the S precursor in different CdS samples

| Catalyst | Na2S solution amount (mL) | Drop speed |
| --- | --- | --- |
| CdS-1 | 3 | 0.05 mL/min |
| CdS-2 | 6 | 0.10 mL/min |
| CdS-3 | 9 | 0.15 mL/min |
| CdS-4 | 12 | 0.20 mL/min |
| CdS-5 | 15 | 0.25 mL/min |
| CdS-6 | 18 | 0.30 mL/min |
| CdS-8 | 24 | 0.40 mL/min |

Table S2. BET surface area of CdS with different S vacancy

| Samples | BET Surface Area (m2 g-1) |
| --- | --- |
| CdS-6 | 113.1 |
| CdS-5 | 133.7 |
| CdS-4 | 146.0 |
| CdS-3 | 145.6 |
| CdS-2 | 144.1 |
| CdS-1 | 147.3 |

Table S3. The molar ratio of Cd to S in CdS

| Samples | ICP-OES | XPS |
| --- | --- | --- |
| CdS-6 | 0.98 | 1.01 |
| CdS-5 | 1.12 | 1.14 |
| CdS-4 | 1.20 | 1.18 |
| CdS-3 | 1.25 | 1.30 |
| CdS-2 | 1.32 | 1.39 |
| CdS-1 | 1.50 | 1.60 |

Figure S1. TEM images of CdS with different Cd:S molar ratio.

Figure S2. N2 adsorption-desorption isotherms for CdS with different Cd:S ratio.

Figure S3. High-resolution XPS spectra of a Cd 3d, b S 2p for CdS with different sulfur vacancy content.

Figure S4. 1H NMR spectra of reaction mixture. Reaction conditions: 200 mg PLA, 10 mg CdS-3, 4 mL aqueous NH3 25% solution, 16 mL deaerated water, 50 ℃, 4 h, 1 bar N2, visible light. DSS: 2,2-dimethyl-2-silapentane-5-sulfonic acid.

Figure S5. Catalytic conversion of PLA to alanine at different a time (at 50 ℃) and b temperature (for 4 h). Reaction conditions: 200 mg PLA, 10 mg CdS-3, 4 mL aqueous NH3 25% solution, 16 mL deaerated water, 1 bar N2, visible light.

Figure S6. Mechanism study for the photocatalytic amination of lactic acid to alanine. a Control experiments with different scavengers. Reaction conditions: scavengers, 10 mg CdS-3, 20 mmol lactic acid, 4 mL aqueous NH3 25% solution, 16 mL deaerated water, 50 °C, 4 h, 1 bar N2. C3H8O: isopropanol, C6H5NO2: nitrobenzene, DMPO: 5,5-dimethyl-1-pyrroline N-oxide. b Reaction pathways for the photocatalytic amination of lactic acid and side reaction. c In situ ESR spectra for CdS in a mixture of lactic acid, ammonia and the spin-trapping agent (DMPO) with or without visible-light irradiation.

Figure S7. FT-IR of lactic acid and the CdS NCs mixed with lactic acid. LA: lactic acid.

Fig. S8. Catalytic performances with pyruvic acid as substrates over CdS. Reaction conditions: 1.76 g pyruvic acid, 10 mg catalyst, 4 mL aqueous NH3 25% solution, 16 mL deaerated water, 50 ℃, 4 h, 1 bar N2, visible light.

Figure S9. TEM image of CdS-3 after five cycles. Reaction conditions: 200 mg PLA, 10 mg CdS-3, 4 mL aqueous NH3 25% solution, 16 mL deaerated water, 50 ℃, 4 h, 1 bar N2, visible light.