Supplementary Information

RISM-assisted analysis of the role of alkali metal hydroxides in the solvation of cellulose in alkali/urea aqueous solutions

Eugene Huh†, Ji-Hyun Yang†, Chang-Ha Lee†, Ik-Sung Ahn*, †, Byung Jin Mhin*,‡

†Department of Chemical and Biomolecular Engineering, Yonsei University, Seoul 120-749, South Korea

‡Department of Chemistry, Paichai University, Daejeon 302-735, South Korea

Corresponding Author

* iahn@yonsei.ac.kr

* mhin@pcu.ac.kr

Contents

| - Calculation Method | S3 |
| --- | --- |
| - Table S1 | S4 |
| - Table S2 | S5 |
| - Table S3 | S6 |
| - Table S4 | S7 |
| - Table S5 | S8 |
| - Table S6 | S9 |
| - Table S7 | S10 |
| - Table S8 | S11 |
| - Reference | S12 |

Calculation method

The initial configurations were made by packing the solvent species into a rectangular box of size 32 x 40 x 72 Å3 using the PACKMOL package (Martínez et al., 2009). By following the experimental conditions employed for the solvation of cellulose (Cai et al., 2006; Cai and Zhang, 2005; Cai et al., 2007; Cai et al., 2008), the concentrations of MOH and urea were all assigned to be 2 M. Hence, 3080 water molecules, 111 alkali hydroxide molecules (MOH), and 111 urea molecules were initially assigned in the simulation box. The MD simulations were first performed in a canonical (constant NVT) ensemble for 10 ns, and then the production runs were performed in an isothermal-isobaric (constant NPT) ensemble for 5 ns to calculate the appropriate volume. The scale factor was calculated as follows:

scale factor=volume of the simulation box calculated at constant NPT initial volume of the simulation box 32 x 40 x 72 Å3	     (S1)

Then, the number of solvent species in the 32 x 40 x 72 Å3 box was changed by multiplying the scale factor by its initial number. The numbers of solvent species in each solvent are shown in Table S3.

VC (cavity volume) and VI (interaction volume) along with their components, VC,γ and VI,γ, were calculated in 3D-RISM:

VC=γVC,γ								     (S2)

VI=γVI,γ								     (S3)

Table S1. Initial densities and pressures of the solvents used for the 3D-RISM-KH calculations

| solvent | Density (g/ml) | Pressure (MPa) |
| --- | --- | --- |
| WO | 1.0143 | 532.2 |
| LO | 1.0740 | 536.6 |
| NO | 1.1102 | 612.8 |
| KO | 1.1409 | 722.7 |
| UO | 1.0500 | 646.3 |
| LU | 1.1057 | 433.7 |
| NU | 1.1399 | 806.2 |
| KU | 1.1637 | 925.1 |

Table S2. Radii of bare ion and ion hydrate (Volkov et al., 1997)

| ion | Radius of bare ion (Å) | Radius of ion hydrate (Å) |
| --- | --- | --- |
| Li+ | 0.94 | 3.82 |
| Na+ | 1.17 | 3.58 |
| K+ | 1.49 | 3.31 |

Table S3. Number of solvent species in the simulation boxa recalculated with the scale factor

| solvent | water | MOHb | urea |
| --- | --- | --- | --- |
| WO | 3080.3 |  |  |
| LO | 3080.3 | 111.0 |  |
| NO | 3080.3 | 111.0 |  |
| KO | 3080.3 | 111.0 |  |
| UO | 2895.4 |  | 104.3 |
| LU | 2926.2 | 105.5 | 105.5 |
| NU | 2926.2 | 105.5 | 105.5 |
| KU | 2926.2 | 105.5 | 105.5 |

a The simulation box has a size of 32 x 40 x 72 Å3 with one molecule of cellulose inside.

b MOH denotes the alkali metal hydroxide including LiOH, NaOH, and KOH.

Table S4. Excess number of solvent species γ (Nγexcess) in various solvents.

| solvent | Water | LiOH/NaOH/KOH |
| --- | --- | --- |
| WO | 2.3 |  |
| LO | 1.9 | 0.0 |
| NO | 3.0 | –1.0 |
| KO | 4.8 | –2.1 |

Table S5. Cavity volume (VC), interaction volume (VI), ideal fluctuation volume (Vid), and partial molar volume (V) of cellulose in solvents LO, NO, and KO a

| solvent | VC | VI | Vid | V | VT b |
| --- | --- | --- | --- | --- | --- |
| LO | 1335.4 | –58.1 | 1.7 | 1277.4 | 162.1 |
| NO | 1336.7 | –60.7 | 1.6 | 1276.0 | 163.3 |
| KO | 1339.4 | –58.0 | 1.5 | 1281.4 | 166.1 |
| WO c | 1330.5 | –67.9 | 2.0 | 1262.6 | 157.2 |

a V=VC+VI+Vid. The unit is Å3 per cellulose molecule.

b VT is the thermal volume and is calculated from VT=VC-VM, where VM=1173.3 Å3.

c Data in solvent WO are given for comparison.

Table S6. Components of VC and VI in Table S3 a

| solvent | VC,water | VC,MOH | VI,water | VI,MOH |
| --- | --- | --- | --- | --- |
| LO | 1321.4 | 14.0 | –54.5 | –3.5 |
| NO | 1290.4 | 46.0 | –56.5 | –4.2 |
| KO | 1260.3 | 79.2 | –53.2 | –4.8 |
| WO b | 1330.5 | – | –67.9 | – |

a The unit is Å3 per cellulose molecule. Values of VC and VI are shown in Table S2.

b Data in solvent WO are given for comparison.

Table S7. Solvation energy and solvation entropy of cellulose in solvents LO, NO, and KO at 261 K a

| solvent | ∆E | Euv | ∆ER (≈T∆SR) | T∆S | -T∆Suv |
| --- | --- | --- | --- | --- | --- |
| LO | –208.6 | –368.3 (–333.9) [–34.4] | 142.6 (130.4) [12.1] | –271.6 | –414.1 (–393.0) [–21.1] |
| NO | –203.0 | –366.0 (–341.2) [–24.8] | 162.9 (151.5) [11.4] | –279.8 | –442.7 (–421.2) [–21.5] |
| KO | –190.3 | –364.8 (–346.1) [–18.7] | 174.6 (162.1) [12.5] | –289.1 | –463.6 (–438.6) [–25.0] |
| WO b | –214.7 | –361.1 (–361.1) | 146.4 (146.4) | –253.3 | –399.7 (–399.7) |

a ΔH= ∆Huv+∆HR and T∆S= T∆Suv+T∆SR. The superscripts uv and R denote solute-solvent interaction and solvent reorganization (solvent-solvent interaction), respectively. Numbers in round and square brackets indicate the contributions of water and MOHs, respectively. The unit of energy is kcal per mole of cellulose.

b Data in solvent WO are given for comparison.

Table S8. Chemical potentials of cellulose solvation without (Δμ) and with (∆μPC+) the advanced pressure correction (PC+) in solvents LO, NO, and KO at 261 K a

| solvent | Δμ | ∆μPC+ |
| --- | --- | --- |
| LO | 62.9 | 139.8 |
| NO | 76.8 | 138.6 |
| KO | 98.8 | 138.1 |
| WOb | 38.6 | 137.5 |

a The unit of energy is kcal per mole of cellulose.

b Data in solvent WO are given for comparison.

References

- Cai, J., Liu, Y., Zhang, L., 2006. Dilute solution properties of cellulose in LiOH/urea aqueous system. Journal of Polymer Science Part B: Polymer Physics 44, 3093-3101.

- Cai, J., Zhang, L., 2005. Rapid dissolution of cellulose in LiOH/urea and NaOH/urea aqueous solutions. Macromolecular bioscience 5, 539-548.

- Cai, J., Zhang, L., Chang, C., Cheng, G., Chen, X., Chu, B., 2007. Hydrogen‐bond‐induced inclusion complex in aqueous cellulose/LiOH/urea solution at low temperature. ChemPhysChem 8, 1572-1579.

- Cai, J., Zhang, L., Liu, S., Liu, Y., Xu, X., Chen, X., Chu, B., Guo, X., Xu, J., Cheng, H., 2008. Dynamic self-assembly induced rapid dissolution of cellulose at low temperatures. Macromolecules 41, 9345-9351.

- Martínez, L., Andrade, R., Birgin, E.G., Martínez, J.M., 2009. PACKMOL: a package for building initial configurations for molecular dynamics simulations. Journal of computational chemistry 30, 2157-2164.

- Volkov, A., Paula, S., Deamer, D., 1997. Two mechanisms of permeation of small neutral molecules and hydrated ions across phospholipid bilayers. Bioelectrochemistry and Bioenergetics 42, 153-160.