Table 1. Optimization of the reaction conditionsa

| Entry | Solvent (mL) | Catalyst (mol%) | Temp. (°C) | Timeb (h) | Yield (%) |
| --- | --- | --- | --- | --- | --- |
| 1 | EtOAc | Pd@HQBI-SPION (0.1) | 50 | 12 | 63 |
| 2 | EtOAc | Pd@HQBI-SPION (0.1) | reflux | 12 | 86 |
| 3 | EtOAc | Pd@HQBI-SPION (0.1) | reflux | 16 | 88 |
| 4 | EtOAc | Pd@HQBI-SPION (0.1) | reflux | 10 | 56 |
| 5 | Toluene | Pd@HQBI-SPION (0.1) | reflux | 12 | 83 |
| 6 | EtOAc/Toluene | Pd@HQBI-SPION (0.1) | reflux | 12 | 74 |
| 7 | DMF | Pd@HQBI-SPION (0.1) | reflux | 12 | 43 |
| 8 | EtOAc | Pd@HQBI-SPION (0.1) | reflux | 12 | 94 |
| 9 | EtOAc | HQBI-SPION (0.1) | reflux | 12 | 26 |
| 10 | EtOAc | Pd@HQBI-SPION (0.05) | reflux | 12 | 56 |
| 11 | EtOAc | Pd@HQBI-SPION (0.2) | reflux | 12 | 94 |
| 12 | EtOAc | Pd@HQBI-SPION (0.1) | reflux | 12 | 51 |
| 13 | EtOAc | Pd@HQBI-SPION (0.1) | reflux | 12 | 94 |

a Reaction conditions: 1 (2 mmol), 2a (2 mmol), dimedone 4 (2.2 mmol, 1.1 eq.), solvent (4 mL), catalyst (mol%), at given temperatures for different times. b Time of step 1. Time of step 2 = 8 h.

Table 2. Screening of the substrate scopea

| Entry | Benzyl bromides | Products | Timeb (h) | Yields (%) |
| --- | --- | --- | --- | --- |
| 1 |  |  | 12 | 94 |
| 2 |  |  | 14 | 83 |
| 3 |  |  | 16 | 79 |
| 4 |  |  | 12 | 87 |
| 5 |  |  | 12 | 79 |
| 6 |  |  | 12 | 90 |
| 7 |  |  | 16 | 77 |
| 8 |  |  | 16 | 75 |

a Reaction conditions: 1 (2 mmol), 2a (2 mmol), dimedone 4 (2.2 mmol, 1.1 eq.), MaCN (4 mL), Pd@HQBI-SPION (0.1 mol%), under reflux conditions. b Time of step 1. Time of step 2 = 8 h.